Supplementary Information

AQUEOUS PREPARATION OF SELF-SUPPORTED HYDROXYPROPYL METHYLCELLULOSE-POLYANILINE CONDUCTING FILMS AND THE EVALUATION OF THEIR ELECTRICAL AND MECHANICAL PROPERTIES

Vinicius Cavalheiro Maedaa, Cintia Marques Correaa, Marcos Henrique Mamoru Otsuka Hamanakab, Viviane Nogueira Hamanakab, Celso Molinaa and Fernanda F. Camiloa*

aDepartment of Chemistry, Federal University of São Paulo, Rua São Nicolau, 210 – Laboratório de Materiais Híbridos, CEP: 09913-030, Diadema, SP, Brazil

bAutocoat Equipamentos e Processos de Deposição LTDA, Rua Daniel Hogan, 434 - sala 25 - Cidade Universitária, CEP 13083-836, Campinas, SP, Brazil

Corresponding author: Fernanda Ferraz Camilo

Laboratório de Materiais Híbridos, Instituto de Ciências Ambientais, Químicas e Farmacêuticas, Universidade Federal de São Paulo

Rua São Nicolau, 210, CEP: 09913-030, Diadema – SP, Brazil

Phone: +55 11 3319-3568

E-mail: ffcamilo@unifesp.br

Figure 1S: Artwork representing the preparation of PANI_HPMC films

Figure 2S: SEM images of HPMC (A), PANI (B) and PANI_40%HPMC (C)

Figure 3S: Stress–strain curves of the samples

Note 1

Chemical equation of polymerization of aniline by ammonium persulfate

Table 1S: Amounts of reagents

|  | Aniline | (NH4)2S2O8 | PANI/ doped with 2 Cl- | PVP* |
| --- | --- | --- | --- | --- |
| molar mass (g mol-1) | 93 | 228 | 435 | -- |
| Initial number of mol (mmol) | 20 | 25 | ---- | ---- |
| Final number of mol (mmol) | ---- |  | 5.0 |  |
| Final mass (g) | ---- | ---- | 2.18 | 2.00 |

*it was added 50 mg of an aqueous solution of PVP (40 g L–1)

- Considering the stoichiometry of the reaction and the complete conversion (100 % yield), the total mass of the dispersion would be 4.18 g (2.18 g (PANI/2Cl-) + 2.00 g (PVP)

- Therefore, the PANI dispersion has 52 wt % of PANI and 48 wt% of PVP.