Supplementary Material

Instantaneous synthesis of organic-inorganic laccase-cobalt phosphate hybrid nanoflowers: Structural and biocatalytic characterization

Khashayar Vojdanitalaba,b,#, Hossein Jafari-Nodoushana,#, Somayeh Mojtabavia, Mahtab Shokria,b, Hoda Jahandarb, and Mohammad Ali Faramarzia,*

a Department of Pharmaceutical Biotechnology, Faculty of Pharmacy & Biotechnology Research Center, Tehran University of Medical Sciences, P.O. Box 14155−6451, Tehran 1417614411, Iran

b Pharmaceutical Sciences Research Center, Tehran Medical Sciences Branch, Islamic Azad University, Tehran, Iran

-------------------------------------------------

*Corresponding author: M.A. Faramarzi, Telefax: +98-21-66954712, E-mail: faramarz@tums.ac.ir

#K. Vojdanitalab and H. Jafari-Nodoushan contributed equally as first author.

Fig. S1. Scanning electron microscopy (SEM) image of the constructed Co3(PO4)2•NFs. The spherical flower-shaped nanostructures are formed by the “concentrated method.”

Fig. S2. Scanning electron microscopy (SEM) image of the constructed Co3(PO4)2•NFs revealed that the flower-shaped nanostructures were composed of ultrathin nanosheets.

Fig. S3. Elemental map analysis of Co3(PO4)2•NFs that mostly composed of P, Co, and O elements.

Fig. S4. Energy dispersive X-Ray spectroscopy (EDX) analysis of the constructed Co3(PO4)2•NFs.

Fig. S5. Brunauer-Emmett-Teller (BET) plot of laccase@Co3(PO4)2•HNFs (a) and Co3(PO4)2•NFs (b). Both materials exhibited type IV isotherm with a narrow hysteresis loop, which is attributed to the mesoporous structure of the synthesized HNFs and NFs.

Figure S6. Circular dichroism (CD) spectra of laccase@Co3(PO4)2•HNFs and the free enzyme recorded at 180–240 nm. Coordination of laccase with zinc phosphate significantly altered the secondary structure of the enzyme.

Figure S7. Tryptophan fluorescence intensity of laccase@Co3(PO4)2•HNFs and the free enzyme for estimation the protein 3rd structure.

Figure S8. Thermogravimetric analysis of laccase@Co3(PO4)2•HNFs and Co3(PO4)2. Laccase composed 5% of the weight of the synthesized HNFs. The experiment was conducted after the complete degassing of samples under N2 atmosphere with a heating rate of 10 °C/min.

Figure S9. Liquid chromatography-mass spectrometry (LC-MS) analysis of moxifloxacin (Rt = 11.9 min) (a) and its corresponding detected degradation products (b). Mass spectra of the degradation products are presented as II) compound II (m/z: 280, Rt = 3.9 min), III) compound III (m/z: 262, Rt = 6 min), IV) compound IV (m/z: 294, Rt = 8.7 min), and V) compound V (m/z: 358, Rt = 9 min) (c).

Table S1. Weight percentage of elements in laccase@Co3(PO4)2•HNFs and Co3(PO4)2 measured by Energy dispersive X-Ray spectroscopy (EDX) analysis.

| Type of material | Co (%) | O (%) | P (%) | N (%) |
| --- | --- | --- | --- | --- |
| Laccase@Co3(PO4)2•HNFs | 42.3 | 29.5 | 16.7 | 11.5 |
| Co3(PO4)2•NFs | 54.7 | 10 | 31.3 | 4 |

Table S2. Mean pore diameter, total pore volume, and Brunauer-Emmett-Teller (BET) specific surface area of laccase@Co3(PO4)2•HNFs.

| Material | Mean pore diameter (nm) | Total pore volume × 10-3 (cm3/g) | Specific surface area (m2/g) |
| --- | --- | --- | --- |
| Laccase@Co3(PO4)2•HNFs | 29.5 | 128.5 | 17.4 |
| Co3(PO4)2•NFs | 22.3 | 98.1 | 17.6 |

Table S3. Growth inhibition percentage (GI%) of untreated and treated antibiotics with laccase@Co3(PO4)2 HNFs against four bacterial strains. Values are averages of three replicates ± standard deviation.

| Antibiotics | Bacterial strains |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | S. aureus |  | S. epidermidis |  | P. aeruginosa |  | E. coli |  |
|  | Untreated | Treated | Untreated | Treated | Untreated | Treated | Untreated | Treated |
| Moxifloxacin | 75.2 ± 0.6 % | 56.7 ± 1.2 % | 81.2 ± 0.4 % | 41.6 ± 0.7 % | 76.2 ± 0.3 % | 25.1 ± 2.1 % | 64.5 ± 0.4 % | 56.7 ± 1.2 % |

* p < 0.05 vs. untreated