Table 2. Synthesis of β-thiol-1,2,3-triazoles from thiiranes in the presence of Fe3O4@SiO2-PMA-Cu nanocatalysta

| Entry | Thiirane (a) | Alkyne | Triazole (b) | Time (h) | Yield (%)b |
| --- | --- | --- | --- | --- | --- |
| 1 |  |  |  | 1.5 | 98 |
| 2 |  |  |  | 2.5 | 90 |
| 3 |  |  |  | 2.5 | 86 |
| 4 |  |  |  | 3 | 90 |
| 5 |  |  |  | 3 | 88 |
| 6 |  |  |  | 2 | 90 |
| 7 |  |  |  | 2.4 | 92 |
| 8 |  |  |  | 3.5 | 85 |
| 9 |  |  |  | 2.3 | 92 |
| 10 |  |  |  | 3.5 | 90 |
| 11 |  |  |  | 1.8 | 95 |

aAll reactions were performed with of thiirane (1 mmol), alkyne (1 mmol), sodium azide (1.2 mmol) and nano- Fe3O4@SiO2-PMA-Cu (0.1 g) in water at 55 °C. bYields are related  to isolated pure triazoles.