Supplementary Information for

NIR-laser activated polydopamine-coated Fe3O4 nanoparticles used as a novel precise photothermal insecticide

Haijun Wang1,3#, Qian Zhang1,2#, Xinyu Zhang1,2, Kexin Zhang1,2, Xichen Zhao3, Ruiling Zhang1,2*, Zhong Zhang1,2*

1 Collaborative Innovation Center for the Origin and Control of Emerging Infectious Diseases, Shandong First Medical University and Shandong Academy of Medical Sciences, Tai’an 271016, China.

2 School of Basic Medical Sciences, Shandong First Medical University and Shandong Academy of Medical Sciences, Tai’an 271016, China

3 School of Life Sciences, Shandong First Medical University and Shandong Academy of Medical Sciences, Tai’an 271016, China.

*Corresponding authors: zhangz@sdfmu.edu.cn (Zhong Zhang), rlzhang@sdfmu.edu.cn (Ruiling Zhang)

# The authors contributed equally to this work.

Experimental Section

Materials

Fe3O4 magnetic nanoparticles solution (Fe3O4 NPs; 100–300 nm, 250 μg/mL in H2O), Dopamine hydrochloride (DA·HCl) were purchased from Aladdin (Shanghai, China). Tris (hydroxymethyl) aminomethane buffer (Tris-HCl buffer; 10 mM, pH 8.6) was acquired from phygene (Fuzhou, China). Deionized (DI) water purified using a Millipore system and then sterilized was used for all experiments. Musca domestica: The housefly colony was reared in the Laboratory of Vector and Vector-borne Diseases of Shandong First Medical University since 2005. The housefly adults were fed with brown sugar and water, and the larvae were fed with wet wheat bran and milk powder (Wheat bran (g): DI water (mL): milk powder (g) = 1:1:0.4). They were raised in an artificial climate incubator with a temperature of 25 ± 1 ℃ and 70% relative humidity with a photoperiod of 12/12 h (Light/Dark).

Synthesis of Fe3O4@PDA NPs

The Fe3O4@PDA NPs were synthesized following the reported methods with some modifications1. Briefly, 160 μL of Fe3O4 NPs (250 μg/mL in H2O) were dispersed in tris-HCl buffer (400 mL), followed by sonication for 5 min. DA·HCl (400 mg) were then added and mechanical stirring (260 rpm) for 3 h. The Fe3O4@PDA NPs were collected after centrifugation and washed with deionized (DI) water.

Characterization of Fe3O4@PDA NPs

The morphology of Fe3O4 and Fe3O4@PDA NPs were observed by Transmission electron microscopy (TEM, FEI-TECNAI G2 20) and scanning electron microscopy (SEM, FEI-QUANTA250, FEI Company). Energy-dispersive X-ray spectroscopy detector system (EDS, Oxford X-MAX 65T) were employed to observe the structure of the resulting nanoparticles. The weight of Fe3O4 in Fe3O4@PDA lyophilized powder was analyzed by measuring Fe elements using inductively coupled Optical emission spectrometry (ICP-OES, Agilent 725). Fourier transform infrared (FTIR) analysis was carried out to confirm the chemical composition of PDA modified Fe3O4 NPs on a Nicolet-Nexus 670 spectrometer over the range 4000–500 cm-1 and with a resolution of 1 cm-1.

Photothermal Effects of NPs

The photothermal conversion efficacy in vitro was measured. Briefly, a Fe3O4 or Fe3O4@PDA NP suspension (200 μL) at concentrations of 0.1, 0.5 and 1.0 mg/mL was transferred into an Eppendorf tube, respectively, and exposed to NIR laser irradiation (808 nm, 1 W/cm2) for 5 min. The influence of the laser power density was ascertained by irradiating a 200 μL suspension of Fe3O4 or Fe3O4@PDA NPs (1.0 mg/mL) under different power densities from 0.5 to 2.0 W/cm2. In addition, the temperature of an Fe3O4 or Fe3O4@PDA NPs (1.0 mg/mL) suspension (1 mg/mL) was monitored under continuous NIR laser irradiation (1 W/cm2) for 5 min using an infrared thermal imaging system (IRBIS 3.1, InfraTec). DI water was employed as a control.

Biosafety evaluation of the NPs toward housefly larvae

Varied volume (1, 3, 5, 10 mL) of Fe3O4 NP suspension (10 mg/mL, in DI water) was mixed with wheat bran and milk powder (Wheat bran (g): DI water (mL): milk powder (g) = 1:1:0.4), this giving feeding materials, and termed F1, F3, F5, F10, respectively. Fe3O4@PDA NPs-included feeding materials was mixed used the same mixture ratio, and termed FP1, FP3 and FP5, FP10. Ten normal-breeding, good-growing and uniform-sized 1-day-old housefly larvae were fed with F1, F3, F5, F10, FP1, FP3 and FP5, FP10 in gauze covered porous centrifuge tube (10 mL), respectively. NPs-free feeding material was used as control group. Then, all housefly larvae were placed in an artificial climate incubator with a temperature of 25 ± 1°C, relative humidity of 70 ± 5%, and a photoperiod of 12/12 h (L/D). At predetermined time points (1, 2, 3, 4 day), the equal number of larvae were taken from each tube, and the body length, body weight, pupal weight, pupation rate and emergence rate were recorded. Data are reported as mean ± SD, with three independent experiments of each group containing three replicates performed.

The effect of FP5 before and after NIR laser irradiation (808 nm, 1 W/cm2) on intestinal microbial population of housefly larvae was systematically evaluated. Housefly larvae were fed with FP5, and Fe3O4@PDA NPs-free feeding material was used as control. After 24 h, the same number of larvae were taken from two groups, and then given 30 s laser irradiation (808 nm, 1 W/cm2), followed by putting them back into the feed and cultured for another 30 min. After removing the surface debris, the larvae were transferred into a 75% alcohol-contained eppendorf (EP) tube (1.5 mL), and soaked, disinfected for 10-15 min before rinsed with sterile deionized water 3 times to remove the bacteria attached to the larvae surface. This disinfection and rinsing process was repeated 3 times. After strict body surface disinfection, the housefly larvae samples were stored at -80 °C. Finally, the samples were sent for high-throughput sequencing, including Extraction of the intestine DNA, PCR amplification, Illumina MiSeq sequencing and bioinformatics analysis according to our previous studies2, 3. The larvae taken out of different treatment groups and control groups each time were used as a sampling unit, and each sampling unit had 3 replicates.

Housefly larval uptake evaluation and NIR imaging in vivo

In order to investigate the larval uptake of Fe3O4 and Fe3O4@PDA NPs, the 2-day-old housefly larvae were fed with F3, FP3, F5 or FP5 in EP tube and cultured for 24 h. Next, the larvae from each tube were collected and weighted. Finally, the Fe content in each group was quantified by inductively coupled plasma optical emission spectrometer (ICP-OES).

When feeding with F3, FP3, F5 or FP5 in EP tube and cultured for 24 h, these housefly larvae were anesthetized with diethyl ether and then given 3 min of laser irradiation (808 nm, 1 W/cm2) throughout the whole body of larvae. At given time points, NIR images were captured with an infrared thermal imaging system. NPs-free feeding materials treated housefly larvae were used as control.

Photothermal control of housefly larvae in vivo

1-day-old housefly larvae were fed with F1, FP1, F3, FP3, F5, and FP5, respectively. At predetermined day (day 2, 3, 4, 5), five uniform-sized housefly larvae of each group were collected, and given laser irradiation (808 nm, 1 W/cm2) until to death. The time to death was recorded, and data are reported as mean ± SD.

The influence of the laser power density was ascertained by irradiating the 1-day-old housefly larvae after feeding 2 day’s F5 and FP5 under different power densities from 0.5 to 2.0 W/cm2. The deadtime was recorded, and data are reported as mean ± SD, n=5.

SEM observation of intestinal tract and histopathology assay

1-day-old housefly larvae were fed with F5, FP5, and cultured for 24 h. Then, three housefly larvae of each group were collected, and given laser irradiation (808 nm, 1 W/cm2) for 1 min. Finally, housefly larvae were fed with F5, FP5 without/with laser irradiation were immediately excised and processed for hematoxylin and eosin (H&E) staining and SEM observation. NPs-free feeding materials treated housefly larvae were used as control.

Intestinal bacteria leakage assay

F5, FP5-fed housefly larvae were cultured for 2 days, and then given laser irradiation (808 nm, 1 W/cm2) for 1 min. After removing the surface debris, the larvae of each group were transferred into a EP tube containing 75% alcohol, and soaked, disinfected for 20 min. These housefly larvae were rinsed with sterile DI water 3 times to remove the bacteria attached to the larvae surface. This disinfection and rinsing process was repeated 3 times. After strict body surface disinfection, the larva’s epidermis was punctured with sterilizing needle, then the sterile cotton swab was dipped into the larva’s surface skin to absorb spilled body fluid, evenly coated for 3 times in three directions on the nutrient agar, and finally coated along the edge of the nutrient agar plate. The plates were cultured at 37 ℃ for 48 h and observe whether there is bacterial growth.

Recovery of NPs

The residual NPs in feeding materials was recycled and the photothermal effects of NPs was measured again. Briefly, the F5 and FP5 after feeding housefly larvae for 2 days was collected. All wheat bran was filtered with ddH2O, and these two kinds of magnetic Fe3O4-based NPs were recovered by magnetic absorption. The obtained NPs were dried and weighted, and a Fe3O4@PDA NP suspension (200 μL) at concentrations 0.5 mg/mL was exposed to NIR laser irradiation (808 nm, 1 W/cm2) for 5 min to measure the photothermal effects. Finally, the samples were irradiated for 5 min each time with three on-off cycles to determine the thermal stability of Fe3O4@PDA NPs.

Statistical analysis

The experimental data were analyzed by Microsoft Excel 2010 and IBM SPSS Statistics 20 statistical software. All the data are given as Mean ± SD. Each treatment consisted of three biological replicates. Pupation rate, emergence rate and pupal weight of housefly larvae among different treatment groups were compared by using one-way ANOVA followed by Fisher’s LSD test (p < 0.05).

References

1.	Park J, Brust TF, Lee HJ, Lee SC, Watts VJ, Yeo YJAn. Polydopamine-based simple and versatile surface modification of polymeric nano drug carriers. ACS nano, 8, 3347-3356 (2014).

2.	Zhang Q, Wang S, Zhang X, Zhang R, Zhang Z. Negative Impact of Pseudomonas aeruginosa Y12 on Its Host Musca domestica. Front. Microbiol. 12, 691158 (2021).

3.	Li T, et al. Transcriptome and microbiome analyses of the mechanisms underlying antibiotic-mediated inhibition of larval development of the saprophagous insect Musca domestica (Diptera: Muscidae). Ecotoxicol. Environ. Saf. 223, 112602 (2021).

Supplementary Figures and Tables

Supplementary Figure 1. The particle size distribution of Fe3O4 NPs and Fe3O4@PDA NPs which was calculated from the analysis of around 100 nanoparticles in TEM images, using the Image J software.

Supplementary Figure 2. EDS analysis of Fe3O4@PDA NPs.

Supplementary Figure 3. FTIR spectroscope of Fe3O4@PDA NPs.

Supplementary Figure 4. UV/Vis absorption spectra of (a) Fe3O4 and (b) Fe3O4@PDA NP suspensions (0.25 mg/mL).

Supplementary Figure 5. Temperature vs. time plots for water at different concentrations with a laser power density of 1 W/cm2 for 5 min.

Supplementary Figure 6. The temperature variation curves of larvae after exposure to NIR irradiation (1 W/cm2) for 3 min.

Supplementary Figure 7. The temperature variation curves of recycled Fe3O4@PDA NP suspensions (0.5 mg/mL) after exposure to NIR irradiation (1 W/cm2) for 5 min.

Supplementary Figure 8. Plot showing the temperature changes of a 0.5 mg/mL suspension of Fe3O4@PDA NP irradiated by an 808 nm laser (1.0 W/cm2) over three on−off cycles.

Supplementary Table 1. Effects of different doses of Fe3O4@PDA NPs on the pupal weight, pupation rate and emergence rate of housefly larvae.

| Treatment | Pupal weight (g) | Pupation rate (%) | Emergence rate (%) |
| --- | --- | --- | --- |
| CT | 2.14 ± 0.08 | 88.33 ± 2.89 | 88.89 ± 9.62 |
| FP1 | 2.08 ± 0.22 | 93.33 ± 5.77 | 87.78 ± 10.72 |
| FP3 | 2.01 ± 0.06 | 85.00 ± 5.00 | 88.44 ± 5.21 |
| FP5 | 2.00 ± 0.02 | 86.67 ± 2.89 | 84.64 ± 3.15 |
| FP10 | 1.94 ± 0.05 | 88.33 ± 2.89 | 86.93 ± 6.23 |