Table S1 Physical properties of porous carriers.

| Materials | Dry weight (g)/100 mL | Specific gravity | Bulk density (g/mL) | Solid phase (%) | Liquid phase (%) | Gas phase (%) | Porosity (%) | WFPS (%) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Oyster shell lime (2–4 mm) | 69.38 | 1.82 | 0.6938 | 38.1 | 27.5 | 34.4 | 61.9 | 44.4 |
| Rice husk charcoal | 11.02 | 0.63 | 0.1102 | 19.4 | 63.3 | 17.3 | 80.6 | 78.5 |
| Rockwool (granular) | 21.97 | 1.29 | 0.2197 | 22.8 | 71.6 | 5.6 | 77.2 | 48.0 |
| Coconut husk | 44.97 | 1.46 | 0.4497 | 30.9 | 32.6 | 36.6 | 69.2 | 47.1 |
| Vermiculite | 14.76 | 0.54 | 0.1476 | 28.9 | 50.5 | 20.6 | 71.1 | 71.1 |
| AQ-20 | 2.27 | 0.18 | 0.0227 | 12.3 | 15.2 | 72.5 | 87.7 | 17.4 |
| AQ-15 | 1.85 | 0.19 | 0.0185 | 9.9 | 31.6 | 58.5 | 90.1 | 35.1 |
| AQ-14 | 2.13 | 0.17 | 0.0213 | 12.7 | 32.2 | 55.1 | 87.3 | 36.9 |
| Pumice | 40.87 | 1.01 | 0.4087 | 40.4 | 23.8 | 35.7 | 59.6 | 40.0 |

Physical properties were measured as follows. First, 100 mL (bulk volume, V) of each material was prepared and weighed (W). The material was transferred to a 500-mL graduated cylinder, which was filled to 100 mL with water. The amount of water added (WW) was measured. The water was decanted, and the total amount discharged (Wf) was measured. The dry weight (Wd) of 100 mL of each material was measured after drying at 100 °C for 24 h. From the results, we calculated the specific gravity of each material, the bulk density, the solid phase ratio, the liquid phase ratio after decantation, the gas phase ratio after decantation, porosity, and the water-filled pore space (WFPS) as follows:

Solid phase (%) = {100 − WW − (W − Wd)}/V × 100

Liquid phase (%) = {W + (W − Wd) − Wf}/V × 100

Gas phase (%) = 100 − (Solid phase) − (Liquid phase)

Specific gravity = Wd/100 − WW − (W − Wd)

Bulk density (g/mL) = Wd/100

Porosity (%) = (Liquid phase + Gas phase)

WFPS (%) = (Liquid phase) / (Porosity) × 100