Supplementary Information

Depolymerization of polyesters by a binuclear catalyst

Shengbo Zhang1,5, Qikun Hu1,5, Yu-Xiao Zhang1,5, Haoyue Guo2, Yanfen Wu1, Mingze Sun1, Xingsong Zhu3, Jiangang Zhang4, Shuyan Gong1, Ping Liu2 & Zhiqiang Niu1,*

1State Key Laboratory of Chemical Engineering, Department of Chemical Engineering, Tsinghua University, Beijing 100084, China

2Chemistry Department, Brookhaven National Laboratory, Upton, NY 11973, USA

3Sinopec Yizheng Chemical Fibre Co., Ltd., Yangzhou, Jiangsu 211900, China

4School of Life Sciences, Tsinghua University, Beijing 100084, China

5These authors contributed equally: Shengbo Zhang, Qikun Hu, Yu-Xiao Zhang

*e-mail: niuzq@tsinghua.edu.cn

Table of Contents

- Characterizations

- Economic analysis

- DFT calculations

- Supplementary Tables 1‒5

- References

- Characterizations

X-ray crystallography: SCXRD data were collected at 173 K on a SuperNova charge-coupled device (CCD) X-ray diffractometer, with Cu-Kα radiation (λ = 1.54184 Å). The crystal structures were resolved by directed methods and refined by full-matrix least-squares fitting on F2 using the SHELXL-2018 software package and OLEX2 program1,2. All non-hydrogen atoms were refined anisotropically. Hydrogen atoms were generated geometrically. Ultimately, the molecule formula of these complexes was calculated from the SCXRD data together with the results of elemental analysis. Supplementary Tables 2‒5 list the crystal data, bond lengths, and bond angles.

X-ray adsorption spectroscopy: The XAFS spectra at Zn K-edge were acquired at the 4B9A station in Beijing Synchrotron Radiation Facility (BSRF), operated at 2.5 GeV with a maximum current of 250 mA. The data for Zn2/C were recorded in fluorescence excitation mode using a Lytle detector. Zn2L(NO3)2, Zn foil, and ZnO were used as reference materials and measured in transmission mode using an ionization chamber. The acquired EXAFS data were processed according to the standard procedures using the ATHENA program integrated within the IFEFFIT (1.2.12) software packages3. The k3-weighted EXAFS spectra χ(k) were Fourier-transformed in a k-range of 3.0‒12.5 Å-1 for the Zn K-edge with a Kaiser-Bessel window function.

Differential scanning calorimetry (DSC): DSC measurements were performed by Q200 of TA Inst. to estimate the crystallinity of different PET sources. The temperature range was from 40 °C to 300 °C and the heating rate was 10 °C min-1. The degree of crystallinity (XC) was calculated by the following equation4-6:

XC=ΔHf-ΔHCΔHf0×100%

ΔHf: the enthalpy of melting

ΔHC: the enthalpy of cold crystallization

ΔHf0: the standard enthalpy of melting for a 100% crystalline PET

ΔHf and ΔHC could be calculated by integrating the endothermic melting peak and exothermic cold crystallization peak of DSC, and ΔHf0 was taken from literature as 140 J/g4-6. The peaks at about 130 °C were cold crystallization peaks and the peaks at about 250 °C were melting peaks.

Matrix assisted laser desorption ionization-time of flight mass spectrometer (MALDI-TOF MS): MALDI-TOF MS was performed by AXIMA-Performance (Shimadzu). Samples were collected at 15 h and 45 h, respectively, from the reaction mixture containing Zn2L(NO3)2 (4 mg), PET (10 mg), and NaOHaq (10-6 M, 10 mL). Methanol was added into the samples to form a 50% (v/v) methanol and water mixture. The samples were diluted 10 times and deposited onto the MALDI-TOF/MS sample plate for measurements.

Diffuse reflection infrared Fourier transform spectroscopy (DRIFTS): DRIFTS experiments were performed via a Fourier transform infrared spectrometer (Thermo Nicolet iS50) equipped with a diffuse reflection accessory (Harrick Inc.). Recrystallized Zn2L(NO3)2 (from water) and ethyl benzoate (EB) were physically mixed by a mole ratio of 1:1 with KBr as diluent. The mixture was heated at 110 oC for 40 minutes, while the recrystallized Zn2L(NO3)2 and EB were separately heated as control groups. The in-situ experiment of chemical adsorption was tested by a homemade high-temperature in-situ cell. 20 mg of mixed sample was packed in the cell and purged with 5 mL min-1 N2 at 60 oC.

1H nuclear magnetic resonance (NMR): 1H NMR was acquired on AVANCE Ⅲ (Bruker). The 1H NMR samples were prepared according to the following procedure: 0.1 mL of the reaction solution and 0.5 mL of D2O with 1 mg mL-1 maleic acid (MA) as the internal standard were added into NMR tube and completely mixed. The peak positions of the monomers used for quantitative analysis are listed in the table below. The molar amount of analyte (nanalyte) in the reaction solution was calculated via the equation below7,8:

nanalyte=SanalyteSstandard×2Nmonomer×mstandardMstandard×100.1

The conversion of PET was calculated by the equation below:

Conversion=nanalyten0×100%

The Sstandard and Sanalyte represent the peak areas of MA and analyte (monomer), respectively. The mstandard and Mstandard represent the mass and molar weight of MA, respectively. The Nmonomer represents the number of hydrogen atoms in the characteristic peak of the monomer used for quantitative analysis. The n0 represents the initial total molar amount of the monomer used for quantitative analysis in polyester.

| Plastic abbreviation | Monomers used for quantitative analysis | Peak positions in 1H NMR/ppm |
| --- | --- | --- |
| PET | disodium terephthalate/EG | 7.80/3.60 |
| PBT | disodium terephthalate | 7.80 |
| PBS | butane-1,4-diol | 3.60 |
| PCL | sodium 6-hydroxyhexanoate | 3.50 |
| PC | 4,4'-(propane-2,2-diyl)diphenol | 1.75 |
| PBAT | disodium terephthalate | 7.80 |
| PLA | sodium 2-hydroxypropanoate | 1.24 |
| P3/4HB | sodium 3-hydroxybutanoate | 4.05 |
| PEF | EG | 3.60 |
| Nylon 66 | sodium adipate | 2.03 |
| PGA | sodium 2-hydroxyacetate | 4.46 |
| PU | EG | 3.60 |
| PHB | sodium 3-hydroxybutanoate | 4.05 |
| PBA | hexane-1,6-diol | 3.56 |

- Economic analysis

2.1 Industrial process simulation (Extended Data Fig. 9): We developed an industrial stimulation based upon Zn2/C to investigate the economic feasibility. Firstly, the collected PET waste is cleaned and shredded into pieces as raw materials. Then the PET pieces, alkali, recycled catalysts, and water are added into a batch reactor. After the reaction, the mixture is pumped to the primary filter to recycle the catalysts. Then, the transparent solution flows through the activated carbon tower to remove pigment. The acidification process is performed by adding sulfate acid into the crystallizer to obtain recycled terephthalic acid. The remaining solution enters the salt crystallizer to separate sodium sulfate from the aqueous phase. Saturate vapor then enters the distillation tower to separate water and ethylene glycol. The whole simulation presumes a capability of 100 thousand tons of PET waste per year.

2.2 Economic calculation: The calculation is based on the above-mentioned simulation. The cost includes capital cost, maintenance cost, labor cost, chemical input, and utility cost. And the sales of PTA and ethylene glycol (EG) are the earnings in the process. The net profit (NP) is as the equation below:

Capital cost: Capital cost is the cost to build a factory from scratch. To simplify the simulation, our calculation of capital cost included the cost of facilities and installation. In this process, as shown in Extended Data Fig. 9b, major facilities include serval batch reactors, filters, an adsorption tower, and a distillation tower. The capital cost wasn’t calculated directly in the NP calculation but was reflected as depreciation.

Depreciation: Depreciation is related to capital cost. It’s a variable to describe capital cost with its service life. In this simulation, we used the straight-line depreciation method, as described by the following equation:

D=(V-Vs)/n

where D means depreciation (USD/year), V means original value, Vs means salvage value, and n means service year. Here we assumed the salvage value would be zero when its service life reached ten years.

Maintenance cost: Maintenance cost is the cost of maintaining facilities, usually considered to be 10 % of capital cost.

Labor cost: Labor cost is related to the cost of hiring workers. The estimation of labor cost was 10% of capital cost.

Chemical input & sales: Chemicals input and sales are the most influential factors in the simulation. It decides whether this simulation or this process can make positive NP. The chemical prices are shown in Extended Data Fig. 9c. All the data was acquired from a chemical trading platform called SunSirs (http://www.sunsirs.com/) and confirmed in another platform called made-in-china (https://www.made-in-china.com/) in 2021.

Basically, PET alkaline hydrolysis is the process of depolymerizing PET into ethylene glycol and terephthalate, in which both monomers are dissolved in the alkaline solution. To further produce terephthalic acid, it’s necessary to add acid to convert terephthalate into terephthalic acid precipitation. In this process, the consumption of acid consists of the neutralization reaction with the remaining alkaline and the acidification of disodium terephthalate. While the consumption of acid for the acidification depends on the production of disodium terephthalate, the consumption of acid for the neutralization reaction, however, depends on the molar amount of remaining alkaline in the reaction system.

It is worth noting that the price of alkali was high and took a considerable part in the chemical cost. In previously reported alkaline hydrolysis methods, all required very high concentrations of alkali (1–5 M), which means massive alkali would be wasted and bring unnecessary cost since the acidification process was needed to acquire terephthalic acid. The hydrolysis of PET in this work was carried out in a base concentration that is 1-6 orders of magnitude lower (0.000001-0.1 M), thus much less acid was consumed during post-reaction acidification, bringing significant cost savings compared with conventional alkaline hydrolysis.

In the presence of Zn2/C, industrially feasible depolymerization rate can be achieved at relatively low concentration of alkali (pH 13), such that little alkali would be wasted. Moreover, this number accurately satisfies the pH of saturated calcium hydroxide, a much cheaper alkali than NaOH. Using calcium hydroxide and hydrochloric acid to bring much more profit became practical via Zn2/C, and it could increase nearly 30% of the material profit. But the problems of using calcium hydroxide, such as the existence of solid calcium carbonate, should be further considered. For this reason, we still used NaOH in this NP calculation.

Utility cost: Utility cost refers to the cost of power, steam, compressed air, etc. In the whole process, separating steps, including evaporation, crystallization, and distillation, were the costliest steps. Therefore, our calculation of the utility cost mainly depended on salt crystallizer and distillation tower. For the capability of 100 thousand tons of PET waste per year, the water annually recycled would be 100 thousand tons, which means recycled water and EG would evaporate twice during evaporation and distillation steps. Roughly, the rest of the utility cost would be estimated as equal to evaporation and distillation. And the evaporation cost was calculated as the price of the same amount of steam, where the price of steam was given by DOE benchmark.

3. DFT calculations

The EGD compound was selected as a prototype model compound for the study of PET depolymerization on the Zn2L(OH)2 compound, which features two neighboring zinc atoms (Zn–Zn 3.44 Å), and each of them is fully coordinated with three oxygen (Zn–O 1.91 Å) and two nitrogen atoms (Fig. 4d). Based on the captured intermediates from the experiments, the detailed reaction pathways were further explored using density functional theory (DFT). The DFT optimized geometries of reactants and intermediates, and the corresponding potential energy profile of EGD decomposition were shown in Fig. 4d.

The process starts with the dissolution of an adsorbed hydroxyl (*OH) group from a Zn atom in the form of OH–, forming Zn2L(OH) with an under-coordinated Zn site (denoted by Zn1). However, the reduced Zn1 is not stable but favoring to be occupied by water from the environment with the Zn1–O(H2O) bond of 2.37 Å and the energy cost of 0.56 eV (Fig. 4d). Wherein, the adsorbed water is further stabilized by the formation of hydrogen bonds with nearby oxygen atoms in Zn2L compound (Fig. 4d). Besides, on adsorption of water at the Zn1 site, the interaction of EGD at the Zn1 site is also promoted, forming Zn2L(OH)(H2O)(EGD) complex via the Zn1–O(EGD) bond (2.58 Å) with the energy release of 0.34 eV. Meanwhile, the existing H2O molecule remains at the Zn1 site; yet the Zn1–O(H2O) bond is elongated to 3.00 Å, suggesting a destabilization of adsorbed *H2O. By comparison, without H2O the reaction is less favorable by 0.37 eV. The adsorbed EGD then undergoes a configurational transition by folding the linear-like motif in a way that the carbon atom in EGD can bind to the oxygen atom of *OH attached to the other zinc atom (denoted by Zn2). It forms the Zn1–O(EGD)–C(EGD)–O(OH)–Zn2 ring (Zn1–O(EGD) bond of 1.99 Å, Zn2–O(OH) bond of 2.16 Å) (Fig. 4d). Although such configurational change is an endothermic process (E = 0.64 eV), according to our experiments the corresponding barrier should be moderate, which can be overcome under the experimental conditions. Notably, the formation of the ring structure can be achieved only when two zinc atoms are within a certain distance, indicating the synergistic effect in the binuclear catalyst. Once the ring structure is formed, *H2O is further destabilized with the Zn1–O(H2O) distance of 3.36 Å and readily desorbs from the Zn1 site. Under alkaline solution, the redeposition of OH– at the Zn1 site is energetically highly favorable (ΔE = –1.91 eV), which triggers the proton transfer from the hydroxyl group on Zn2 to the oxygen atom in EGD, therefore the breaking of C–O bond and the dissociation of EGD to BzO and EGM (Fig. 4d). Since the ring structure has been broken by OH– redeposition, the following sequential desorption of EGM and BzO group only cost energy of 0.51 eV and 0.45 eV, respectively, which should be achievable under the experimental conditions. Note that in experiments, the EGM and BzA are likely to further react with alkali in the alkaline solution.

Overall, the DFT calculations confirm that EGD decomposition on Zn2L(OH)2 compound under alkaline solution is a feasible process, where the formation of Zn1–O(EGD)–C(EGD)–O(OH)–Zn2 ring structure is the most endothermic step with an energy cost of only 0.64 eV. During this process, H2O and OH– in the environment play essential roles by stabilizing the under-coordinated Zn site, strengthening Zn–O(EGD) binding, and enabling the dissociation of EGD to BzO and EGM. The formation of the Zn–O–C–O–Zn ring can solely be achieved in binuclear systems, demonstrating the synergistic effect between two Zn atoms.

4.  Supplementary Tables 1‒5

Supplementary Table 1 | Comparison of different PET recycling approaches.

| Degradation method | Catalyst | pH | T (oC) | Space-time yield (gmono L-1h-1) | aSpecific activity (gPET h-1gcat-1) | References |
| --- | --- | --- | --- | --- | --- | --- |
| Alcoholysis or glycolysis | Zn(OAc)2/EG | - | 198 | 35.7 | 12.5 | 9 |
|  | IL/EG | - | 180 | 70.4 | 4.9 | 10 |
|  | TBD:MSA/EG | Alkaline | 180 | 5.2 | 0.1 | 11 |
|  | SO42--ZnO-TiO2-300℃/EG | - | 180 | 63.5 | 108.0 | 12 |
|  | SO42−/Co−Zn−O-300 °C/EG |  | 180 | 66.1 | 106.7 | 13 |
|  | Urea/ZnCl2 DES/EG | - | 170 | 549.0 | 40.0 | 14 |
|  | ZIF-8/EG | - | 197 | 105.7 | 40.0 | 15 |
|  | ZnTNT/EG | - | 196 | 95.9 | 87.0 | 16 |
|  | Mg-Al(3:1) hydrotalcite/EG | - | 196 | 259.1 | 97.9 | 17 |
|  | TBD/EG | Alkaline | 190 | 49.5 | 31.8 | 18 |
|  | Fe3O4-MWCNT/EG | - | 190 | 66.1 | 10.0 | 19 |
|  | TBD/EDA | Alkaline | 110 | 206.0 | 12.3 | 20 |
|  | DBU/EG | Alkaline | 190 | 828.0 | 149.0 | 21 |
|  | TBD/EA | Alkaline | 165 | 1790.0 | 72.6 | 21 |
|  | ZnO/EG | - | 170 | 181.5 | 117.0 | 22 |
|  | LiOMe/DMC/MeOH | Alkaline | 65 | 9.1 | 9.1 | 23 |
| Hydrolysis and alkaline hydrolysis | ZnCl2 | 7.0 | 180 | 7.0 | 0.0036 | 24 |
|  | H+@ZSM-5-25 | 7.0 | 230 | 16.7 | 3.0 | 25 |
|  | - | 7.0 | 230 | 19.2 | - | 26 |
|  | EtOH:H2O/NaOH | 14.1 | 80 | 49.4 | - | 27 |
|  | TBAI | 14.4 | 90 | 51.3 | 33.3 | 28 |
|  | CTAB | 14.1 | 110 | 1.73 | 0.4 | 29 |
|  | - | 14.6 | 150 | 5.7 | - | 30 |
|  | - | 14.4 | 110 | 30.8 | - | 31 |
|  | Zn2/C | 13.0 | 90 | 50 ± 3 | 577 ± 35 (0.1mgCat/mL) | This work |
|  | Zn2/C | 13.0 | 90 | 51 ± 3 | 147 ± 9 (0.4mgCat/mL) | This work |
|  | Zn2/C | 13.0 | 90 | 64 ± 4 | 93 ± 6 (0.8mgCat/mL) | This work |
|  | Zn2/C | 13.0 | 90 | 70 ± 4 | 79 ± 5 (1.0mgCat/mL) | This work |
| Biocatalysis | TfCa+LCC | 8.0 | 60 | 0.05 | 1.55 | 32 |
|  | WCCG Enzyme | 8.0 | 72 | 16.7 | 37.0 | 6 |
|  | LCC | 8.0 | 65 | 0.007 | 20.8 | 6 |
|  | HiC | 7.0 | 50 | 0.18 | 0.21 | 33 |
|  | HiC | 9.0 | 63 | 0.1 | 0.02 | 34 |
|  | HiC | 7.3 | 55 | 1.79 | 0.49 | 5 |
|  | CALB/HiC | 7.0 | 60 | 0.03 | 0.08 | 35 |
|  | Tfu_0883 (Q132A/T101A) | 8.0 | 60 | 1.4 | 32.5 | 36 |
|  | PETase (I179F) | 8.5 | 30 | 0.02 | 8.5 | 37 |
|  | PETase (W159H/S238F) | 7.2 | 30 | 0 | 0.82 | 38 |
|  | PETase | 7.0 | 30 | 0.01 | 6.4 | 39 |

aBlank correction is not included because the blank data is not available in most literatures.

Supplementary Table 2 | Crystal data and structure refinements for Zn2L(NO3)2, Zn2L(OH)2 and [Zn2L(BDC)]n.

| Compound name | Zn2L(NO3) | Zn2L(OH)2 | [Zn2L(BDC)]n |
| --- | --- | --- | --- |
| CCDC number | 2082457 | 2082456 | 2113556 |
| empirical formula | Zn2C25H28N6O9 | Zn2C24H44N4O12 | Zn2C32H30N4O6 |
| formula weight | 687.27 | 711.37 | 697.34 |
| crystal system | monoclinic | triclinic | monoclinic |
| space group | P21/c | P–1 | P21/n |
| a/Å | 19.9701(3) | 7.3311(7) | 8.742(5) |
| b/Å | 17.0535(3) | 8.5182(9) | 13.900(7) |
| c/Å | 8.0230(2) | 12.7374(11) | 12.904(7) |
| α/° | 90 | 71.482(9) | 90 |
| β/° | 97.808(2) | 87.140(7) | 106.237(17) |
| γ/° | 90 | 78.938(9) | 90 |
| volume/Å3 | 2706.98(9) | 740.17(13) | 1505.5(14) |
| Z | 4 | 1 | 2 |
| ρcalcg/cm3 | 1.686 | 1.596 | 1.538 |
| μ/mm-1 | 2.751 | 2.581 | 1.645 |
| F(000) | 1408 | 372 | 716 |
| Reflections collected | 17712 | 4407 | 28269 |
| Independent reflections | 4551 | 2438 | 3420 |
| Goodness-of-fit on F2 | 1.041 | 1.059 | 1.038 |
| Final R1a indexes [I ≥ 2σ(I)] | 0.0436 | 0.0251 | 0.0863 |
| Final wR2b indexes [I ≥ 2σ(I)] | 0.1180 | 0.0642 | 0.2212 |
| Largest diff. peak/hole / e Å-3 | 0.92/–0.58 | 0.32/–0.29 | 1.56/–1.15 |

aR1 = Σ||F0| – |Fc||/Σ|F0|. bwR2 = |Σw(|F0|2 – |Fc|2)|/Σ|w(F0)2|1/2, where w = 1/[σ2(F02) + (aP)2 + bP]. P = (F02 + 2Fc2)/3.

Supplementary Table 3 | Selective bond lengths (Å) and angles (o) for Zn2L(NO3)2.

| Zn1–Zn2 | 3.153(3) | Zn1A–N2 | 1.957(4) |
| --- | --- | --- | --- |
| Zn1A–Zn2A | 3.249(5) | Zn2–O1 | 2.062(2) |
| Zn1–O1 | 1.963(3) | Zn2–O2 | 2.133(3) |
| Zn1–O2 | 1.986(3) | Zn2–O6 | 2.495(7) |
| Zn1–O3 | 2.485(10) | Zn2–O10 | 2.171(8) |
| Zn1–O9 | 2.171(10) | Zn2–N3 | 2.002(3) |
| Zn1–N1 | 2.033(3) | Zn2–N4 | 1.943(3) |
| Zn1–N2 | 2.094(4) | Zn2A–O1 | 2.043(2) |
| Zn1A–O1 | 2.187(5) | Zn2A–O2 | 1.989(2) |
| Zn1A–O2 | 2.073(3) | Zn2A–O6 | 1.939(6) |
| Zn1A–O3 | 2.010(7) | Zn2A–N3 | 2.082(3) |
| Zn1A–N1 | 2.065(3) | Zn2A–N4 | 2.185(4) |
| O1–Zn1–O2 | 81.30(12) | O1–Zn2–O2 | 75.62(11) |
| O1–Zn1–O3 | 82.12(1) | O1–Zn2–O6 | 86.44(1) |
| O1–Zn1–O9 | 91.6(4) | O1–Zn2–O10 | 87.70(18) |
| O1–Zn1–N1 | 92.34(12) | O2–Zn2–O6 | 92.30(1) |
| O1–Zn1–N2 | 170.6(3) | O2–Zn2–O10 | 92.59(17) |
| O2–Zn1–O3 | 85.06(4) | O6–Zn2–O10 | 175.89(4) |
| O2–Zn1–O9 | 85.1(3) | O6–Zn2–N3 | 87.79(6) |
| O2–Zn1–N1 | 172.1(3) | O6–Zn2–N4 | 81.12(4) |
| O2–Zn1–N2 | 90.51(13) | N3–Zn2–O1 | 162.2(3) |
| O3–Zn1–O9 | 169.03(6) | N3–Zn2–O2 | 87.78(12) |
| O3–Zn1–N1 | 89.40(9) | N3–Zn2–O10 | 99.7(2) |
| O3–Zn1–N2 | 92.67(1) | N4–Zn2–O1 | 92.74(10) |
| N1–Zn1–O9 | 99.9(3) | N4–Zn2–O2 | 167.0(2) |
| N1–Zn1–N2 | 95.42(17) | N4–Zn2–O10 | 92.6(3) |
| N2–Zn1–O9 | 92.3(2) | N4–Zn2–N3 | 103.02(12) |
| O2–Zn1A–O1 | 74.24(16) | O1–Zn2A–N3 | 153.5(3) |
| O3–Zn1A–O1 | 89.17(11) | O1–Zn2A–N4 | 86.55(14) |
| O3–Zn1A–O2 | 96.45(17) | O2–Zn2A–O1 | 79.27(9) |
| O3–Zn1A–N1 | 103.3(2) | O2–Zn2A–N3 | 89.58(10) |
| N1–Zn1A–O1 | 85.32(19) | O2–Zn2A–N4 | 152.0(3) |
| N1–Zn1A–O2 | 151.3(4) | O6–Zn2A–O1 | 103.9(2) |
| N2–Zn1A–O1 | 154.7(4) | O6–Zn2A–O2 | 116.9(3) |
| N2–Zn1A–O2 | 91.95(12) | O6–Zn2A–N3 | 102.56(17) |
| N2–Zn1A–O3 | 113.8(4) | O6–Zn2A–N4 | 89.81(12) |
| N2–Zn1A–N1 | 98.74(12) | N3–Zn2A–N4 | 92.71(18) |

Supplementary Table 4 | Selective bond lengths (Å) and angles (o) for Zn2L(OH)2.

| Zn1–Zn11 | 3.3282(6) | Zn1–O2 | 1.9502(15) |
| --- | --- | --- | --- |
| Zn1–O1 | 2.0496(14) | Zn1–N1 | 2.0994(17) |
| Zn1–O11 | 2.1287(14) | Zn1–N21 | 2.0706(17) |
| O1–Zn1–O11 | 74.42(6) | O2–Zn1–N1 | 103.13(7) |
| O1–Zn1–N1 | 88.30(6) | O2–Zn1–N21 | 104.30(7) |
| O1–Zn1–N21 | 142.83(6) | N1–Zn1–O11 | 148.76(6) |
| O2–Zn1–O11 | 107.34(6) | N21–Zn1–O11 | 85.83(6) |
| O2–Zn1–O1 | 111.46(6) | N21–Zn1–N1 | 93.29(7) |

Symmetry code: 1–X,–Y,1–Z

Supplementary Table 5 | Selective bond lengths (Å) and angles (o) for [Zn2L(BDC)]n.

| Zn1–Zn11 | 3.2819(17) | Zn1–N21 | 2.083(6) |
| --- | --- | --- | --- |
| Zn1–O11 | 2.092(4) | Zn1–O3 | 1.991(7) |
| Zn1–O1 | 2.055(4) | Zn1–N1 | 2.085(6) |
| O1–Zn1–O11 | 75.38(17) | O3–Zn1–O1 | 112.5(3) |
| O1–Zn1–N21 | 144.6(2) | O3–Zn1–O1 | 101.6(3) |
| O1–Zn1–N1 | 87.6(2) | O3–Zn1–O1 | 100.8(3) |
| N21–Zn1–O11 | 86.7(2) | O3–Zn1–N21 | 109.5(3) |
| N21–Zn1–N1 | 92.6(2) | N1–Zn1–N21 | 148.4(2) |

Symmetry code: –X,1–Y,–Z

5.  References

- Dolomanov, O. V., Bourhis, L. J., Gildea, R. J., Howard, J. A. K., & Puschmann, H. OLEX2: a complete structure solution, refinement and analysis program. J. Appl. Cryst. 42, 339–341 (2009).

- Sheldrick, G. M. Crystal structure refinement with SHELXL. Acta Cryst. 71, 3–8 (2015).

- Ravel, B., & Newvile, M. ATHENA, ARTEMIS, HEPHAESTUS: data analysis for X-ray absorption spectroscopy using IFEFFIT. J. Synchrotron Radiat. 12, 537–541 (2005).

- Mehta, A., Gaur, U., & Wunderlich, B. Equilibrium melting parameters of poly(ethylene terephthalate). J. Polym. Sci. Pol. Phys. 16, 289–296 (1978).

- Kaabel, S., Therien, J. D., Deschênes, C. E., Duncan, D., Friščić, T., & Auclair, K. Enzymatic depolymerization of highly crystalline polyethylene terephthalate enabled in moist-solid reaction mixtures. Proc. Natl Acad. Sci. USA, 118, 2026452118 (2021).

- Tournier, V., Topham, C. M., Gilles, A., David, B., Folgoas, C., Moya-Leclair, E., Kamionka, E., Desrousseaux, M.-L., Texier, H., Gavalda, S., Cot, M., Guémard, E., Dalibey, M., Nomme, J., Cioci, G., Barbe, S., Chateau, M., André, I., Duquesne, S., & Marty, A. An engineered PET depolymerase to break down and recycle plastic bottles. Nature 580, 216–219 (2020).

- Uekert, T., Kasap, H., & Reisner, E. Photoreforming of nonrecyclable plastic waste over a carbon nitride/nickel phosphide catalyst. J. Am. Chem. Soc. 141, 15201–15210 (2019).

- Uekert, T., Kuehnel, M. F., Wakerley, D. W., & Reisner, E. Plastic waste as a feedstock for solar-driven H2 generation. Energy Environ. Sci. 11, 2853–2857 (2018).

- Ghaemy, M., & Mossaddegh, K. Depolymerisation of poly (ethylene terephthalate) fibre wastes using ethylene glycol. Polym. Degrad. Stabil. 90, 570–576 (2005).

- Liu, Y., Yao, X., Yao, H., Zhou, Q., Xin, J., Lu, X., & Zhang, S. Degradation of poly (ethylene terephthalate) catalyzed by metal-free choline-based ionic liquids. Green Chem. 22, 3122–3131 (2020).

- Jehanno, C., Demarteau, J., Mantione, D., Arno, M. C., Ruipérez, F., Hedrick, J. L., Dove, A. P., & Sardon, H. Selective Chemical Upcycling of Mixed Plastics Guided by a Thermally Stable Organocatalyst. Angew. Chem. Int. Ed. 60, 6710–6717 (2021).

- Zhu, M., Li, S., Li, Z., Lu, X., & Zhang, S. Investigation of solid catalysts for glycolysis of polyethylene terephthalate. Chem. Eng. J. 185, 168–177 (2012).

- Zhu, M., Li, Z., Wang, Q., Zhou, X., & Lu, X. Characterization of solid acid catalysts and their reactivity in the glycolysis of poly (ethylene terephthalate). Ind. Eng. Chem. Res. 51, 11659–11666 (2012).

- Wang, Q., Yao, X., Geng, Y., Zhou, Q., Lu, X., & Zhang, S. Deep eutectic solvents as highly active catalysts for the fast and mild glycolysis of poly (ethylene terephthalate)(PET). Green Chem. 17, 2473–2479 (2015).

- Suo, Q., Zi, J., Bai, Z., & Qi, S. The glycolysis of poly (ethylene terephthalate) promoted by metal organic framework (MOF) catalysts. Catal Lett. 147, 240–252 (2017).

- Lima, G. R., Monteiro, W. F., Toledo, B. O., Ligabue, R. A., & Santana, R. M. Titanate Nanotubes Modified With Zinc and Its Application in Post‐Consumer PET Depolymerization. Macromol. Symp. 383, 1800008 (2019).

- Chen, F., Wang, G., Li, W., & Yang, F. Glycolysis of poly (ethylene terephthalate) over Mg–Al mixed oxides catalysts derived from hydrotalcites. Ind. Eng. Chem. Res. 52, 565–571 (2013).

- Fukushima, K., Coulembier, O., Lecuyer, J. M., Almegren, H. A., Alabdulrahman, A. M., Alsewailem, F. D., Mcneil, M. A., Dubois, P., Waymouth, R. M., Horn, H. W., Rice, J. E., & Hedrick, J. L. Organocatalytic depolymerization of poly (ethylene terephthalate). J. Polym. Sci. Part A: Polym. Chem. 49, 1273–1281 (2011).

- Al-Sabagh, A. M., Yehia, F. Z., Harding, D. R., Eshaq, G., & ElMetwally, A. E. Fe3O4-boosted MWCNT as an efficient sustainable catalyst for PET glycolysis. Green Chem. 18, 3997–4003 (2016).

- Fukushima, K., Lecuyer, J. M., Wei, D. S., Horn, H. W., Jones, G. O., Al-Megren, H. A., Alabdulrahman, A. M., Alsewailem, F. D., McNeil, M. A., Ricea, J. E., & Hedrick, J. L. Advanced chemical recycling of poly (ethylene terephthalate) through organocatalytic aminolysis. Polym. Chem. 4, 1610–1616 (2013).

- Horn, H. W., Jones, G. O., Wei, D. S., Fukushima, K., Lecuyer, J. M., Coady, D. J., Hedrick, J. L., & Rice, J. E. Mechanisms of organocatalytic amidation and trans-esterification of aromatic esters as a model for the depolymerization of poly (ethylene) terephthalate. J. Phys. Chem. A. 116, 12389–12398 (2012).

- Du, J. T., Sun, Q., Zeng, X. F., Wang, D., Wang, J. X., & Chen, J. F. ZnO nanodispersion as pseudohomogeneous catalyst for alcoholysis of polyethylene terephthalate. Chem. Eng. Sci. 220, 115642 (2020).

- Tanaka, S., Sato, J., & Nakajima, Y. Capturing ethylene glycol with dimethyl carbonate towards depolymerisation of polyethylene terephthalate at ambient temperature. Green Chem. 23, 9412–9416 (2021).

- Wang, Y., Zhang, Y., Song, H., Wang, Y., Deng, T., & Hou, X. Zn-catalyzed ester bond cleavage: Chemical degradation of polyethylene terephthalate. J. Clean. Prod. 208, 1469–1475 (2019).

- Kang, M. J., Yu, H. J., Jegal, J., Kim, H. S., & Cha, H. G. Depolymerization of PET into terephthalic acid in neutral media catalyzed by the ZSM-5 acidic catalyst. Chem. Eng. J. 398, 125655 (2020).

- Kim, H. T., Kim, J. K., Cha, H. G., Kang, M. J., Lee, H. S., Khang, T. U., Yun, E. J., Lee, D-H., Song, B. K., Park, S. J., Joo, J. C., & Kim, K. H. Biological valorization of poly (ethylene terephthalate) monomers for upcycling waste PET. ACS Sustainable Chem. Eng. 7, 19396–19406 (2019).

- Ügdüler, S., Van Geem, K. M., Denolf, R., Roosen, M., Mys, N., Ragaert, K., & De Meester, S. Towards closed-loop recycling of multilayer and coloured PET plastic waste by alkaline hydrolysis. Green Chem. 22, 5376–5394 (2020).

- Khalaf, H. I., & Hasan, O. A. Effect of quaternary ammonium salt as a phase transfer catalyst for the microwave depolymerization of polyethylene terephthalate waste bottles. Chem. Eng. J. 192, 45–48 (2012).

- Wang, Y., Wang, H., Chen, H., & Liu, H. Towards recycling purpose: converting PET plastic waste back to terephthalic acid using pH-responsive phase transfer catalyst. Chin. J. Chem. Eng. https://doi.org/10.1016/j.cjche.2021.10.028.

- Mishra, S., & Goje, A. S. Chemical recycling, kinetics, and thermodynamics of alkaline depolymerization of waste poly (ethylene terephthalate)(PET). Polym. React. Eng. 11, 963–987 (2003).

- Yamashita, M., & Mukai, H. Alkaline hydrolysis of polyethylene terephthalate at lower reaction temperature. Sci. Eng. Rev. Doshisha Univ. 52, 51–56 (2011).

- Barth, M., Honak, A., Oeser, T., Wei, R., Belisário‐Ferrari, M. R., Then, J., Schmidt, J., & Zimmermann, W. A dual enzyme system composed of a polyester hydrolase and a carboxylesterase enhances the biocatalytic degradation of polyethylene terephthalate films. Biotechnol. J. 11, 1082–1087 (2016).

- Quartinello, F., Vajnhandl, S., Volmajer Valh, J., Farmer, T. J., Vončina, B., Lobnik, A., Acero, E. H., Pellis, A., & Guebitz, G. M. Synergistic chemo‐enzymatic hydrolysis of poly (ethylene terephthalate) from textile waste. Microb. Biotechnol. 10, 1376–1383 (2017).

- de Castro, A. M., Carniel, A., Stahelin, D., Junior, L. S. C., de Angeli Honorato, H., & de Menezes, S. M. C. High-fold improvement of assorted post-consumer poly (ethylene terephthalate)(PET) packages hydrolysis using Humicola insolens cutinase as a single biocatalyst. Process Biochem. 81, 85–91 (2019).

- de Castro, A. M., Carniel, A., Nicomedes Junior, J., da Conceição Gomes, A., & Valoni, É. Screening of commercial enzymes for poly (ethylene terephthalate)(PET) hydrolysis and synergy studies on different substrate sources. J. Ind. Microbiol. Biotechnol. 44, 835–844 (2017).

- Silva, C., Da, S., Silva, N., Matamá, T., Araújo, R., Martins, M., Chen, S., Chen, J., Wu, J., Casal, M., & Cavaco‐Paulo, A. Engineered Thermobifida fusca cutinase with increased activity on polyester substrates. Biotechnol. J. 6, 1230–1239 (2011).

- Ma, Y., Yao, M., Li, B., Ding, M., He, B., Chen, S., Zhou, X., & Yuan, Y. Enhanced poly (ethylene terephthalate) hydrolase activity by protein engineering. Engineering, 4, 888–893 (2018).

- Austin, H. P., Allen, M. D., Donohoe, B. S., Rorrer, N. A., Kearns, F. L., Silveira, R. L., Pollard, B. C., Dominick, G., Duman, R., Omari, K. E., Mykhaylyk, V., Wagner, A., Michener, W. E., Amore, A., Skaf, M. S., Crowley, M. F., Thorne, A. W., Johnson, C. W., Woodcock, H. L., McGeehan, J. E., & Beckham, G. T. Characterization and engineering of a plastic-degrading aromatic polyesterase. Proc. Natl Acad. Sci. USA, 115, E4350–E4357 (2018).

- Yoshida, S., Hiraga, K., Takehana, T., Taniguchi, I., Yamaji, H., Maeda, Y., Toyohara, K., Miyamoto, K., Kimura, Y., & Oda, K. A bacterium that degrades and assimilates poly(ethylene terephthalate). Science 351, 1196–1199 (2016).