Supplementary materials

The effect of polyethersulfone and nylon 6 micromembrane filters on the pyraclostrobin detection：Adsorption performance and mechanism

Xiaolan Shao a, b †, Lejun Liu a †, Hui Li c, Yue Luo a, Jingyu Zhao a, Shuai Liu a , Bei Yan a, Dan Wang a, Kun Luo a, Min Liu a, Lianyang Bai a, b, Xiaoyun Li d *, Kailin Liu a, b *

a College of Plant Protection, Hunan Agricultural University, Changsha 410128, PR China

b  Hunan Weed Science Key Laboratory, Hunan Academy of Agricultural Sciences, 410125 Changsha, China

c Department of Crop and Soil Sciences, North Carolina State University, Raleigh, NC

1327695, United States.

d Department of Evironmental Science, School of Geography and Tourism, Shaanxi Normal University, Xi'an 710119

† These authors contributed equally to this work.

Text S1. Extraction experiment

Series of liquid-liquid extraction experiments were carried out i) to enhance the detection sensitivity and decrease the LOD of HPLC, ii) to restrict hydrolysis and degradation of pyraclostrobin, due to its short half-life time (23.1-115.4 d) in solution. The 4 mL of aqueous sample was collected from each treatment using a glass pipette and then extracted with 8 mL of dichloromethane. The lower layer of solution was aspirated through a 1 mL disposable medical syringe, and dissolved in 1 mL methanol after blown dry with N2 (NDK200-2, Hangzhou Miou Instrument Co., Ltd). The methanol solution was filtered through a filter membrane and tested on HPLC. The recovery rate of pyraclostrobin in extraction experiments was verified at concentrations ranging from 0.05 to 1.5 mg/L.

The average extraction recovery rate of pyraclostrobin at an initial concentration of 1.0 mg/L reaches 101.2% and the RSD (relative standard deviation) was 1.6% (Table S3). The average recovery rates of pyraclostrobin were 99.7% (RSD=4.1%) and 86.6% (RSD=6.2%) at initial concentration levels of 0.5 and 0.05 mg/L, respectively. These high recovery rates with low RSD values verified the high credibility of the extraction method within certain ranges of initial concentrations.

Text S2. Statistical analysis

The adsorption rate (AR, %) and the adsorption amount of pyraclostrobin (Q, mg/g) on the micromembrane was calculated as:

AR=1−C1C0×100………………………… (1)

where C1 is the concentration of pyraclostrobin (mg/L) after the volume filtration, and C0 is the concentration (mg/L) of the control treatment.

Q = (C2−C3) × V/M………………………… (2)

where C2 is the initial concentration of pyraclostrobin (mg/L), C3 is the residual concentration of pyraclostrobin (mg/L), V is the volume of the aqueous sample (L), and M is the weight of PES micromembrane (g).

2.1 Adsorption kinetic models

Adsorption kinetic models (pseudo-first-order kinetic model, pseudo-second-order kinetic model, Elovich model, and intra-particle diffusion model) were used to evaluate the performance of the adsorption and to investigate the adsorption mass transfer mechanisms. Non-linear forms of these four models can be expressed as follows:

Pseudo-first order kinetic model (PFO):

Qt=qe1−e−k1t …………………………………. (3)

Pseudo-second order kinetic model (PSO):

Qt=k2qe2t1+k2qet……………………………………………. (4)

where k1 (1/min) and k2 (g/mg/min) are the pseudo-first-order and pseudo-second-order kinetic constants, respectively, qe (mg/g) is the adsorption equilibrium, Qt is the unit adsorption capacity of micromembrane at any time (mg/g), and t is the adsorption time (h).

Elovich model:

Qt=1BlnAB+1Blnt…………………………… (5)

where A (mg/g/min) is the initial adsorption rate constant, B (mg/g) represents the coverage rate and activation energy value of the activated adsorption site.

Intra-particle diffusion model (Weber and Morris (W&M) model):

Qt=kit0.5+C……………………………………………. (6)

where ki (mg/g) is the rate constant of diffusion within the particle. C is the intercept (mg/g), and its value indicates the thickness of the boundary layer of the liquid film. This equation suggests that the adsorption components are interacting in multiple stages.

2.2 Adsorption isotherm models

Adsorption isotherm models can provide information on the mechanisms of the adsorption process. In this paper, four adsorption isotherm models (linear, Freundlich, Langmuir, and Temkin isotherm models) were used to investigate the adsorption mechanism of pyraclostrobin on micromembrane filters.

Linear isotherm model (Henry's law):

Qe=KLCe …………………………………………………… (7)

where Qe (mg/g) and Ce (mg/L) represent for the adsorbed mass of adsorbate and its concentration in the solution, respectively, and KL (L/g) is the partition coefficient.

Freundlich isotherm model:

Qe=KFCe1n ……………………………………………. (8)

where Qe (mg/g) and Ce (mg/L) represent the adsorbed mass of adsorbate and its concentration in the solution, respectively, and KF (L/g) is the partition coefficient.

Langmuir isotherm model:

Qe=qmKlCe1+KlCe …………………………………………… (9)

where K l(L/mg) is the ratio of adsorption rate to the desorption rate, and qm is the adsorption capacity calculated from the Langmuir model.

Temkin isotherm model:

Qe=RTBln⁡(ACe) …………………………………. (10)

where R (8.314J/mol·K) is the molar gas constant, T (K) is the absolute temperature, and A (L/g) and B (J/mol) are both constants.

2.3 Adsorption thermodynamics

The thermodynamic calculation was performed by using the Van't Hoff equation, as follows:

∆G=−RTLnK ………………………………………. (11)

LnK=−∆HRT+∆SR………………………………………. (12)

where Kd stands for the adsorption equilibrium constant or distribution, R (8.314J/(mol∙K)) for the molar gas constant, T (K) for the absolute temperature, ΔG for the Gibbs free energy change (J/mol), ΔH for the enthalpy change (J/mol), and ΔS for the entropy change (J/(mol·K)).

## Table S1 The physicochemical characteristics of pyraclostrobin

| Parameter | Pyraclostrobin |
| --- | --- |
| Molecular formula | C19H18ClN3O4 |
| Molecular weight (g·mol-1) | 387.817 |
| Octanol/water partition coefﬁcient | 3.99 |
| pKa (25 °C) | No dissociation5 |
| Solubility in water | 1.9 mg/L |

## Table S2 The physicochemical characteristics of micromembranes

| material | PES | Nylon 6 |
| --- | --- | --- |
| Wettability | Hydrophobic | Hydrophilic |
| Total pore area (m2/g) | 10.774 | 4.875 |
| Housing | polypropylene |  |
| Capacity (mL) | 10 | 10 |
| Diameter (mm) | 13 | 13 |
| Effective filtration area (cm2) | 0.7 | 0.7 |
| Pore size (µm) | 0.22 | 0.22 |

## Table S3 Recovery rates of the extraction test with different initial concentrations.

| Initial concentration（mg/L） | Average recovery rate (%) | Standard deviation (SD) | RSD (%) |
| --- | --- | --- | --- |
| 1.0 | 101.2 | 1.6 | 1.6 |
| 0.5 | 99.7 | 4.1 | 4.1 |
| 0.05 | 86.6 | 6.2 | 7.1 |

## Table S4 Parameters of different isotherm models for pyraclostrobin adsorption onto PES and Nylon6 micromembranes in the temperature range of 288.15–308.15 K (pH=6.92).

| Micromembrane | Model | Paramters | Temperature |  |  |
| --- | --- | --- | --- | --- | --- |
|  |  |  | 288.15 K | 298.15 K | 308.15 K |
| PES | Linear isotherm | R2 | 0.999 | 0.970 | 0.972 |
|  |  | Kl | 5.381 | 5.170 | 5.856 |
|  | Freundlich isotherm | R2 | 0.992 | 0.957 | 0.946 |
|  |  | KF | 4.034 | 3.499 | 4.046 |
|  |  | n | 1.514 | 1.707 | 1.495 |
|  | Langmuir isotherm | R2 | 0.985 | 0.948 | 0.967 |
|  |  | KL | 1.515 | 2.121 | 1.814 |
|  |  | qm | 5.867 | 4.529 | 5.251 |
| Nylon 6 | Linear isotherm Freundlich isotherm | R2 | 0.996 | 1 | 0.982 |
|  |  | Kl | 1.197 | 1.029 | 0.733 |
|  |  | R2 | 0.942 | 0.999 | 0.901 |
|  |  | KF | 1.072 | 1.011 | 1.130 |
|  |  | n | 1.182 | 1.019 | 0.832 |
|  | Langmuir isotherm | R2 | 0.947 | 0.999 | -5.927 |
|  |  | KL | 0.400 | 0.041 | 8.673 |
|  |  | qm | 3.596 | 25.79 | 10082.5 |

Table S5 Adsorption thermodynamics of pyroclostrobin on PES and Nylon 6 micromembranes and related parameters.

| Micromembrane | T (K) | ∆G（kJ/mol） | ∆H（kJ/mol） | ∆S(J/(mol*K-1)) |
| --- | --- | --- | --- | --- |
| PES | 288.15 | -20.58 | 3.05 | 81.79 |
|  | 298.15 | -21.20 |  |  |
|  | 308.15 | -22.23 |  |  |
| Nylon 6 | 288.15 | -16.98 | -18.02 | -3.33 |
|  | 298.15 | -17.19 |  |  |
|  | 308.15 | -16.86 |  |  |

## Table S6 Binding energies (Eb) obtained from high-resolution C1s and O1s XPS spectra of PES micromembranes before (CKP) and after (0.04P) pyraclostrobin adsorption.

| Element | CKP |  |  | 0.04P |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | Eb（eV） | Type | Percent（%） | Eb（eV） | Type | Percent（%） |
| C1s | 284.60 | C-C(H)/C=C | 52.4 | 284.80 | C-C(H)/C=C | 71.1 |
|  | 285.19 | C-S | 15.3 | 285.30 | C-S | 2.8 |
|  | 285.80 | C-N/C=N | 3.9 | 285.70 | C-N | 5.2 |
|  | 286.10 | C-O | 24.1 | 286.30 | C-O | 13.1 |
|  | 291.76 | π-π* | 4.4 | 291.90 | π-π* | 3.3 |
|  | - | - | - | 287.00 | C-Cl | 3.4 |
|  |  |  |  | 287.70 | C=O | 1.1 |
| O 1s | - | - | - | 531.00 | C=O | 11.7 |
|  | 531.70 | O=S=O | 77.2 | 531.90 | O=S=O | 84.8 |
|  | 533.60 | C-O | 22.8 | 533.60 | C-O | 3.5 |

## Table S7 Binding energies (Eb) obtained from high-resolution C1s, and O1s XPS spectra of Nylon6 micromembranes before (CKN) and after (0.04N) pyraclostrobin adsorption.

| Element | CKN |  |  | 0.04N |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | Eb（eV） | Type | Percent（%） | Eb（eV） | Type | Percent（%） |
| C 1s | 284.80 | C-C(H)/C=C | 63.5 | 284.80 | C-C(H)/C=C | 67.9 |
|  | 285.57 | C-N | 25.8 | 285.57 | C-N | 13.0 |
|  | 287.86 | C=O | 10.7 | 287.86 | C=O | 5.4 |
|  | - | - | - | 286.98 | C-Cl | 4.8 |
|  | - | - | - | 288.06 | C=O | 8.8 |
| O 1s | 531.1 | C=O | 75.3 | 531 | C=O | 49.9 |
|  | 532 | OH in the adsorbed H2O | 24.7 | 532 | OH | 38.5 |
|  | - | - | - | 533 | C-O | 11.6 |

## Fig. S1 The cumulative pore volume and pore size distributions (inset) of PES (a) and Nylon 6 (b) micromembranes obtained from mercury intrusion.

## Fig. S2 Effects of micromembrane dosages on the adsorption(24 h) of pyraclostrobin (1.0 mg/L) onto micromembranes at 298.13 K. (Error bars represent standard deviation from the mean (n = 3)).

## Fig. S3 Stability of pyraclostrobin in aqueous solutions in dark conditions (220 rpm, 298.15 K in a temperature-controlled shaker, error bars represent standard deviation from the mean (n = 3)).

Fig. S4 Adsorption isotherms under different temperature（288.13、298.13 and308.13 K） (a) PES , (b) Nylon 6 micromembrane (PES micromembrane amount = 0.01 g, V = 40 mL；Nylon 6 micromembrane amount = 0.03 g, V = 30 mL； initial concentration of pyraclostrobin is 1.0 mg/L, adsorption time = 30 h, error bars represent standard deviation from the mean (n = 3) and fitted using an adsorption isotherm equation).

## Fig. S5 Plot of lnK against 1/T for the estimation of thermodynamic parameters for the pyraclostrobin adsorption on PES and Nylon 6 micromembranes.

Fig. S6 Infrared spectra of PES and Nylon 6 before and after pyraclostrobin adsorption.

Fig. S7 The N1s(a) XPS spectra of PES micromembrane before (CKP) and after (0.04P) pyraclostrobin adsorption. The N1s(b) XPS spectra of Nylon6  micromembranes before (CKN) and after (0.04N) pyraclostrobin adsorption.