Table S1. Incineration rates of virgin plastics after pyrolysis at the different temperatures¶
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	Incineration rate, %
	
	

	Type of plastics
	Pyrolysis temperature
	
	

	
	500 oC
	600 oC
	700 oC

	LDPE
	99.8 ± 0.1
	99.4 ± 0.1
	100. 0 ± 0.0

	PP
	98.3 ± 0.2
	98.6 ± 0.0
	98.3 ± 0.2

	PVC
	72.8 ± 0.2
	74.0# ± 0.4
	74.3 ± 0.0


LDPE: Low density polyethylene, PP: Polypropylene, and PVC: Polyvinyl chloride
¶ Average ± S.E. (n=3)
# This value is used as RPVC in calculations of the recovery rate for PVC particles. 

