Table S1. Incineration rates of virgin plastics after pyrolysis at the different temperatures¶

|  | Incineration rate, % |  |  |
| --- | --- | --- | --- |
| Type of plastics | Pyrolysis temperature |  |  |
|  | 500 oC | 600 oC | 700 oC |
| LDPE | 99.8 ± 0.1 | 99.4 ± 0.1 | 100. 0 ± 0.0 |
| PP | 98.3 ± 0.2 | 98.6 ± 0.0 | 98.3 ± 0.2 |
| PVC | 72.8 ± 0.2 | 74.0# ± 0.4 | 74.3 ± 0.0 |

LDPE: Low density polyethylene, PP: Polypropylene, and PVC: Polyvinyl chloride

¶ Average ± S.E. (n=3)

# This value is used as RPVC in calculations of the recovery rate for PVC particles.