Biocompatible carbon dot decorated α-FeOOH nanohybrid for an effective fluorometric sensing of Cr (VI) in wastewater and living cells

Bidisha Ghosh1#, Shubham Roy1#, Souravi Bardhan1, Dhananjoy Mondal1, Ishita Saha2, Saheli Ghosh1, Ruma Basu3, Parimal Karmakar2, Kaustuv Das1*, Sukhen Das1*

1 Department of Physics, Jadavpur University, Kolkata-700032, India
2 Department of Life Science and Biotechnology, Jadavpur University, Kolkata-700032, India

3 Department of Physics, Jogamaya Devi College, Kolkata- 700026, India

Supporting information

*Corresponding Authors:

Prof. Sukhen Das

sdasphysics@gmail.com (+91 9433091337)

Dr. Kaustuv Das

kaustuv12@gmail.com (+ 91 9433116177)

# These two authors have contributed equally in this work.

Table S1: Microstructural information obtained from Rietveld refinement

| Parameters | Values |
| --- | --- |
| a (Å) | 10.00903 |
| b (Å) | 2.9612691 |
| c (Å) | 4.510796 |
| V (Å^3) | 133.697 |
| Size ( Å) | 598.5741 |
| Microstrain | 1.25x10-3 |
| Rp (%) | 0.03 |
| Rwp (%) | 0.04 |
| χ2 | 1.33 |

Table S2: Comparative range of sensing activity of other sensors

| Probe | Method of synthesis | Linear Range | LOD | Ref |
| --- | --- | --- | --- | --- |
| 1.C dots from Poria cocos polysaccaride as an effective “’on off” fluorescence sensor for chromium (VI) detection. (2021) | Hydrothermal, 200°C for 5hrs | 1-100 µM | 0.25µM | [51] |
| 2. Nitrogen Carbon dot decorated natural microcline an ameliorative dual fluorescent probe for Fe3+ and Cr6+ detection (2020) | Hydrothermal 190°C for 12hrs | 0-68µM | 4µM | [36] |
| 3. A fluorometric paper test for chromium (VI) based on the use of N-doped C-dots. (2019) | Microwave synthesis,900watts,90s | 80-1000µM | 140µM | [52] |
| 4.C-Dots with red emission as a fluorescent and colorimetric dual read out probe for detection of chromium (VI) and cysteine and its logic gate operation. (2018) | Hydrothermal, 180°C, 4hrs | 0.5-263µM | 0.26µM | [53] |
| 5.Green and facile synthesis of water-soluble carbon dots from ethanolic shallot extract for chromium ion sensing in milk, fruit juices and waste water samples (2020) | Hydrothermal,180°C,4hrs | 20-100µM | 3-5µM | [54] |
| 6. Biocompatible carbon dot decorated α-FeOOH nanohybrid for an effective fluorometric sensing of Cr (VI) in wastewater and living cells . | Hydrothermal, 180°C, 2.5hrs | 0-10µM | 81nM | This work |

Table S3: Physical parameters of the collected water samples

| Type of Water | pH | TDS (ppm) |
| --- | --- | --- |
| Drinking Water | 8.22 | 85 |
| Tap Water | 7.76 | 675 |
| Pond water | 8.64 | 897 |
| Waste Water | 2.86 | 1894 |

Table S4: ICP-AES data of the collected wastewater

| Constituents | Amount (ppm) |
| --- | --- |
| Cadmium | Not Found |
| Iron | 8.76 |
| Chromium | 16.53 |
| Lead | 0.14 |

Additional figures:

Figure S1 a) DTA and b) TGA data; c) graph showing fluorescence lifetime data of the synthesized probe