Table S1. Correlation coefficients (Pearson’s correlation analysis) of soluble contents of Si and other nutrients released from the Phyt400, Phyt600 and Phyt800.
	Phyt400 

	 
	 
	Si
	K
	Ca
	Mg
	P

	Si
	With CO2 support
	1
	0.971**
	0.894**
	0.943**
	0.410

	
	Without CO2 support
	1
	0.865*
	0.918**
	0.987**
	0.966**

	K
	With CO2 support
	 
	1
	0.972**
	0.993**
	0.566

	
	Without CO2 support
	 
	1
	0.860*
	0.810*
	0.934**

	Ca
	With CO2 support
	 
	 
	1
	0.984**
	0.699

	
	Without CO2 support
	 
	 
	1
	0.874*
	0.861*

	Mg
	With CO2 support
	 
	 
	 
	1
	0.576

	
	Without CO2 support
	 
	 
	 
	1
	0.954**

	P
	With CO2 support
	 
	 
	 
	 
	1

	
	Without CO2 support
	 
	 
	 
	 
	1

	
	
	

	Phyt600 

	 
	 
	Si
	K
	Ca
	Mg
	P

	Si
	With CO2 support
	1
	0.885**
	0.902**
	0.894**
	0.824*

	
	Without CO2 support
	1
	0.827*
	0.975**
	0.946**
	0.911**

	K
	With CO2 support
	 
	1
	0.991**
	0.998**
	0.988**

	
	Without CO2 support
	 
	1
	0.763*
	0.816*
	0.969**

	Ca
	With CO2 support
	 
	 
	1
	0.992**
	0.965**

	
	Without CO2 support
	 
	 
	1
	0.958**
	0.867*

	Mg
	With CO2 support
	 
	 
	 
	1
	0.982**

	
	Without CO2 support
	 
	 
	 
	1
	0.926**

	P
	With CO2 support
	 
	 
	 
	 
	1

	
	Without CO2 support
	 
	 
	 
	 
	1

	
	
	

	Phyt800 

	 
	 
	Si
	K
	Ca
	Mg
	P

	Si
	With CO2 support
	1
	0.881**
	0.711
	0.731
	0.490

	
	Without CO2 support
	1
	0.991**
	0.943**
	0.830*
	0.761*

	K
	With CO2 support
	 
	1
	0.956**
	0.957**
	0.749

	
	Without CO2 support
	 
	1
	0.964**
	0.870*
	0.805*

	Ca
	With CO2 support
	 
	 
	1
	0.976**
	0.866*

	
	Without CO2 support
	 
	 
	1
	0.965**
	0.921**

	Mg
	With CO2 support
	 
	 
	 
	1
	0.753

	
	Without CO2 support
	 
	 
	 
	1
	0.987**

	P
	With CO2 support
	 
	 
	 
	 
	1

	
	Without CO2 support
	 
	 
	 
	 
	1

	** Correlation is significant at the 0.01 level (2-tailed).  

	* Correlation is significant at the 0.05 level (2-tailed).  
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