Synthesis and comparative assessment of ESIPT core containing lightfast fluorescent monoazo dyes

Supriya H. Ramugade , Sekar Nagaiyan N.

1Department of Dyestuff Technology, Institute of Chemical Technology, Matunga, Mumbai 400 019, India.

Supriya H. Ramugade: ORCID ID – 0000-0001-8504-9927

Sekar Nagaiyan N: ORCID ID - 0000-0001-7568-5129

Corresponding author: Sekar Nagaiyan N.

Corresponding author email id: n.sekar@ictmumbai.edu.in, nethi.sekar@gmail.com (N. Sekar).

Table S1 Reported dyes and lightfastness by nanoemulsion method

| Dyes | structure | Lightfastness |  | References |
| --- | --- | --- | --- | --- |
|  |  | C-method | N-method |  |
| Disperse Blue 337 C.I.11337 |  | 8 | 8 | [9] |
| Disperse Red 184 |  | 8 | 8 | [9] |
| Solvent Yellow 163 C.I.58840 |  | - | - | [9] |
| Disperse Red 60 C.I. 60756 |  | - | - | [9] |
| (C.I. Disperse Orange 25) C.I.11227 |  | 8 | 8 | [59] |
| (C.I. Disperse Red 73) C.I. 11116 |  | 8 | 8 | [59] |
| (C.I. Disperse Red 79.2) C.I.60510 |  | 8 | 8 | [60] |
| C-method-conventional method, N-method - nanoemulsion method |  |  |  |  |

Table S2: 1H NMR of dye “(E)-1-((3-(Benzo[d]oxazol-2-yl)-4-hydroxyphenyl) diazenyl) naphthalen-2-ol(6aA)

| Sr.No. | Proton NMR |  |  |  |
| --- | --- | --- | --- | --- |
|  | δ ppm | Proton | multiplicity | J value in Hz |
| 1 | 7.69,7.59 | Hb, Hc | s, |  |
| 2 | 8.42 | He | s |  |
| 3 | 7.47,7.47 | Ha, Hd | d | 13.4 |
| 4 | 6.74, 6.74 | Hj, Hk | d | 9.3 |
| 5 | 6.69,6.62 | Hg, Hf | m, |  |
| 6 | 7.91,7.91 | Hm, Hn | d | 9.6 |
| 7 | 8.11 | Hg | s |  |
| 8 | 7.82 | Hl,Ho | s |  |

Table S3- 1H NMR of dye (E)-1-((3-(Benzo[d]oxazol-2-yl)-5-((4-hydroxyphenyl) diazenyl) naphthalen-2-ol(7aA)

| Sr.No. | Proton NMR |  |  |  |
| --- | --- | --- | --- | --- |
|  | δ ppm | Proton | multiplicity | J value in Hz |
| 1 | 8.79,8.79 | Hb, Hc | s |  |
| 2 | 11.1 | He | d |  |
| 3 | 7.46,7.46 | Ha, Hd | d | 8.2 |
| 5 | 7.10, 7.1 | Hg, Hj | s |  |
| 6 | 8.01, | Hk | s |  |
| 7 | 7.85,7.85 | Hm, Hn | d | 23.1 |
| 8 | 8.68, 8.63 | Hl, Ho | s |  |

Table S4- 1H NMR of dye -“(Z)-2-(Benzo[d]oxazol-2-yl)-5-((4-(diethylamino)-2-hydroxyphenyl) diazenyl) phenol” (7bA)

| Sr.No. | Proton NMR |  |  |  |
| --- | --- | --- | --- | --- |
|  | δ ppm | Proton | multiplicity | J value in Hz |
| 1 | 13.25 | Hh | s |  |
| 2 | 11.95 | Hi | s |  |
| 3 | 8.60 | He | s | 2.0 |
| 4 | 8.15 | Ha | d | 7.8 |
| 5 | 8.11 | Hd | d | 8.1 |
| 6 | 7.86 | Hf | d | 6.8 |
| 7 | 7.62 | Hj | d | 9.1 |
| 8 | 7.59-7.52 | Hb | m |  |
| 9 | 7.46 | Hc | t | 7.6 |
| 10 | 7.20 | Hg | d | 8.8 |
| 11 | 6.53 | Hk | d | 8.9 |
| 12 | 6.14 | Hl | s |  |
| 13 | 3.46 | Ho, Hp, Hn | q | 7.0 |
| 14 | 1.15 | Hm | t | 6.9 |

Table  S5:  Photophysical data 6bA

| Solvent |  | λ Absorption |  | λ Emission |  | Stokes Shift ∆ν (cm-1) |  | FWHM |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | nm | cm-1 | nm | cm-1 | nm | cm-1 | nm | cm-1 |
| THF |  | 465 | 21505.38 | 608 | 16447.37 | 143 | 5058.008 | 79.64 | 125565 |
| EA |  | 461 | 21691.97 | 606 | 16501.65 | 145 | 5190.324 | 79.44 | 125881.2 |
| ACN |  | 464 | 21551.72 | 607 | 16474.46 | 143 | 5077.26 | 77.7 | 125470.5 |
| DCM |  | 465 | 21505.38 | 618 | 16181.23 | 153 | 5324.147 | 77.67 | 128749.8 |
| ETOH |  | 463 | 21598.27 | 603 | 16583.75 | 140 | 5014.524 | 78.162 | 127939.4 |
| DMF |  | 469 | 21321.96 | 620 | 16129.03 | 151 | 5192.929 | 80.43 | 124331.7 |

Table S6: Photophysical data 7aA

| Solvent | λ Absorption |  | λ Emission |  | Stokes Shift ∆ν (cm-1) |  | FWHM |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | nm | cm-1 | nm | cm-1 | nm | cm-1 | nm | cm-1 |
| THF | 320 | 31250 | 644 | 15527.95 | 324 | 15722.05 | 236 | 42372.88 |
| EA | 324 | 30864.2 | 645 | 15503.88 | 321 | 15360.32 | 236.29 | 42320.88 |
| ACN | 326 | 30674.85 | 645 | 15503.88 | 319 | 15170.97 | 236.56 | 42272.57 |
| DCM | 328 | 30487.8 | 650 | 15384.62 | 322 | 15103.19 | 242.81 | 41184.47 |
| ETOH | 496 | 20161.29 | 647 | 15455.95 | 151 | 4705.34 | 104.887 | 95340.7 |
| DMF | 503 | 19880.72 | 651 | 15360.98 | 148 | 4519.733 | 94.5852 | 105724.8 |

| Solvent | λ Absorption |  | λ Emission |  | Stokes Shift ∆ν (cm-1) |  | FWHM |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | nm | cm-1 | nm | cm-1 | nm | cm-1 | nm | cm-1 |
| THF | 495 | 20202.02 | 610 | 16393.44 | 115 | 3808.578 | 85.25 | 117304.5 |
| EA | 490 | 20408.16 | 607 | 16474.46 | 117 | 3933.699 | 87.23 | 114636.8 |
| ACN | 490 | 20408.16 | 626 | 15974.44 | 136 | 4433.722 | 88.71 | 112729.4 |
| DCM | 492 | 20325.2 | 619 | 16155.09 | 127 | 4170.114 | 87.04 | 114895.8 |
| ETOH | 482 | 20746.89 | 554 | 18050.54 | 72 | 2696.346 | 88.07 | 117.7 |
| DMF | 485 | 20618.56 | 621 | 16103.06 | 136 | 4515.497 | 88.03 | 108201.7 |

Table S7: Photophysical data of 7bA