Solvent dependency of adsorption of mercaptopurine on CC, AlN and BN nanotubes and the evaluation of noncovalent interactions

Jamelah S.Al-Otaibia*, Y.Sheena Maryb, Y.Shyma Maryb, Renjith Thomasc

a Department of Chemistry, College of Science, Princess Nourah bint Abdulrahman University, P.O. Box 84428, Riyadh 11671, Saudi Arabia

bThushara, Neethinagar-64, Kollam, Kerala, India

c Deparment of Chemistry, St Berchmans College (Autonomous), Mahatma Gandhi University, Changanassery, Kerala, India

*Author for correspondence: email:  jamelah2019@rediffmail.com

Abstract

The performance of nanotubes (NT) of carbon (CC), aluminium-nitrogen (AlN) and boron-nitrogen (BN) as a sensor and nanocarrier for mercaptopurine (MCP) was investigated by means of theoretical approach. The calculated negative values of adsorption energy showed the interaction and adsorption of the drug. HOMO and LUMO distributions were only found on the NT counter portion of drug-nanotube not on MCP for AlN-NT and BN-NT while HOMO is over MCP and LUMO is over NT for CC-NT.The polarizability of MCP-NTs is greater than that of MCP. Raman wavenumbers of MCP are enhanced in NTs and hence NTs can act as a sensor for detection of MCP. Solvent dependency on adsorption behavior is also presented in the manuscript, where we found that AlN nanotube showed exceptionally high free energy of adsorption over other nanotubes in all solvent medium. Solvation free energies were also reported. Non covalent interaction scattered plot also showed significant inter molecular interaction between AlN nanotubes and the mercaptopurine when compared to other nanotubes under study.

Keywords: Nanotubes: Adsorption; mercaptopurine; Reactivity analysis

Introduction

The invention of carbon nanotubes (CNT) in 1991 piqued researcher’s interest, prompting them to focus their efforts on establishing the novel material’s different properties[1].Until far, the efforts have resulted in the development of a massive amount of data on the characterization of properties of nanostructures[2-6].CNT applications of in living systems have long been a major priority for harnessing this unique material to improve human life quality[7].Investigating possible applications of carbon nanotubes for drug delivery has been deemed critical in light of the need for focused drug delivery techniques, according to the findings[8]. The impact of covalent and non-covalent loading of different drugs on distinct nanostructures on the characteristics of each counterpart has been explored[9].For this goal, all in silico, in vitro and in vivo approaches have been studied[10].Indeed, nanostructures have been anticipated as vehicles for pharmaceutical substances to convey them into biological systems, a function that must satisfy a slew of constraints[11].As a result, producing precise information for a topic like nanostructures application in biological systems has long been a high priority for researchers in related domains. To do this, computer based in silico research could very well yield useful information for the materials under investigation at the atomic level[12-15].The non-covalent loading of pharmaceuticals at CNTs has previously been explored using computer based studies, with the results confirming the importance of nanostructures for drug delivery[16].Purines and analogues are the most frequent class of nitrogen containing heterocyclic molecules that serve critical roles in a wide range of biological processes[17]. The thiopurine derivative mercaptopurine (1,7-dihydro-6H-purine-6-thione) is used for treatment of cancer [18].DFT studies of nanotubes with drugs are reported in literature [19,20].In the present works, the interaction of mercaptopurine (MCP) with nanotubes is reported. To achieve optimum geometries for the explored model and the accompanying descriptors, quantum chemical computations were used. The main purpose of this research was to investigate the possibility of loading MCP onto CC-NT, AlN-NT and BN-NT and to evaluate various properties using computer modeling.

Methods

Fig.1	Optimized geometries of (a) mercaptopurine (MCP) (b) MCP-CC-NT (c) MCP-AlN-NT (d) MCP-BN-NT

In this study, representative models of nanotubes (carbon:CC-NT, 50 atoms, aluminium-nitrogen:AlN-NT, Al 20, N 20 atoms and boron-nitrogen: BN-NT, B25, N 25 atoms) of MCP were chosen to provide a nanostructure for MCP (Fig.1). After minimizing energy for each nanotube and drug, a combination of already optimized nanotube and drug was constructed to maximize the drug relaxation at the nanotube’s surface. The model of the loaded drug at nanotube was obtained for further exploration by doing such optimizations. Furthermore, various chemical parameters are analyzed in order to better describe electrical attributes for the studied models. The CAM-B3LYP/6-311++G(d)basis implemented in the Gaussian 16 program with Gaussview 6.1 were used to do computations using the DFT technique[21, 22].We estimated the drug’s solvated structures in addition to gas phase computations.  For solvent effect, PCM was utilized [23]. The solvation energies are also determined in different solvents, of low to high dielectric constants of 2.38, 8.93, 32.70 and 80.40.Multiwfn software was used to perform NCI and ELF analysis [24].

Results and discussion

Solvation effects and adsorption studies

Truhlar's SMD, which uses a set of parameters calculated along-side IEF-PCM, was used to get solvation free energies (SFE) in toluene, dichloromethane, methanol and water [25]. Solvation free energy (SFE) give the free energy change associated with transfer of a molecule between gas and solvent. SFE not only tell us how much a molecule prefers one phase over another, but they also can provide insight into how solvent behaves in different environments.SFE calculates the free energy change in a molecule’s shift from an ideal gas to solvent environment, which is useful for determining features like activity coefficients and solubilities [26].The SFEs were calculated via SMD model in toluene, dichloromethane, methanol and water for all NT systems with MCP (table S1). In the case of all MCP-NT systems, in all solvents the SFE is greater than that in vacuum with maximum value for water and minimum value for toluene. The SFEs are maximum in MCP-AlN-NT systems and minimum for MCP-CC-NT systems. All the SFEs are increasing with increase in dielectric constant of the solvent.Despite the fact that all of the values obtained were negative, a comparison of the predicted SFE values suggests that water and ethanol may be preferable for CPP solubilization.The SFE in water and methanol implies high solubility in an aqueous medium, a feature that supports biological activity in the sense that bioorganic activities take place in water and methanol.

Table 1.1. Thermochemical (Thermodynamic) quantities

| System | E/Hartree | H/Hartree | G/Hartree | S/cal/molK |
| --- | --- | --- | --- | --- |
| MCP (vacuum) | -810.037897 | -810.029783 | -810.070314 | 85.304 |
| MCP (Toluene) | -810.048222 | -810.040113 | -810.080652 | 85.323 |
| MCP (dichloromethane) | -810.057166 | -810.049068 | -810.089590 | 85.284 |
| MCP (methanol) | -810.060227 | -810.052140 | -810.092633 | 85.224 |
| MCP (water) | -810.060954 | -810.052870 | -810.093353 | 85.203 |
| CC-NT | -1904.075864 | -1904.055253 | -1904.118795 | 133.735 |
| MCP-CC-NT (vaccum) | -2714.117823 | -2714.087589 | -2714.179583 | 193.619 |
| MCP-CC-NT (toluene) | -2714.127124 | -2714.098696 | -2714.182723 | 176.848 |
| MCP-CC-NT (dichloromethane) | -2714.135384 | -2714.107858 | -2714.188476 | 169.676 |
| MCP-CC-NT (methanol) | -2714.138360 | -2714.110832 | -2714.191428 | 169.628 |
| MCP-CC-NT (water) | -2714.139087 | -2714.111561 | -2714.192128 | 169.567 |
| AlN-NT | -5944.963022 | -5944.923383 | -5944.029771 | 215.493 |
| MCP-AlN-NT (vacuum) | -6755.044157 | -6754.995747 | -6755.118742 | 258.863 |
| MCP-AlN-NT (toluene) | -6755.070732 | -6755.022206 | -6755.145547 | 259.594 |
| MCP-AlN-NT (dichloromethane) | -6755.095426 | -6755.047630 | -6755.168169 | 253.695 |
| MCP-AlN-NT (methanol) | -6755.104789 | -6755.056955 | -6755.177729 | 254.191 |
| MCP-AlN-NT (Water) | -6755.107176 | -6755.059356 | -6755.180126 | 254.182 |
| BN-NT | -1991.478964 | -1991.455257 | -1991.524166 | 145.031 |
| MCP-BN-NT (vacuum) | -2801.524575 | -2801.491805 | -2801.582824 | 191.566 |
| MCP-BN-NT (toluene) | -2801.539283 | -2801.507365 | -2801.594828 | 184.081 |
| MCP-BN-NT (dichloromethane) | -2801.552317 | -2801.520358 | -2801.608149 | 184.772 |
| MCP-BN-NT (methanol) | -2801.556916 | -2801.524945 | -2801.612853 | 185.017 |
| MCP-BN-NT (Water) | -2801.558023 | -2801.526050 | -2801.613992 | 185.090 |

Table 1.2. Changes of the thermochemical quantities

| systems | ΔE/kcal/mol | ΔH/kcal/mol | ΔG/kcal/mol | S/cal/molK |
| --- | --- | --- | --- | --- |
| MCP-CC-NT (vacuum) | -2.55 | -1.60 | -5.98 | 25.42 |
| MCP-CC-NT (toluene) | -1.91 | -2.09 | -10.49 | 42.21 |
| MCP-CC-NT (dichloromethane) | -1.48 | -2.22 | -12.49 | 49.343 |
| MCP-CC-NT (methanol) | -1.42 | -2.16 | -12.55 | 49.331 |
| MCP-CC-NT (water) | -1.42 | -2.16 | -12.56 | 49.371 |
| MCP-AlN-NT (vacuum) | -27.13 | -26.72 | -639.22 | 41.934 |
| MCP-AlN-NT (toluene) | -20.65 | -36.84 | -649.55 | 40.876 |
| MCP-AlN-NT (dichloromethane) | -47.21 | -47.18 | -658.14 | 47.082 |
| MCP-AlN-NT (methanol) | -26.26 | -51.10 | -662.23 | 46.526 |
| MCP-AlN-NT (water) | -52.20 | -52.15 | -663.28 | 46.514 |
| MCP-BN-NT (vacuum) | -4.84 | -4.25 | -7.31 | 38.788 |
| MCP-BN-NT (toluene) | -7.59 | -7.53 | -6.29 | 46.273 |
| MCP-BN-NT (dichloromethane) | -10.16 | -10.06 | -3.52 | 45.543 |
| MCP-BN-NT (methanol) | -11.12 | -11.01 | -2.48 | 45.505 |
| MCP-BN-NT (water) | -11.36 | -11.25 | -2.21 | 45.144 |

In addition, the thermochemical quantities and their changing were presented in table 1. Accordingly, for MCP-AlN-NT, in all solvents the changes are high in comparison with MCP-CC and MCP-BN systems. The changes of the entropy during the process for all solvents are positive. Besides, the changing of the free energy (ΔG) with solvents indicated the process happen in spontaneously except for all solvents in AlN-NT systems. Namely, the ΔG quantities of MCP were calculated as -5.98, -639.22 and -7.31kcal/mol, in vacuum for MCP-CC/AlN/BN-NT systems. Also, the lowest ΔS quantities of MCP with vacum was calculated as 25.42kcal/molK for MCP-CC-NT.The binding energies in the gaseous phase are -2.89, -27.50 and -5.04 kcal/mol for MCP-CC-NT, MCP-AlN-NT and MCP-BN-NT systems, respectively. The values of binding energy approved the development of the MCP-NT complex, which was also approved by MEP  [27, 28].

Chemical and electronic properties

Fig.2	HOMO-LUMO plots (a) CC-NT (b) AlN-NT (c) BN-NT

Fig.3	HOMO-LUMO plots of (a) mercaptopurine (MCP) (b) MCP-CC-NT (c) MCP-AlN-NT (d) MCP-BN-NT

The primary successes of this work were evaluated based on the acquired results in relation to the goal of this work, which was to load drug on NT for drug delivery reasons. HOMO and LUMO distribution patterns were presented in Fig.2 (individual NTs) and Fig.3 (MCP and MCP@NT systems). In CC-NT, FMOs are over the entire system with interchange in polarity, while in AlN-NT, HOMO is at the Al atoms on edge side, LUMO is over Al and N atoms near to N edge of the tube and in BN-NT tube, HOMO and LUMO are over the edge with interchange in polarity (Fig.2). Surprisingly, HOMO and LUMO distributions were only found on the NT counter portion of MCP@NT combination and not on the drug counterpart for AlN-NT and BN-NT while HOMO is over MCP and LUMO is over NT for MCP@CC-NT. This is a significant achievement that demonstrates the critical role of NT in the correct transport of MCP. It means, putting drug at the NT causes the drug to lose its reactivity since the HOMO and LUMO distributions are only localized at the NT. The continuous representation of MEP surface for MCP@NT was used to approve the complex formation. In this situation, NT might serve as both a carrier and a biosensor, identifying the specific position and delivering MCP. The resulting graphical findings revealed that a single drug-other chemical reactions are possible, but that its reactivity was diminished when loaded at the NT counterpart. As a result, it is possible that the delivery of such a system might be done more precisely, minimizing unwanted effects [29, 30].

The results (table 2) showed that the values of dipole moment for MCP@NT were greater than the dipole moment for single drug and NT equivalents. In the complex systems, the dipole moment values vary in the order, 9.4788 > 8.7138 > 5.8607 for AlN-NT, BN-NT and CC-NT systems. The polarizability of allMCP clusters is greater than that of MCP which gives NLO activity [31, 32].

Table 2 NLO properties

|  | Dipole Moment (Debye) | Polarizability (×10-23 esu) | First order Hyperpolarizability (×10-30 esu) | Second order Hyperpolarizability (×10-37 esu) |
| --- | --- | --- | --- | --- |
| MCP | 5.8209 | 1.4075 | 1.3933 | 3.1560 |
| CC-NT | 1.3908 | 7.1310 | 8.7572 | 36.9010 |
| AlN-NT | 7.1287 | 8.9264 | 69.0260 | 20.7570 |
| BN-NT | 4.6813 | 4.9826 | 20.3880 | 26.2240 |
| MCP-CC-NT | 5.8607 | 8.7565 | 95.500 | 63.171 |
| MCP-AlN-NT | 9.4788 | 10.735 | 74.951 | 78.415 |
| MCP-BN-NT | 8.7138 | 6.7557 | 14.684 | 60.347 |

Levels of HOMO and LUMO detect the impacts of such perturbation to molecular orbital systems yielding different values in complex of MCP-NT. As a result of the influences of FMOs, energy gaps are changed (table 3). Eg of MCP-NTs are less than that of MCP (3.0163 eV) with minimum value (0.4146 eV) for CC-NT-MCP and maximum value (1.0367 eV) for AlN-NT-MCP complexes. As a result, a novel situation has emerged for MCP-NT in comparison with each individual drug and NT revealing the significance of complex formation in determining the structural functions [33]. As a result, we can conclude that MCP-NTs aid in drug delivery. It is worth noting that molecular size research could provide information while avoiding the impacts of external interferers, allowing for the identification and characterization of pure materials. The electrophilicity indices of all MCP-NTs are higher than that of MCP (11.4893 eV) and MCP-NT was considered as a stable complexpreferable for research in drug delivery [34]. MEP/ESP plots (Fig.4 and Fig.5) show the most reactive sites in the systems which are evident for biological activity.

Table 3 Chemical descriptors (All in eV)

|  | EHOMO | ELUMO | Energy gap | Hardness | Chemical potential | Electrophilicity index |
| --- | --- | --- | --- | --- | --- | --- |
| MCP | -7.3951 | -4.3788 | 3.0163 | 1.5082 | -5.8870 | 11.4893 |
| CC-NT | -7.5511 | -6.9875 | 0.5636 | 0.2818 | -7.2693 | 93.7593 |
| AlN-NT | -6.1845 | -5.1701 | 1.0144 | 0.5072 | -5.6773 | 31.7742 |
| BN-NT | -7.7090 | -6.7287 | 0.9803 | 0.4902 | -7.2189 | 53.1536 |
| MCP-CC-NT | -7.4006 | -6.986 | 0.4146 | 0.2073 | -7.1933 | 124.8036 |
| MCP-AlN-NT | -6.1774 | -5.1407 | 1.0367 | 0.5184 | -5.6591 | 30.8882 |
| MCP-BN-NT | -6.7315 | -5.7274 | 1.0041 | 0.5021 | -6.2295 | 38.6437 |

Fig.4	MEP and ESP plots (a) CC-NT (b) AlN-NT (c) BN-NT

Fig.5	MEP and ESP plots of (a) mercaptopurine (MCP) (b) MCP-CC-NT (c) MCP-AlN-NT (d) MCP-BN-NT

Charge distribution of MCP-NT is analyzed using Mulliken charge values (table 4) [35]. In MCP-CC-NT, MCP is interacted near to the NT, through the C8, S1, N5, C6, and C10 atoms near to NT. Charges of atoms of pristine MCP, -0.2606 (S1), -0.4189 (N5), 0.2808 (C6), 0.1445 (C8) and 0.2389 (C10) changes to -0.2627 (S1), -0.4400 (N5), 0.2787 (C6), 0.1515 (C8) and 0.2518 (C10) in the complex due to interaction. In MCP-AlN/BN-NT, MCP is interacted near to the NT, through the S1, N2, C6, and C8 atoms near to NT. Charges of atoms of MCP in the complex become -0.1051 (S1), -0.7074 (N2), 0.3108  (C6) and 0.1099 (C8) in the complex due to interaction and this deviations are high which means a strong interaction in this case. In MCP-BN-NT, charges of atoms of MCP in the complex become -0.0124 (S1), -0.6912 (N2), 0.2873(C6) and 0.1206 (C8) in the complex due to interaction. Also distances of the MCP to NTs are 3.6822/ 2.4414/2.2747 for MCP-CC/AlN/BN-NTs which are suitable for hydrogen bonding [36, 37].

Table 4 Mulliken Charges (e)

| Atoms | MCP | MCP-CC-NT | MCP-AlN-NT | MCP-BN-NT |
| --- | --- | --- | --- | --- |
| S1 | -0.2606 | -0.2627 | -0.1051 | -0.0124 |
| N2 | -0.6382 | -0.6398 | -0.7074 | -0.6912 |
| N3 | -0.6609 | -0.6617 | -0.6481 | -0.6521 |
| N4 | -0.4862 | -0.4835 | -0.4854 | -0.4837 |
| N5 | -0.4189 | -0.4400 | -0.4207 | -0.4245 |
| C6 | 0.2808 | 0.2787 | 0.3108 | 0.2873 |
| C7 | 0.4799 | 0.4826 | 0.4889 | 0.4929 |
| C8 | 0.1445 | 0.1515 | 0.1099 | 0.1206 |
| C9 | 0.2400 | 0.2421 | 0.2426 | 0.2432 |
| C10 | 0.2389 | 0.2518 | 0.2455 | 0.2451 |

The TD-DFT gives UV absorption at 296.6 nm for MCP, while the corresponding values for the complexes are, 1255.61 (MCP-CC-NT), 725.96 (MCP-AlN-NT) and 791.17 and 398.41 for MCP-BN-NT (Fig.S1). In the BN-NT, there is a doublet for the UV absorption and in all cases there is a shift to higher wavenumber with a maximum for CC-NT system. In the theoretical Raman spectra (Fig.S2) of MCP and MCP-complex, functional modes are enhanced which means theNTs can act as a sensor for detection of MCP.

Noncovalent interactions (NCI)

The NCI assay explains noncovalent interactions as well as nonbond interactions between two molecules via hydrogen interactions [38-41]. The hydrogen interactions are strong hydrogen bond by high electronegative atoms, weak hydrogen interactions also called van der Waals interactions, and hydrogen repulsions or steric interactions of bulky groups and aromatic ring or pi-system. NCI can be supported by reduced density gradient (RDG) of molecules.

Fig.6	NCI plots of (a) MCP-AlN-NT (b) MCP-BN-NT (c) MCP-CC-NT; RDG plots of (d) MCP-AlN-NT (e) MCP-BN-NT (f) MCP-CC-NT

Fig.6 displays the NCI, and NCI-RDG graph of MCP with AlN, BN, and CC NTs. The blue colour range from -0.05 to -0.03 a.u. represent strong hydrogen attractions of MCP with AlN-NT shows sulphur atom and aluminium atoms, hydrogen atoms attached with nitrogen and carbon in MCP and nitrogen and aluminium atoms in NT, and all nitrogen atoms cavity in NT, likewise BN-NT shows sulphur atoms in MCP and nitrogen and boron atoms in NT, and hydrogen atoms in MCP and nitrogen atoms in NT, similarly CC-NT shows intra attractions between hydrogen and sulphur in MCP. The green colour range from -0.02 to 0.01 a.u. represent weak hydrogen bond or van der Waals interactions of MCP with AlN-NT shows hydrogen atoms attached with carbon and nitrogen and carbon atoms in MCP and nitrogen atoms in cube, sulphur atom and aluminium and nitrogen atoms in NT and all intra interaction of aluminium and nitrogen atoms (inner NT), alike BN-NT shows hydrogen atoms attached with nitrogen and carbon atoms and boron atoms in NT and all intra interaction of boron and nitrogen atoms (inner NT), like CC-NT shows nitrogen and sulphur atoms in MCP and carbon atoms in NT. The red colour range from 0.02 to 0.05 a.u. represent hydrogen repulsion or steric interactions and pi-system of MCP with AlN-NT shows pi-system of MCP, sulphur in MCP and aluminium atoms in NT and all aluminium cavities in NT, similarly BN-NT shows pi-system of MCP, sulphur in MCP and boron atoms in NT and all boron cavities in NT, like CC-NT shows pi-system of MEP, sulphur in MRP and carbon atoms in NT.

Fig.7	ELF plots of (a) MCP-AlN-NT (b) MCP-BN-NT (c) MCP-CC-NT

The graph plotted energy against RDG of MCP with AlN-NT shows greater density of strong hydrogen bond interactions than repulsion interactions, in oppositely BN-NT and CC-NT shows greater density of repulsion interactions than strong hydrogen bond interactions.

Electron localized function (ELF)

ELF is evidence of nature of electrons in molecules, explains by the probability of electrons with localization or delocalization. The localized electrons are core and multiple-bonded electrons, and delocalized electrons are hydrogen bonds and lone-pairs of electrons in the molecules [42-47]. Fig.7 shows the ELF of MCP with AlN/BN/CC-NT. The colour from blue to red with the range from 0.00 to 1.00 shows the probability of electrons from localization to delocalization. The blue colour represent localized electrons of MCP with AlN-NT shows at all heavy atoms like Al, N and C atoms (1s2, 2s2 of N & C and including 2p6 for Al) core electrons, like BN-NT shows at all heavy atoms like B, N and C atoms (1s2, 2s2 of N & C) core electrons, alike CC-NT shows at all heavy atoms like N and C atoms (1s2, 2s2 of N & C) core electrons. The colour red represent delocalized electrons of all H, C, N and S atoms, which means hydrogen atoms can localized with more electronegative elements, alike nitrogen and sulphur atoms having lone-pairs of electrons and carbon atoms having pi-electrons for resonance of MCP with AlN/BN/CC-NT complexes.

Conclusion

In this manuscript, we presented the adsorption behaviour of MCP over AlN, BN and CC nanotubes. It is found that the compound adsorbs well with all the three tubes under consideration. Free energy values indicated that the free energy of adsorption is high when ALN nanotube is used, which may be attricuted to high polarity of the tube over CC and BN tubes. NCI-RDG scattered plot supports this whith evidence of very high noncovalent  interaction between the compound and AlN. Dipolemoment of that cluster is high over the other two. Also, it is found that in all the three cases, presence of solvents positively enhances the free energy of solvation comapred to that of vaccum. Thus, it can be concluded that AlN clusters can efefctively find with mercaptopurine and hence can used as better carriers of similar drugs to the target positions.

Acknowledgments

The authors express their gratitude to Princess Nourah bint Abdulrahman University Researchers Supporting Project number (PNURSP2022R13), Princess Nourah bint Abdulrahman University, Riyadh, Saudi Arabia

Author contribution

Jamelah S.Al-Otaibi: Software, Supervision, manuscript preparation and data analysis

Y.Sheena Mary: Supervision, manuscript preparation, conceiving the problem and data analysis

Y.Shyma Mary: Manuscript preparation, conceiving the problem and data analysis and correction

Renjith Thomas: Manuscript preparation, conceiving the problem and data analysis and correction

Data availability: The supplementary information files include additional materials

Code availability: No new codes have been created. Existing codes were utilized and quoted correctly

Conflict of interest The authors declare no competing interests

References

[1]	S.Iijima, Helical microtubes of graphitic carbon, Nature 354 (1991) 56-58. https://doi.org/10.1038/354056a0

[2]	M.Mirzaei, The NMR parameters of the SiC-doped BN nanotubes: a DFT study, Physica E: Low-dimensional Systems and Nanostructures, 42 (2010) 1954-1957. https://doi.org/10.1016/j.physe.2010.03.015

[3]	M.Mirzaei, M.Mirzaei, A computational study of oxygen-termination of a (6,0) boron nitride nanotube, Montatschefte fur Chemie 141 (2010) 491-494. https://doi.org/10.1007/s00706-010-0287-3

[4]	M.Mirzaei, M.Mirzaei, Electronic structure of sulfur terminated zigzag boron nitride nanotube: a computational study, Soldi State Sciences 12 (2010) 1337-1340. https://doi.org/10.1016/h.solidstatesciences.2010.05.004

[5]	M.Mirzaei, M.Meskinfarm, Computational studies of effects of tubular lengths on the NMR properties of pristine and carbon decorated boron phosphide nanotubes, Soldi State Sciences 13 (2011) 1926-1930. https://doi.org/10.1016/j.solidstatesciences.2011.08.018

[6]	M.Mirzaei, M.Mirzaei, The C-doped AlP nanotubes: a computational study, Soldi State Sciences, 13 (2011) 244-250. https://doi.org/10.1016/j.solidstatesciences.2010.11.022

[7]	W.Yang, P.Thordarson, J.J.Gooding, S.P.Ringer, F.Braet, Carbon nanotubes for biological and biomedical applications, Nanotechnology 18 (2007) 412001. https://doi.org/10.1088/0957-4484/18/41/412001

[8]	A.Bianco, K.Kostarelos, M.Prato, Applications of carbon nanotubes in drug delivery, Current Opinion in Chemical Biology 9 (2005) 674-679.  https://doi.org/10.1016/j.cbpa.2005.10.005

[9]	L.Minati, V.Antonini, M.D.Serra, G.Speranza, Multifunctional branched gold-carbon nanotube hybrid for cell imaging and drug delivery, Langmuir 28 (2012) 15900-15906. https://doi.org/10.1021/la303298u

[10] 	Z.Liu, S.Tabakman, K.Welsher, H.Dai, Carbon nanotubes in biology and medicine: in vitro and in vivo detection, imaging and drug delivery, Nano Research 2 (2009) 85-120. https://doi.org/10.1007/s12274-009-9009-8

[11]	M.Karimi, N.Solati, M.Amiri, H.Mirshekari, E.Mohamed, M. Taheri, M.Hashemkhani, A.Saeidi, MA.Estiar, P.Kiani, A.Ghasemi, S.M.M.Basri, A.R.Aref, M.R.Hamblin, Carbon nanotubes part I: preparation of a novel and versatile drug-delivery vehicle, Expert Opinion on Drug Delivery, 12 (2015) 1071-1087. https://doi.org/10.1517/17425247.2015.1003806

[12]	M.Mirzaei, O.Gulseren, N.Hadipour, DFT explorations of quadrupole coupling constants for planar 5-fluorouracil pairs, Computational and Theoretical Chemistry 1090 (2016) 67-73. https://doi.org/10.1016/j.comptc.2016.06.004

[13]	K.Harismah, M.Mirzaei, Steviol and iso-steviol vs. cyclooxygenase enzymes: in silico approach, Lab-in-Silico 1 (2020) 11-15. https://doi.org/10.22034/lins20011011

[14]	M.Mirzaei, H.R.Kalhor, N.L.Hadipour, Covalent hybridization of CNT by thymine and uracil: a computational study, Journal of Molecular Modeling, 17 (2011) 695-699. https://doi.org/10.1007/s00894-010-0771-z

[15]	K.Harismah, O.M.Ozkendir, M.Mirzaei, Lithium adsorption at the C20 fullerene like case: DFT approach, Advanced Journal of Science and Engineering 1 (2020) 74-79. https://doi.org/10.22034/AJSE.2013074

[16] 	R.Faramarzi, M.Falahati, M.Mirzaei, Interactions of fluorouracil by CMT and BNNT: DFT analyses, Advanced Journal of Science and Engineering 1 (2020) 62-66. https://doi.org/10.22034/AJSE.2012062

[17]	DE.Thurston, Chemistry and Pharmacology of anticancer drugs, CRC Press, Taylor and Francis group, Boca Raton, Florida, USA 2007

[18]	D.Trivedi, MK.Trivedi, G.Nayak, S.Jana, Complementary and alternative medicine: Impact of consciousness energy healing treatment on the physicochemical and thermal properties of 6-mercaptopurine, Research in Medical & Engineering Sciences, 7 (2018) RMES.000658. https://doi.org/10.31031/RMES.2018.07.000658

[19]	M.Keyvanfard, V.Khosravi, H.Karimi-Maleh, K.Alizad, B.Rezaei,  Voltammetric determination of 6-mercaptopurine using a multiwall carbon nanotubes paste electrode in the presence of isoprenaline as a mediator, J. Mol.  Liquid. 177 (2013) 182-189. https://doi.org/10.1016/j.molliq.2012.10.020

[20]	R.Bhuvaneswari, V.Nagarajan, R.Chandiramouli, Interaction studies of nitrotoluene and toludine molecules on novel square-octagon aresene nanotubes based on DFT method, J. Mol. Liquid. 325 (2021) 115260. https://doi.org/10.1016/j.molliq.2020.115260

[21]	Gaussian 16, Revision A.03, M.J. Frisch, G.W. Trucks, H.B. Schlegel, G.E.  Scuseria, M.A. Robb, J.R. Cheeseman, G. Scalmani, V. Barone, G.A. Petersson, H. Nakatsuji, X. Li, M. Caricato, A.V. Marenich, J. Bloino, B.G. Janesko, R. Gomperts, B. Mennucci, H.P. Hratchian, J.V. Ortiz, A.F. Izmaylov, J.L. Sonnenberg, D. Williams-Young,  F. Ding, F. Lipparini, F. Egidi, J. Goings, B. Peng, A. Petrone,  T. Henderson, D. Ranasinghe, V.G. Zakrzewski, J. Gao, N. Rega,  G. Zheng, W. Liang, M. Hada, M. Ehara, K. Toyota, R. Fukuda,  J. Hasegawa, M. Ishida, T. Nakajima, Y. Honda, O. Kitao, H. Nakai,  T. Vreven, K. Throssell, J.A. Montgomery, Jr., J.E. Peralta,  F. Ogliaro, M.J. Bearpark, J.J. Heyd, E.N. Brothers, K.N. Kudin,  V.N. Staroverov, T.A. Keith, R. Kobayashi, J. Normand,  K. Raghavachari, A.P. Rendell, J.C. Burant, S.S. Iyengar,  J. Tomasi, M. Cossi, J.M. Millam, M. Klene, C. Adamo, R. Cammi,  J.W. Ochterski, R.L. Martin, K. Morokuma, O. Farkas,  J.B. Foresman, and D. J. Fox, Gaussian, Inc., Wallingford CT, 2016.

[22]	GaussView, Version 6.1, Roy Dennington, Todd A. Keith, and John M. Millam, Semichem Inc., Shawnee Mission, KS, 2016

[23]	B.Mennucci, J.Tomasi, Continuum solvation models: A new approach to the problem of solute’s charge distribution and cavity boundaries, J. Chem. Phys. 106 (1997) 5151-5158. https://doi.org/10.1063/1.473558

[24]		T. Lu, F. Chen, Multiwfn: A multifunctional wavefunction analyzer, J. Comput. Chem. 33 (2012) 580–592. https://doi.org/10.1002/jcc.22885

[25]	A.V.Marenich, C.J.Cramer, D.G.Truhlar, Universal solvation model based on solute electron density and on a continuum model of the solvent defined by the bulk dielectric constant and atomic surface tensions, J. Phys. Chem. B 113 (2009) 6378-6396. https://doi.oreg/10.1021/jp810292n

[26]	G.D.R.Matos, D.Y.Kyu, H.H.Loeffler, J.D.Chodera, M.R.Shirts, D.L.Mobley, Approaches for calculating solvation free energies and enthalpies demonstrated with an update of the FreeSolv database, J. Chem.Eng. Data 62 (2017) 1559-1569. https://doi.org/10.1021/acs.jced.7b00104

[27]	J.S.Al-Otaibi, Y.S.Mary, Y.S.Mary, S.Kaya, G.Serdaroglu, DFT computational study of trihalogenated aniline derivative’s adsorption onto graphene/fullerene/fullerene-like nanocages, X12Y12 (X=Al, B and Y=N,P),  Journal of Biomolecular Structure and Dynamics (2020). https://doi.org/10.1080/07391102.2021.1914172

[28]	J.S.Al-Otaibi, Y.S.Mary, Y.S.Mary, G.Serdaroglu, Adsorption of adipic acid in Al/B-N/P nanocages: DFT investigations,  Journal of Molecular Modeling, 27 (2021) 113. https://doi.org/10.1007/s00894-021-04742-z

[29]	Y.S.Mary, Y.S.Mary, Z. Ullah, Computational study of sorbic acid drug adsorption onto coronene/fullerene/fullerene-like X12Y12 (X=Al, B and Y=N,P) nanocages: DFT and molecular docking investigations, Journal of Cluster Science (2021). https://doi.org/10.1007/s10876-021-02106-4

[30] 	Y.S.Mary, Y.S.Mary, Adsorption of phenothiazine derivatives on graphene-DFT, docking and MD simulation, Polycyclic Aromatic Compounds (2021). https://doi.org/10.1080/10406638.2021.1946570

[31] 	A.H.Almuqrin, J.S.Al-Otaibi, Y.S.Mary, Y.S.Mary, DFT computational study towards investigating psychotropic drugs, promazine and trifluoperazine adsorption on graphene, fullerene and carbon cyclic ring nano clusters,  Spectrochim. Acta 246 (2021) 119012. https://doi.org/10.1016/j.saa.2020.119012

[32]  	Y.S.Mary, Y.S.Mary, Utilization of doped/undoped graphene quantum dots for ultrasensitive detection of duphaston, a SERS platform, Spectrochim. Acta 244 (2021) 118865. https://doi.org/10.1016/j.saa.2020.118865

[33]	R.Padash, M.R.Esfahani, A.S.Rad, The computational quantum mechanical study of sulfamide drug adsorption onto X12Y12 fullerene-like nanocages: detailed DFT and QTAIM investigations, Journal of Biomolecular Structure and Dynamics, (2020) https://doi.org/10.1080/07391102.2020.1792991

[34] 	J.S.Al-Otaibi, Y.S.Mary, Y.S.Mary, R.Thomas, Evidence of cluster formation of croconic acid with Ag, Au and Cu cages, enhancement of electronic properties and Raman activity, Spectrochim. Acta 264 (2022) 120233.https://doi.org/10.1016/j.saa.2021.120233

[35]	R.Padash, M.Rahimi-Nasrabadi, A.S.Rad, A.Sobhani-Nasab, T.Jesionowski, H.Ehrlich, A comparative computational investigation of phosgene adsorption on (XY)12 (X=Al,B and Y=N,P) nanoclusters: DFT investigations, Journal of Cluster Science 30 (2019) 203-218. https://doi.org/10.1007/s10876-018-1479-y

[36] 	Y.S.Mary, Y.S.Mary, S.Armakovic, S.J.Armakovic, R.Yadav, I.Celik, P.Mane, B.Chakraborty, Stability and reactivity study of bio-molecules brucine and colchicines towards electrophile and nucleophile attacks: Insight from DFT and MD simulations,  Journal of Molecular Liquids 335 (2021) 116192. https://doi.org/10.1016/j.molliq.2021.116192

[37] 	P.Albrycht, J.S.Al-Otaibi, Y.S.Mary, Y.S.Mary, R.Trivedi, B.Chakraborty, Surface enhanced Raman scattering investigation of pioglitazone on silver and silver-gold substrates-Experimental analysis and theoretical modeling, J. Mol. Struct. 1244 (2021) 130992. https://doi.org/10.1016/j.molstruc.2021.130992

[38]	R.A.Boto, J.P.Piquemal, J. Contreras-Garcia, Revealing strong interactions with the reduced density gradient: a benchmark for covalent, ionic and charge-shift bonds, Theor. Chem. Acc. 136 (2017) 1-9. https://doi.org/10.1007/s00124-017-2169-9

[39]	A.Karshikoff, Non-covalent interactions in proteins, World Scientific Publishing Co., (2006). https://doi.org/10.1142/p477

[40]	P.Surendar, T.Pooventhiran, N.Al-Zaqri, S.Rajam, D.Jagadesswara Rao, R.Thomas, Synthesis of three quasi liquid Schiff bases between hexanal and adenine, cytosine and l-leucine, structural interpretation, quantum mechanical studies and biological activity prediction, J. Mol. Liquid. 341 (2021) 117305.

[41]	A.Paul, R.Thomas, Evidences for sulfur centered hydrogen bond with sulfur atoms as a donor in aromatic thiols and aliphatics thiols in aqueous solution, J. Mol. Liquid. (2021) 118078. https://doi.org/10.1016/j.molliq.2021.118078

[42]	G.V.Gibbs, D.F.Cox, M.B.Boisen Jr., R.T.Downs, N.L.Ross, The electron localization function: a tool for locating favourable proton docking sites in the silica polymorphs, Phys. Chem. Miner. 30 (2003) 305-316. https://doi.org/10.1007/s00269-003-0318-2

[43]	K.Koumpouras, J.A.Larsson, Distinguishing between chemical bonding and physical binding using electron localization function (ELF), J. Phys. Condens. Matter. 32 (2020) 315502. https://doi.org/10.1088/1361-648x/ab7fd8

[44]	F.Fuster, A.Sevin, B.Silvi, Topological analysis of the electron localization function (ELF) applied to the electrophilic aromatic substitution, J. Phys. Chem. A 104 (2000) 852-858. https://doi.org/10.1021/jp992783k

[45]	S.PriyaYeddu, P.Thangaiyan, A.Veeraiah, D.Vijay, K.S.Srikanth, A.Irfan, R.Thomas, Vibrational spectral studies, quantum mechanical properties and biological activity prediction and inclusion of molecular self-assembly formation of N-N’-dimethylethylene urea, Biointerface Res. Appl. Chem. 12 (2022) 3996-4017. https://doi.org/10.33263/BRIAC123.39964017

[46]	A.Matondo, R.Thomas, P.V.Tsalu, C.T.Mukeba, V.Mudogo, α-methylation and α-fluorination electronic effects on the regioselectivity of carbonyl groups of uracil by H and triel bonds in the interaction of U, T and 5FU with HCl and TrH3 (Tr=B,Al), J. Mol. Graph. Model. 88 (2019) 237-246. https://doi.org/10.1016/j.jmgm.2019.02.006

[47]	S.Hosna, D.E.Janzen, Y.S.Mary, K.S.Resmi, R.Thomas, R.Mohamed, S.Wajda, Molecular structure, spectroscopic, dielectric and thermal study, nonlinear optical properties, natural bond orbital, HOMO-LUMO and molecular docking analysis of (C6Cl2O4)(C10H14N2F).2H2O, Spectrochim. Acta 204 (2018) 328-339. https://doi.org/10.1016/j.saa.2018.06.062