Supplementary information for Large-area flexible Visible-Short wavelength Infrared Photodetection based on III-V compound semiconductor membrane photodetector with high performance

Xuanzhang Li1,2, Junyang Zhang1,2, Chen Yue1,2, Xiansheng Tang3, Zhendong Gao1,2, Yang Jiang1,4, Chunhua Du1,4,5, Zhen Deng1,4,5, *, Haiqiang Jia1,4,6, Wenxin Wang1,4,6S and Hong Chen1,4,5,6

1 Key Laboratory for Renewable Energy, Beijing Key Laboratory for New Energy Materials and Devices, Beijing National Laboratory for Condensed Matter Physics, Institute of Physics, Chinese Academy of Sciences, Beijing 100190

2 University of Chinese Academy of Sciences, Beijing 100049, China

3 Laser Institute, Qilu University of Technology (Shandong Academy of Sciences), Jinan 250014, China

4 Center of Materials and Optoelectronics Engineering, University of Chinese Academy of Sciences, Beijing 100049, China

5 The Yangtze River Delta Physics Research Center, Liyang 213000, China

6 Songshan Lake Materials Laboratory, Dongguan 523808, China

*zhen.deng@iphy.ac.cn

- Material growth of InGaAs PIN PD on InP substrate

The material for InGaAs PIN photodetector was grown on a n-type (1017 cm−3) InP wafer in a metal organic chemical vapor deposition reactor. First, a n-InP buffer layer (~1018 cm−3, thickness >200 nm) was grown to stabilize the wafer surface, followed by a 500nm lattice-matched n-type(~1018 cm−3) In0.53Ga0.47As, a 500 nm n-type(~1018 cm−3) InP layer, 2.2 μm i- In0.53Ga0.47As layer (~1016 cm−3), a 600 nm n-type(~1016 cm−3) InP layer and a 50 nm n-type(~1016 cm−3) In0.53Ga0.47As layer, respectively. After the epitaxy, the p-type InGaAs layer and InP layer were achieved by single MOCVD diffusion of zinc. The concentrations of p-InGaAs and p-InP layer were about 1019 cm−3 and 2×1018 cm−3, respectively. Figure S1 shows the InGaAs PIN photodetector based on InP substrate.

Figure S1. The InGaAs PIN photodetector based on InP substrate

- Material Characterization

After the epitaxial growth, the material quality was assessed by using atomic force microscopy (AFM), high resolution X-ray diffraction (HR-XRD) and photoluminescence (PL). AFM image showed that the sample exhibited a good surface morphology with clear atomic steps and small roughness of 1.66 Å over a 5 × 5 μm2 area Fig.10(a). Furthermore, as shown in Figure S2(b) and (c), the HR-XRD and PL results showed that the Indium composition is very close to 0.53, which means that the InGaAs layer is well fitted to the design composition. In addition, the full width at half maximum (FWHM) value of the InGaAs epilayer was 126 arcsec. All the results reveals that the high-quality materials were obtained.

Figure S2.  (a) The AFM image of a 5 μm × 5 μm surface area of the as-grown material, with rms roughness value of 1.66 Å. (b) the HR-XRD ω/2θ curve of the InGaAs PIN photodetector structure. L1 represents the epitaxy InGaAs layer, and S represents the InP substrate. (c) PL spectra of InGaAs PIN photodetector structure at room temperature. The peak of curve is 1642 nm (~ 0.755 eV), which is close to the band gap of lattice-matched InGaAs on InP substrate.