Supporting information of High friction mechanism of ZDDP tribofilm based on in-situ AFM observation of

nano-friction and adhesion properties

Kaisei Sato a*, Seiya Watanabe b**, and Shinya Sasaki b

a Graduate School, Tokyo University of Science, 6-3-1 Niijuku, Katsushika-ku, Tokyo, 125-8585, Japan.

b Tokyo University of Science, 6-3-1 Niijuku, Katsushika-ku, Tokyo, 125-8585, Japan.

*Corresponding author: Kaisei Sato

** Current affiliation: Osaka University 1-3 Yamadaoka, Suita 565-0871, Japan.

Tel.: +81 3 5876 1334, E-mail address: 4520701@ed.tus.ac.jp

Fig. S1　Tip radius of cantilever used at in-situ AFM sliding test with sliding cycle number. To investigate the tip radius in our experiments, we observed the tip radius by using SEM-EDS () and AFM as following conditions: the load of 2000 nN, the sliding speed of 20 Hz, the range of 2.0 µm × 2.0 µm on SUJ2. We confirmed that the tip radius of the cantilever increased up to about 140 nm and the values became stable.

Fig. S2 Arithmetic average roughness on ZDDP tribofilm with sliding cycle number. This result showed that roughness of ZDDP tribofilm steadily increased until 600 cycles.