Supporting Information

Advanced Cu-free Bipolar Solid-state Lithium-ion Battery Promoted by Li+ Conductive Matrix Enabled Excellent Iron Oxide Anode

Wujie Dong,1 Yantao Zhao,2 Mingzhi Cai,2 Chenlong Dong,2 Wenqin Ma,1 Jun Pan,1 Zhuoran Lv, 1 Hang Dong, 1 Yufeng Tang1*, Fuqiang Huang1*

1State Key Laboratory of High Performance Ceramics and Superfine Microstructure, Shanghai Institute of Ceramics, Chinese Academy of Sciences, Shanghai 200050, P. R. China

2State Key Laboratory of Rare Earth Materials Chemistry and Applications, College of Chemistry and Molecular Engineering, Peking University, Beijing 100871, P.R. China

Figure S1. Schematic images of classic LIBs.

Figure S2. Conversion rate from theoretical (A) gravimetric and (B) volumetric energy density to practical values.

Figure S3. (A) Selected area electron diffraction of FeOx-LFBO sample. (B) TEM and (C) HRTEM images of FeOx sample.

Figure S4. (A) XRD patterns and (B) N2 adsorption-desorption isotherms of unannealed Fe(OH)3 and Fe(OH)3-LFBO.

Figure S5. Cycling performance of FeOx-LFBO and bare FeOx at 0.1 A g–1.

Figure S6. CV curves of (A) FeOx-LFBO and (B) FeOx at 0.3 mV s–1.

Figure S7. Long-term cycling of FeOx-LFBO at 1 A–1  10 A–1.

Figure S8. Rate capability of MnOx-LBO, CoOx-LBO, and SnO2-LBO electrodes at 1 A–1  20 A–1.

Figure S9. GCD curves of FeOx-LFBO electrode and Al foil.

Figure S10. (A) Rate capability of FeOx-LFBO electrode under the voltage range of 3.0 - 0.5 V. (B) Long-term cycling of FeOx-LFBO electrode at 5 A g1 under the voltage range of 3.0 - 0.5 V. Inset: GCD curves of FeOx-LFBO anodes before and after 1000 cycles.

Figure S11. Schematic microstructure evolves during charging/discharging process of FeOx-LFBO anode. (A) The initial electrode and (B) the partial enlarged view of FeOx-LFBO anode; (B-1) and (B-2) are the enlarged interface of FeOx/LFBO/FeOx and FeOx/LFBO/electrolyte; (C) Lithiation reaction begins and form Fe+Li2O precipitates uniformly, (C-1) and (C-2) are the enlarged interface of FeOx/Fe+Li2O/LFBO/Fe+Li2O/FeOx and FeOx/Fe+Li2O/LFBO/electrolyte; (D) Lithiation reaction completes in the whole FeOx-LFBO electrode to form isolated small Fe+Li2O precipitates in LFBO matrix, (D-1) and (D-2) are the enlarged interface of Fe+Li2O/LFBO/Fe+Li2O and Fe+Li2O/LFBO/electrolyte.

Figure S12. Schematic microstructure evolves during charging/discharging process of common FeOx anode. (A) The initial FeOx electrode; (B) The partial enlarged view of FeOx electrode when lithiation reaction begin and form Fe + Li2O precipitates; (C-D) Lithiation reaction completes in the initial FeOx particles and extends to neighboring particles; (E) Lithiation reaction completes in the whole FeOx electrode to form aggregated Fe + Li2O precipitates, when delithiation reaction starts; (F) Delithiation reaction completes to form a much bigger aggregated FeOx particle; (G) Huge FeOx particle cracks into fragments after some cycles.

Figure S13. TEM images of (A) FeOx after 100 cycles and (B) FeOx-LFBO electrodes after 500 cycles at 2 A g1.

Figure S14. CV curves of (A) FeOx-LFBO and (B) FeOx electrodes at the scan rate spanning over 0.3 - 0.7 mV s1. (C) Logarithmic relationship between the peak current and scan rates of FeOx-LFBO, the red line is obtained by linear fitting with the shope (b-value) of 0.88.

Figure S15. (A) GDC curves FeOx-LFBO electrode after different cycles at 2 A g1, and (B) the relevent capacity contribution vs. cycle number in different votage ranges of 3.0 - 0.7 V and 0.7 - 0.01 V. (C) Ex-situ B 1s XPS spectrums of FeOx-LFBO electrodes after first discharge to 0.01 V and 0.01 V/3.0 V at 500th cycle.

Figure S16. Rate capabilities of FeOx-LFBO electrodes with different loading mass spanning over 1.5 – 6 mg cm2 at the current density of 0.1 – 20 A g1.

Figure S17. Theoretical GDC curves of perfectly matched LiCoO2 cathode (red line, 3.0 – 4.2 V) and FeOx-LFBO (blue line, 3.0 – 0.01 V).

Figure S18. The digital image of pouch-type bipolar solid-state cell, which can light a red LED bulbs at (A) normal, (B) bended, (C) heated, and (D) cut conditions.