Table 1. Zeta potential and size related to Fe3O4 magnetite nanoparticles (MNPs), PEI-MNPs (PM) binary complex including MNPs and polyethylenimine (PEI) and three-component magnetic nanocomplexes (PMC) comprising PEI, MNP and cisplatin.

| PMC | PM | MNPs | PEI |  |
| --- | --- | --- | --- | --- |
| 16±6 | 19 ± 2 | -25±4 | 34±3 | Zeta potential (eV) |
| 151±21 | 88±15 | 69±5 | 91±17 | Size (nm) |

Table 2. The inhibitory concentration 50% (IC50) of CIS, PEI, PC, PM, PM/C and PMC treatments were calculated in A2780/CP and A2780 cells in presence and absence of 20 mT static magnetic field (SMF).

| PMC |  | PM/C |  | PM |  | PC |  | PEI |  | CIS |  | Cells |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 3.9± 0.9 | 4.8± 0.9 | 4.7± 0.8 | 5.9± 1.3 | 14.5± 2.2 | 25.9± 2.3 | 13.2± 3.1 | 14± 1.1 | 27.4± 2.2 | 28.4± 1.3 | 15.2± 2.3 | 15.7± 1.1 | A2780/CP (24 h) |
| 3.2± 0.7 | 3.9± 0.7 | 4± 1.1 | 5.1± 0.8 | 12.5± 3.1 | 23.6± 3.4 | 7.9± 2.9 | 8.5± 0.5 | 20.2± 0.9 | 23.8± 3.1 | 10.1± 3.2 | 11.1± 0.6 | A2780 (24 h) |
| 1.6± 0.2 | 2.7± 0.2 | 2.7± 0.2 | 3.7± 0.8 | 11± 0.9 | 17.3± 1.7 | 10.1± 0.8 | 11± 1.1 | 18.9± 0.9 | 21.9 ± 2.4 | 13.1 ± 0.3 | 14 ± 0.8 | A2780/CP (48 h) |
| 0.6± 0.2 | 1.6± 0.3 | 2.3± 0.3 | 3.2± 0.3 | 9.3± 1.8 | 19.8± 1.9 | 7.3± 0.4 | 8.4± 0.6 | 15.9± 0.3 | 18.4± 1.6 | 9.5± 0.4 | 10.6± 1.2 | A2780 (48 h) |
| + | - | + | - | + | - | + | - | + | - | + | - | SMF (20 mT) |

Table 3. The mechanisms, functions, isoelectric point (pI) and net charge of enzymes involved in the drug resistance of cancer cells.

| Net charge | Isoelectric point (pI) | Function | Mechanism | Enzyme |
| --- | --- | --- | --- | --- |
| -1 | 3.3 | GSH scavenges electrophiles and ROS (14) | pre-target resistance | GSH, reduced glutathione |
| -3 | 5.3 | inactivation of cisplatin can occur through conjugation with GSH (13) | pre-target resistance | GST glutathione S-transferase |
| -13 | 5.7 | GST conjugates GSH to CDDP,thus facilitating its extrusion | pre-target resistance | γ-GCS, g-glutamylcysteine synthetase |
| -11.9 | 6.2 | Copper ion transmembrane transporter involved in the export of copper and CDDP out of the cells (9, 10) | pre-target resistance | ATP7B |
| -19.9 | 5.9 | Copper ion transmembrane transporter involved in the export of copper and CDDP out of the cells (10) | pre-target resistance | ATP7A |