# TABLE NO- 3: STRENGTHS OF INDIAN

# COAL MEASURE ROCKS/CONCRETE

| Type of rocks Coal-measure | Comp. Strength KPa | Tensile Strength KPa | Shear Strength KPa | Protodeakonov Index |
| --- | --- | --- | --- | --- |
| Massive sandstone | 61.1 | 24.5 | 23.8 | 7.25 |
| Laminated -do- | 36.9 | 15.5 | 8.6 | 5.76 |
| Siltstone | 43.3 | 13.2 | 13.7 | 3.81 |
| Argillaceous shale | 26.8 | 7.1 | 6.7 | 1.54 |
| Carbonaceous shale | 19.0 | 6.1 | 4.5 | 1.20 |
| Coal | 7.0 | 5.5 | 2.5 | 0.80 |
| Concrete (M-200) | 7.0 | 1.3 | 0.7 | 1.47 |