Supplementary Information

Intensification of CO2 absorption and desorption by metallic and non-metallic nanoparticles in bubble columns

Fariba Zarei, Peyman Keshavarz*1

*School of Chemical and Petroleum Engineering, Shiraz University, Shiraz, Iran

-

1. Corresponding author. Tel.: þ98 7116133713; Fax: +98 7116473180.

E-mail address: pkeshavarz@shirazu.ac.ir (P. Keshavarz).

To investigate the performance presence of nanoparticles in improving CO2 desorption from amine solutions, the CO2 loading at the end of absorption and desorption process were determined for all nanofluids. Also, the Falling percentage of each one of the nanofluids was calculated. The results of final CO2 loading after absorption and regeneration experiments are demonstrated in Table S1.

Table S1. acid gas pick up

| solvent | CO2 loading after absorption time* | CO2 loading at the end of regeneration at 60oC temperature* | Falling percentage | CO2 loading at the end of regeneration at 70oC temperature* | Falling percentage |
| --- | --- | --- | --- | --- | --- |
| MDEA | 0.48 | 0.42 | 12.11 | 0.40 | 15.66 |
| 0.1%wt SiO2 | 0.52 | 0.43 | 17.23 | 0.41 | 20.78 |
| 0.05%wt SiO2 | 0.51 | 0.42 | 18.89 | 0.40 | 22.08 |
| 0.01%wt SiO2 | 0.49 | 0.43 | 13.37 | 0.42 | 15.53 |
| 0.1%wt ZnO | 0.61 | 0.47 | 22.30 | 0.46 | 24.49 |
| 0.05%wt ZnO | 0.57 | 0.43 | 24.37 | 0.42 | 26.36 |
| 0.01%wt ZnO | 0.54 | 0.47 | 13.19 | 0.45 | 16.28 |
| 0.1%wt Fe3O4 | 0.53 | 0.36 | 31.76 | 0.35 | 34.45 |
| 0.05%wt Fe3O4 | 0.59 | 0.37 | 37.80 | 0.36 | 39.51 |
| 0.01%wt Fe3O4 | 0.65 | 0.48 | 25.59 | 0.48 | 25.92 |
| 0.1%wt CuO | 0.52 | 0.32 | 38.47 | 0.30 | 41.87 |
| 0.05%wt CuO | 0.60 | 0.34 | 44.37 | 0.32 | 46.28 |
| 0.01%wt CuO | 0.59 | 0.42 | 28.50 | 0.41 | 30.53 |

*  mole of CO2 per mole of amine