Additional file 1

Vancomycin-conjugated polydopamine-coated magnetic nanoparticles for molecular diagnostics of Gram-positive bacteria in whole blood

Abdurhaman Teyib Abafogi1+, Tepeng Wu2+, Daekyu Lee1, Jinyeop Lee1,2, Gyoujin Cho3,4, Luke P. Lee3,4,5, Sungsu Park 1,4,*

1School of Mechanical Engineering, Sungkyunkwan University (SKKU), Suwon 16419, Korea

2KingoBio Inc., 31 Digital-ro 30-gil, Guro-gu, Seoul 08390, Korea

3Department of Biophysics, Sungkyunkwan University (SKKU), Suwon 16419, Korea

4Institute of Quantum Biophysics (IQB), Sungkyunkwan University (SKKU), Suwon 16419, Korea

5Renal Division, Department of Medicine, Brigham and Women’s Hospital, Harvard Medical School, MA 02139, USA

+Each author contributed equally to this work

*Corresponding authors: S. Park, School of Mechanical Engineering, Sungkyunkwan University (SKKU), Seobu-ro 2066, Jangan-gu, Suwon 16419, Korea. Tel: +82-31-290-7431. E-mail: nanopark@skku.edu

Fig. S1. Schematic representing the synthesis of vancomycin-conjugated silica oxide-coated magnetic nanoparticles (van-SiO2-MNPs). Freshly prepared MNPs form larger MNPs through SiO2 coating.  SiO2-MNPs are conjugated with van after amino group functionalization [1]. Tetraethyl orthosilicate (TEOS; Sigma-Aldrich). 3-Aminopropyltriethoxysilane (APTES; Sigma-Aldrich).

Fig. S2. (a) Transmission electron microscopy images and (b) energy dispersive spectroscopy (EDS) mapping of van-SiO2-MNPs.

Fig. S3. Zeta potential of MNPs, SiO2-MNPs and van-SiO2-MNPs. The potential was measured using Zetasizer Nano ZS (Malvern Instruments, Malvern, UK). Student’s t-test. **: P < 0.01. *: P < 0.05. n = 3.

Fig. S4. (a) qPCR and (b) the standard curve (Ct value vs bacterial concentration) of S. aureus at different concentrations (10-104 CFU/mL) in PBS preconcentrated by van-SiO2-MNPs and van-PDA-MNPs. Forward (5'-ACACCTGAAACAAAGCATCC-3') and reverse (5'-TAGCCAAGCCTTGACGAACT-3') primers were used, to amplify a 207-bp of nuc gene from S. aureus [2].

References

1.

2. L.E. O'Donnell, K. Smith, C. Williams, C.J. Nile, D.F. Lappin, D. Bradshaw, M. Lambert, D.P. Robertson, J. Bagg, V. Hannah. Dentures are a reservoir for respiratory pathogens. J. Prosthodont. 2016; 25: 99-104.