Supplementary Information

Displacement-mediated bound states in the continuum in all-dielectric superlattice metasurfaces

Tan Shi1, Zi-Lan Deng1*, Qing-An Tu1, Yaoyu Cao1, Xiangping Li1

1 Guangdong Provincial Key Laboratory of Optical Fiber Sensing and Communications, Institute of Photonics Technology, Jinan University, Guangzhou, 510632, China.
* Correspondence: Z L Deng, E-mail: zilandeng@jnu.edu.cn

Fig. S1. Transmission spectra with variation of other structural parameters for TE-polarized normal incidences. (a) The unit cell of the superlattice metasurface with silicon nanobeams embedded in the vacuum. Parameters of the structure: px = 700 nm, py = 750 nm, wx = 150 nm, wy = 700 nm, h = 110 nm, d1 = 60 nm, and d2 = 130 nm. (b-f) The transmission spectra with respect to the px, py, h, wx and wy for the superlattice metasurface, respectively. It shows that the other structural parameters (py, wx, wy and h) can only regulate and control the peak position of double asymmetric Fano resonances, but cannot adjust the linewidth to infinitesimal. Only by adjusting the relationship between local displacement and global displacement (△d = 0 or px) can the linewidth be controlled or even disappeared.

Fig. S2. Quasi-BIC mediated by incident angles for TE-polarized incidences. (a) Calculated band structure along MΓ and ΓX directions as a function of k(px/2π) with the parameter px = 700 nm, py = 750 nm, wx = 150 nm, wy = 700 nm, h = 110 nm, and △d = 0. (b and c) Q-factor values along MΓ and ΓX directions for different types of modes. Q-factor speedily raises towards the Γ point for two different resonances. Insets represent the normalized electric field intensity diagram on the surface of a unit cell.

Fig. S3. The superlattice metasurface supporting a BIC for TE-polarized incidences when considering the nanobeams on the transparent low-index glass (n = 1.5) substrate. (a) The unit cell of the superlattice metasurface with the same parameters as Fig. 2a on glass substrate. (b) The transmission spectra with respect to the △d for superlattice metasurfaces. (c) Transmission spectra with respect to the angle and wavelength of incidence along x-direction. It can be seen that the Q-factor decrease with the existence of substrate (Compare with Fig. 1c), which is due to the fact that the substrate will convert the BIC into a resonant state, thus leaking through the radiation channel in the substrate. However, it still remains of high Q-factors and can be easily adjust the desired values by the introduced the parameter △d. And the whole spectra shift towards the long wave direction. (d) Transmission spectra with respect to the angle and wavelength of incidence.

Fig. S4. Extinction cross-section spectra by multipolar expansion of the superlattice metasurface with different modes in air for TE-polarized incidence with respect to angle 2°. ED (red line) denotes electric dipole; MD (blue line) denotes magnetic dipole; TD (yellow line) denotes toroidal dipole; EQ (green line) denotes electric quadrupole; MQ (violet line) denotes magnetic quadrupole and gray line denotes total scattering intensity. Figs. S4 (b) and (c) are local enlarged views of Fig. S4 (a). It reveals that the absorbing phenomenon can be largely attributed to the coexistence of dominant multipoles. The quasi-BIC caused by the parameter △d is dominated by TD mode, coupled with concomitance of other multipoles inclusive of MD mode and MQ mode with distinct strengths, while the quasi-BIC caused by the incident angle is produced by the concomitance of predominant multipoles including MD mode and EQ mode with unequal strengths.

Fig. S5. Transmission spectra of other structural parameters for TM-polarized incidence of the superlattice metasurface with the same parameters as Fig. S1. (a-e) The transmission spectra with respect to the wx, wy, h, px and py for superlattice metasurface, respectively. (f) Schematic diagram of TM-polarized oblique incidence at an angle of θ along x direction. As can be seen, when px = 630 nm, d1 = 60 nm, d2 = 60 nm, that is △d = 0, the quasi-BIC bandwidth of the short-wave band disappears. When py = wy, the two-dimensional metasurface becomes a one-dimensional metasurface, and the Fano linewidth disappears in the longer wavelength band.