Integration of plasmonic AgPd alloy nanoparticles with single-layer graphitic carbon nitride as Mott-Schottky junction toward Photo-promoted H2 evolution

Behnam Gholipour b, Sadegh Rostamnia *, a, Afsaneh Zonouzi b

a Organic and Nano Group (ONG), Department of Chemistry, Iran University of Science and Technology (IUST), PO Box 16846-13114, Tehran, Iran Email: rostamnia@iust.ac.ir; srostamnia@gmail.com

b University of Tehran, Department of Chemistry, P.O. Box 14155-6455, Tehran, Iran

Email: zonouziafsaneh@ut.ac.ir

Abstract

Plasmonic AgPd alloy nanoparticles (AgPdNPs) decorated on single-layer carbon nitride (AgPdNPs/SLCN) for the designing of Mott-Schottky junction wereconstructed with the ultrasonically assisted hydrothermal method and used toward photoevolution H2 from formic acid (FA) at near room temperature (30 oC). The Pd atom contains active sites that are synergistically boosted by the localized surface plasmon resonance (LSPR) effect of Ag atoms, leading to considerably enhanced photocatalytic properties. The photoactive AgPdNPs/SLCN obtained supreme catalytic activity to produce 50 mL of gas (H2+CO2) with the initial turnover frequency of 224 h-1 under light irradiation. The catalyst showed stable catalytic performance during successive cycles.

Keywords: Plasmonic, graphitic carbon nitride, Mott-Schottky junction, formic acid, H2 evolution

Introduction

In line with the rising increasing demand for energy and the decrease in the utilization of usual fossil fuels, the outreach of surrogate and clean energy sources has become one of the most considerable issues1–3. Due to the exhaustion of fossil fuels and ecological issues, hydrogen-based fuel is one of the most hopeful sources of cleanse and sustainable energy for current society4–8. Currently, the industrial manufacture of hydrogen is chiefly produced through vapor reforming and coal gasification, which is based on confined fossil sources such as natural gas, coal, and oil. Based on mid to long-term plans, there is a growing requirement for substitute feedstocks for the production of H2 in a more sustainable way9,10. In recent years, various chemical hydrogen storing materials, such as methanol, formic acid, formaldehyde and boron ammonia have been extensively studied11–20. Formic acid (FA) as a hopeful material in H2 production/storage has engrossed much consideration owing to its great gravimetric/volumetric H2 capacity, easiness of use, non-toxicity, ambient temperature stability and plentiful supply from the transformation of biomass and carbon dioxide21–26.

For the use of FA as a liquid organic H2 carrier (LOHC), the expansion of competent catalysts, especially heterogeneous catalysts for FA decomposition, is a challenging issue27,28. On the other hand, over the past decades the field of heterogeneous photocatalysis has extension rapidly and has faced variant developments, particularly in regarding to energy and the environment29,30. Accordingly, in recent years, photocatalytic degradation of FA to CO2 and H2 has been broadly studied in the literature31–35. Recent reports have shown that the design and manufacture of conjugated semiconductor polymers due to their advantages such as constancy in aqueous-medium, visible light absorbency, intramolecular charge transition, the low expense is one of the effective strategies36–38. Supported semiconductors with visible light absorption can be used to modify the photocatalytic operation of heterogeneous metal based catalysts for photo- decomposition formic acid31,32,35. This is owing to the electronic interaction and electron handover betwixt the metal and the semiconductor due to the Mott–Schottky effect on the surface of the metal basedsemiconductor interfaces39. The integration of plasmonic based alloy (AgPd and AuPd) and semiconductors to make Mott-Schottky photocatalysts is an effective manner to improve photocatalytic operation by accelerating the charge kinetics of photocatalytic reactions32,35 .

Carbon nitride (g-C3N4) has been widely used as one of the most important photocatalyst in the production of hydrogen by visible light40,41. This is due to the π-conjugated graphitic carbon nitride structure that provides a specific electronic property for charge transfer41. On the other hand, as an active semiconductor in visible light, it has a relatively narrow bandgap of 2.7 eV and favorable conduction band (Cb) and valence band (Vb), which is appropriate for UV-vis light absorption for hydrogen evolution41. The most important point is that the performance of most noble metals is betwixt the Cb and the Vb of graphitic carbon nitride, which leads to the high reinforcement of the handover of photogenerated electrons from graphitic carbon nitride to metal nanoparticles owing to the Mott-Schottky effect 32,35. Recently, Cheng et al. reported graphite carbon nitride nanosheet containing AgPd bimetallic nanoparticles with Ag plasmonic effect as an effective mott-schottky photocatalyst to catalyzing the evolution of H2 from the formic acid under visible light42. Inspired by the aforesaid considerations and in line with our recent efforts in the field of clean energy and hydrogen production26,43–48, here we offer the synthesis of bimetallic AgPdNPs decorated on single layer carbon nitride (SLCN) as an active plasmonic photocatalyst for the evolution of H2 from FA.

Experimental

Materials and methods.

Melamine (Aldrich, 99%), AgNO3 (Aldrich, 99.99%), K2PdCl4 (Aldrich, 99.9%), Formic acid (Merck, 98-100%), KCl (Merck, 99.99%), NaBH4 (Merck, 99%) were used without additional refinement. Ultrapure water (18.5 MΩ Milli Q) was utilized for all experimentations.

Characterization.

FT-IR spectrums were recorded by a Shimadzu IR-460 spectrometer. Powder X-ray diffraction (PXRD) patterns were performed for samples using Bruker D8 ADVANCE X-ray diffractometer diffraction system with Cu Kα radiation (λ =1.5406 Å). UV-vis absorption and diffuse reflectance spectra were recorded using SHIMADZU, uv-2450. The surface morphology of samples was determined by the Hitachi S4700 FE-SEM. TEM images were captured with a Zeiss EM 900 electron microscope. The generated gas molecules (H2 + CO2) were monitored by gas chromatography (GC) armed with a TCD detector and the results were contrastedd with the automatic CO2 gas measuring apparatus.

Synthesis of g-C3N4.

g-C3N4 was synthesized by thermal polymerization of melamine from ambient temperature up to 550 °C with heating rate of 2.3 °C per minute and in the following by keeping the temperature constant at 550 oC for 4 h48.

Synthesis of SLCN.

Synthesis of g-C3N4 was executed using a complementary two-step manner (ultrasonic-hydrothermal method). For this purpose, 0.1 g of as-made bulk g-C3N4 was first exposed to ultrasonic waves for 2 h. In the following, after resting the obtained solution for 5 min, the upper part of the solution was separated and rendered into a Teflon-lined stainless autoclave (100 ml) and then heated at 120 °C for 10 h. Eventually, after the desired time had elapsed and the autoclave temperature reached ambient temperature, the almost yellowish white mixture was isolated by centrifugation (5000 rpm) and dried up at 50 °C for 12 h.

Synthesis of AgPdNPs/SLCN.

For the synthesis of AgPdNPs/SLCN, 0.1 g SLCN was dispersed in 40 mL distilled water and then sonicated at 25 oC for 30 min. Subsequently aqueous AgNO3 and K2PdCl4 (mole ratio= 1:0, 2:1, 1:1, 1:2, 0:1) was extra, and then magnetically stirred for overnight at ambient temperature. Afterward, 2.5 mL of aqueous NaBH4 (0.15 M) was added drop by drop into the mixture and stirred for another 2 h. After 2 h, the samples were gathered by centrifugation (5000 rpm) and rinsed with distilled water several times. The samples were dried in aoven at 50 °C for 15 h.

Photocatalytic dehydrogenation of FA.

The photocatalytic H2 evolution assessment was performed in a closed 50 mL reactor by a 24 W LED-SMD lamp. For this purpose, in 10 ml of deionized water, 20 mg of AgPdNPs/SLCN catalyst was dispersed by sonication and the reactor oxygen was purged by N2 before the reaction. Then 0.38 ml of 98% FA was injected into the catalyst solution at room temperature. The gas molecules produced were analyzed by a gas chromatograph. The amount of gas (H2 + CO2) evolution during the photocatalytic reaction was evaluated by a gas burette system. The TOFs are calculated within the initial 10 min conforming to the subsequent equation32:

TOF = ngas produced /(nAgPd × h)

Results and discussion

As shown in Scheme 1, we constructed the Mott-Schottky junction based ultra-thin carbon nitride single layers decorated with AgPd alloy nanoparticles with a simple strategy through a strong interaction between AgPdNPs and SLCN toward enhancement photocatalytic dehydrogenation of FA.

Scheme 1. Schematic illustration for the synthesis of AgPdNPs/SLCN

The chemical structure of SLCN as well as SLCN decorated with AgPd nanoparticles was analyzed by FT-IR spectrum (Fig 1a). The band appeared at 809 cm-1 is ascribed to the specific breathing mode of the triazine ring. Multiple peaks in the proximity to each other ​and in the range of 1200-1700 cm-1 are related to the stretching modes of aromatic C-N heterocycles. Wide absorption in the area of 3000-3500 cm-1 is attributed to the N-H stretching mode49. UV-vis absorption spectra of AgPdNPs/SLCN samples were inspected (Fig 1b). For Ag nanoparticles, the LSPR with high intensity in a region of 390-410 nm is observed. In the case of AgPd alloy, the intensity of the peak’s changes with a change in the Ag:pd ratio, so that for a ratio of 1:1 compared to 2:1, the effect of LSPR shows a greater reduction, which can be due to charge transfer to the AgNPs surface37,50–52. XRD patterns of the balk g-C3N4, SLCN and AgPd alloy nanoparticles supported on SLCN with different Ag:Pd ratios were revealed in Fig 1c and d. For bulk g-C3N4, a slight peak at 13.1o is observed, which is assigned to the (100) plan, attribute to the in-plane structural packaging motif of tri-s-triazine units. The strong diffraction at 27.5o also belongs to the (0 0 2) plan, which is related to the accumulation between the inter-layer stacking of conjugated aromatic rings. The peak with low intensity at 27.5o is related to the SLCN, which indicates the interlayer structure of balk CN was annihilated after exfoliation.49 For AgPd alloy nanoparticles with different ratios, the peak appears at a 39o, which shifted to elder angles with increasing Pd:Ag ratio, signifying that the AuPd alloy is formed on SLCN31.

Figure 1. (a) FT-IR spectrum, (b) UV-vis spectra of SLCN, Ag/SLCN, Ag2Pd1/SLCN, Ag1Pd1/SLCN and Pd/SLCN, (c) XRD patterns of the balk g-C3N4 and SLCN, (d) XRD patterns of SLCN, Ag/SLCN, Ag2Pd1/SLCN, Ag1Pd1/SLCN and Pd/SLCN.

Fig 2a demonstrates the general spectrum of Ag2Pd1/SLCN in which the characteristic peaks C1 s, N 1 s, Ag 3d and Pd 3d are clearly visible. In the high-resolution XPS spectrum for the C element, the binding energy at 284.7 eV attributed to the C-C bond and at 288 eV to C=N-C at SLCN (Fig 2b)53–55. Figure 2c also shows the XPS spectrum of element N in Ag2Pd1/SLCN, which corresponds to the energy bands C-N-C and C=N-H and -C=N53–55. Photoelectron spectroscopy (XPS) analysis was executed to further explore the effect of SLCN on the electronics of Ag and Pd structures in Ag2Pd1/SLCN. Examination of the XPS spectra of Ag 3d and Pd 3d shows that the binding energies for Pd 3d3/2 in Ag2Pd1/SLCN is shifted to lower values due to the handover of electrons from SLCN and Ag to Pd, while the binding energies for Ag 3d3/2 in Ag2Pd1/SLCN shift to higher values (Fig 2d and e)31,35,56. In fact, this indicates the redistribution of charge from higher Fermi level (Ag) to lower Fermi level (Pd)31.

Figure 2. (a) general XPS of Ag2Pd1/SLCN, (b) C1s regions of Ag2Pd1/SLCN, (c) N1s regions of Ag2Pd1/SLCN (d), Ag 3d regions of Ag2Pd1/SLCN and (e) Pd 3d regions of Ag2Pd1/SLCN.

Fig 2a exhibitions the SEM image of the balk g-C3N4 and SL-CN after ultrasonic exfoliation and then hydrothermal procedure. The presence of many sheets with laminar morphology proves SLCN synthesis. The SEM-EDS image and elemental mapping images approve the attendance of all composing elements (C, N, Ag, Pd) in the Ag2Pd1/SLCN structure. Fig 2e displays the EDS-SEM line scan profiles of Ag2Pd1/SLCN containing C, N, Ag and Pd atoms, which clearly confirm the approximately homogeneous distribution of atoms.

Fig 3. (a) SEM images of balk g-C3N4, (b, c and d) SEM images of SLCN, (e) EDS-SEM line scan profiles of Ag2Pd1/SLCN, (f) general map of Ag2Pd1/SLCN and (g-j) elemental mappings of SEM-EDX mappings of Ag2Pd1/SLCN.

The TEM image for SLCN and AgPdNPs/SLCN (Ag: Pd in a ratio of 1: 1) is revealed in Fig 3a and b. As is clear, a single-layer structure is beheld for the SLCN, which is also concord with the SEM image. The TEM image also shows 6 nm spherical AgPdNPs that are well embedded on the surface of SLCN.

Fig 4. (a) TEM image of SLCN, (b) TEM image of Ag1Pd1/SLCN, (c) the average diameter histogram of AgPdNPs for Ag1Pd1/SLCN and (d) the average particle area histogram of AgPdNPs for Ag1Pd1/SLCN.

The optical bandgap for the photocatalysts was obtained using the Tauc’s equation57:

αhυ= A(hυ - Eg) n

α: is the absorption coefficient

Eg: band gap

h: Planck’s constant

υ: the frequency of light

n: the electron transition process constant (the value of n is considered to be as 1/2.)

A: constant (in the ideal case A=1)

For each of the desired photocatalysts, the optical energy bandgap was appointed by extrapolation of the lined area of the plot of (αhυ)2 versus hυ (Fig 4a-d).

Fig 5. (a-d) plots of (αhυ)2 versus hυ for balk g-C3N4, SLCN, Ag2Pd1/SLCN and Ag1Pd1/SLCN.

Catalytic H2 evolution for 10 ml of 1.0 M aqueous FA was tested for all synthesized samples in the utilization of 0.2 g of the catalyst under dark conditions at ambient temperature. No gas was produced for SLCN or Ag/SLCN. In comparison, when Pd/SLCN, AgPd/SLCN were used, gas release was observed within 60 min, which the highest production value (15 cc) was obtained for Pd/SLCN (Fig 6a). Examination of the above conditions under visible light irradiation showed a comparable increased activity compared to the dark conditions for all Pd-comprising photocatalysts. Among the bimetallic photocatalysts for the 1: 1 ratio of Ag/Pd, the amount of gas produced was 50 ml, which shows the highest evolution rate compared to the 1: 3 and 3: 1 ratio (39 and 28 ml, respectively) (Fig 6b). Specifically, the activity of bimetallic AgPdNPs photocatalysts is superior to that of PdNPs under the same  situationss. This can be credited to the higher activity of AgPd alloys which occurs as a result of stoutinterplays and charge redistribution betwixt Ag and Pd and thus accelerate the photocatalytic dehydrogenation of FA. Figure 6c illustrations the TOFs value versus the ratio of Ag:Pd for the SLCN-supported photocatalysts in both dark and visible light conditions. Specifically, Ag1Pd1/SLCN disclosed the upmost activity with a TOF value of 224 h-1 under visible light irradiation. The highest TOF value in the dark condition was also obtained for Pd/SLCN, which was equal to 53 h-1. The results specify that alloying Ag with Pd leads to a synergistic effect and thus increases the activity of the desired photocatalyst. Accordingly, Ag1Pd1/SLCN was the best photocatalyst among the catalysts we studied for the evolution of hydrogen from the FA.

Fig 6. (a) Time-dependent gas evolution plots from FA in the dark at ~30 oC, (b) in the light irradiation at ~30 oC and (c) the TOFs ratio of various catalysts in the dark and light
irradiation.

Based on the above findings, we focused our studies in line with the influence of different amounts of Ag1Pd1/SLCN catalysts for the photocatalytic evolution of hydrogen. Accordingly, we tested values of less and more than 20 mg of Ag1Pd1/SLCN catalyst for achieving a better result. Using the values of 5 and 10 mg of catalyst showed less gas evolution. For 30 mg of the catalyst, a similar result was obtained with the amount of 20 mg catalyst (Fig 7a). In the following, by achieving the optimal amount of catalyst, we also studied the effect of different concentrations of FA. It is necessary to mention this point, we performed all of our studies at a concentration of 1 M, 10 mL of formic acid in accordance with valid reports in the literature. However, due to our interest in completing our research results, we also evaluated different concentrations of formic acid. At low concentrations, for example, 0.25 and 0.5 M, the amount of gas production was lower (20 and 30 ml, respectively), while at a concentration of 2 M, the amount of gas produced was 51 ml. This specifies that for high concentrations the evolution of hydrogen with increased intensity is not observed (Fig 7b). The rate of photocatalytic dehydrogenation of FA augmented linearly with increasing concentration (Fig 7c).

Fig 7. (a) The volume of gas evolution in the use of different amount of Ag1Pd1/SLCN for the photo-decomposition of FA, (b) the volume of gas evolution in the use of different concentrations for the photocatalytic decomposition of FA and (c) Initial TOF versus concentrations for Ag1Pd1/SLCN under light irradiation.

In the next step, the effect of light intensity on photo-decomposition of FA was explored using Ag1Pd1/SLCN and it was observed that the rate of dehydrogenation of FA enlarged linearly with increment light intensity (Fig 8a and b).

Fig 8. (a) The volume of gas evolution in the use of different light intensities for the photocatalytic decomposition of FA and (b) Initial TOF versus luminous power for Ag1Pd1/SLCN under visible light irradiation.

To ascertain the molar ratio of CO2:H2, a NaOH trap (10M NaOH based on gas burette system) was utilized to absorb CO235,58. In this experiment, the gas mixture produced was passed through a NaOH trap. The volume of gas produced in the use of the NaOH trap was reduced by half compared to the state without traps, which indicates that the volume of gas produced is 1: 1 (Fig 9a).

Fig 9. The comparison of the volume of gas produced by using Ag1Pd1/SLCN for dehydrogenation of aqueous FA solution with and without NaOH trap under visible light irradiation.

The activation energy (Ea=+31.2 KJmol-1) of reaction for Ag1Pd1/SLCN catalyst was calculated from the (Ln TOF = -Ea/R+(1/T) + LnA, R = 8.314 J/mol. K) relationship (Fig 10a and b). The value of R-square 0.97 was attained, which indicates that the points are the lined trend line.

Fig 10. Ln TOF versus 1/T plot in course of FA dehydrogenation by Ag1Pd1/SLCN at diverse temperatures, (b) Initial TOF versus temperatures plot for Ag1Pd1/SLCN.

Ag1Pd1/SLCN activity after four times exposure to visible light exposed that this catalyst is entirely stable and recyclable below visible light irradiation (Fig 11).

Fig 11. The recycling capability of Ag1Pd1/SLCN below visible light irradiation.

Conclusions

In summary, a series of AgPd alloy nanoparticles decorated on an SLCN semiconductor surface was designed to optimize plasmonic Mutt-Schottky catalysts toward the competent evolution of photocatalytic hydrogen from FA. Exhaustive studies revealed that the being of coordinated unsaturated N atoms on the SLCN surface is indispensable for the concurrent stabilization of Ag and Pd as uniform alloy nanoparticles. On the other hand, the desirable charge handover from SLCN and Ag to Pd leads to the enrichment of Pd with electrons and thus affords more catalytic activity and stability for the H2 evolution below visible light. This study presents a new path for designing plasmonic matte-Schottky heterogeneous catalysts with synergistic effects and high efficiency for photocatalytic hydrogen evolution by using formic acid.

References

1.	Tian, Y., Liu, X., Chen, F. & Zheng, Y. Harvesting energy from sun, outer space, and soil. Sci. Rep. 10, 1–9 (2020).

2.	Vavilapalli, D. S. et al. Nitrogen Incorporated Photoactive Brownmillerite Ca2Fe2O5 for Energy and Environmental Applications. Sci. Rep. 10, 1–13 (2020).

3.	Chu, S. & Majumdar, A. Opportunities and challenges for a sustainable energy future. Nature 488, 294–303 (2012).

4.	Luo, J. et al. Water photolysis at 12.3% efficiency via perovskite photovoltaics and Earth-abundant catalysts. Science (80-. ). 345, 1593–1596 (2014).

5.	Cabán-Acevedo, M. et al. Efficient hydrogen evolution catalysis using ternary pyrite-type cobalt phosphosulphide. Nat. Mater. 14, 1245–1251 (2015).

6.	Sanderson, K. Hydrogen fuel goes liquid. Nature 748, 70820 (2007).

7.	Van Noorden, R. Liquid storage could make hydrogen a feasible fuel. Nature 1–2 (2013) doi:10.1038/nature.2013.12518.

8.	Staffell, I. et al. The role of hydrogen and fuel cells in the global energy system. Energy Environ. Sci. 12, 463–491 (2019).

9.	Eppinger, J. & Huang, K. W. Formic Acid as a Hydrogen Energy Carrier. ACS Energy Lett. 2, 188–195 (2017).

10.	Grasemann, M. & Laurenczy, G. Formic acid as a hydrogen source - Recent developments and future trends. Energy Environ. Sci. 5, 8171–8181 (2012).

11.	Joó, F. Breakthroughs in hydrogen storage\-formic acid as a sustainable storage material for hydrogen. ChemSusChem 1, 805–808 (2008).

12.	Fellay, C., Dyson, P. J. & Laurenczy, G. A viable hydrogen-storage system based on selective formic acid decomposition with a ruthenium catalyst. Angew. Chemie - Int. Ed. 47, 3966–3968 (2008).

13.	Enthaler, S., Von Langermann, J. & Schmidt, T. Carbon dioxide and formic acid - The couple for environmental-friendly hydrogen storage? Energy Environ. Sci. 3, 1207–1217 (2010).

14.	Boddien, A. et al. Efficient dehydrogenation of formic acid using an iron catalyst. Science (80-. ). 333, 1733–1736 (2011).

15.	Kar, S., Rauch, M., Leitus, G., Ben-David, Y. & Milstein, D. Highly efficient additive-free dehydrogenation of neat formic acid. Nat. Catal. 4, 193–201 (2021).

16.	Zhu, Q. L., Tsumori, N. & Xu, Q. Immobilizing Extremely Catalytically Active Palladium Nanoparticles to Carbon Nanospheres: A Weakly-Capping Growth Approach. J. Am. Chem. Soc. 137, 11743–11748 (2015).

17.	Zhang, S. et al. Photocatalytic hydrogen evolution from formate and aldehyde over molecular iridium complexes stabilized by bipyridine-bridging organosilica nanotubes. Appl. Catal. B Environ. 236, 466–474 (2018).

18.	Nielsen, M. et al. Low-temperature aqueous-phase methanol dehydrogenation to hydrogen and carbon dioxide. Nature 495, 85–89 (2013).

19.	Verma, P., Yuan, K., Kuwahara, Y., Mori, K. & Yamashita, H. Enhancement of plasmonic activity by Pt/Ag bimetallic nanocatalyst supported on mesoporous silica in the hydrogen production from hydrogen storage material. Appl. Catal. B Environ. 223, 10–15 (2018).

20.	Hu, H., Jiao, Z., Ye, J., Lu, G. & Bi, Y. Highly efficient hydrogen production from alkaline aldehyde solutions facilitated by palladium nanotubes. Nano Energy 8, 103–109 (2014).

21.	Wang, Z. L., Yan, J. M., Wang, H. L., Ping, Y. & Jiang, Q. Pd/C synthesized with citric acid: An efficient catalyst for hydrogen generation from formic acid/sodium formate. Sci. Rep. 2, 1–6 (2012).

22.	Sordakis, K. et al. Homogeneous Catalysis for Sustainable Hydrogen Storage in Formic Acid and Alcohols. Chem. Rev. 118, 372–433 (2018).

23.	Mellmann, D., Sponholz, P., Junge, H. & Beller, M. Formic acid as a hydrogen storage material-development of homogeneous catalysts for selective hydrogen release. Chem. Soc. Rev. 45, 3954–3988 (2016).

24.	Mori, K., Futamura, Y., Masuda, S., Kobayashi, H. & Yamashita, H. Controlled release of hydrogen isotope compounds and tunneling effect in the heterogeneously-catalyzed formic acid dehydrogenation. Nat. Commun. 10, 1–10 (2019).

25.	Mori, K., Sano, T., Kobayashi, H. & Yamashita, H. Surface Engineering of a Supported PdAg Catalyst for Hydrogenation of CO 2 to Formic Acid: Elucidating the Active Pd Atoms in Alloy Nanoparticles. J. Am. Chem. Soc. 140, 8902–8909 (2018).

26.	Farajzadeh, M., Alamgholiloo, H., Nasibipour, F., Banaei, R. & Rostamnia, S. Anchoring Pd-nanoparticles on dithiocarbamate-functionalized SBA-15 for hydrogen generation from formic acid. Sci. Rep. 10, 1–9 (2020).

27.	Jin, M. H. et al. Mesoporous silica supported Pd-MnOx catalysts with excellent catalytic activity in room-temperature formic acid decomposition. Sci. Rep. 6, 1–12 (2016).

28.	van Putten, R., Wissink, T., Swinkels, T. & Pidko, E. A. Fuelling the hydrogen economy: Scale-up of an integrated formic acid-to-power system. Int. J. Hydrogen Energy 44, 28533–28541 (2019).

29.	Manuscript, A. Energy & Environmental Science. 0–179 (2019) doi:10.1039/C9EE00717B.

30.	Chen, X., Shen, S., Guo, L. & Mao, S. S. Semiconductor-based photocatalytic hydrogen generation. Chem. Rev. 110, 6503–6570 (2010).

31.	Xiao, L. et al. Carbon nitride supported AgPd alloy nanocatalysts for dehydrogenation of formic acid under visible light. J. Mater. Chem. A 5, 6382–6387 (2017).

32.	Zhang, S. et al. Plasmonic AuPd-based Mott-Schottky photocatalyst for synergistically enhanced hydrogen evolution from formic acid and aldehyde. Appl. Catal. B Environ. 252, 24–32 (2019).

33.	Liu, P. et al. Visible-light-driven catalytic activity enhancement of Pd in AuPd nanoparticles for hydrogen evolution from formic acid at room temperature. Appl. Catal. B Environ. 204, 497–504 (2017).

34.	Wen, M., Mori, K., Kuwahara, Y. & Yamashita, H. Plasmonic Au@Pd nanoparticles supported on a basic metal-organic framework: Synergic boosting of H2 production from formic acid. ACS Energy Lett. 2, 1–7 (2017).

35.	Liu, H. et al. Photocatalytic dehydrogenation of formic acid promoted by a superior PdAg@g-C 3 N 4 Mott-Schottky heterojunction. J. Mater. Chem. A 7, 2022–2026 (2019).

36.	Niu, W. et al. Enhancing Electron Transfer and Electrocatalytic Activity on Crystalline Carbon-Conjugated g-C3N4. ACS Catal. 8, 1926–1931 (2018).

37.	Zou, W. et al. Advantageous Interfacial Effects of AgPd/g-C 3 N 4 for Photocatalytic Hydrogen Evolution: Electronic Structure and H 2 O Dissociation. Chem. - A Eur. J. 25, 5058–5064 (2019).

38.	Fan, X. et al. Construction of Conjugated Intramolecular for Donor-Acceptor Copolymers Photocatalytic Hydrogen Evolution. 1–24.

39.	Li, X. ChemInform Abstract : Metal Nanoparticles at Mesoporous N-Doped Carbons. (2014) doi:10.1039/c3cs60067j.

40.	Corp, K. L. & Schlenker, C. W. Ultrafast Spectroscopy Reveals Electron-Transfer Cascade That Improves Hydrogen Evolution with Carbon Nitride Photocatalysts. J. Am. Chem. Soc. 139, 7904–7912 (2017).

41.	Ong, W., Tan, L., Ng, Y. H., Yong, S. & Chai, S. Graphitic Carbon Nitride ( g ‑ C 3 N 4 ) ‑ Based Photocatalysts for Arti fi cial Photosynthesis and Environmental Remediation : Are We a Step Closer To Achieving Sustainability ? (2016) doi:10.1021/acs.chemrev.6b00075.

42.	Wan, C. et al. Boosting visible-light-driven hydrogen evolution from formic acid over. Chem. Eng. J. 396, 125229 (2020).

43.	Alamgholiloo, H., Rostamnia, S., Hassankhani, A., Liu, X. & Eftekhari, A. Journal of Colloid and Interface Science Formation and stabilization of colloidal ultra-small palladium nanoparticles on diamine-modified Cr-MIL-101 : Synergic boost to hydrogen production from formic acid. J. Colloid Interface Sci. 567, 126–135 (2020).

44.	Nouruzi, N. et al. Selective catalytic generation of hydrogen over covalent organic polymer supported Pd nanoparticles (COP-Pd). Mol. Catal. 493, 111057 (2020).

45.	Manuscript, A. ChemComm. (2018) doi:10.1039/C8CC00275D.

46.	Shokouhimehr, M. & Alonso, D. A. mesoporous organosilica as efficient photocatalyst for oxidative formic acid decomposition. doi:10.1002/cctc.201900486.

47.	Doustkhah, E. et al. Organosiloxane tunability in mesoporous organosilica and punctuated Pd nanoparticles growth; theory and experiment. Microporous Mesoporous Mater. 293, 109832 (2020).

48.	Ma, T. Y., Dai, S., Jaroniec, M. & Qiao, S. Z. Graphitic carbon nitride nanosheet-carbon nanotube three-dimensional porous composites as high-performance oxygen evolution electrocatalysts. Angew. Chemie - Int. Ed. 53, 7281–7285 (2014).

49.	Zhao, H. et al. Fabrication of atomic single layer graphitic-C3N4 and its high performance of photocatalytic disinfection under visible light irradiation. Appl. Catal. B Environ. 152–153, 46–50 (2014).

50.	Mohan, S. et al. Dual probes of Ag/Pd bimetallic NPs facilely synthesized by green process using Catharanthus leaf extract on textile dye removal and free radical capability. Appl. Nanosci. 11, 1565–1574 (2021).

51.	Eken Korkut, S., Küçükkeçeci, H. & Metin, Ö. Mesoporous Graphitic Carbon Nitride/Black Phosphorus/AgPd Alloy Nanoparticles Ternary Nanocomposite: A Highly Efficient Catalyst for the Methanolysis of Ammonia Borane. ACS Appl. Mater. Interfaces 12, 8130–8139 (2020).

52.	Ma, J. et al. The preparation and photocatalytic activity of Ag-Pd/g-C3N4 for the coupling reaction between benzyl alcohol and aniline. Mol. Catal. 476, 110533 (2019).

53.	Fang, J., Fan, H., Li, M. & Long, C. Nitrogen self-doped graphitic carbon nitride as efficient visible light photocatalyst for hydrogen evolution. J. Mater. Chem. A 3, 13819–13826 (2015).

54.	Wang, P., Guan, Z., Li, Q. & Yang, J. Efficient visible-light-driven photocatalytic hydrogen production from water by using Eosin Y-sensitized novel g-C3N4/Pt/GO composites. J. Mater. Sci. 53, 774–786 (2018).

55.	Qiao, F., Wang, J., Ai, S. & Li, L. As a new peroxidase mimetics: The synthesis of selenium doped graphitic carbon nitride nanosheets and applications on colorimetric detection of H2O2 and xanthine. Sensors Actuators, B Chem. 216, 418–427 (2015).

56.	Fu, G. T., Liu, C., Zhang, Q., Chen, Y. & Tang, Y. W. Polyhedral palladium-silver alloy nanocrystals as highly active and stable electrocatalysts for the formic acid oxidation reaction. Sci. Rep. 5, 1–9 (2015).

57.	Khan, S. et al. A Semiconducting Copper(II) Coordination Polymer with (4,4) Square Grid Topology: Synthesis, Characterization, and Application in the Formation of a Photoswitch. Cryst. Growth Des. 18, 651–659 (2018).

58.	Gu, X., Lu, Z. H., Jiang, H. L., Akita, T. & Xu, Q. Synergistic catalysis of metal-organic framework-immobilized au-pd nanoparticles in dehydrogenation of formic acid for chemical hydrogen storage. J. Am. Chem. Soc. 133, 11822–11825 (2011).