A multi-component reaction for covalent immobilization of lipases on amine-functionalized magnetic nanoparticles: production of biodiesel from waste cooking oil

Yalda Aminia, Zohreh Habibi a*, Maryam Yousefi b*, Maryam Ashjari a,c, Mehdi Mohammadi c, Mansour Shahedia

a Department of Organic Chemistry and Oil, Faculty of Chemistry, Shahid Beheshti University,    Tehran, Iran

b  Nanobiotechnology Research Center, Avicenna Research Institute, ACECR, Tehran, Iran

c Bioprocess Engineering Department, Institute of Industrial and Environmental Biotechnology, National Institute of Genetic Engineering and Biotechnology (NIGEB), Tehran, Iran

Table 1S Sequential Model Sum of Squares (RML)

| Source | Sum of Squares | df | Mean Square | F value | Prob > F |  |
| --- | --- | --- | --- | --- | --- | --- |
| Mean vs Total | 72404.28 | 1 | 72404.28 |  |  |  |
| Linear vs Mean | 410.11 | 5 | 82.02 | 1.89 | 0.1181 |  |
| 2FI vs Linear | 1165.36 | 10 | 116.54 | 6.42 | < 0.0001 | Suggested |
| Quadratic vs 2FI | 70.70 | 5 | 14.14 | 0.75 | 0.5975 |
| Cubic vs Quadratic | 167.98 | 15 | 11.20 | 0.35 | 0.9647 | Aliased |
| Residual | 287.42 | 9 | 31.94 |  |  |  |
| Total | 74506.12 | 45 | 1655.69 |  |  |  |

Table 2S Sequential Model Sum of Squares (CALB)

| Source | Sum of Squares | df | Mean Square | F value | Prob > F |  |
| --- | --- | --- | --- | --- | --- | --- |
| Mean vs Total | 73071.74 | 1 | 73071.74 |  |  |  |
| Linear vs Mean | 237.87 | 5 | 47.57 | 1.13 | 0.3627 |  |
| 2FI vs Linear | 1249.81 | 10 | 124.98 | 9.12 | < 0.0001 | Suggested |
| Quadratic vs 2FI | 113.08 | 5 | 22.62 | 1.91 | 0.1304 |
| Cubic vs Quadratic | 118.69 | 15 | 7.91 | 0.43 | 0.9288 | Aliased |
| Residual | 165.82 | 9 | 18.42 |  |  |  |
| Total | 74957.01 | 45 | 1665.71 |  |  |  |

Table 3S experimental design for five-level five-factor surface response design on transesterification of waste cooking oil using immobilized RML

| Run | A:Reaction | B:Water | C:Enzym | D:t-butanol | E:Methanol | FAME yield |
| --- | --- | --- | --- | --- | --- | --- |
|  | Temperature | absorbent |  |  | to oil | % |
| 1 | 40 | 50 | 20 | 20 | 4 | 59.9 |
| 2 | 40 | 50 | 20 | 50 | 4 | 47.1 |
| 3 | 55 | 40 | 15 | 35 | 5 | 32.1 |
| 4 | 35 | 40 | 15 | 35 | 5 | 40.8 |
| 5 | 40 | 30 | 20 | 50 | 4 | 42.5 |
| 6 | 45 | 40 | 15 | 35 | 3 | 35.8 |
| 7 | 40 | 50 | 10 | 50 | 6 | 42.3 |
| 8 | 40 | 50 | 10 | 20 | 6 | 30.6 |
| 9 | 50 | 50 | 10 | 50 | 4 | 39.8 |
| 10 | 45 | 40 | 15 | 35 | 5 | 40.9 |
| 11 | 45 | 60 | 15 | 35 | 5 | 37.8 |
| 12 | 50 | 50 | 20 | 50 | 4 | 39.2 |
| 13 | 40 | 30 | 10 | 20 | 4 | 35.3 |
| 14 | 45 | 40 | 15 | 35 | 7 | 43.6 |
| 15 | 50 | 30 | 10 | 50 | 6 | 60.9 |
| 16 | 50 | 30 | 20 | 50 | 6 | 41.5 |
| 17 | 50 | 50 | 10 | 50 | 6 | 39.1 |
| 18 | 50 | 30 | 10 | 20 | 4 | 34.9 |
| 19 | 40 | 30 | 20 | 20 | 6 | 44.2 |
| 20 | 50 | 30 | 10 | 50 | 4 | 47.6 |
| 21 | 45 | 40 | 15 | 35 | 5 | 35.8 |
| 22 | 50 | 30 | 20 | 50 | 4 | 33.1 |
| 23 | 40 | 30 | 10 | 50 | 4 | 42.1 |
| 24 | 45 | 40 | 5 | 35 | 5 | 33.1 |
| 25 | 45 | 40 | 25 | 35 | 5 | 42.5 |
| 26 | 40 | 30 | 10 | 50 | 6 | 47.5 |
| 27 | 50 | 30 | 10 | 20 | 6 | 41.9 |
| 28 | 50 | 50 | 20 | 20 | 6 | 30.6 |
| 29 | 50 | 50 | 20 | 50 | 6 | 39.8 |
| 30 | 40 | 50 | 20 | 20 | 6 | 47.9 |
| 31 | 40 | 30 | 10 | 20 | 6 | 37.8 |
| 32 | 45 | 40 | 15 | 35 | 5 | 35.2 |
| 33 | 50 | 50 | 20 | 20 | 4 | 35.3 |
| 34 | 50 | 30 | 20 | 20 | 6 | 43.6 |
| 35 | 40 | 50 | 10 | 50 | 4 | 45.9 |
| 36 | 45 | 40 | 15 | 5 | 5 | 32.7 |
| 37 | 40 | 50 | 20 | 50 | 6 | 49.1 |
| 38 | 50 | 30 | 20 | 20 | 4 | 34.9 |
| 39 | 45 | 40 | 15 | 65 | 5 | 44.2 |
| 40 | 50 | 50 | 10 | 20 | 6 | 34.6 |
| 41 | 50 | 50 | 10 | 20 | 4 | 31.2 |
| 42 | 40 | 30 | 20 | 50 | 6 | 35.4 |
| 43 | 45 | 20 | 15 | 35 | 5 | 35.8 |
| 44 | 40 | 50 | 10 | 20 | 4 | 46.5 |
| 45 | 40 | 30 | 20 | 20 | 4 | 30.2 |

Table 4S experimental design for five-level five-factor surface response design on transesterification of waste cooking oil using immobilized TLL

| Run | A: Reaction | B: Water | C: Enzyme | D: t-butanol | E: Methanol | FAME yield |
| --- | --- | --- | --- | --- | --- | --- |
|  | Temperature |  |  |  | to oil | % |
| 1 | 40 | 10 | 20 | 20 | 4 | 38.2 |
| 2 | 50 | 30 | 20 | 20 | 6 | 44.9 |
| 3 | 40 | 10 | 20 | 20 | 6 | 61.9 |
| 4 | 45 | 0 | 15 | 35 | 5 | 50.3 |
| 5 | 50 | 30 | 20 | 50 | 6 | 40.9 |
| 6 | 50 | 30 | 20 | 20 | 4 | 49.4 |
| 7 | 45 | 20 | 5 | 35 | 5 | 29.3 |
| 8 | 50 | 30 | 10 | 50 | 6 | 54.3 |
| 9 | 50 | 10 | 10 | 50 | 4 | 38.5 |
| 10 | 40 | 10 | 20 | 50 | 4 | 30.4 |
| 11 | 50 | 10 | 20 | 50 | 6 | 51.5 |
| 12 | 45 | 20 | 15 | 35 | 5 | 46.8 |
| 13 | 40 | 30 | 10 | 50 | 6 | 42.8 |
| 14 | 40 | 10 | 20 | 50 | 6 | 28.2 |
| 15 | 50 | 10 | 10 | 20 | 4 | 25.3 |
| 16 | 45 | 40 | 15 | 35 | 5 | 30.3 |
| 17 | 50 | 30 | 10 | 20 | 4 | 22.1 |
| 18 | 45 | 20 | 15 | 65 | 5 | 41.2 |
| 19 | 50 | 30 | 10 | 20 | 6 | 19.0 |
| 20 | 45 | 20 | 15 | 35 | 3 | 30.9 |
| 21 | 40 | 10 | 10 | 50 | 4 | 33.7 |
| 22 | 50 | 10 | 20 | 20 | 6 | 53.1 |
| 23 | 55 | 20 | 15 | 35 | 5 | 37.8 |
| 24 | 45 | 20 | 15 | 35 | 5 | 38.8 |
| 25 | 40 | 10 | 10 | 20 | 4 | 23.4 |
| 26 | 45 | 20 | 25 | 35 | 5 | 56.0 |
| 27 | 40 | 30 | 20 | 20 | 4 | 48.3 |
| 28 | 40 | 30 | 20 | 20 | 6 | 44.4 |
| 29 | 40 | 30 | 10 | 20 | 6 | 22.2 |
| 30 | 40 | 30 | 10 | 50 | 4 | 33.2 |
| 31 | 50 | 10 | 10 | 20 | 6 | 46.2 |
| 32 | 40 | 10 | 10 | 50 | 6 | 40.4 |
| 33 | 50 | 30 | 20 | 50 | 4 | 42.2 |
| 34 | 40 | 30 | 20 | 50 | 6 | 26.0 |
| 35 | 40 | 30 | 10 | 20 | 4 | 13.3 |
| 36 | 40 | 10 | 10 | 20 | 6 | 42.1 |
| 37 | 45 | 20 | 15 | 5 | 5 | 32.0 |
| 38 | 50 | 10 | 20 | 20 | 4 | 35.3 |
| 39 | 45 | 20 | 15 | 35 | 5 | 38.8 |
| 40 | 40 | 30 | 20 | 50 | 4 | 31.4 |
| 41 | 45 | 20 | 15 | 35 | 7 | 44.3 |
| 42 | 50 | 10 | 20 | 50 | 4 | 28.6 |
| 43 | 35 | 20 | 15 | 35 | 5 | 24.7 |
| 44 | 50 | 30 | 10 | 50 | 4 | 39.6 |
| 45 | 50 | 10 | 10 | 50 | 6 | 54.1 |

Table 5S experimental design for five-level five-factor surface response design on transesterification and esterification of waste cooking oil using immobilized CALB

| Run | A:Reaction | B:Water | C:Enzyme | D:t-butanol | E:Methanol | FAME yield |
| --- | --- | --- | --- | --- | --- | --- |
|  | Temperature | absorbent |  |  | to oil | % |
| 1 | 40 | 50 | 20 | 20 | 4 | 49.0 |
| 2 | 40 | 50 | 20 | 50 | 4 | 49.0 |
| 3 | 55 | 40 | 15 | 35 | 5 | 35.6 |
| 4 | 35 | 40 | 15 | 35 | 5 | 34.1 |
| 5 | 40 | 30 | 20 | 50 | 4 | 42.4 |
| 6 | 45 | 40 | 15 | 35 | 3 | 43.0 |
| 7 | 40 | 50 | 10 | 50 | 6 | 48.9 |
| 8 | 40 | 50 | 10 | 20 | 6 | 52.2 |
| 9 | 50 | 50 | 10 | 50 | 4 | 28.6 |
| 10 | 45 | 40 | 15 | 35 | 5 | 50.6 |
| 11 | 45 | 60 | 15 | 35 | 5 | 38.1 |
| 12 | 50 | 50 | 20 | 50 | 4 | 27.6 |
| 13 | 40 | 30 | 10 | 20 | 4 | 35.3 |
| 14 | 45 | 40 | 15 | 35 | 7 | 44.5 |
| 15 | 50 | 30 | 10 | 50 | 6 | 39.4 |
| 16 | 50 | 30 | 20 | 50 | 6 | 31.9 |
| 17 | 50 | 50 | 10 | 50 | 6 | 41.4 |
| 18 | 50 | 30 | 10 | 20 | 4 | 34.0 |
| 19 | 40 | 30 | 20 | 20 | 6 | 29.0 |
| 20 | 50 | 30 | 10 | 50 | 4 | 41.5 |
| 21 | 45 | 40 | 15 | 35 | 5 | 39.6 |
| 22 | 50 | 30 | 20 | 50 | 4 | 45.4 |
| 23 | 40 | 30 | 10 | 50 | 4 | 47.1 |
| 24 | 45 | 40 | 5 | 35 | 5 | 41.0 |
| 25 | 45 | 40 | 25 | 35 | 5 | 40.3 |
| 26 | 40 | 30 | 10 | 50 | 6 | 36.4 |
| 27 | 50 | 30 | 10 | 20 | 6 | 45.9 |
| 28 | 50 | 50 | 20 | 20 | 6 | 40.9 |
| 29 | 50 | 50 | 20 | 50 | 6 | 33.0 |
| 30 | 40 | 50 | 20 | 20 | 6 | 47.1 |
| 31 | 40 | 30 | 10 | 20 | 6 | 32.0 |
| 32 | 45 | 40 | 15 | 35 | 5 | 40.3 |
| 33 | 50 | 50 | 20 | 20 | 4 | 34.1 |
| 34 | 50 | 30 | 20 | 20 | 6 | 44.3 |
| 35 | 40 | 50 | 10 | 50 | 4 | 49.0 |
| 36 | 45 | 40 | 15 | 5 | 5 | 42.4 |
| 37 | 40 | 50 | 20 | 50 | 6 | 36.0 |
| 38 | 50 | 30 | 20 | 20 | 4 | 37.5 |
| 39 | 45 | 40 | 15 | 65 | 5 | 38.7 |
| 40 | 50 | 50 | 10 | 20 | 6 | 49.4 |
| 41 | 50 | 50 | 10 | 20 | 4 | 31.4 |
| 42 | 40 | 30 | 20 | 50 | 6 | 33.1 |
| 43 | 45 | 20 | 15 | 35 | 5 | 38.6 |
| 44 | 40 | 50 | 10 | 20 | 4 | 49.0 |
| 45 | 40 | 30 | 20 | 20 | 4 | 42.4 |

Table 6S analysis of variance (ANOVA) for fitted quadratic polynominal model for optimization of transesterification parameters (RML)

|  | Sum of squares | df | Mean square | F value | p-value Prob>F |  |
| --- | --- | --- | --- | --- | --- | --- |
| Model | 1575.47 | 15 | 105.03 | 5.79 | < 0.0001 | Significant |
| A-Temprature | 134.54 | 1 | 134.54 | 7.42 | 0.0108 |  |
| B-Water adsorbance | 2.28 | 1 | 2.28 | 0.13 | 0.7258 |  |
| C-Enzyme | 5.58 | 1 | 5.58 | 0.31 | 0.5834 |  |
| D-t-butanol | 233.87 | 1 | 233.87 | 12.89 | 0.0012 |  |
| E-Methanol to oil | 33.84 | 1 | 33.84 | 1.87 | 0.1825 |  |
| AB | 331.74 | 1 | 331.74 | 18.29 | 0.0002 |  |
| AC | 112.54 | 1 | 112.54 | 6.20 | 0.0187 |  |
| AD | 37.12 | 1 | 37.12 | 2.05 | 0.1633 |  |
| AE | 80.17 | 1 | 80.17 | 4.42 | 0.0443 |  |
| BC | 206.66 | 1 | 206.66 | 11.39 | 0.0021 |  |
| BD | 15.13 | 1 | 15.13 | 0.83 | 0.3687 |  |
| BE | 215.20 | 1 | 215.20 | 11.86 | 0.0018 |  |
| CD | 159.19 | 1 | 159.19 | 8.77 | 0.0060 |  |
| CE | 0.056 | 1 | 0.056 | 3.089E-003 | 0.9561 |  |
| DE | 7.54 | 1 | 7.54 | 0.42 | 0.5241 |  |
| Residual | 526.10 | 29 | 18.14 |  |  |  |
| Lack of Fit | 506.97 | 27 | 18.78 | 1.96 | 0.3935 | not significant |
| Pure Error | 19.13 | 2 | 9.56 |  |  |  |
| Cor Total | 2101.57 | 44 |  |  |  |  |

Table 7S. Analysis of variance (ANOVA) for fitted quadratic polynominal model for optimization of transesterification parameters (TLL)

|  | Sum of squares | df | Mean square | F value | p-value Prob>F |  |
| --- | --- | --- | --- | --- | --- | --- |
| Model | 4346.32 | 15 | 289.75 | 8.80 | < 0.0001 | significant |
| A-Temprature | 310.02 | 1 | 310.02 | 9.42 | 0.0046 |  |
| B-Water | 234.49 | 1 | 234.49 | 7.12 | 0.0123 |  |
| C-Enzyme | 622.96 | 1 | 622.96 | 18.92 | 0.0002 |  |
| D-t-butanol | 50.77 | 1 | 50.77 | 1.54 | 0.2242 |  |
| E-Methanol to oil | 686.48 | 1 | 686.48 | 20.85 | < 0.0001 |  |
| AB | 8.31 | 1 | 8.31 | 0.25 | 0.6193 |  |
| AC | 3.64 | 1 | 3.64 | 0.11 | 0.7420 |  |
| AD | 210.88 | 1 | 210.88 | 6.41 | 0.0171 |  |
| AE | 22.40 | 1 | 22.40 | 0.68 | 0.4162 |  |
| BC | 104.41 | 1 | 104.41 | 3.17 | 0.0854 |  |
| BD | 140.39 | 1 | 140.39 | 4.26 | 0.0480 |  |
| BE | 374.62 | 1 | 374.62 | 11.37 | 0.0021 |  |
| CD | 1504.35 | 1 | 1504.35 | 45.70 | < 0.0001 |  |
| CE | 63.13 | 1 | 63.13 | 1.92 | 0.1767 |  |
| DE | 10.07 | 1 | 10.07 | 0.31 | 0.5844 |  |
| Residual | 954.64 | 29 | 32.92 |  |  |  |
| Lack of Fit | 911.82 | 27 | 33.77 | 1.58 | 0.4618 | not significant |
| Pure Error | 42.81 | 2 | 21.41 |  |  |  |
| Cor Total | 5300.96 | 44 |  |  |  |  |

Table 8S analysis of variance (ANOVA) for fitted quadratic polynominal model for optimization of transesterification parameters (CALB)

|  | Sum of squares | df | Mean square | F value | p-value Prob>F |  |
| --- | --- | --- | --- | --- | --- | --- |
| Model | 1486.95 | 13 | 114.38 | 8.90 | < 0.0001 | significant |
| A-Temprature | 116.85 | 1 | 116.85 | 9.09 | 0.0051 |  |
| B-Water adsorbance | 58.01 | 1 | 58.01 | 4.51 | 0.0417 |  |
| C-Enzyme | 40.31 | 1 | 40.31 | 3.14 | 0.0864 |  |
| D-t-butanol | 22.70 | 1 | 22.70 | 1.77 | 0.1935 |  |
| AB | 421.55 | 1 | 421.55 | 32.81 | < 0.0001 |  |
| AD | 37.54 | 1 | 37.54 | 2.92 | 0.0974 |  |
| AE | 281.34 | 1 | 281.34 | 21.90 | < 0.0001 |  |
| BC | 23.65 | 1 | 23.65 | 1.84 | 0.1847 |  |
| BD | 98.91 | 1 | 98.91 | 7.70 | 0.0093 |  |
| BE | 132.87 | 1 | 132.87 | 10.34 | 0.0030 |  |
| CD | 26.29 | 1 | 26.29 | 2.05 | 0.1626 |  |
| CE | 119.94 | 1 | 119.94 | 9.33 | 0.0046 |  |
| DE | 107.00 | 1 | 107.00 | 8.33 | 0.0070 |  |
| Residual | 398.31 | 31 | 12.85 |  |  |  |
| Lack of Fit | 322.56 | 29 | 11.12 | 0.29 | 0.9531 | not significant |
| Pure Error | 75.76 | 2 | 37.88 |  |  |  |
| Cor Total | 1885.27 | 44 |  |  |  |  |

a

b

Fig.1S. Stability of immobilized derivatives MNPs-RML (a) and MNPs-TLL (b) in the presence of 10, 20 and 50% of various co-solvents

a                                                                                      b

c

Fig.2S. Predicted fatty acid methyl ester yield versus experimental fatty acid methyl ester yield for MNPs-RML (a), MNPs-TLL (b) and MNPs-CALB(c)

a		              b

c

Fig.3S. Normal probability plots of residuals for (a) MNPs-TLL (b), MNPs-RML and MNPs-CALB(c).

Figure 4S. Response surface curves showing the interactions for RML

Fig.5S. Response surface curves showing the interactions for CALB