Breaking Symmetry of Single-Atom Catalysts Enables Extremely Low Energy Barrier and High Stability for Large-Current-Density Water Splitting

Xueqin Mu,1,2 Xiangyao Gu,1,3 Shipeng Dai,1 Jiabing Chen,1 Qu Chen,1 Min Yu,1 Changyun Chen,1 Wenxin Chen,4 Suli Liu,1* Shichun Mu2 *

X. Q. Mu, X. Y. Gu, S. P. Dai and J. B. Chen contributed equally to this work.

1Key Laboratory of Advanced Functional Materials of Nanjing, Nanjing Xiaozhuang University, Nanjing 211171, China.

2State Key Laboratory of Advanced Technology for Materials Synthesis and Processing, Wuhan University of Technology, Wuhan 430070, China.

3Guangxi Key Laboratory of Low Carbon Energy Materials, Guangxi Normal University, Guilin 541004, China.

4Beijing Key Laboratory of Construction Tailorable Advanced Functional Materials and Green Applications, School of Materials Science and Engineering, Beijing Institute of Technology, Beijing 100081, China

Corresponding E-mails: msc@whut.edu.cn; liusuli@njxzc.edu.cn

Experiment Section

Chemicals

2,5-Dihydroxyterephthalic acid (H4DOT, 98%, Maklin), Iron(II) acetate (Fe(ac)2, 90%, Energy Chemical), Cobaltous(II)nitrate hexahydrate (Co(NO3)2·6H2O, ≥98.5%), N,N-Dimethyl formamide, RuCl3·nH2O.

Preparation of FeCo-LDH/NF

First, a piece of nickel foam (NF, 2.0 cm × 3.0 cm) was taken in anhydrous ethanol, 0.5 M HCl and deionized water, respectively, after ultrasonic treatment for 15min, the NF was vacuum-dried at 60℃. Next, 30 mL DMF was added into a teflon liner (50 mL) containing H4DOT (0.090 g), Fe(ac)2  (0.047 g), Co(NO3)2·6H2O (0.210 g) to mix evenly, and then the 2.0 cm × 3.0 cm NF after treatment was vertically dipped into the solution. The mixed reactor was reacted in the oven at 120 ℃ for 24 h. After the reaction, the solution was cooled to room temperature, the surface of the nickel foam was carefully washed with anhydrous ethanol, and then placed in 60 ℃ vacuum drying for 6 h to obtain FeCo-LDH/NF.

Preparation of Ru1 SACs@FeCo-LDH/NF

The Ru1FeCo-LDH/NF were prepared at room temperature. First, 100 mg RuCl3·nH2O was dissolved in 25 mL methanol, and a piece of 2.0 cm × 3.0 cm FeCo-LDH/NF was vertically immersed into the solution in a small beaker and reacted for 15 min. After the reaction, Ru1FeCo-LDH/NF was obtained by vacuum drying at 60 ℃ for 6 h.

Preparation of Ru2 SACs@FeCo-LDH/NF

At the beginning, 100 mg RuCl3·nH2O was dissolved in teflon liner containing 25 mL methanol. After uniform mixing, a piece of 2.0 cm × 3.0 cm FeCo-LDH/NF was vertically immersed into the solution, and the high-pressure reactor was reacted at 130 ℃ for 3.5 h. When the reaction completed, the solution was cooled to room temperature, the surface of the nickel foam was carefully washed with anhydrous ethanol, and then placed in 60 ℃ vacuum drying for 6 h to obtain Ru2FeCo-LDH/NF.

Preparation of Ru1/NF

In preparation of Ru1FeCo-LDH/NF, it is only necessary to change the FeCo-LDH/NF into 2.0 cm × 3.0 cm NF, and other steps remain unchanged to obtain Ru/NF.

Preparation of Ru2/NF

In the preparation of Ru2FeCo-LDH/NF, it is only necessary to change the FeCo-LDH/NF into 2.0 cm × 3.0 cm NF, and other steps remain unchanged to prepare Ru/NF.

Method and Model

The Co and Fe atoms embed FeCo-LDH (001), Co, Fe and Ru atoms embed RuxFeCo-LDH (001) have been built. The intermediates of OH, O and OOH groups have absorbed on Co or Fe or Ru atom. The bottom LDH atom layers were fixed and the top LDH atom layers were allowed to relax to the minimum in the enthalpy without any constraints. The first principles calculations in the framework of density functional theory, including structural, electronic performances, were carried out based on the Cambridge Sequential Total Energy Package known as CASTEP.1 The exchange–correlation functional under the generalized gradient approximation (GGA)2 with norm-conserving pseudopotentials and Perdew–Burke–Ernzerhof functional was adopted to describe the electron–electron interaction.3 An energy cutoff of 750 eV was used and a k-point sampling set of 7 x 7 x 1 were tested to be converged. A force tolerance of 0.01 eV Å -1, energy tolerance of 5.0x10-7eV per atom and maximum displacement of 5.0x10-4 Å were considered. The GGA+U with spin polarization was adopted to describe the localized d states,4 where U = 3.42, 3.29 and 3.29 eV was applied for Co, Fe and Ru ions. The Grimme method for DFT-D correction is considered for all calculations.5

Thermodynamics and photocatalysis

Adsorption energy ΔE of A = OH, O and OOH groups on the surface of substrates was defined as:6

ΔE = E*A – (E*+ EA)                              (1)

where *A and * denote the adsorption of A groups on substrates and the bare substrates, EA denotes the energy of A groups.

Free energy change ΔG of the reaction was calculated as the difference between the free energies of the initial and final states as shown below:6-7

ΔG= ΔE + ΔZPE - TΔS                         (2)

where ∆E is the energy change between the reactant and product obtained from DFT calculations; ∆ZPE is the change of zero point energy; T and ∆S denote temperature and change of entropy, respectively. In here, T = 300K was considered.

- M. D. Segall, P. J. D. L. M. J. Probert, C. J. Pickard, P. J. Hasnip, S. J. Clark and M. C. Payne, J. Phys.: Condens. Matter, 2002, 14, 2717.

- J. P. Perdew, K. Burke and M. Ernzerhof, Phys. Rev. Lett., 1996,77, 3865.

- D. R. Hamann, M. Schl¨ uter and C. Chiang, Phys. Rev. Lett., 1979,43, 1494.

- Xu, H.X., Cheng, D.J., Cao, D.P., et al., A universal principle for a rational design of single-atom electrocatalysts, Nat. Catal., 2018, 5:339-348.

- S. Grimme, J. Comput. Chem., 2006, 27, 1787–1799.

- H. H. Li, Y. Wu, C. Li, Y. Y. Gong, L. Y. Niu, X. J. Liu, Q. Jiang, C. Q, Sun and S. Q. Xu, Appl. Catal. B: Environ., 2019, 251, 305–312.

- M. Bajdich, M. García-Mota, A. Vojvodic, J.K. Nørskov, A.T. Bell, Journal of the American Chemical Society, 135 (2013) 13521-13530.

Table S1. The mass atomic percentage from ICP analysis for different samples.

| Mass% | Ru1 SACs@FeCo-LDH | Ru2 SACs@FeCo-LDH | FeCo-LDH |
| --- | --- | --- | --- |
| Ru | 30% | 96.7% | - |
| Fe | 25% | 1.51% | 27.0% |
| Co | 45% | 0.23% | 73.0% |
| atomic ratio (Fe:Co:Ru) | 1:1.81:1.19 | 1:0.15:65 | 1:2.7 |

Figure S1. (a) SEM, (b) STEM and (c) TEM images of Ru2 SACs@FeCo-LDH.

Figure S2. (a) SEM, (b) STEM and (c) TEM images of Ru1 SACs@FeCo-LDH.

Figure S3. HAADF-STEM image for Ru1 SACs@FeCo-LDH.

Figure S4. XRD spectra of Ru1 SACs@FeCo-LDH and FeCo-LDH, respectively.

Figure S5. HRTEM images of Ru1 SACs@FeCo-LDH.

Figure S6. XPS spectra of Ru1 SACs@FeCo-LDH, Ru2 SACs@FeCo-LDH and FeCo-LDH

Table S2. The elemental atomic percentage from XPS analysis for different samples.

| Atomic%(XPS) | Ru1 SACs@FeCo-LDH | Ru2 SACs@FeCo-LDH | FeCo-LDH |
| --- | --- | --- | --- |
| Ru | 3.28% | 3.43% | - |
| O | 72.98% | 80.69% | 77.79% |
| Fe | 5.64% | 4.48% | 6.11% |
| Co | 4.79% | 1.46% | 7.78% |
| Ni | 13.31% | 9.94% | 8.32% |
| atomic ratio (Fe:Co:Ru) | 1:0.85:0.58 | 1:0.33:0.77 | 1:1.27 |

Figure S7. Fe 2p XPS spectra of Ru1 SACs@FeCo-LDH and FeCo-LDH.

Figure S8. Co 2p XPS spectra of Ru1 SACs@FeCo-LDH and FeCo-LDH.

Figure S9. Ru 3p XPS spectra of Ru1 SACs@FeCo-LDH and Ru2 SACs@FeCo-LDH.

Figure S10. O 1s XPS spectra of Ru1 SACs@FeCo-LDH, Ru2 SACs@FeCo-LDH and FeCo-LDH.

Figure S11. Polarization curves in 1.0 M KOH for OER electrocatalysis.

Table S3. Comparison of OER activities of other catalysts in KOH solution.

| Catalysts | η at 500 mA cm-2 (mV) | Reference |
| --- | --- | --- |
| Rux SACs@FeCo-LDH | 230@500 246@1000 | This work |
| NiMoOx/NiMoS | 278@500 334@1000 | Nat. Commun. 11, 5462 (2020) |
| MoNi4/SSW‖SSW Rs-12h | 285@500 | Adv. Energy Mater. 10, 1904020 (2020) |
| Ni3Nb-doped NiFe-OOH | 236@500 249@1000 | Adv. Energy Mater. 11, 2100968 (2021). |
| Ru-CoOx/NF | 370@1000 | Small 17, 2102777 (2021) |
| Ni0.8Fe0.2-AHNA | 260 @1078 | Energy Environ. Sci. 13, 86-95 (2020) |
| FeP/Ni2P | 293 @1000 | Nat. Commun. 9, 2551 (2018) |
| F0.25C1CH/NF | 308 @1000 | Adv. Energy Mater. 8, 1800175 (2018) |
| nano-KFO/NF | 308 @100 421 @2000 | J. Mater. Chem. A, 9, 7586–7593 (2021) |
| 5h-ANF | 350 @500 | ACS Nano 2021, 15, 3468−3480 |
| Fe-CoP/NF | 295 @500 428 @1000 | Adv. Sci. 5, 1800949 (2018) |
| (Ni,Fe)OOH | 259 @500 289 @1000 | Energy Environ. Sci. 11, 2858-2864 (2018) |
| NFN-MOF/NF | 360 @500 | Adv. Energy Mater. 8, 1801065 (2018) |
| SSW Rs-12 h | 287 @500 | Adv. Energy Mater. 10, 1904020 (2020) |
| Ni3S2/Fe-NiPx/NFc | 270 @500 291 @1000 | Adv. Sci. 2022, 2104846 |

Table S4. Comparison of HER activities of other catalysts in KOH solution.

| Catalysts | η at 500 mA cm-2 (mV) | Reference |
| --- | --- | --- |
| Rux SACs@FeCo-LDH | 84@500 117@1000 | This work |
| (Ni,Fe)OOH | 259 @500 289 @1000 | Energy Environ. Sci. 11, 2858-2864 (2018) |
| NFN-MOF/NF | 293 @500 | Adv. Energy Mater. 8, 1801065 (2018) |
| Pt@ Cu-0.3 | 438 @1000 | Adv. Funct. Mater. 31, 2105579 (2021) |
| Ni-Mo-B HF | 257 @500 | Adv. Funct. Mater. 2107308 (2021) |
| Ni3Nb doped NiFe-OOH | 236 @500 249 @1000 261 @2000 | Adv. Energy Mater. 11, 2100968 (2021) |
| Ni2P/NF | 306 @1000 368 @ 1500 | J. Am. Chem. Soc. 141, 7537 (2019) |
| h-NiMoFe | 97 @1000 | Energy Environ. Sci. 14, 4610 (2021) |
| F0.25C1CH/NF | 256 @1000 | Adv. Energy Mater. 8, 1800175 (2018) |

Table S5. Comparison of OWS activities of other catalysts in KOH solution.

| Catalysts | Voltage (V) at mA cm-2 | Reference |
| --- | --- | --- |
| Rux SACs@FeCo-LDH | 1.47 @500 1.52 @1000 | This work |
| (Ni,Fe)OOH // MoNi4 | 1.586 @500 1.657 @1000 | Energy Environ. Sci. 11, 2858-2864 (2018) |
| NFN-MOF/NF | 1.96 @500 | Adv. Energy Mater. 8, 1801065 (2018) |
| Ni nanowire array(−)//Ni0.8Fe0.2-AHNA(+) | 1.70 @500 | Energy Environ. Sci. 13, 86-95 (2020) |
| Ni-Mo-B HF | 1.88 @500 | Adv. Funct. Mater. 2107308 (2021) |
| FeP/Ni2P | 1.72 @500 1.78 @1000 | Nat. Commun. 2551 (2018) |
| FeCo carbonate hydroxide | 1.52 @500 | Adv. Energy Mater. 8, 1800175 (2018) |

Figure S12. The equivalent circuit of (a)-(c) of Ru1 SACs@FeCo-LDH, FeCo-LDH and Ru/NF electrocatalysts in 1.0 M KOH solution, respectively.

Figure S13. (a)Co 2p and (b) Fe 2p XPS spectra of Ru1 SACs@FeCo-LDH and after 1000 h.

Figure S14. Polarization curves in 1.0 M KOH for HER electrocatalysis.

Figure S15. Cyclic voltammograms of (a)-(c) of Ru2 SACs@FeCo-LDH, FeCo-LDH and Ru/NF electrocatalysts at various scan rates.

Figure S16. The equivalent circuit of (a)-(c) of Ru2 SACs@FeCo-LDH, FeCo-LDH, Ru/NF and Bare NF electrocatalysts, respectively.

Figure S17. (a, b) SEM images, (c)Co 2p and (d) Fe 2p XPS spectra of Ru2 SACs@FeCo-LDH and after 1000 h.

Figure S18. (a) Schematic of the electrolyzed water reaction. (b) H2 (Green) and O2 (Red) generated at 5, 10, 15, 20 min, respectively.

Figure S19. (a-b) Energy profile for the OER process on the FeCo-LDH and (c-e) Rux SACs@FeCo-LDH.

Figure S20. Top view of representative OER mechanism on Co active site over the FeCo-LDH and Rux SACs@FeCo-LDH

Figure S21. (a) Top and (b) side view of representative OER mechanism on Fe active site over the FeCo-LDH and Rux SACs@FeCo-LDH

Figure S22. (a) Top and (b) side view of representative OER mechanism on Ru active site over the FeCo-LDH and Rux SACs@FeCo-LDH