Electronic Supporting Information

for

Hollow and Oval-Configured Ultrafine Co3O4 as a Highly-Efficient Activator of Monopersulfate for Catalytic Elimination of Azorubin S

Text S1.

  - Materials

All chemical reagents employed in this study were commercially-purchased from commercial suppliers and used directly without any purifications. Cobalt nitrate (Co(NO3)2) (>98%) was acquired from Showa Chemicals, Japan. 2-methylimidazole (C4H6N2) (2-MIM) (99%) was obtained from ACROS Organics, Belgium. Oxone (monopersulfate compound) (KHSO5.0.5KHSO4.0.5K2SO4), azorubin S (ARS) (C20H11N2Na3O10S3), tannimum (C76H52O46), methyl alcohol (99.9%), ethyl alcohol (>99.8%), tert-butyl alcohol (>99.5%), sodium chloride (NaCl) (>99%), cetyltrimethylammonium bromide (CTAB) (>98%), and sodium dodecyl sulfate (SDS) (>99%) were purchased from Sigma-Aldrich, USA. Deionized water was prepared up to less than 18 MOhm-cm.

  - Synthesis of HOCO and characterizations

The synthesis procedure for preparing HOCO is depicted in Fig. 1(a). Initially, a Co-MOF with oval-like morphology was firstly prepared [27], followed by a modification step with tannimum via chemical-etching process before being calcined in air to obtain the final product. In a typical preparation, a solution containing 40 mL of Co(NO3)2 was slowly added into another solution bearing 40 mL of 2-MIM where the ratio of Co precursor to 2-MIM = 1:8 (in mole). The mixture was then stirred vigorously at ambient temperature for 4 h. Subsequently, the resultant purple-colored precipitate was assembled via centrifugation, rinsed by deionized water, and dried at 65 oC overnight to afford oval-like Co-MOF. Next, a certain amount of the as-prepared oval-like Co-MOF (i.e., 200 mg) was then immersed into a solution containing 300 mL mixture of deionized water and ethyl alcohol (ratio = 1:1 in volume) and tannimum (1 mg/mL) for 10 min to complete the chemical-etching process [26]. The resulting product was then collected via centrifugation (8000 rpm), washed thoroughly by ethyl alcohol several times, and dried at 80 oC in a vacuum oven to acquire hollow oval-like Co-MOF. Finally, this as-prepared hollow oval-like Co-MOF was calcined in air at 600 oC for 4 h at a ramping rate of 2 oC/min to afford hollow-structured oval-like Cobalt Oxide, abbreviated as HOCO.

For material characterizations, the appearance of all materials was determined using SEM and TEM (JEOL JSM-7800 F and JEM-1400, Japan). The elemental composition of HOCO was also analyzed using energy-dispersive X-ray spectroscopy (EDS) (Oxford Instruments, UK). Moreover, the crystalline structures of all as-prepared materials were characterized using an X-ray diffractometer (Bruker, USA). Besides, Raman spectroscopies of HOPO and commercial Co3O4 NP were verified using a Raman spectrometer (TII Nanofinder 30, Japan). The surface chemistry of HOCO was further examined using X-ray photoelectron spectroscopy (XPS) (ULVAC-PHI, PHI 5000, Japan). Additionally, the reducible behaviors of HOCO and commercial Co3O4 NP were further analyzed by H2-temperature-programmed reduction (H2-TPR) profiles using a chemisorption analyzer coupled with a TCD detector (Anton Paar, ASIQ TPx, Austria). Next, the BET surface area and pore volume of HOCO were determined by N2 sorption isotherms using a volumetric analyzer (Anton Paar Autosorb IQ, Austria). The surface charges of HOCO were also verified using a zetasizer (Nano-ZS, Malvern Instruments Ltd, UK).

  - Degradation of ARS

The degradation of ARS using HOCO-activated MPS was conducted using batch-type experiments. Typically, a certain amount of HOCO (i.e., 100 mg/L) was firstly added into ARS solution with the initial concentration (C0) of ARS was 50 mg/L for 30 min to verify the adsorption of ARS. Next, 100 mg/L of MPS was instantly introduced to the ARS solution to start the degradation experiment. At a certain reaction time (t), sample aliquots (3 mL) were taken out and filtered to separate HOCO from the ARS solution. The remaining ARS concentration in the filtrate at t min (Ct) was subsequently determined by UV-vis spectrophotometer with the absorption wavelength of 520 nm. For experimental sections, the effects of different parameters including different HOCO dosages, MPS dosages, various ARS concentrations, initial pH values, co-existing surfactants and salt, and inhibitors are investigated. Moreover, for comparison, commercial Co3O4 NP (size 50~80 nm) was also used for MPS activation. The reactive oxygen species (ROS) involving in the degradation of ARS by HOCO+MPS system were revealed by electron paramagnetic resonance (EPR) with a typical radical spin-trapping agent, namely 5,5-Dimethyl-1-pyrroline N-oxide (DMPO). The recyclability of HOCO for multiple ARS degradation cycles was also evaluated by re-using HOCO. Besides, the degradation intermediates produced from ARS degradation were further identified using a mass spectrometer (Thermo Finnigan Corporation, LCQ ion-trap mass spectrometer, USA).

Table S1. Textural properties of HOCO and commercial Co3O4 NPs.

| Materials | Specific surface area (m2/g) | Pore volume (cm3/g) |
| --- | --- | --- |
| HOCO | 43.57 | 0.26 |
| Commercial Co3O4 | 2.5 | 0.001 |

Table S2. A comparison of activation energy (Ea) values for ARS degradation using different catalytic systems.

| Catalytic Systems | Ea (kJ/mol) | Reference |
| --- | --- | --- |
| HOCO+MPS | 30.9 | This work |
| Fc+SPC | 70.4 | [1] |
| MIL-N+MPS+vis-light | 38.8 | [2] |

Table S3. Detected by-products of ARS degradation by HOCO+MPS

|  | Structure | Formula | m/z |
| --- | --- | --- | --- |
| M1 |  | C20H11N2O10S33- | 178 |
| M2 |  | C20H14N2O4 | 347 |
| M3 |  | C10H8O2 | 160 |
| M4 |  | C10H8O4 | 192 |
| M5 |  | C6H4O2 | 108 |
| M6 |  | C4H4O4 | 116 |
| M7 |  | CH2O3 | 62 |

Fig. S1. XRD pattern of hollow oval-like Co-MOF after chemical etching process with tannium.

Fig. S2. (a) EDX analysis, (b-d) elemental mapping of HOCO.

100 nm

Fig. S3. SEM image of commercial Co3O4 NP.

(a)

(b)

(d)

(c)

Fig. S4. Calculated kobs values of (a) different temperatures, (b) pH variation, (c) co-existing compounds, and (d) scavengers. (Reaction conditions: HOCO = 100mg/L, MPS = 100 mg/L, T = 30 oC).

(b)

(a)

LUMO

HOMO

Fig. S5. Molecular orbitals of geometrically-optimized BP1: (a) HOMO; (b) LUMO.

Fig. S6. ESI mass spectrum of intermediates of ARS degradation.

Reference

1.	Lin, K.-Y.A., J.-T. Lin, and Y.-F. Lin, Heterogeneous catalytic activation of percarbonate by ferrocene for degradation of toxic amaranth dye in water. Journal of the Taiwan Institute of Chemical Engineers, 2017. 78: p. 144-149.

2.	Zhang, M.-W., et al., Enhanced degradation of toxic azo dye, amaranth, in water using Oxone catalyzed by MIL-101-NH2 under visible light irradiation. Separation and Purification Technology, 2019. 227: p. 115632.