Enzymatic upgrading of nanochitin using an ancient Lytic Polysaccharide Monooxygenase

Leire Barandiaran1±, Borja Alonso-Lerma1±, Antonio Reifs1, Izaskun Larraza2, Raquel Olmos-Juste2, Alba Fernández-Calvo1, Arantxa Eceiza2, Raul Perez-Jimenez1,3*.

1CIC nanoGUNE BRTA, San Sebastian, Spain. Tolosa Hiribidea, 76, 20018 Donostia, Gipuzkoa

2Group ‘Materials+Technologies’, Department of Chemical and Environmental Engineering, Faculty of Engineering of Gipuzkoa, University of the Basque Country, Elias Salaberria Kalea, 20018 Donostia, Gipuzkoa, San Sebastian, Spain

3Ikerbasque Foundation for Science, Bilbao, Spain.

±These authors contributed equally to the work

*Corresponding author E-mail: r.perezjimenez@nanogune.eu

Supplementary Figure 1. Posterior probability of all the inferred residues of the LFACA-LPMO (Ancestral LPMO). The residue with the highest posterior probability is assigned at each position and average posterior probability value for the inferred LFACA-LPMO is above 0.9.

Supplementary Figure 2. Predicted values for local Distance Difference Test (lDDT) per residue position provided by Alphafold2 for the two enzymes tested.

Supplementary Figure 3. (a) SDS-PAGE electrophoresis of purified LFACA-LPMO and Bt LPMO. A band at around 20 kDa is observed in both cases, indicating the correct size of the proteins. We also observe a higher production of LFACA-LPMO using the exact same culture volume and expression conditions. (b). LPMO production. LFACA is produced at higher quantity than BtLPMO, around 25% more protein is recovered after purification from 100 mL culture.

Supplementary Figure 4. Size distribution of CNCh particles produced with (a) LFACA-LPMO and (b) BtLPMO using -Chitin as substrate at different times, with darker color lines for longer times. The distribution was calculated with the length of 100 particles from each condition.

Supplementary Figure 5. (a) FTIR spectra of EnCNCh produced by LFACA-LPMO at 24-, 48-, 72- and 96-hours hydrolysis of α-chitin. Spectra collected from 4000 to 750 cm-1, (b) Highlight from 2000 to 750 cm-1. (c) Details of the significant incipient peaks of EnCNCh at 1710 cm-1 and C-O stretching and bending peak shape change detail at 1070 and 1008 cm-1.

Supplementary Figure 6. (a) FTIR spectra of EnCNCh produced by BtLPMO at 24, 48, 72 and 96 hours hydrolysis of α-chitin. Spectra collected from 4000 to 750 cm-1, (b) Zoom in from 2000 to 750 cm-1. (c) details of the significant incipient peaks of CNCh at 1710 cm-1 and C-O stretching and bending shape change detail at 1070 and 1008 cm-1.

Supplementary Figure 7. CNCh films immersion into water. After immersion films challenged by orbital agitation to test film integrity. AcCNCh film did not maintain shape and disintegrated shortly after sinking into water, whereas EnCNCh maintained a solid and consistent shape.

Supplementary Figure 8. EnCNCh + n% GO films pictures. From left to right rGO wt % increases.

Supplementary Figure 9. SEM images of films prepared with EnCNCh with different graphene oxide concentrations: 0.3, 2, 5, 10 and 15 wt%. The surface of the films seems rougher when rGO content increases.

### Supplementary Figure 10. FTIR spectra of EnCNCh and EnCNCh + n%GO films.

Supplementary Figure 11. (a) Representation of 2D EnCNCh+5% rGO paper. (b) Graphic representation of HEK293 cells seeded on top of 2D EnCNCh+5% rGO paper. (c) Confocal microscopy image at 10X and 100X of HEK293T stained nuclei with DAPI and cell membrane with Orange Plasma. Cells sticked and proliferated embedded on EnCNCh+5% rGO 2D paper after 3 days of culture.

Supplementary table 1: Average length and diameter and L/D aspect ratio of EnCNCh particles obtained from α-chitin hydrolysis with LFACA-LPMO and extant BtLPMO at times of 24 hours, 48 hours, 72 hours, and 96 hours, as well as CNCh obtained by hydrochloric acid hydrolysis. Average parameters and S.D. were calculated with the length and diameters of 100 particles for each condition.

| Enzyme | Time (Hours) | Length (nm) | Diameter (nm) | L/D |
| --- | --- | --- | --- | --- |
|  | 24 | 1258.2±823.2 | 58.1±22.3 | 21.7 |
|  | 48 | 850.3±562,3 | 52.3±18.8 | 16.4 |
| LFACA-LPMO EnCNCh | 72 | 458.3±365,0 | 32.3±18.2 | 14.2 |
|  | 96 | 975.6±804.5 | 48.3±22.1 | 20.1 |
|  | 24 | 1334.2±863.5 | 62.0±23.6 | 21.5 |
|  | 48 | 968.5±496.3 | 57.0±14.2 | 16.9 |
| BtLPMO EnCNCh | 72 | 502.6±215.1 | 35.2±1=3 | 14.3 |
|  | 96 | 1058.3±65.3 | 51.7±22.5 | 20.5 |
| Ac CNCh | - | 178.6±67.2 | 15.8±8.3 | 11.3 |

Supplementary table 2. Onset degradation temperature (To), maximum thermal degradation temperature (Td) and char residue (%) of α-chitin, LFACA-LPMO EnCNCh, Bt LPMO-EnCNCh, and Ac CNCh.

| Sample | To (ºC) | Td (ºC) | Char residue (wt%) |
| --- | --- | --- | --- |
| α-Chitin | 286.01 | 394 | 13.4 |
| LFACA-EnCNCh | 170.73 | 374 | 20.06 |
| BtEnCNCh | 176.22 | 374 | 18.25 |
| AcCNCh | 263.66 | 385 | 13.18 |

Supplementary table 3:  Crystallinity index (CI%) and crystallite size of chitin, EnCNCh produced with LFACA-LPMO enzymatic hydrolysis, EnCNCh produces with extant BtLPMO enzymatic hydrolysis and AcCNC produced by HCl hydrolysis. The CI% was calculated by Segal method and the Scherrer's equation was used for the crystallite size.

| Enzyme | CI (%) | Crystallite size (nm) |
| --- | --- | --- |
| α-Chitin | 88 | 7.2 |
| LFACA-EnCNCh | 89 | 5.8 |
| BtEnCNCh | 90 | 6.3 |
| AcCNCh | 82 | 4.9 |

Supplementary table 4. Comparison of conductive properties of EnCNCh films with reduced graphene.

| Sample | Conductivity (S/m) |
| --- | --- |
| EnCNCh | 0 |
| EnCNCh + 0.3% rGO | 8.8 x 10-5 ±1.0 x 10-5 |
| EnCNCh + 1% rGO | 1.3 x 10-4 ±3 x 10-5 |
| EnCNCh + 2% rGO | 2.8 ± 1.2 |
| EnCNCh + 5% rGO | 7.4 ± 2.1 |
| EnCNCh + 10% rGO | 11.1 ± 3.0 |
| EnCNCh + 15% rGO | 16.0 ± 2.4 |
| EnCNCh | 0 |
| WEnCNCh + 0.3% rGO | 4.2 x 10-4 ±5.0 x 10-5 |
| WEnCNCh + 1% rGO | 2.4 x 10-1 ± 4.0 x 10-5 |
| WEnCNCh + 2% rGO | 2.6 ± 1.0 |
| WEnCNCh + 5% rGO | 13.1 ± 1.2 |
| WEnCNCh + 10% rGO | 16.4 ± 1.5 |
| WEnCNCh + 15% rGO | 18.4 ± 4.0 |

Supplementary note1. LPMO sequences from the species used in the construction of the phylogenetic tree. On the left hand the NCBI ID and on the right hand the species where the sequence belongs.

| NCBI ID | Species |
| --- | --- |
| WP_098855344.1 | Bacillus thuringiensis |
| WP_000742280.1 | Bacillus cereus |
| WP_097855297.1 | Bacillus toyonensis |
| WP_017149289.1 | Bacillus bingmayongensis |
| WP_033676157.1 | Bacillus gaemokensis |
| WP_084157953.1 | Bacillus manliponensis |
| WP_089967265.1 | Lihuaxuella thermophila |
| WP_006676405.1 | Paenibacillus dendritiformis |
| WP_087435284.1 | Paenibacillus apiarius |
| WP_087445137.1 | Paenibacillus thiaminolyticus |
| WP_036222403.1 | Lysinibacillus sphaericus |
| WP_082332692.1 | Lysinibacillus contaminans |
| WP_036094696.1 | Listeria newyorkensis |
| WP_070239340.1 | Listeria monocytogenes |
| WP_010772090.1 | Enterococcus caccae |
| WP_069664391.1 | Enterococcus termitis |
| WP_034688872.1 | Enterococcus mundtii |
| WP_076633771.1 | Lactobacillus plantarum |
| WP_021731441.1 | Lactobacillus |
| WP_055538846.1 | Streptomyces neyagawaensis |
| WP_055712380.1 | Streptomyces torulosus |
| WP_005486591.1 | Streptomyces bottropensis |
| WP_033531196.1 | Streptomyces galbus |
| WP_046731057.1 | Streptomyces humi |
| WP_093654234.1 | Streptomyces wuyuanensis |
| WP_026416933.1 | Actinomadura oligospora |
| WP_017615731.1 | Nocardiopsis salina |
| WP_039991854.1 | Serratia odorifera |
| WP_044552811.1 | Serratia liquefaciens |
| WP_054307289.1 | Serratia rubidaea |
| WP_085118064.1 | Serratia proteamaculans |
| WP_050539174.1 | Yersinia mollaretii |
| WP_051714045.1 | Shewanella |
| WP_099457584.1 | Shewanella xiamenensis |
| WP_009837614.1 | Pseudoalteromonas tunicata |
| WP_082916329.1 | Pseudoalteromonas neustonica |
| WP_072034004.1 | Rahnella aquatilis |
| WP_042289422.1 | Citrobacter |
| WP_077227974.1 | Leclercia adecarboxylata |
| WP_045353104.1 | Enterobacter cloacae complex |
| WP_059288204.1 | Enterobacter hormaechei |
| WP_053064552.1 | Klebsiella oxytoca |
| WP_064352001.1 | Klebsiella |
| WP_084204703.1 | Aeromonas popoffii |
| WP_079516857.1 | Kosakonia oryzae |
| WP_062702299.1 | Chryseobacterium indologenes |
| WP_084694528.1 | Chryseobacterium vrystaatense |
| WP_090024402.1 | Chryseobacterium oleae |
| WP_082798703.1 | Chryseobacterium cucumeris |
| WP_089695525.1 | Chryseobacterium culicis |
| WP_083997416.1 | Chryseobacterium angstadtii |

Supplementary note2. Ancestral and query LPMO sequences.

WP_098855344.1 Bacillus thuringiensis (Query), BtLPMO

MKKNSLQKMKKVILSGGVLLTGLLTFGFSEKASAHGYVESPASRSYLCKQGVNVNCGPIQYEPQSVEGIGGFPQLGPSDGQIAGAGHFPALDVQTVDRWKKVTLNGGTNTFKWKLTAPHSTKEWKYYITKKGWNPNKPLTRSDLDLVPFYVKNDGGARPGTTVTHEANVPTDRSGYHLILAVWEIADTGNAFYQVIDVNLLNNGLVSNFAFNNVVQTPTLF

LFACA-LPMO ancestral enzyme

VMKKMLMKSKKISIAVALLMAGLLTLLFASSASAHGYVSSPASRAYLCSLGKNTNCGSVQYEPQSVEAPKGFPAAGPADGQIASGGKFSQLDEQTANRWTKTPIKAGANTFTWHFTAPHATTKWHYYITKQGWNPNKPLTRADLELIPFCEIDDNGATPSTNVTHQVNVPSDRSGYHVILAVWDIADTGNAFYQVIDVNVGGGGATTAPANPTATGDKVTY