# RAW DATA

Table 1 – Detorque measurement for implant sets and implant abutments, with the respective mean and standard deviation values.

|  | IIA | NIIA | IIAMC | NIIAMC |
| --- | --- | --- | --- | --- |
| Sample 1 | 19,60 | 18,00 | 55,00 | 17,80 |
| Sample 2 | 20,00 | 20,00 | 56,00 | 19,70 |
| Sample 3 | 19,80 | 20,00 | 58,00 | 19,90 |
| Sample 4 | 20,00 | 21,00 | 55,00 | 20,30 |
| Sample 5 | 20,10 | 21,00 | 58,00 | 20,10 |
| Sample 6 | 20,00 | 19,00 | 52,00 | 18,90 |
| Sample 7 | 20,30 | 20,00 | 58,00 | 19,70 |
| Sample 8 | 19,80 | 20,00 | 52,00 | 19,20 |
| Sample 9 | 19,90 | 20,00 | 56,00 | 19,90 |
| Sample 10 | 20,10 | 20,00 | 52,00 | 19,60 |
| Mean value | 19,96 | 19,90 | 55,20 | 19,51 |
| Standard Deviation Value | 0,19 | 0,83 | 2,36 | 0,69 |

IIA – Indexed Morse taper implants and indexed implant abutments;

NIIA – Indexed Morse taper implants and non-indexed implant abutments;

IIAMC – Indexed Morse taper implants and indexed implant abutments submitted to mechanical cycling;

NIIAMC – Indexed Morse taper implants and non-indexed implant abutments submitted to mechanical cycling.

Table 2 – Results of bacterial colony forming units counts in the first dilution of the bacterial suspension of Streptococcus mutans, in Brain Heart Infusion Agar, after bacterial infiltration technique in the implant sets and implant abutments.

| Dilution D1 |  |  |  |  |
| --- | --- | --- | --- | --- |
|  | IIA | NIIA | IIAMC | NIIAMC |
| Sample 1 | 0 | 10 | 0 | 0 |
| Sample 2 | 0 | 12354 | 0 | 0.0001 |
| Sample 3 | 0 | 10 | 0 | 0 |
| Sample 4 | 0 | 185 | 0 | 0 |
| Sample 5 | 0 | 0 | 0.0001 | 0 |
| Sample 6 | 0 | 4480 | 0 | 0 |
| Sample 7 | 0 | 9595 | 0 | 0 |
| Sample 8 | 0 | 5 | 0 | 0 |
| Sample 9 | 60 | 0 | 0 | 0 |
| Sample 10 | 60 | 0 | 0 | 0 |

IIA – Indexed Morse taper implants and indexed implant abutments;

NIIA – Indexed Morse taper implants and non-indexed implant abutments;

IIAMC – Indexed Morse taper implants and indexed implant abutments submitted to mechanical cycling;

NIIAMC – Indexed Morse taper implants and non-indexed implant abutments submitted to mechanical cycling.

Table 3 – Analysis of the bacterial contamination, with reference to the first dilution (D1) of the bacterial suspension of Streptococcus mutans for all groups.