Extended Data Fig. 1| DFT results for BaH2 with H− defects. DFT calculations revealed that the (100) surface is the most stable in BaH2. The work function of BaH2 with H− defects that trap electrons was estimated to be 2.6 eV.

Extended Data Fig. 2| The Arrhenius plots for ammonia synthesis activity of the BaH2-BaO/Fe and Ru/BaH2-BaO at 0.9 MPa. The apparent activation energy of BaH2-BaO/Fe and Ru/BaH2-BaO was 40 kJ mol‒1 and 68 kJ mol‒1, respectively.

Extended Data Fig. 3| The Arrhenius plots for 14N2-15N2 isotropic exchange reaction over the BaO-BaH2/Fe. The apparent activation energy was about 86 kJ mol-1.

Extended Data Table 1| Catalytic activities of various transition metals for ammonia synthesis (300 °C)

| Catalysts | SBET (m2 g–1) | Metal particle size (nm) | Pressure (MPa) | WHSV (mL g–1 h–1) | rNH3 (mmol g–1 h–1) | Ref. |
| --- | --- | --- | --- | --- | --- | --- |
| BaH2-BaO /Fe | 7 | 21.7 | 0.9 | 36000 | 5.5 | This work |
| Promoted Fe | - | - | 0.9 | 36000 | 5.4 | 8 |
|  |  |  | 0.9 | 60000 | 9.0a |  |
|  |  |  | 0.9 | 72000 | 10.8a |  |
| Ru (10%)/BaO-BaH2 | 20 | 4.0 | 0.9 | 36000 | 11.5 | This work |
| Ru (10%)/Ba-Ca(NH2)2 | 101 | 2.7 | 0.9 | 36000 | 23.3 | 8 |
| Cs-Ru (10%)/MgO | 12 | 5.2 | 0.9 | 36000 | 0.6 | 8 |
| Ru (2%)/C12A7:e‒ | 1 | 28.7 | 0.9 | 36000 | 0.8 | 8 |
| Fe-LiH | 16 | 29.6 | 1.0 | 60000 | 4.4 | 9 |
| Co-LiH | 43 | 27.6 | 1.0 | 60000 | 4.7 | 9 |
| BaH2-Co/CHTs | 53 | 42.0 | 1.0 | 60000 | 4.8 | 10 |
| Ru/La0.5Ce0.5O1.75 | 42 | 1.7 | 1.0 | 72000 | 10.7 | 16 |
| Ru/La0.5Pr0.5O1.75 | 30 | 2.9 | 1.0 | 72000 | 8.9 | 17 |

aAmmonia formation rate estimated based on rNH3 at the WHSV at 36000 mL g–1 h–1.

Extended Data Table 2| TOF for ammonia synthesis on various transition metal catalysts

| Catalysts | Temperature (°C) | Pressure (MPa) | TOF (s–1) | Ea (kJ mol-1) | Ref. |
| --- | --- | --- | --- | --- | --- |
| BaO-BaH2/Fea | 300 | 0.9 | 12.2 | 40 | This work |
|  | 200 |  | 1.7 |  | This work |
|  | 100 |  | 0.2 |  | This work |
| Ru (10%)/BaO-BaH2a | 300 | 0.9 | 3.5x10-3 | 69 | This work |
|  | 200 |  | 3.2x10-4 |  | This work |
|  | 100 |  | - |  | This work |
| Ru (10%)/Ba-Ca(NH2)2b | 300 | 0.9 | 1.3x10-2 | 59 | 8 |
| Cs-Ru (10%)/MgOa | 300 | 0.9 | 8.0x10-4 | 124 | 8 |
| Ru/C12A7:e‒a | 300 | 0.9 | 5.6x10-2 | 49 | 8 |
| Co/C12A7:e‒b | 400 | 0.9 | 9.3x10-3 | 50 | 30 |
| Ni/LaN bulka | 400 | 0.9 | 0.17 | 60 | 11 |

aTOF calculated from the rate of ammonia synthesis divided by the number of surface Ns.

bTOF calculated from the rate of ammonia synthesis divided by the number of surface metal sites calculated, on the basis of the morphological mean particle sizes of transition metal particles. .