| B obs. [°2Th] | B std. [°2Th] | Peak pos. [°2Th] | B struct. [°2Th] | Crystallite size [Å] |
| --- | --- | --- | --- | --- |
| 0.614 | 0.008 | 32.053 | 0.606 | 136 |
| 0.154 | 0.008 | 40.999 | 0.146 | 583 |
| 0.307 | 0.008 | 53.726 | 0.299 | 298 |
| 0.409 | 0.008 | 64.173 | 0.401 | 234 |
| The average crystallite size of Hydroxyapatite(HA): 312.75 Å |  |  |  |  |

| B obs. [°2Th] | B std. [°2Th] | Peak pos. [°2Th] | B struct. [°2Th] | Crystallite size [Å] |
| --- | --- | --- | --- | --- |
| 0.984 | 0.008 | 32.242 | 0.976 | 85 |
| 0.246 | 0.008 | 38.249 | 0.238 | 353 |
| 0.197 | 0.008 | 53.854 | 0.189 | 471 |
| 0.787 | 0.008 | 62.282 | 0.779 | 119 |
| The average crystallite size of HA/MMT: 275 Å |  |  |  |  |

| B obs. [°2Th] | B std. [°2Th] | Peak pos. [°2Th] | B struct. [°2Th] | Crystallite size [Å] |
| --- | --- | --- | --- | --- |
| 0.512 | 0.008 | 32.09 | 0.504 | 164 |
| 0.256 | 0.008 | 40.369 | 0.248 | 341 |
| 0.307 | 0.008 | 53.57 | 0.299 | 298 |
| 0.512 | 0.008 | 66.35 | 0.504 | 188 |
| The average crystallite size of HA/SA: 247.75 Å |  |  |  |  |

| B obs. [°2Th] | B std. [°2Th] | Peak pos. [°2Th] | B struct. [°2Th] | Crystallite size [Å] |
| --- | --- | --- | --- | --- |
| 0.59 | 0.008 | 32.061 | 0.582 | 142 |
| 0.246 | 0.008 | 41.799 | 0.238 | 357 |
| 0.59 | 0.008 | 53.51 | 0.582 | 153 |
| 0.492 | 0.008 | 67.68 | 0.484 | 198 |
| The average crystallite size of HA/SA: 212.5 Å |  |  |  |  |

S.Table.1 The crystallite size of prepared HA and their Biopolymer composite.

| Spectrum: Element (HA) | unn. C | norm. C |  | Atom. C | Error (3 Sigma) |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | [wt.%] | [wt.%] |  | [at.%] | [wt.%] |  |
| Carbon | 4.56 | 7.38 |  | 13.62 | 2.82 |  |
| Oxygen | 23.46 | 37.95 |  | 52.59 | 10.00 |  |
| Fluorine | 0.88 | 1.43 |  | 1.66 | 0.86 |  |
| Phosphorus | 9.98 | 16.13 |  | 11.55 | 1.25 |  |
| Calcium | 22.48 | 36.35 |  | 20.11 | 2.06 |  |
| Silicon | 0.10 | 0.16 |  | 0.13 | 0.10 |  |
| Aluminium | 0.13 | 0.20 |  | 0.17 | 0.10 |  |
| Manganese | 0.25 | 0.40 |  | 0.16 | 0.12 |  |
| Spectrum: Element (HA/MMT) | unn. C | norm. C | Atom. C |  |  | Error (3 Sigma) |
|  | [wt.%] | [wt.%] | [at.%] |  |  | [wt.%] |
| Carbon | 4.66 | 8.73 | 15.20 |  |  | 2.95 |
| Oxygen | 21.08 | 39.47 | 51.60 |  |  | 8.55 |
| Magnesium | 0.25 | 0.48 | 0.41 |  |  | 0.13 |
| Aluminium | 2.61 | 4.89 | 3.79 |  |  | 0.46 |
| Silicon | 8.71 | 16.30 | 12.14 |  |  | 1.20 |
| Phosphorus | 4.72 | 8.84 | 5.97 |  |  | 0.64 |
| Potassium | 0.16 | 0.30 | 0.16 |  |  | 0.10 |
| Calcium | 9.95 | 18.63 | 9.72 |  |  | 0.96 |
| Iron | 1.07 | 2.00 | 0.75 |  |  | 0.20 |
| Spectrum: Element (HA/SA) | unn. C | norm. C | Atom. C |  |  | Error (3 Sigma) |
|  | [wt.%] | [wt.%] | [at.%] |  |  | [wt.%] |
| Carbon | 7.53 | 11.95 | 21.35 |  |  | 4.05 |
| Oxygen | 22.66 | 35.93 | 48.21 |  |  | 9.75 |
| Sodium | 0.16 | 0.25 | 0.24 |  |  | 0.12 |
| Phosphorus | 9.47 | 15.02 | 10.41 |  |  | 1.19 |
| Calcium | 22.74 | 36.06 | 19.32 |  |  | 2.08 |
| Silicon | 0.07 | 0.12 | 0.09 |  |  | 0.09 |
| Magnesium | 0.11 | 0.17 | 0.15 |  |  | 0.10 |
| Aluminium | 0.07 | 0.10 | 0.08 |  |  | 0.09 |
| Manganese | 0.26 | 0.41 | 0.16 |  |  | 0.12 |
| Spectrum: Element (HA/MMT/SA) | unn. C | norm. C | Atom. C |  |  | Error (3 Sigma) |
|  | [wt.%] | [wt.%] | [at.%] |  |  | [wt.%] |
| Carbon | 12.55 | 24.03 | 35.33 |  |  | 5.52 |
| Oxygen | 23.02 | 44.07 | 48.64 |  |  | 9.03 |
| Aluminium | 0.56 | 1.08 | 0.71 |  |  | 0.17 |
| Silicon | 2.40 | 4.60 | 2.89 |  |  | 0.39 |
| Phosphorus | 3.55 | 6.79 | 3.87 |  |  | 0.50 |
| Calcium | 9.30 | 17.81 | 7.85 |  |  | 0.90 |
| Iron | 0.44 | 0.84 | 0.26 |  |  | 0.13 |
| Chlorine | 0.08 | 0.16 | 0.08 |  |  | 0.09 |
| Sodium | 0.18 | 0.34 | 0.26 |  |  | 0.12 |
| Potassium | 0.05 | 0.09 | 0.04 |  |  | 0.09 |
| Manganese | 0.10 | 0.20 | 0.06 |  |  | 0.10 |

S.Table.2 Elemental weight percentages of HA, HA/MMT, HA/SA, HA/MMT/SA.

| S.No. | Name of the compound | Porosity (ϕ) of the prepared HA, HA/MMT, HA/SA, HA/MMT/SA in percentage |
| --- | --- | --- |
| 1 | Hydroxyapatite (HA) | 1.1 |
| 2 | Hydroxyapatite/Montmorillonite(HA/MMT) | 4.2 |
| 3 | Hydroxyapatite/Sodium alginate (HA/SA) | 3.3 |
| 4 | Hydroxyapatite/Montmorillonite/Sodium alginate (HA/MMT/SA) | 5.6 |

S.Table.3 Porosity (ϕ) of prepared HA, HA/MMT, HA/SA, HA/MMT/SA composites.

| S. No. | Drug substrate | Compounds | Drug release (%) | Hours | References |
| --- | --- | --- | --- | --- | --- |
| 1 | Curcumin | hydroxyapatite bilayer coated iron oxide nanoparticle composite (IONP/HAp-NaAlg) | 99 | 180 | 1 |
| 2 | Doxorubicin | PVA/chitosan/PU/HAp/DOX core-shell nanofiber | 72 | 72 | 2 |
| 3 | Doxorubicin | Poly(L-Lactic Acid)/Hydroxyapatite/Gelatin | 78 | 72 | 3 |
| 4 | Curcumin & Doxorubicin | Hydroxyapatite/Montmorillonite/Sodium alginate (HA/MMT/SA) composite | 70 & 81 | 32 | Present work |

S.Table. 4 Drug release efficacies of reported compounds and HA/MMT/SA composite.

Reference

1. Manatunga, D. C., de Silva, R. M., de Silva, K. M. N., de Silva, N., Bhandari, S., Yap, Y. K., & Costha, N. P. (2017). pH responsive controlled release of anti-cancer hydrophobic drugs from sodium alginate and hydroxyapatite bi-coated iron oxide nanoparticles. European Journal of Pharmaceutics and Biopharmaceutics, 117, 29–38. doi:10.1016/j.ejpb.2017.03.014

2. Qavamnia, S. S., Rad, L. R., & Irani, M. (2020). Incorporation of Hydroxyapatite/Doxorubicin into the Chitosan/Polyvinyl Alcohol/Polyurethane Nanofibers for Controlled Release of Doxurubicin and Its Anticancer Property. Fibers and Polymers, 21(8), 1634–1642. doi:10.1007/s12221-020-9809-8.

3. Zhao, Q., Wang, B., Liu, R., Gong, M., Dong, M., Fang, M., & Jiang, T. (2018). Drug Release Behavior of Doxorubicin Hydrochloride-Loaded Poly(L-Lactic Acid)/Hydroxyapatite/Gelatin by Surface Modification of Hydroxyapatite. Journal of Nanoscience and Nanotechnology, 18(10), 7225–7230. doi:10.1166/jnn.2018.15507

| Name of the compound | pH | Zero Order |  | First order |  | Higuchi Model |  | Korsmeyer –Peppas Model |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | k | R2 | k | R2 | k | R2 | k | R2 | n |
| HA | 5.5 | 0.9101 | 0.9217 | 0.0048 | 0.9464 | 5.8661 | 0.9913 | 0.9041 | 0.8963 | 0.3889 |
|  | 6.8 | 0.4781 | 0.9478 | 0.0022 | 0.9575 | 3.0327 | 0.9847 | 0.7789 | 0.9851 | 0.1089 |
|  | 7.4 | 0.3440 | 0.9196 | 0.0015 | 0.9247 | 2.1659 | 0.9399 | 0.7622 | 0.9343 | 0.2802 |
| HA/SA | 5.5 | 0.9833 | 0.9105 | 0.0053 | 0.9411 | 6.3820 | 0.9940 | 0.9348 | 0.8413 | 0.4910 |
|  | 6.8 | 0.5267 | 0.9500 | 0.0025 | 0.9604 | 3.3353 | 0.9830 | 0.7994 | 0.9777 | 0.1273 |
|  | 7.4 | 0.4110 | 0.9358 | 0.0019 | 0.9427 | 2.5805 | 0.9509 | 0.7825 | 0.9466 | 0.2371 |
| HA/MMT | 5.5 | 1.1578 | 0.9098 | 0.0065 | 0.9456 | 7.5115 | 0.9923 | 0.9482 | 0.8289 | 0.4901 |
|  | 6.8 | 0.6170 | 0.9520 | 0.0030 | 0.9648 | 3.9039 | 0.9841 | 0.8060 | 0.9731 | 0.1622 |
|  | 7.4 | 0.4673 | 0.9240 | 0.0021 | 0.9324 | 2.9462 | 0.9471 | 0.7898 | 0.9535 | 0.1866 |
| HA/MMT/SA | 5.5 | 1.5367 | 0.9266 | 0.0097 | 0.9700 | 9.8932 | 0.9939 | 0.9680 | 0.8060 | 0.6016 |
|  | 6.8 | 0.7658 | 0.9492 | 0.0038 | 0.9650 | 4.8561 | 0.9852 | 0.8278 | 0.9518 | 0.2509 |
|  | 7.4 | 0.5834 | 0.9330 | 0.0027 | 0.9435 | 3.6710 | 0.9526 | 0.8192 | 0.9671 | 0.1134 |

S.Table.5a The kinetic curcumin drug release values of prepared HA and their composites with respect to the correlation coefficient (R2) for zero order, first order, Higuchi Model and Korsmeyer Peppas Model.

| Name of the compound | pH | Zero Order |  | First order |  | Higuchi Model |  | Korsmeyer –Peppas Model |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | k | R2 | k | R2 | k | R2 | k | R2 | n |
| HA | 5.5 | 1.0144 | 0.8984 | 0.0055 | 0.9291 | 6.5952 | 0.9844 | 0.7631 | 0.8369 | 0.5155 |
|  | 6.8 | 0.5338 | 0.8591 | 0.0026 | 0.9183 | 3.5304 | 0.9773 | 0.6804 | 0.8811 | 0.3483 |
|  | 7.4 | 0.3921 | 0.9482 | 0.0018 | 0.9547 | 2.4706 | 0.9709 | 0.6414 | 0.9504 | 0.1839 |
| HA/SA | 5.5 | 1.0772 | 0.8998 | 0.0060 | 0.9348 | 7.0150 | 0.9897 | 0.7201 | 0.7663 | 0.5942 |
|  | 6.8 | 0.6115 | 0.8535 | 0.0030 | 0.9180 | 4.0514 | 0.9744 | 0.6547 | 0.8135 | 0.4601 |
|  | 7.4 | 0.4286 | 0.9378 | 0.0020 | 0.9472 | 2.7276 | 0.9811 | 0.6161 | 0.9074 | 0.2859 |
| HA/MMT | 5.5 | 1.2585 | 0.9131 | 0.0074 | 0.9530 | 8.1513 | 0.9964 | 0.7357 | 0.7491 | 0.6374 |
|  | 6.8 | 0.6778 | 0.8233 | 0.0034 | 0.9123 | 4.5425 | 0.9641 | 0.6648 | 0.7856 | 0.4988 |
|  | 7.4 | 0.4785 | 0.9148 | 0.0023 | 0.9277 | 3.0727 | 0.9757 | 0.6266 | 0.8760 | 0.3385 |
| HA/MMT/SA | 5.5 | 1.6990 | 0.9047 | 0.0110 | 0.9605 | 11.035 | 0.9880 | 0.7087 | 0.7316 | 0.7829 |
|  | 6.8 | 0.9464 | 0.8533 | 0.0050 | 0.9380 | 6.2758 | 0.9762 | 0.5757 | 0.7707 | 0.7147 |
|  | 7.4 | 0.6761 | 0.9447 | 0.0030 | 0.9582 | 4.2905 | 0.9821 | 0.3997 | 0.8638 | 0.6796 |

S.Table.5b The kinetic doxorubicin drug release values of prepared HA and their composites with respect to the correlation coefficient (R2) for zero order, first order, Higuchi Model and Korsmeyer Peppas Model.

S.Fig.1 X-ray diffraction spectra analysis of prepared (a) HA, (b) HA/MMT, (c) HA/SA, (d) HA/MMT/SA composites for Low angle ( from 0 ˚ to 10 ˚).