Supplementary information: Utilizing ferrorestorable polarization in energy storage ceramic capacitors

Hiroki Matsuo1,* Masashi Utsunomiya2 and Yuji Noguchi3,*

1 International Research Organization for Advanced Science & Technology (IROAST), Kumamoto University, 2-39-1, Kurokami, Chuo-ku, Kumamoto 860-8555, Japan

2 Monozukuri R&D Laboratory, KYOCERA Corporation, 1-4 Kokubuyamashita-cho, Kirishima-shi, Kagoshima 899-4312, Japan

3 Division of Information and Energy, Faculty of Advanced Science and Technology, Kumamoto University, 2-39-1, Kurokami, Chuo-ku, Kumamoto 860-8555, Japan

FIG. S1. a, Total energy (Etotal) of VOn••-Cu3+ in the high-spin (HS) and the low-spin (LS) states as a function of n. The LS state with a CuO5 pyramid has a low Etotal compared with the HS state having an CuO6 octahedron for n < 4. The HS state is lower in energy for n ≥ 4. Relative Etotal of b, VOn••-Cu3+, c, VOn••-Cu2+, d, VOn••-Cu+ and e, VOn••-V2+ as a function of n.

FIG. S2. Temperature dependence of inverse magnetic susceptibility (1/) for the Cu (1.5 %) samples annealed at various pO2900 C. Data were fitted with the Curie-Weiss law expressed as 1χ=T-ΘC, where T is temperature, C is Curie constant, and  is paramagnetic Curie temperature. A slope of the linear regression line of the data plots corresponds to 1/C. Effective magnetic moment (μeff) is expressed as μeff=1μB3kBC/N, where N is the number of Cu atoms per unit weight of the sample, μB is the Bohr magneton, and kB is the Boltzmann constant.

FIG. S3. Schematics for energy levels of Cu-3d orbitals in C4v symmetry. A spin quantum number (S) and spin-only magnetic moment (μeffspin) are also displayed. μeffspin is expressed as μeffspin=gS(S+1) where g is the Landé g-factor. For Cu3+ with d8 electron configuration, both the low-spin (LS) and high-spin (HS) states are possible. Our DFT calculations for VOn-Cu3+ indicate that the LS state is energetically favorable for n = 1–3 that has a CuO5 pyramid while the HS state is stable for n = 4 having a CuO6 octahedron as shown in Supplementary Fig. 1a.

FIG. S4. Polarization properties of the aged samples with Cu (1.5 %) a, c, e, g. without the poling pretreatment and b, d, f, h with the poling pretreatment (controlled). pO2900 C is a, b, 3.0  10−6 atm, c, d, 1.6  10−6 atm, e, f, 4.0  10−11 atm, and g, h, 2.0  10−20 atm. To assess the contribution of ferrorestorable polarization to recyclable energy density (Urec), the maximum electric field (Emax) was adjusted to be Emax  Ei + 30 kV/cm, where Ei denotes internal electric field.

FIG. S5. Polarization properties of the Cu (0.3 %) samples. a, As-prepared. b, After the ageing without the poling pretreatment. c, After the ageing with the poling pretreatment (controlled). pO2900 C is 0.2 atm for all the samples. In spite of the low Cu concentration, b, an antiferroelectric-like pinched hysteresis and c, a shifted hysteresis were observed.

FIG. S6. Polarization properties of the V (0.3 %) samples. a, As-prepared, b, After the ageing without the poling pretreatment. c, After the ageing with the poling pretreatment (controlled). pO2900 C is 0.2 atm for all the samples. In contrast to the results of the Cu samples, the polarization loops are influenced neither by the ageing nor the poling pretreatment.

FIG. S7. pO2900 C dependence of Urec and  of the aged samples with Cu (1.5 %) with the poling pretreatment (controlled).

FIG. S8. Schematics of domain structure of the Cu (1.5 %) samples. a, During the thermal treatment at 200 C (> Curie temperature TC). b, After the thermal treatment followed by successive cooling to room temperature. Black and Red arrows indicate defect dipole vector (def) and spontaneous polarization vector (Ps), respectively. Because of the attractive interaction between Cu and VO••, VO•• migrates to the O site adjacent to Cu in the paraelectric cubic lattice during the thermal treatment at T = 200 C. In the cooling process, a phase transition from the paraelectric cubic phase to the ferroelectric tetragonal phase occurs accompanied by a formation of a multidomain (MD) structure with zero net polarization.

FIG. S9. Polarization property and corresponding domain configurations of the aged Cu (1.5 %) sample without the poling treatment at pO2900 C = 3.0  10−6 atm. a. Unipolar polarization and energy storage properties. b, Domain configuration in State 1’ at E of zero and c, that in State 2’ at E of Emax. In a MD structure formed after the thermal treatment at 200 C (Supplementary Fig. 8b), VO•• is stabilized on the O1 site in each ferroelectric domain. During the successive ageing at 80 C, def, 1 parallel to Ps in each ferroelectric domain is dominant because VO•• migrates to the O1 site, which corresponds to State 1’. An application of E = Emax induces a quasi-SD state with P = Pmax which corresponds to State 2’. Though typical ferroelectric materials can retain the domain structure with the non-zero Pr [as in the unipolar P-E loop of the as-prepared sample at pO2900 C = 3×10−6 atm (Fig. 5c)], the characteristic def configuration established by the ageing enables a complete back switching from State 2’ to State 1’ with a small hysteresis.

Table S1. Performance of energy storage capacitors in polycrystalline film and bulk forms displayed in Fig. 6 of the main text.

| Type | Material/composition | Form | Urec (J cm−3) | η (%) | Emax (MV cm−1) | r,eff (-) | Ref |
| --- | --- | --- | --- | --- | --- | --- | --- |
| PE | Ba0.7Sr0.3FexTi1-xO3 | Film | 7.6 | 65 | 0.4 | 1073 | 1 |
| FE | Pb0.8La0.1Ca0.1Ti0.975iO3 | Film | 14.9 | 77.6 | 0.4 | 2104 | 2 |
| FE | 0.9(0.94Na0.5Bi0.5TiO3–0.06BaTiO3)–0.1NaNbO3 | Film | 32 | 90 | 3.17 | 72 | 3 |
| FE | Mn-doped 0.97(0.93Na0.5Bi0.5TiO3-0.07BaTiO3)-0.03BiFeO3 | Film | 81.9 | 64.4 | 2.285 | 354 | 4 |
| AF | Pb0.835La0.11Zr0.85Ti0.15O3 gradient | Film | 44 | 71 | 1.95 | 261 | 5 |
| AF | Pb0.79Ba0.11La0.1(Zr0.9Ti0.1)O3 | Film | 42.3 | 68 | 2.3 | 181 | 6 |
| AF | Pb0.97Y0.02(Zr0.6Sn0.4)0.925 Ti0.075O3 | Film | 21 | 91.9 | 1.3 | 281 | 7 |
| RF | 0.65Na0.5Bi0.5TiO3-0.35Sr0.7Bi0.2TiO3 | Film | 21.5 | 80 | 1 | 486 | 8 |
| RF | Ba(Zr0.2Ti0.8)O3 (Thickness t = 350 nm) | Film | 166 | 77 | 5.7 | 115 | 9 |
| AFE | AgNb0.8Ta0.2O3 | Ceramic | 4 | 77 | 0.24 | 1569 | 10 |
| AFE | (Pb0.858Ba0.1La0.02Y0.008)(Zr0.65Sn0.3Ti0.05)O3- (Pb0.97La0.02)(Zr0.9Sn0.05Ti0.05)O3 | Ceramic | 4.65 | 60 | 0.191 | 2879 | 11 |
| AFE | (Pb0.92Ba0.05La0.02)(Zr0.68Sn0.27Ti0.05)O3 | Ceramic | 2.3 | 76.8 | 0.098 | 5410 | 12 |
| RF | 0.89(Bi0.5Na0.5)TiO3- 0.06BaTiO3-0.05NaNbO3 | Ceramic | 0.71 | 66 | 0.07 | 3273 | 13 |
| RF | 0.85BaTiO3-0.15Bi(Zn0.67Nb0.33)O3 | Ceramic | 0.79 | 93.5 | 0.131 | 1040 | 14 |
| RF | Na0.84Bi0.08Nb0.92Zr0.08O3 | Ceramic | 4.9 | 88 | 0.43 | 599 | 15 |
| RF | BaTiO3-Sr0.7Bi0.2TiO3-Li2CO3 | Ceramic | 3.54 | 80 | 0.41 | 476 | 16 |
| RF | 0.55Bi0.5Na0.5TiO3-0.45Sr0.7La0.2TiO3 | Ceramic | 4.14 | 92.2 | 0.315 | 942 | 17 |
| RF | 0.75Bi0.4465Na0.4465Ba0.057La0.05TiO3-0.25Sr0.85Bi0.1TiO3 | Ceramic | 4.55 | 90 | 0.32 | 1004 | 18 |
| AFE | 0.92Na0.5Bi0.49Nd0.01TiO3-0.08BaTiO3 | Ceramic | 1.27 | 83.8 | 0.0726 | 5443 | 19 |
| AFE | 1%Mn, 1.25%Nb-doped BaTiO3 | Ceramic | 0.43 | 86 | 0.105 | 881 | 20 |
| FE | Cu (1.5%)-BaTiO3 (Aged without poling pretreatment pO2900 C = 3.0 ´ 10−6 atm) | Ceramic | 1.11 | 90 | 0.075 | 4450 | This study |
| FE | Cu (1.5 %)-BaTiO3 (Controlled, pO2900 C = 3.0 ´ 10−6 atm) | Ceramic | 1.77 | 89 | 0.076 | 7014 | This study |
| FE | Cu (1.5 %)-BaTiO3 (Controlled, pO2900 C = 1.6 ´ 10−7 atm) | Ceramic | 1.12 | 84 | 0.057 | 7734 | This study |
| FE | Cu (0.3 %)-BaTiO3 (Controlled, pO2900 C = 0.2 atm) | Ceramic | 0.28 | 68 | 0.028 | 3481 | This study |

PE: Paraelectric, FE: Ferroelectric, AFE: Antiferroelectric, RE: Relaxor

REFERENCES

1.	Xie, J. et al. Energy storage properties of low concentration Fe-doped barium strontium titanate thin films. Ceram. Int. 44, 5867–5873 (2018).

2.	Zhu, H., Ma, H. & Zhao, Y. Enhanced energy storage and pyroelectric properties of highly (100)-oriented (Pb1−x−yLaxCay)Ti1−x/4O3 thin films derived at low temperature. Phys. Lett. Sect. A Gen. At. Solid State Phys. 382, 1409–1412 (2018).

3.	Yao, Y. et al. High energy-storage performance of BNT-BT-NN ferroelectric thin films prepared by RF magnetron sputtering. J. Alloys Compd. 750, 228–234 (2018).

4.	Yang, C. et al. Fatigue-Free and Bending-Endurable Flexible Mn-Doped Na0.5Bi0.5TiO3-BaTiO3-BiFeO3 Film Capacitor with an Ultrahigh Energy Storage Performance. Adv. Energy Mater. 9, 1–10 (2019).

5.	Zhao, Y., Hao, X. & Zhang, Q. Enhanced energy-storage performance and electrocaloric effect in compositionally graded Pb(1−3x/2)LaxZr0.85Ti0.15O3 antiferroelectric thick films. Ceram. Int. 42, 1679–1687 (2016).

6.	Gao, H. et al. Enhanced electrocaloric effect and energy-storage performance in PBLZT films with various Ba2+ content. Ceram. Int. 42, 16439–16447 (2016).

7.	Ahn, C. W. et al. Antiferroelectric Thin-Film Capacitors with High Energy-Storage Densities, Low Energy Losses, and Fast Discharge Times. ACS Appl. Mater. Interfaces 7, 26381–26386 (2015).

8.	Li, J. et al. Grain-orientation-engineered multilayer ceramic capacitors for energy storage applications. Nat. Mater. 19, 999–1005 (2020).

9.	Cheng, H. et al. Demonstration of ultra-high recyclable energy densities in domain-engineered ferroelectric films. Nat. Commun. 8, 1999 (2017).

10.	Zhao, L., Liu, Q., Gao, J., Zhang, S. & Li, J. Lead‐Free Antiferroelectric Silver Niobate Tantalate with High Energy Storage Performance. Adv. Mater. 29, 1701824 (2017).

11.	Zhang, L., Jiang, S., Fan, B. & Zhang, G. High energy storage performance in (Pb0.858Ba0.1La0.02Y0.008)(Zr0.65Sn0.3Ti0.05)O3-(Pb0.97La0.02)(Zr0.9Sn0.05Ti0.05)O3 anti-ferroelectric composite ceramics. Ceram. Int. 41, 1139–1144 (2015).

12.	Chen, L., Hao, X., Zhang, Q. & An, S. Energy-storage performance of PbO–B2O3–SiO2 added (Pb0.92Ba0.05La0.02)(Zr0.68Sn0.27Ti0.05)O3 antiferroelectric ceramics prepared by microwave sintering method. J. Mater. Sci. Mater. Electron. 27, 4534–4540 (2016).

13.	Xu, Q. et al. Enhanced energy storage properties of NaNbO3 modified Bi0.5Na0.5TiO3 based ceramics. J. Eur. Ceram. Soc. 35, 545–553 (2015).

14.	Wu, L., Wang, X. & Li, L. Lead-free BaTiO3–Bi(Zn2/3Nb1/3)O3 weakly coupled relaxor ferroelectric materials for energy storage. RSC Adv. 6, 14273–14282 (2016).

15.	Yang, L., Kong, X., Cheng, Z. & Zhang, S. Enhanced Energy Storage Performance of Sodium Niobate-Based Relaxor Dielectrics by a Ramp-to-Spike Sintering Profile. ACS Appl. Mater. Interfaces 12, 32834–32841 (2020).

16.	Liu, G. et al. Ultrahigh dielectric breakdown strength and excellent energy storage performance in lead-free barium titanate-based relaxor ferroelectric ceramics via a combined strategy of composition modification, viscous polymer processing, and liquid-phase sintering. Chem. Eng. J. 398, 125625 (2020).

17.	Qiao, X. et al. Superior comprehensive energy storage properties in Bi0.5Na0.5TiO3-based relaxor ferroelectric ceramics. Chem. Eng. J. 388, 124158 (2020).

18.	Ye, H. et al. Significantly Improvement of Comprehensive Energy Storage Performances with Lead-free Relaxor Ferroelectric Ceramics for High-temperature Capacitors Applications. Acta Mater. 203, 116484 (2021).

19.	Kandula, K. R., Banerjee, K., Raavi, S. S. K. & Asthana, S. Enhanced Electrocaloric Effect and Energy Storage Density of Nd-Substituted 0.92NBT-0.08BT Lead Free Ceramic. Phys. Status Solidi Appl. Mater. Sci. 215, 1–5 (2018).

20.	Liu, W., Gao, J., Zhao, Y. & Li, S. Significant enhancement of energy storage properties of BaTiO3-based ceramics by hybrid-doping. J. Alloys Compd. 843, (2020).