Supplementary Materials for

Imaging current distribution in a topological insulator Bi2Se3 in the presence of competing surface and bulk contributions to conductivity

Amit Jash1, Ankit Kumar1, Sayantan Ghosh1, A. Bharathi2, S. S. Banerjee1*

1Department of Physics, Indian Institute of Technology, Kanpur 208016, Uttar Pradesh, India

2UGC-DAE Consortium for Scientific Research, Kalpakkam-603104, India

corresponding author email: satyajit@iitk.ac.in.

Section I: Bi2Se3 thin film:

The Bi2Se3 thin film has been grown on SrTiO3(111) substrate by the RF magnetron sputtering. A commercially available stoichiometric Bi2Se3 target from ALB Materials Inc of high purity of 99.999% was used as the sputtering target. The distance between the substrate and the sputtering gun was 6.4 cm. The base pressure of the sputtering chamber was kept at 5 ×10-6 mBar, and 8 ×10-3 mBar argon gas (99.99% purity) pressure was maintained during deposition. The SrTiO3 substrate temperature was kept at 390 oC before and during the deposition. Before deposition, the substrates were carefully cleaned with acetone, alcohol, de-ionized water and purged with nitrogen gas. The RF power was fixed at 30 watt and average growth rate of Bi2Se3 thin film was 1 nm/min, with film thickness between 5 nm to 40 nm. After deposition, the film was post-annealed in the sputtering chamber in argon environment at temperature 350 oC for four hours. Figure below shows the XRD (X-ray diffraction) pattern only displaying (0 0 3n) direction Bragg peaks of the Bi2Se3 thin film due to the three-fold symmetry of the Bi2Se3 crystal structure, the same as reported in past. The XRD direction was carried out in gazing angle mode which avoids the Bragg peak from the SrTiO3 substrate. The direction peaks of (0 0 3n) indicates the rhombohedral structure and the thin film growth along the (111) direction. The sharp XRD peaks indicate the high quality, epitaxial nature of our films.

Fig. S1. XRD characterization. Figure shows the XRD peaks of Bi2Se3 thin film, grown on STO (111) substrate.

Section II: Observation of SdH oscillation in the Bi2Se3 single crystal and location of the Fermi level within the bulk gap of the material:

Figure (a) shows distinct SdH oscillation in longitudinal magneto-resistance (ΔRxx vs magnetic field (B)) measurements at 10 K using standard Van der Pauw geometry. This data is reproduced from A. Jash, et al., Phys. Rev. Appl. 12, 014056 (2019) (Ref. 26 in main MS). ΔRxx is calculated by subtracting from the experimental Rxx(B) values with a polynomial fit to the data (Rpoly (B)), i.e, ΔRxx = Rxx(B) - Rpoly (B). The polynomial form of R is , where R0 = 9.26×10-3 Ω, R1  = -1.71×10-6 Ω.T-1, R2=2.91×10-5 Ω.T-2. Upper inset shows the variation of Rxx as a function of magnetic field B measured at 10 K. Lower inset shows the SdH oscillation at different low temperature. We use Lifshitz-Kosevich (LK) equation: to analyse the SdH oscillation seen in our Bi2Se3 sample, where F and β are the fitting parameter. From the oscillation period (F) of the SdH oscillations seen in the transport data, the measured surface carrier density per area is found to be ns=(2.268±0.012) × 10 12 cm-2, which corresponds to a Fermi wavevector for the 2D surface state to be kF=2πns = (0.0377±0.0027) Å-1. By placing the location of kF on the ARPES spectrum of Bi2Se3 (see kF marked by a vertical yellow line in the Fig. (b) which is Fig. 1 ARPES data of Bi2Se3 as published by M. Bianchi et al., Nature Commun. 1, 128 (2010)), we see that the Fermi energy is approximately 30 meV above the Dirac point and about 100 meV below the bottom of the bulk conduction band (shown by green dash line). The position of the Fermi level suggests the carriers are from surface states and not from bulk bands. The charge carriers from bulk conduction do not contribute which suggests we do not have a non-topological two-dimension gas contributing to conductivity.

Fig. S2. SdH oscillation. (a) shows the SdH oscillation at 10 K. Upper inset shows the longitudinal resistance as function of magnetic field. Lower inset shows SdH oscillation at different temperature. (b) ARPES data of Bi2Se3, showing the position of the Fermi level.

The 2D carrier density corresponding to this Fermi wave vector (kF) is (2.268 ±0.012) ×1012 cm-2. Suppose, the origin of the SdH oscillation is assumed to be due to bulk electrons, the bulk carrier density should be cm-3 (per spin), where c=28.64 Å is the lattice spacing along c axis. However the bulk carrier density in the TI material as calculated from the hall coefficient, is  cm-3. This comparison shows that the features of our transport data at low T cannot be reconciled with bulk conduction electrons contributing to conductivity rather they are arising from 2D surface electrons.

Furthermore, from the LK fitting, one also obtains a value of the Berry phase as 0.86π at 4.2 K. For the two-dimensional Dirac fermion in the massless limit, the Berry phase is π which leads to a suppression of the back scattering from disorder due to destructive interference. In general, the Berry phase value being close to π is taken to suggests that SdH oscillation arises from the Dirac electron. From LK fitting of our data, shows the phase factor (Berry phase) is closer to π below 10 K (Fig.  4(d)) suggesting the SDH oscillation arises from Dirac surface state. The Berry phase values decreases from π with increasing temperature until above 30 K where bulk contribution to conductivity begins to dominate, the SdH oscillations are lost. This also suggests that at low T the SdH oscillations are related to 2D surface electrons contributing to electrical conductivity. Hence, the sheet current distributions at low temperature arises due to the topological surface current of Bi2Se3 single crystal (Fig. 5A in MS).

Section III: Self-field due to different amplitude of current:

Figure below shows the magnetic field profiles at 18 K for different applied current through the Bi2Se3 sample. Line scan is taken along the solid line to each image at different current.  The  at 35 mA is 2.05 Oe (at the edge) which decreases to 0.60 Oe when 15 mA current is applied through the sample. The self-magnetic field strength increases linearly with the applied current which justifies the linearity response of driving current to the captured distributions.

Fig. S3. Linear behaviour of self-field with applied current. Figure shows the profiles of at 18 K for different applied current. Inset figure shows the self-field image at 18 K.

Section IV: Behaviour of fb (T):

Figure below shows the bulk fraction () as function of temperature. The  value is calculated from  or from the   profile  fitting using  the equation  at different temperature. Figure shows the bulk fraction increases with temperature and above 200 K, saturates. The black dash line is the fitted line with the form, , where Δ ~ 18 ± 2.2 meV. So, this growth of the bulk fraction from 70 K arises due to the thermally activated type conduction. Similar type of behaviour is also observed in non-contact measurement, which is shown in Fig. S5. Due to activation of charges from Se vacancies, the bulk conduction dominates after 70 K. The electrical conductivity of the pure high conducting surface states decreases with increasing T, as , where A and B coefficients related to electron-electron and electron-phonon interactions. Hence, the observed activated temperature dependence of  occurs due to the thermal activation of doped charges in the bulk and its temperature dependence above 70 K is different from the behaviour of .

Fig. S4. The bulk fraction with temperature. Shows the bulk fraction as function of temperature.

Section V: Thermally activated behaviour at 70 K.

Fig. S5. Thermally activated conduction from 70 K. Shows the real part of mutual inductance (M') as function of temperature of Bi2Se3 single crystal. Surface and bulk conduction dominated regions are observed at temperature window.

The data presented above is measurement of inphase component of the mutual inductance M' of a pickup coil setup. Briefly in the setup, between a primary excitation coil and a secondary pickup coil a Bi2Se3 single crystal is placed (for details see A. Jash, et al., Phys. Rev. Appl. 12, 014056 (2019) (Ref. 27 in main MS)). An AC current in the primary coil generates a magnetic field which induces a pickup voltage in the secondary coil. The two coils are coupled via the TI sample placed in between the two coils.  As the flux linkage between the two coils is through the TI sample, hence the mutual inductance depends on the properties of the TI crystal. The inphase component of the pickup voltage V'=M'ωIprimary where  is the angular frequency of the current in the primary coil, Iprimary. One can show that V'(and hence also M')∝σ, where  is the conductivity of the TI sample (see above reference). From V' one can get a measure of M'.

We have identified the thermally activated type of conduction in the bulk of Bi2Se3 from 70 K onwards using our two-coil setup. Figure S6 shows the M'(T) behaviour at 55 kHz of Bi2Se3 single crystal (sample thickness 69 µm). Below 70 K the M'(T) data fits (solid blue line) to a form   , which corresponds to the T dependence of σ. , is the typical temperature dependence of the topological conducting surface states in a TI (Ref.26 and reference there in). While above 70 K to 170 K the data is fitted (dashed line) which corresponds to bulk contribution to σ of the form , Δ ~ 25.2 ± 1.25 meV, where Δ is an activation energy scale and is the high temperature conductance of the bulk state. Electron doping by Se vacancies generates a disorder band in the Bi2Se3 crystal. This disorder band lies Δ below the bulk conduction band minima in the bulk gap (~ 0.3 eV) of Bi2Se3. As shown in the main MS, concomitant with the onset of conduction in the bulk beyond 70 K, patches of high and low current density region proliferate the uniform conducting, topological uniform current carrying sheet on the surface of Bi2Se3 single crystal starts (see fig. 5 in main MS).

Section VI: Spatial resolution and background signal

At low T, a nearly uniform current density (Deep Blue, 770 A/cm2 - 900 A/cm2) is distributed all across the crystal surface (Fig 5(a) in the MS). As the temperature rises, above 70 K a significant concentration of Se vacancy doped conventional electron fluid appears in the material bulk and we see the inhomogeneity in J distribution with patches of high J (770 A/cm2 - 900 A/cm2) region embedded in low bulk current density ( 450 A/cm2). The minimum spatial resolution of our MOI setup is 0.8 micron. We can’t refer this as noise as the typical area of the blue region is much larger than the 1 micron size. Figures S6(a) and S6(b) show the grey and coloured scale image of current distribution of the sample with background at 15 K and 210 K. The graininess we see at 210 K is not related to any noise in the imaging. Infact if it was noise then we must see the same level of graininess outside the sample as well. We demonstrate this below.

Figures S6(a) and S6(b) below show at 15 K and 210 K, in both grey and coloured scale images of current distribution inside the sample along with a significant region outside the sample boundary. These regions have similar contrast for 15 K and 210 K while inside the sample the current distribution evidently becomes grainy with increasing T. At 210 K the graininess in the current distribution inside the sample is clearly very different from the smooth contrast outside the sample. Hence the graininess we observe inside the sample at 210 K is not a result of noise. Furthermore, the coloured images below show that, by using the same colour scale to colour the J, we see at 210 K the graininess in the images obtained outside the sample is completely different from that inside the sample.  If the speckle feature was due to a noise, then the speckle feature should be seen outside the sample at both 15 K and also more importantly at 210 K. However, we do not observe this. Therefore, the high temperature feature we see in the current distribution is not due to noise. Outside the sample we never observe the generation of any blue coloured speckle feature.

Fig. S6. Background signal at low and high temperature. The coloured and grey scale image of sample with background at (a) 15 K and (b) 210 K.