Supplementary Material

Core-shell Au@Ag Nanoparticles Synthetized with Polyphenols as

Antimicrobial Agents

Mauro Villalobos-Noriegaa, Ericka Rodríguez-Leóna, César Rodríguez-Beasa, Eduardo Larios-Rodríguezc, Maribel Plascencia-Jatomeab, Aarón Martínez-Higueraa, Heriberto Acuña-Campa and Ramón A. Iñiguez-Palomaresa*

aPhysics Department, University of Sonora, Rosales and Transversal 83000, Hermosillo, Sonora, México.

bDepartment of Research and Postgraduate in Food, University of Sonora, Rosales and Transversal 83000, Hermosillo, Sonora, México.

cDepartment of Chemical Engineering and Metallurgy, University of Sonora, Rosales and Transversal 83000, Hermosillo, Sonora, México.

dDepartment of Polymers and Materials Research, University of Sonora, Rosales and Transversal 83000, Hermosillo, Sonora, México.

*Corresponding author: ramonalfonso.iniguez@gmail.com

Figure S1  corresponds to Rumex hymenosepalus aqueous solution absorption spectrum.

Figure S2 STEM images gallery of individual Au@AgNPs. The first column corresponds to Bright Field images and the middle column to HAADF. The last column is shown manipulated images using ImageJ to enhance contrast. We can observe the uniformity of Ag-shell.

Figure S3. AuNPs HRTEM (A), region 1 FFT plot (B), and integrated image from FFT (C).  Region 2 FFT plot is shown in (D) and integrated image from FFT with interplanar distances in (E).

Figure S4. AgNPs HRTEM (A), FFT plot (B) and, integrated image from FFT with interplanar distances (C).

Figure S5. C. albicans dose-response curve comparative between Ag and Au@AgNPs.

Bacterial growth analysis using a modified Gompertz model and origin 2018 software. The parameters obtained of adjust are a, xc y k, which are related to the following equations:

μ=kae

Growth Rate µ

λ=k*xc-1a

and Time LagPhase λ.

S.aureus + AuNPs

S.aureus without AuNPs

Table S1. Adjust parameters of the curve by modified Gompertz Model (Origin 2018 software)

| Parameter | Mean Value | Standard Deviation |
| --- | --- | --- |
| a | 1.15528 | 0.00734 |
| Xc | 289.0 | 0.50 |
| k | 0.0090 | 1.3E-4 |
| R^2 ADJUST | 0.9801 |  |

Table S2. Physical Parameters of Bacterial Growth obtained with Adjust Parameters

| Parameter | Mean Value | Standard Deviation |
| --- | --- | --- |
| Growth Rate µ (D.O./minutes) | 0.00383 | 7.95526E-5 |
| Time LagPhase λ (minutes) | 177.8888 | 5.4467 |

Table S3. S.aureus + 1µg/mL  AuNPs

Adjust parameters of the curve by modified Gompertz Model (Origin 2018 software)

| PARAMETER | MEAN VALUE | STANDARD DEVIATION |
| --- | --- | --- |
| a | 0.98751 | 0.00431 |
| Xc | 291.599 | 3.17369 |
| k | 0.0075 | 2.05E-4 |
| R^2 ADJUST | 0.99153 |  |

Table S4. PHYSICAL PARAMETERS OF BACTERIAL GROWTH OBTAINED WITH ADJUST PARAMETERS

| PARAMETER | Mean Value | Standard Deviation |
| --- | --- | --- |
| Growth Rate µ (D.O./minutos) | 0.00272 | 8.44162E-5 |
| Time LagPhase λ (minutes) | 158.2366 | 10.16166 |

S.aureus + 10µg/mL  AuNPs

Table S5. Adjust parameters of the curve by modified Gompertz Model (Origin 2018 software)

| PARAMETER | MEAN VALUE | STANDARD DEVIATION |
| --- | --- | --- |
| a | 0.91793 | 0.00471 |
| Xc | 315.5396 | 2.72545 |
| k | 0.0068 | 1.01252E-4 |
| R^2 ADJUST | 0..98746 |  |

Table S6. PHYSICAL PARAMETERS OF BACTERIAL GROWTH OBTAINED WITH ADJUST PARAMETERS

| PARAMETER | Mean Value | Standard Deviation |
| --- | --- | --- |
| Growth Rate µ (D.O./minutos) | 0.0023 | 4.5974E-5 |
| Time LagPhase λ (minutes) | 168.48078 | 6.4726 |

S.aureus + 50µg/mL  AuNPs

Table S7. Adjust parameters of the curve by modified Gompertz Model (Origin 2018 software)

| PARAMETER | MEAN VALUE | STANDARD DEVIATION |
| --- | --- | --- |
| a | 0.51 | 0.012 |
| Xc | 787.111 | 11.825 |
| k | 0.00615 | 3.989E-4 |
| R^2 ADJUST | 0..8844 |  |

Table S8. PHYSICAL PARAMETERS OF BACTERIAL GROWTH OBTAINED WITH ADJUST PARAMETERS

| PARAMETER | Mean Value | Standard Deviation |
| --- | --- | --- |
| Growth Rate µ (D.O./minutos) | 0.00115 | 1.01991E-4 |
| Time LagPhase λ (minutes) | 624.50937 | 90.39578 |

S.aureus + AgNPs

Table S9. S.aureus without AgNPs

Adjust parameters of the curve by modified Gompertz Model (Origin 2018 software)

| PARAMETER | MEAN VALUE | STANDARD DEVIATION |
| --- | --- | --- |
| a | 1.1122 | 0.00304 |
| Xc | 274.6266 | 1.69846 |
| k | 0.00904 | 1.77493E-4 |
| R^2 ADJUST | 0.9971 |  |

Table S10. PHYSICAL PARAMETERS OF BACTERIAL GROWTH OBTAINED WITH ADJUST PARAMETERS

| PARAMETER | Mean Value | Standard Deviation |
| --- | --- | --- |
| Growth Rate µ (D.O./minutos) | 0.0037 | 8.27335E-5 |
| Time LagPhase λ (minutes) | 164.00716 | 7.45461 |

S.aureus 1µg/mL  AgNPs

Table S11. Adjust parameters of the curve by modified Gompertz Model (Origin 2018 software)

| PARAMETER | MEAN VALUE | STANDARD DEVIATION |
| --- | --- | --- |
| a | 0.90218 | 0.00282 |
| Xc | 269.47342 | 0.88062 |
| k | 0.01016 | 1.0549E-4 |
| R^2 ADJUST | 0.99931 |  |

Table S12. PHYSICAL PARAMETERS OF BACTERIAL GROWTH OBTAINED WITH ADJUST PARAMETERS

| PARAMETER | Mean Value | Standard Deviation |
| --- | --- | --- |
| Growth Rate µ (D.O./minutes) | 0.00337 | 4.55516E-5 |
| Time LagPhase λ (minutes) | 171.04822 | 4.11092 |

S.aureus 10µg/mL  AgNPs

Table S13. Adjust parameters of the curve by modified Gompertz Model (Origin 2018 software)

| PARAMETER | MEAN VALUE | STANDARD DEVIATION |
| --- | --- | --- |
| a | 0.79089 | 0.01121 |
| Xc | 224.28364 | 2.04417 |
| k | 0.01616 | 6.61164E-4 |
| R^2 ADJUST | 0.98434 |  |

Table S14. PHYSICAL PARAMETERS OF BACTERIAL GROWTH OBTAINED WITH ADJUST PARAMETERS

| PARAMETER | Mean Value | Standard Deviation |
| --- | --- | --- |
| Growth Rate µ (D.O./minutes) | 0.0047 | 2.5901E-4 |
| Time LagPhase λ (minutes) | 162.40245 | 14.76911 |

S.aureus 50µg/mL  AgNPs

Table S15. Adjust parameters of the curve by modified Gompertz Model (Origin 2018 software)

| PARAMETER | MEAN VALUE | STANDARD DEVIATION |
| --- | --- | --- |
| a | 0.74 | 0.001 |
| Xc | 967.54471 | 6.30715 |
| k | 0.00587 | 3.49063E-4 |
| R^2 ADJUST | 0.973 |  |

Table S16. PHYSICAL PARAMETERS OF BACTERIAL GROWTH OBTAINED WITH ADJUST PARAMETERS

| PARAMETER | Mean Value | Standard Deviation |
| --- | --- | --- |
| Growth Rate µ (D.O./minutes) | 0.0016 | 9.71851E-5 |
| Time LagPhase λ (minutes) | 797.18696 | 100.00702 |

S.aureus + Au@AgNPs

S.aureus without Au@AgNPs

Table S17. Adjust parameters of the curve by modified Gompertz Model (Origin 2018 software)

| PARAMETER | MEAN VALUE | STANDARD DEVIATION |
| --- | --- | --- |
| a | 1.1122 | 0.00304 |
| Xc | 274.6266 | 1.69846 |
| k | 0.00904 | 1.77493E-4 |
| R^2 ADJUST | 0.9971 |  |

Table S18. PHYSICAL PARAMETERS OF BACTERIAL GROWTH OBTAINED WITH ADJUST PARAMETERS

| PARAMETER | Mean Value | Standard Deviation |
| --- | --- | --- |
| Growth Rate µ (D.O./minutes) | 0.0037 | 8.27335E-5 |
| Time LagPhase λ (minutes) | 164.00716 | 7.45461 |

S.aureus 1µg/mL  Au@AgNPs

Table S19. Adjust parameters of the curve by modified Gompertz Model (Origin 2018 software)

| PARAMETER | MEAN VALUE | STANDARD DEVIATION |
| --- | --- | --- |
| a | 0.90551 | 9.2098E-4 |
| Xc | 268.4542 | 1.16359 |
| k | 0.00926 | 1.20901E-4 |
| R^2 ADJUST | 0.99959 |  |

Table S20. PHYSICAL PARAMETERS OF BACTERIAL GROWTH OBTAINED WITH ADJUST PARAMETERS

| PARAMETER | Mean Value | Standard Deviation |
| --- | --- | --- |
| Growth Rate µ (D.O./minutes) | 0.00308 | 4.34117E-5 |
| Time LagPhase λ (minutes) | 160.46284 | 4.8856 |

S.aureus 10µg/mL  Au@AgNPs

Table S21. Adjust parameters of the curve by modified Gompertz Model (Origin 2018 software)

| PARAMETER | MEAN VALUE | STANDARD DEVIATION |
| --- | --- | --- |
| a | 0.76728 | 0.00446 |
| Xc | 283.117 | 2.55475 |
| k | 0.00968 | 1.9955E-4 |
| R^2 ADJUST | 0.99754 |  |

Table S22. PHYSICAL PARAMETERS OF BACTERIAL GROWTH OBTAINED WITH ADJUST PARAMETERS

| PARAMETER | Mean Value | Standard Deviation |
| --- | --- | --- |
| Growth Rate µ (D.O./minutes) | 0.00273 | 7.22087E-5 |
| Time LagPhase λ (minutes) | 179.81121 | 9.03605 |

S.aureus 50µg/mL  Au@AgNPs

Table S23. Adjust parameters of the curve by modified Gompertz Model (Origin 2018 software)

| PARAMETER | MEAN VALUE | STANDARD DEVIATION |
| --- | --- | --- |
| a | 0.73517 | 0.01493 |
| Xc | 802.288 | 14.5 |
| k | 0.00797 | 0.00104 |
| R^2 ADJUST | 0.99428 |  |

Table S24. PHYSICAL PARAMETERS OF BACTERIAL GROWTH OBTAINED WITH ADJUST PARAMETERS

| PARAMETER | Mean Value | Standard Deviation |
| --- | --- | --- |
| Growth Rate µ (D.O./minutes) | 0.00216 | 3.25047E-4 |
| Time LagPhase λ (minutes) | 676.81749 | 188.86726 |

E.coli + AuNPs

E.coli without AuNPs

Table S25. Adjust parameters of the curve by modified Gompertz Model (Origin 2018 software)

| PARAMETER | MEAN VALUE | STANDARD DEVIATION |
| --- | --- | --- |
| a | 0.83539 | .00546 |
| Xc | 284.94644 | 4.2278 |
| k | 0.00651 | 2.43998E-4 |
| R^2 ADJUST | 0.98643 |  |

Table S26. PHYSICAL PARAMETERS OF BACTERIAL GROWTH OBTAINED WITH ADJUST PARAMETERS

| PARAMETER | Mean Value | Standard Deviation |
| --- | --- | --- |
| Growth Rate µ (D.O./minutes) | 0.002 | 8.80623E-5 |
| Time LagPhase λ (minutes) | 131.33661 | 11.79379 |

E.coli + 1µg/mL  AuNPs

Table S27. Adjust parameters of the curve by modified Gompertz Model (Origin 2018 software)

| PARAMETER | MEAN VALUE | STANDARD DEVIATION |
| --- | --- | --- |
| a | .75065 | .00531 |
| Xc | 275.93547 | 4.77869 |
| k | 0.00666 | 2.79881E-4 |
| R^2 ADJUST | 0.98267 |  |

Table S28. PHYSICAL PARAMETERS OF BACTERIAL GROWTH OBTAINED WITH ADJUST PARAMETERS

| PARAMETER | Mean Value | Standard Deviation |
| --- | --- | --- |
| Growth Rate µ (D.O./minutes) | 0.00184 | 9.02987E-5 |
| Time LagPhase λ (minutes) | 125.78532 | 12.75042 |

E.coli + 10µg/mL  AuNPs

Table S29. Adjust parameters of the curve by modified Gompertz Model (Origin 2018 software)

| PARAMETER | MEAN VALUE | STANDARD DEVIATION |
| --- | --- | --- |
| a | 0.76901 | 0.00527 |
| Xc | 267.52651 | 4.67208 |
| k | 0.00658 | 2.67281E-4 |
| R^2 ADJUST | 0.98318 |  |

Table S30. PHYSICAL PARAMETERS OF BACTERIAL GROWTH OBTAINED WITH ADJUST PARAMETERS

| PARAMETER | Mean Value | Standard Deviation |
| --- | --- | --- |
| Growth Rate µ (D.O./minutes) | 0.00186 | 8.83714E-5 |
| Time LagPhase λ (minutes) | 115.55083 | 11.40538 |

E.coli + 50µg/mL  AuNPs

Table S31. Adjust parameters of the curve by modified Gompertz Model (Origin 2018 software)

| PARAMETER | MEAN VALUE | STANDARD DEVIATION |
| --- | --- | --- |
| a | 0.76171 | 0.00367 |
| Xc | 304.8801 | 3.18269 |
| k | 0.00644 | 1.77262E-4 |
| R^2 ADJUST | 0.99301 |  |

Table S32. PHYSICAL PARAMETERS OF BACTERIAL GROWTH OBTAINED WITH ADJUST PARAMETERS

| PARAMETER | Mean Value | Standard Deviation |
| --- | --- | --- |
| Growth Rate µ (D.O./minutes) | 0.0018 | 5.83667E-5 |
| Time LagPhase λ (minutes) | 149.6006 | 9.79726 |

E.coli + 100µg/mL  AuNPs

Table S33. Adjust parameters of the curve by modified Gompertz Model (Origin 2018 software)

| PARAMETER | MEAN VALUE | STANDARD DEVIATION |
| --- | --- | --- |
| a | 0.89091 | 0.00462 |
| Xc | 299.24812 | 3.447 |
| k | 0.00496 | 1.21086E-4 |
| R^2 ADJUST | 0.99318 |  |

Table S34. PHYSICAL PARAMETERS OF BACTERIAL GROWTH OBTAINED WITH ADJUST PARAMETERS

| PARAMETER | Mean Value | Standard Deviation |
| --- | --- | --- |
| Growth Rate µ (D.O./minutes) | 0.00163 | 4.81157E-5 |
| Time LagPhase λ (minutes) | 97.63522 | 5.89169 |

E.coli + AgNPs

E.coli  without AgNPs

Table S35. Adjust parameters of the curve by modified Gompertz Model (Origin 2018 software)

| PARAMETER | MEAN VALUE | STANDARD DEVIATION |
| --- | --- | --- |
| a | 1.11606 | 0.00401 |
| Xc | 260.85241 | 2.32122 |
| k | 0.00795 | 1.90302E-4 |
| R^2 ADJUST | 0.99519 |  |

Table S36. PHYSICAL PARAMETERS OF BACTERIAL GROWTH OBTAINED WITH ADJUST PARAMETERS

| PARAMETER | Mean Value | Standard Deviation |
| --- | --- | --- |
| Growth Rate µ (D.O./minutes) | 0.00326 | 8.98612E-5 |
| Time LagPhase λ (minutes) | 135.06625 | 7.66816 |

E.coli  + 1µg/mL  AgNPs

Table S37. Adjust parameters of the curve by modified Gompertz Model (Origin 2018 software)

| PARAMETER | MEAN VALUE | STANDARD DEVIATION |
| --- | --- | --- |
| a | 0.8839 | 0.00112 |
| Xc | 251.07818 | 0.84028 |
| k | 0.00844 | 7.54709E-5 |
| R^2 ADJUST | 0.99932 |  |

Table S38. PHYSICAL PARAMETERS OF BACTERIAL GROWTH OBTAINED WITH ADJUST PARAMETERS

| PARAMETER | Mean Value | Standard Deviation |
| --- | --- | --- |
| Growth Rate µ (D.O./minutes) | 0.00274 | 2.80183E-5 |
| Time LagPhase λ (minutes) | 132.59477 | 2.81509 |

E.coli  + 10µg/mL  AgNPs

Table S39. Adjust parameters of the curve by modified Gompertz Model (Origin 2018 software)

| PARAMETER | MEAN VALUE | STANDARD DEVIATION |
| --- | --- | --- |
| a | 0.88798 | 0.00202 |
| Xc | 331.74964 | 1.4728 |
| k | .00579 | 6.8597E-5 |
| R^2 ADJUST | 0.99873 |  |

Table S40. PHYSICAL PARAMETERS OF BACTERIAL GROWTH OBTAINED WITH ADJUST PARAMETERS

| PARAMETER | Mean Value | Standard Deviation |
| --- | --- | --- |
| Growth Rate µ (D.O./minutes) | 0.00189 | 2.67112E-5 |
| Time LagPhase λ (minutes) | 159.03807 | 4.47445 |

E.coli  + 50µg/mL  AgNPs

Table S41. Adjust parameters of the curve by modified Gompertz Model (Origin 2018 software)

| PARAMETER | MEAN VALUE | STANDARD DEVIATION |
| --- | --- | --- |
| a | 0.24357 | 0.00853 |
| Xc | 999.37678 | 8.83407 |
| k | 0.00703 | 6.84646E-4 |
| R^2 ADJUST | 0.96459 |  |

Table S42. PHYSICAL PARAMETERS OF BACTERIAL GROWTH OBTAINED WITH ADJUST PARAMETERS

| PARAMETER | Mean Value | Standard Deviation |
| --- | --- | --- |
| Growth Rate µ (D.O./minutes) | 6.29919E-4 | 8.34075E-5 |
| Time LagPhase λ (minutes) | 857.12927 | 174.52691 |

E.coli  + 100µg/mL  AgNPs

Table S43. Adjust parameters of the curve by modified Gompertz Model (Origin 2018 software)

| PARAMETER | MEAN VALUE | STANDARD DEVIATION |
| --- | --- | --- |
| a | 0.16375 | 0.02129 |
| Xc | 1263.27391 | 14.211 |
| k | 0.01491 | 7.126E-4 |
| R^2 ADJUST | 0.64714 |  |

Table S44. PHYSICAL PARAMETERS OF BACTERIAL GROWTH OBTAINED WITH ADJUST PARAMETERS

| PARAMETER | Mean Value | Standard Deviation |
| --- | --- | --- |
| Growth Rate µ (D.O./minutos) | 8.98182E-4 | 1.59705E-4 |
| Time LagPhase λ (minutes) | 1196.20483 | 127.79797 |

E.coli + Au@AgNPs

E.coli  without Au@AgNPs

Table S45. Adjust parameters of the curve by modified Gompertz Model (Origin 2018 software)

| PARAMETER | MEAN VALUE | STANDARD DEVIATION |
| --- | --- | --- |
| a | 1.11762 | .00371 |
| Xc | 267.82612 | 2.214 |
| k | 0.0077 | 1.68698E-4 |
| R^2 ADJUST | 0.99587 |  |

Table S46. PHYSICAL PARAMETERS OF BACTERIAL GROWTH OBTAINED WITH ADJUST PARAMETERS

| PARAMETER | Mean Value | Standard Deviation |
| --- | --- | --- |
| Growth Rate µ (D.O./minutes) | 0.00317 | 7.98693E-5 |
| Time LagPhase λ (minutes) | 137.95599 | 7.18533 |

E.coli  + 1µg/mL Au@AgNPs

Table S47. Adjust parameters of the curve by modified Gompertz Model (Origin 2018 software)

| PARAMETER | MEAN VALUE | STANDARD DEVIATION |
| --- | --- | --- |
| a | 0.90492 | .00157 |
| Xc | 258.17945 | 1.15103 |
| k | 0.00812 | 9.64081E-5 |
| R^2 ADJUST | 0.99879 |  |

Table S48. PHYSICAL PARAMETERS OF BACTERIAL GROWTH OBTAINED WITH ADJUST PARAMETERS

| PARAMETER | Mean Value | Standard Deviation |
| --- | --- | --- |
| Growth Rate µ (D.O./minutes) | 0.0027 | 3.67843E-5 |
| Time LagPhase λ (minutes) | 135.02674 | 3.80831 |

E.coli  + 10µg/mL Au@AgNPs

Table S49. Adjust parameters of the curve by modified Gompertz Model (Origin 2018 software)

| PARAMETER | MEAN VALUE | STANDARD DEVIATION |
| --- | --- | --- |
| a | 0.88673 | 0.00207 |
| Xc | 432.0806 | 1.3607 |
| k | 0.00578 | 6.48403E-5 |
| R^2 ADJUST | 0.99907 |  |

Table S50. PHYSICAL PARAMETERS OF BACTERIAL GROWTH OBTAINED WITH ADJUST PARAMETERS

| PARAMETER | Mean Value | Standard Deviation |
| --- | --- | --- |
| Growth Rate µ (D.O./minutes) | 0.00189 | 2.55531E-5 |
| Time LagPhase λ (minutes) | 259.07022 | 6.62838 |

E.coli  + 50µg/mL Au@AgNPs

Table S51. Adjust parameters of the curve by modified Gompertz Model (Origin 2018 software)

| PARAMETER | MEAN VALUE | STANDARD DEVIATION |
| --- | --- | --- |
| a | 0.48624 | .02697 |
| Xc | 1355.71203 | 4.580 |
| k | 0.01526 | 9.04012E-4 |
| R^2 ADJUST | 0.98815 |  |

Table S52. PHYSICAL PARAMETERS OF BACTERIAL GROWTH OBTAINED WITH ADJUST PARAMETERS

| PARAMETER | Mean Value | Standard Deviation |
| --- | --- | --- |
| Growth Rate µ (D.O./minutos) | 0.00273 | 3.13113E-4 |
| Time LagPhase λ (minutes) | 1290.18123 | 157.22091 |

E.coli  + 100µg/mL Au@AgNPs

Table S53. Adjust parameters of the curve by modified Gompertz Model (Origin 2018 software)

| PARAMETER | MEAN VALUE | STANDARD DEVIATION |
| --- | --- | --- |
| a | 0.03487 | 3.31568E-4 |
| Xc | 1721.68697 | 5.0138 |
| k | 0.00351 | 2.81594E-5 |
| R^2 ADJUST | 0.99414 |  |

Table S54. PHYSICAL PARAMETERS OF BACTERIAL GROWTH OBTAINED WITH ADJUST PARAMETERS

| PARAMETER | Mean Value | Standard Deviation |
| --- | --- | --- |
| Growth Rate µ (D.O./minutes) | 4.50261E-5 | 7.89367E-7 |
| Time LagPhase λ (minutes) | 1436.78669 | 27.23772 |