| Table 1. Optimization of conditions in the reaction of ethyl acetoacetate (2), 4-chlorobenzaldehyde (3a), urea (4) under different conditions.a |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Yieldb (%) 5a | Time (min) | Temperature (°C) | Solvent | Catalyst loading (mg) | Entry |
| 26 | 180 | r.t | MeOH | 20 | 1 |
| 69 | 90 | Reflux | EtOH | 20 | 2 |
| 45 | 90 | Reflux | CH2Cl2 | 20 | 3 |
| 78 | 120 | 60 | CH3CN | 20 | 4 |
| 62 | 100 | Reflux | DMF | 20 | 5 |
| 48 | 150 | Reflux | Toluene | 20 | 6 |
| 35 | 240 | r.t | Et2O | 20 | 7 |
| 75 | 120 | 60 | CHCl3 | 20 | 8 |
| 77 | 55 | Reflux | EtOH/ H2O (1:2) | 20 | 9 |
| 73 | 70 | Reflux | EtOH/ H2O (1:1) | 20 | 10 |
| 95 | 35 | 80 | Solvent-free | 15 | 11 |
| 69 | 65 | 80 | Solvent-free | 10 | 12 |
| 60 | 90 | 80 | Solvent-free | 5 | 13 |
| 57 | 120 | 80 | Solvent-free | 2 | 14 |
| 15 | 180 | 80 | Solvent-free | 0 | 15 |
| aReaction conditions: ethyl acetoacetate (2, 2 mmol), 4-chlorobenzaldehyde (3a, 1 mmol), urea (4, 1.2 mmol), MCM-41-APS-PMDA-SO3H (1) under different conditions. |  |  |  |  |  |

| Table 2. Scope of the Biginelli 3,4-dihydropyrimidin-2-(1H)-ones catalyzed ), MCM-41-APS-PMDA-SO3H (1)a |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Entry | Aldehyde (3) | Product | Time (min) | Yield (%)b | mp °C (Obs.) | mp °C (Lit.) |
| 1 | 4-ClC6H4 |  | 35 | 95 | 210-211 | 210-21162 |
| 2 | C6H5 |  | 55 | 87 | 235-236 | 234-23663 |
| 3 | 4-NO2C6H4 |  | 50 | 80 | 204 | 20464 |
| 4 | 3-NO2C6H4 |  | 60 | 82 | 293-295 | 224-22765 |
| 5 | 4-CH3OC6H4 |  | 55 | 89 | 201-203 | 202-20466 |
| 6 | 2-ClC6H4 |  | 60 | 90 | 211-213 | 211-21364 |
| 7 | 4-OHC6H4 |  | 55 | 82 | 234–236 | 233-23567 |
| 8 | 2- Thiophenecarboxaldehyde |  | 45 | 84 | 212-214 | 210-21268 |
| 9 | 4-Dimethylaminobenzaldehyde |  | 45 | 92 | 213-215 | 213-21569 |
| 10 | 4-FC6H4 |  | 60 | 85 | 180 | 18070 |
| aReaction conditions: : ethyl acetoacetate (2, 2 mmol), aldehydes (3, 1 mmol), urea (4, 1.2 mmol), MCM-41-APS-PMDA-SO3H (1) under solvent-free conditions was heated to 80 ᵒC. b Isolated yields were reported. |  |  |  |  |  |  |

Table 3. Comparison of the catalytic activity of the MCM-41-APS-PMDA-SO3H (1) with other catalysts

| Entry | Catalyst | Amount of catalyst | Solvent | Temp. (oC) | Time (min) | Yield (%) | References |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | PPF-SO3H | 250 mg | EtOH | Reflux | 480 | 81 | 63 |
| 2 | PANI-FeCl3 | 200 mg | CH3CN | Reflux | 1440 | 83 | 71 |
| 3 | Fe3O4/PAA-SO3H | 60 mg | Solvent-free | RT | 120 | 90 | 72 |
| 4 | H2SO4.Silica gel | 30 mol ⁒ | Solvent-free | 60 °C | 120 | 89 | 73 |
| 5 | Zr(H2PO4)2 | 7 mol ⁒ | Solvent-free | 90 °C | 60 | 92 | 74 |
| 6 | MCM-41-APTES-PMDA-SO3H | 15 mg | Solvent-free | 80 °C | 35 | 96 | This work |