Supporting information for

Biogenic Synthesis and Congo Red Dye Removal, Cytotoxic, Antioxidant and Antimicrobial Activities of supermagnetic Fe3O4 Nanoparticles Using Plantago lanceolata L. Leaf Extracts

Semih GÖKDAĞ1, Fatma CAF2, Fulya DOĞANER1, Bülent KAYA3*, Adnan AYNA4, Gürkan AYKUTOĞLU3

Affiliations

1Faculty of Sciences and Arts, Molecular Biology and Genetics Department, University of Aksaray, 68000 Turkey

2Vocational School of Food, Agriculture and Livestock, University of Bingöl,12000 Turkey

3Faculty of Sciences and Arts, Molecular Biology and Genetics Department, University of Bingöl, 12000 Turkey

4Faculty of Sciences and Arts, Chemistry Department, University of Bingöl, 12000 Turkey

3.2. Adsorption isotherms, adsorption kinetics, and thermodynamic analysis

Fig. S1. The possible mechanism of dye degradation activity of PLE@FeNPs.

3.6 Antimicrobial activity

| Well arrangement | 1 | 2 | 3 | 4 | 5 | 6 |
| --- | --- | --- | --- | --- | --- | --- |
|  | 5 mg/mL | 2.5 mg/mL | 1.25 mg/mL | 0.625 mg/mL | 0.3125mg/mL | 0.15625mg/mL |

Figure S3. Photograph of plate showing antimicrobial activity of PLE@FeNPs. Well arrangement: A: Klebsiella pneumoniae, B: Escherichia coli, C: Saccharomyces cerevisiae, D:  Staphylococcus aureus.

After PLE@FeNPs were applied to microorganisms, they were incubated for 24 hours. Then, measurements were taken on the ELISA device. The results are shown in Table 3.

3.2. Adsorption isotherms, adsorption kinetics, and thermodynamic analysis

Table S1: Forms of different Fe+3 species at various pH levels [1-3]

| Fe | pH |
| --- | --- |
| Fe(H2O)63+ | 1-2 |
| Fe(OH)(H2O)5 2+ | 2-3 |
| Fe(OH)2(H2O)4+ | 3-4 |
| Fe(OH)3 | 7-10 |

Table S2.  Estimated kinetic parameters and isotherm models for CR adsorption on PLE@FeNPs. (Nidheesh et al. 2013, Gomattiet al. 2009, Neamtu et al.2003)

| Isotherm model | Isotherm parameters | Temperature (°C) |  |
| --- | --- | --- | --- |
|  |  | 25 | 40 |
| Langmuir | qm (mg g-1) | 136.7989056 | 115.8748552 |
|  | KL (L mg-1 ) | 0.094432 | 0.143427 |
|  | RL | 0.174776 | 0.122379 |
|  | R2 | 0.85844 | 0.96012 |
| Freundlich | Kf (mg g-1)(L mg-1)1/n | 29.33054 | 22.87231 |
|  | 1/n | 0.29108 | 0.38157 |
|  | R2 | 0.60642 | 0.9554 |
| Temkin | BT (J mol-1) | 18.6799 | 27.91593 |
|  | KT (L mg-1) | 3.25451846 | 0.98200296 |
|  | R2 | 0.77629 | 0.85746 |
| Kinetic model | Kinetic parameters |  |  |
| Pseudo-first-order | qe exp (mg/g) | 77.10702 | 67.6058 |
|  | qe cal (mg/g) | 19.91115 | 6.53002 |
|  | k1 (dk-1) | -0.00025 | 0.000118 |
|  | R2 | 0.25751 | 0.24786 |
| Pseudo-second-order | qe cal (mg/g) | 79.11392 | 71.736 |
|  | k2 (mg g-1 min-1) | 0.001911 | 0.00207 |
|  | qe2 | 6259.013 | 5146.06 |
|  | R2 | 0.99268 | 0.98708 |

References

[1]. Gomathi Devi, L., Girish Kumar, S., Mohan Reddy, K., Munikrishnappa, C., 2009. Photo degradation of Methyl Orange an azo dye by Advanced Fenton Process using zero valent metallic iron: Influence of various reaction parameters and its degradation mechanism. J. Hazard. Mater. 164(2-3), 459-467. https://doi.org/10.1016/j.jhazmat.2008.08.017.

[2].Neamtu, M., Yediler, A., Siminiceanu, I., Kettrup, A., 2003. Oxidation of commercial reactive azo dye aqueous solutions by the photo-Fenton and Fenton-like processes. J. Photochem. Photobiol. A: Chem. 161(1), 87-93. https://doi.org/10.1016/S1010-6030(03)00270-3

[3]. Nidheesh, P.V., Gandhimathi, R., Ramesh, S.T., 2013. Degradation of dyes from aqueous solution by Fenton processes: a review. Environ. Sci. Pollut. Res. 20(4), 2099-2132. https://doi.org/10.1007/s11356-012-1385-z.