Micro-structural investigations on oppositely charged mixed surfactant gels with potential dermal applications

Manas Barai,1 Emili Manna,2 Habiba Sultana,1 Manas Mandal,1 Kartik Chandra Guchhait,3 Tuhin Manna,3 Anuttam Patra,4 Chien-Hisang Chang,5 Parikshit Moitra,6 Chandradipa Ghosh,3 Anna-Carin Larsson,4 Santanu Bhattacharya6  and Amiya Kumar Panda1,*

1 Department of Chemistry, Vidyasagar University, Midnapore - 721102, West Bengal, India

2Centre for Life Sciences, Vidyasagar University, Midnapore-721102, West Bengal, India

3 Department of Human Physiology, Vidyasagar University, Midnapore - 721102, West Bengal, India

4 Chemistry of Interfaces Group, Luleå University of Technology–SE-97187, Luleå, Sweden

5 Department of Chemical Engineering, National Cheng Kung University, Tainan, Taiwan

6 Indian Associations for the Cultivation of Science, Jadavpur, Kolkata-700032, India

Fig. S1.(a) Variations in relative areas of precipitation, viscous, and gel phaseof C12MalNa2+HTAB, (b); C12AspNa2+HTAB, and (c); C12GluNa2 +HTAB mixtures at different surfactant concentrations [C]. Temperature:  298K.

Fig.S2. POM images of C12MalNa2+HTAB mixtures at different compositions. a1, a2, a3, a4, and a5: 1, 2, 3, 4, 5wt%; a1, b1, c1, d1, and e1: 4/1, 3/2, 1/1, 2/3, 1/4 w/w. Scale bars in (µm) are shown inside the images. Temperature: 298K.

Fig. S3. POM images of (C12AspNa2+ HTAB; a1, b1, and c1) and (C12GluNa2+ HTAB; a2, b2, and c2) at 5 wt%, 50, 60, and 80 weight ratio of HTAB. Scale bars in (µm) are shown inside the figure. Temperature: 298K.

Fig. S4. FE-SEM images of C12MalNa2+HTAB at different compositions. a1, a2, a3, a4, and a5: 1, 2, 3, 4, 5wt. %; a1, b1, c1, d1, and e1: 4/1, 3/2, 1/1, 2/3, 1/4 w/w. Scale bars in (µm) are shown inside the images.

Table S1. Results on the POM and SEM images at different wt.% of AAS+HTAB aggregates at 298K.

|  | POM liquid crystal |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| (AAS+HTAB) wt.% | HTAB/AAS (w/w) |  |  |  |  |
|  | 20 | 40 | 50 | 60 | 80 |
| 1 | nematic | smectic | columnar | rod | disk |
| 2 | calamitic | nematic | smectic | columnar | flower |
| 3 | nematic | spherulite | cholesteric | flower | flower |
| 4 | smectic | discotic | smectic | flower | flower |
| 5 | spherulite | flower | calamitic | flower | flower |
|  | SEM(morphology) |  |  |  |  |
| 1 | rolled | wrinkled | wet | cloth | coral |
| 2 | wrinkled | ribbon | fiber | sponge | flower |
| 3 | pumice | snowball | flower | fiber | flower |
| 4 | porous | flower | clumped | sponge | flower |
| 5 | honeycomb | flower | flower | flower | flower |

Fig. S5. FE-SEM images of C12AspNa2+HTAB; a1, b1, and c1) and (C12GluNa2+ HTAB, a2, b2, and c2) at 50, 60, and 80 wt% of HTAB. Scale bar in (µm) was shown inside the figure.

Fig. S6. TGA thermograms of pure AASs and HTAB. Systems: blue; C12MalNa2, red; C12AspNa2, black; C12GluNa2, and magenta; HTAB where a1, b1, c1, d1, a2, b2, c2, a3, b3, c3, a4, b4and c4 represent the different phase transitions. Scan rate 2°C min-1.

Table S2. Results on the thermo gravimetric analysis of pure and AAS+HTAB mixed gels system.

| Surfactant | temperature range | %wt. remaining |
| --- | --- | --- |
| pure C12MalNa2 | 80-105 | 89 |
|  | 105-186 | 79 |
|  | 247-310 | 68 |
|  | 351-412 | 25 |
| pure C12AspNa2 | 86-125 | 93 |
|  | 260-310 | 77 |
|  | 310-345 | 51 |
| pureC12GluNa2 | 73-123 | 96 |
|  | 330-406 | 82 |
|  | 422-508 | 55 |
| pure HTAB | 51-120 | 94 |
|  | 113-158 | 81 |
|  | 185-263 | 77 |
|  | 294-360 | 41 |
| C12MalNa2+HTAB (100mM, AAS: HTAB = 40:60, M/M). | 43-102 | 67 |
|  | 232-259 | 27 |
| C12AspNa2+HTAB (100mM, AAS: HTAB = 40:60, M/M). | 69-120 | 66 |
|  | 268-300 | 18 |
| C12GluNa2+HTAB (100mM, AAS: HTAB = 40:60, M/M). | 43-109 | 81 |
|  | 119-288 | 63 |