Supplementary Information

Magnetic, Synergistic interaction of SnO2/ZnFe2O4 nanocomposite participated catalytic degradation performance of Coordination complex under UV light illumination

D. Venkatesh, R. Silambarasan, and K. Anbalagan*

Department of Chemistry, Pondicherry University, Pondicherry 605014, India

E-mail:venkichem23@gmail.com; Tel: +91 413 2654509

Fig. S1 TEM micrographs of SnO2 nanoparticles (a) magnifications at 200 nm (b) particle size distribution histogram (c) lattice fringes (d) SAED pattern

Fig. S2 TEM micrographs of ZnFe2O4 (a-c) magnifications at 200 nm and 100 nm, respectively distribution histogram (d) lattice fringes.

Fig. S3 FT-IR spectra of SnO2/ZnFe2O4 nanocomposites, nano SnO2, and ZnFe2O4 in the range 4000-400 cm−1 at room temperature.

Fig. S4 Absorption spectral traces of cis-[Co(en)2(Im)Cl]Cl2 complex observed in the adsorption of cobalt(III) complex on SnO2/ZnFe2O4 nanocomposite in A) H2O: DMSO (70/30% v/v)).  The rate constant of surface adsorption measurements in B) H2O, C) H2O: PriOH, D) H2O: CH3CN, E) H2O: DMSO, F) H2O: ButOH (70/30% v/v)) at room temperature. Ionic strength:1M NaNO3. Dosage of catalyst: 300 mg/100ml. Concentration of Cobalt(III) Complex: 2.6 x 10-3 M.

Fig. S5 Absorption spectral traces of cis-[Co(en)2(Im)Cl]Cl2 complex observed in the photochemical reduction of Cobalt(III) complex on SnO2/ZnFe2O4 nanocomposite in a) neat water. The rate constant of surface adsorption measurements in b) H2O, c) H2O: PriOH, d) H2O: CH3CN, e) H2O: DMSO, f) H2O: ButOH at room temperature. Ionic strength:1M NaNO3. Wavelength of excitation, λ = 365 nm; light intensity: 8.50 x1017 photon/sec; Dosage of catalyst: 300 mg/100ml. Concentration of Cobalt(III) Complex: 2.6 x 10-3 M.

Table T1 Room temperature of M-H loops of magnetic retentivity, Coercivity and saturated magnetism values of nano SnO2, SnO2/ZnFe2O4 nanocomposites, nano ZnFe2O4 at room temperature.

| Sample | Hc, Oe | MR, cm3.mol-1 x 10-4 | Ms, (emu/g) |
| --- | --- | --- | --- |
| SnO2 | 115.1542 | 1.3266 | 0.0115 |
| SnO2/ZnFe2O4 | 78.3654 | 0.5423 | 0.7128 |
| ZnFe2O4 | 147.7164 | 0.0672 | 3.0698 |

| Reaction conditions | Adsorbent | Time (min) |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | 5 | 10 | 15 | 30 | 45 | 60 |
|  |  | Removal efficiency (%) |  |  |  |  |  |
| Water$ | SnO2 | 0 | 0 | 1 | 1 | 1 | 1 |
|  | SnO2/ZnFe2O4 | 13 | 15 | 16 | 16 | 17 | 19 |
|  | ZnFe2O4 | 9 | 9 | 10 | 10 | 10 | 10 |
| H2O: PriOH@ | SnO2 | 0 | 1 | 3 | 4 | 4 | 5 |
|  | SnO2/ZnFe2O4 | 14 | 14 | 14 | 14 | 14 | 15 |
|  | ZnFe2O4 | 2 | 3 | 7 | 7 | 8 | 8 |
| H2O: CH3CN@ | SnO2 | 1 | 8 | 9 | 10 | 11 | 11 |
|  | SnO2/ZnFe2O4 | 2 | 4 | 10 | 11 | 12 | 13 |
|  | ZnFe2O4 | 0 | 1 | 3 | 4 | 5 | 7 |
| H2O: DMSO@ | SnO2 | 7 | 7 | 12 | 13 | 14 | 16 |
|  | SnO2/ZnFe2O4 | 7 | 25 | 30 | 31 | 36 | 40 |
|  | ZnFe2O4 | 0 | 4 | 4 | 13 | 21 | 29 |
| H2O: ButOH@ | SnO2 | 3 | 4 | 6 | 8 | 9 | 10 |
|  | SnO2/ZnFe2O4 | 14 | 23 | 34 | 35 | 36 | 36 |
|  | ZnFe2O4 | 5 | 5 | 22 | 22 | 24 | 29 |

Table T2 Time-dependent removal efficiency data of surface adsorption of cis-[Co(en)2(im)Cl]Cl2 complex using SnO2/ZnFe2O4 nanocomposite and nano SnO2 and nano ZnFe2O4 by varying ratio of solvents at room temperature. Ionic strength: 1 M NaNO3; Dosage of catalyst: 300 mg/100ml. Concentration of Cobalt(III) Complex: 2.6 x 10-3 M.

$- triply distilled water; @- ratio of the solvent medium maintained 70:30% (v/v)

Table T3 Time-dependent photochemical degradation efficiency data of reduction of cis-[Co(en)2(im)Cl]Cl2 complex using SnO2/ZnFe2O4 nanocomposite and nano SnO2 and nano ZnFe2O4 by varying ratio of solvents at room temperature. Ionic strength: 1 M NaNO3. wavelength of excitation, λ = 254 nm; light intensity: 8.50 x1017 photon/sec; Dosage of catalyst: 300 mg/100ml. Concentration of Cobalt(III) Complex: 2.6 x 10-3 M

| Reaction conditions | Catalyst | Time (min) |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  | 3 | 6 | 9 | 12 | 18 |
|  |  | Photo efficiency (%) |  |  |  |  |
| Water$ | SnO2 | 6 | 7 | 9 | 10 | 14 |
|  | SnO2/ZnFe2O4 | 8 | 11 | 12 | 20 | 20 |
|  | ZnFe2O4 | 1 | 1 | 3 | 6 | 11 |
| H2O: PriOH@ | SnO2 | 4 | 7 | 9 | 17 | 21 |
|  | SnO2/ZnFe2O4 | 0 | 8 | 24 | 30 | 56 |
|  | ZnFe2O4 | 8 | 13 | 14 | 19 | 23 |
| H2O: CH3CN@ | SnO2 | 8 | 9 | 9 | 10 | 13 |
|  | SnO2/ZnFe2O4 | 3 | 7 | 8 | 9 | 19 |
|  | ZnFe2O4 | 3 | 5 | 8 | 17 | 17 |
| H2O: DMSO@ | SnO2 | 1 | 1 | 4 | 5 | 5 |
|  | SnO2/ZnFe2O4 | 4 | 4 | 8 | 8 | 11 |
|  | ZnFe2O4 | 0 | 1 | 4 | 6 | 9 |
| H2O: ButOH@ | SnO2 | 0 | 1 | 4 | 5 | 6 |
|  | SnO2/ZnFe2O4 | 4 | 4 | 10 | 15 | 19 |
|  | ZnFe2O4 | 10 | 12 | 13 | 15 | 17 |

$- triply distilled water; @- ratio of the solvent medium maintained 70:30% (v/v)

Table T4 Time-dependent photochemical degradation efficiency data of reduction of cis-[Co(en)2(im)Cl]Cl2 complex using SnO2/ZnFe2O4 nanocomposite and nano SnO2 and nano ZnFe2O4 by varying ratio of solvents at room temperature. Ionic strength: 1 M NaNO3. Wavelength of excitation, λ = 365 nm; Dosage of catalyst: 300 mg/100ml. Concentration of Cobalt(III) Complex: 2.6 x 10-3 M.

| Reaction conditions | Catalyst | Time (min) |  |  |  |  | Rate constant (k sec-1) | R2 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | 3 | 6 | 9 | 12 | 18 |  |  |
|  |  | Photo efficiency (%) |  |  |  |  |  |  |
| Water$ | SnO2 | 1 | 2 | 3 | 3 | 3 | 0.0020 | 0.8589 |
|  | SnO2/ZnFe2O4 | 2 | 2 | 3 | 4 | 6 | 0.0035 | 0.9830 |
|  | ZnFe2O4 | 0 | 0 | 4 | 5 | 7 | 0.0048 | 0.8898 |
| H2O: PriOH@ | SnO2 | 1 | 3 | 3 | 4 | 5 | 0.0031 | 0.9074 |
|  | SnO2/ZnFe2O4 | 1 | 3 | 9 | 17 | 27 | 0.0209 | 0.9185 |
|  | ZnFe2O4 | 1 | 12 | 14 | 26 | 31 | 0.0254 | 0.9267 |
| H2O: CH3CN@ | SnO2 | 1 | 2 | 3 | 7 | 11 | 0.0157 | 0.8991 |
|  | SnO2/ZnFe2O4 | 1 | 2 | 13 | 15 | 16 | 0.0075 | 0.9070 |
|  | ZnFe2O4 | 2 | 2 | 12 | 16 | 20 | 0.0146 | 0.7566 |
| H2O: DMSO@ | SnO2 | 3 | 5 | 8 | 11 | 11 | 0.0074 | 0.8178 |
|  | SnO2/ZnFe2O4 | 2 | 6 | 7 | 9 | 13 | 0.0079 | 0.9371 |
|  | ZnFe2O4 | 1 | 4 | 6 | 11 | 13 | 0.0079 | 0.9030 |
| H2O: ButOH@ | SnO2 | 1 | 2 | 6 | 7 | 9 | 0.0073 | 0.9054 |
|  | SnO2/ZnFe2O4 | 0 | 4 | 5 | 9 | 10 | 0.0076 | 0.9364 |
|  | ZnFe2O4 | 1 | 3 | 5 | 7 | 12 | 0.0075 | 0.9646 |

$- triply distilled water; @- ratio of the solvent medium maintained 70:30% (v/v)