Supplementary information

Rational Design on Polymorphous Phase Switching in Molybdenum Diselenide-based Memristor Assisted by All-Solid-State Reversible Intercalation Toward Neuromorphic Application

Ling Lee1,2,3, Chun-Hsiu Chiang1,2,3, Ying-Chun Shen1,2,3, Shu-Chi Wu1,2,3, Yu-Chuan Shih1,2,3, Tzu-Yi Yang1,2,3, Yu-Chieh Hsu1,2,3, Ruei-Hong Cyu1,2,3, Yi-Jen Yu4, Shang-Hsien Hsieh5, Chia-Hao Chen5, Mikhail Lebedev6, and Yu-Lun Chueh1,2,3*

1Department of Materials Science and Engineering, National Tsing Hua University, Hsinchu 30013, Taiwan,

2Department of Physics, National Sun Yat-Sen University, Kaohsiung 80424, Taiwan.

3Frontier Research Center on Fundamental and Applied Sciences of Matters, National Tsing Hua University, Hsinchu 30013, Taiwan.

4Instrument Center, National Tsing Hua University, Hsinchu 30013, Taiwan

5National Synchrotron Radiation Research Center, Hsinchu 30076, Taiwan.

6Laboratory of functional films and coatings, Nikolaev Institute of inorganic chemistry SB RAS, Lavrent'ev ave. 3, Novosibirsk, 630090, Russia

Figure S1 Schematic procedure flows. Fabrication steps preparing self-patterned MoSe2 films, starting from a and b the selection of synthesized location, c the preparation of precursor, and d the selenization process, followed by the two-terminal memristor devices, starting from e and f for the active Cu electrode, and g and h for the Au electrode.

Figure S2 Fundamental electrical characteristics of vertical lamellar 1T-rich MoSe2 films fabricated by PACVR. a The n-type characteristics proved by the reduction of temporal current under the ambient filled with oxidizing NO2 gases. b The sheet resistance of MoSe2 film extrapolated by the transmission line method (TLM).

Figure S3 Self-patterning of large-scaled continuous MoSe2 films. a Optical microscopy image of MoSe2 patterns with various sizes fabricated by PACVR. b Raman spectra measured in each location illustrated in a.

Figure S4 Evidence of controllable orientations in vertical lamellar MoSe2 films. X-ray diffraction spectra of a lateral- and b vertical-aligned MoSe2 films prepared by PACVR measured along the surface normal (black) and in-plane (red) orientation.

Figure S5 Stoichiometric investigations on copper distributions in Au/MoSe2/Cu devices. a, b Plan-view scanning electron microscopy (SEM) images of as-deposited electrodes on MoSe2. c Correlated EDX spectra and the atomic ratio of Cu in each region of interest (ROI) illustrated in a. d, e SEM images of annealed Cu electrode on MoSe2. f Correlated EDX spectra in each ROI illustrated in d.

Figure S6 Forming process of vertical lamellar MoSe2 film. The current-voltage relationship of a Au/MoSe2:CuSex/Cu device with a forming process at 15 V.

Figure S7 SPEM mapping image of memristor. The SPEM mapping of the Au/MoSe2:CuSex/Cu channel. The red spot indicates the location for collecting pseudo-operando XPS spectra.

Figure S8 Stoichiometric evolution related to Cu. Pseudo-operando local XPS spectra at the center of Au/MoSe2:CuSex/Cu channel after SET (black) and RESET (red) processes.

Figure S9 a priori information of MoSe2 films regarding polymorphous phase-changed memristive behaviors. a The XPS spectra of the Mo 3d core level for a 2H-rich film synthesized at 450 ℃ together with fitting components from 1T phase (blue), 2H phase (pink), amorphous MoSe3 (dark yellow), and MoO3 (green). b Current-voltage relationships and sheet resistances of 1T-rich (250-℃-synthesized, black) and 2H-rich (450-℃-synthesized, red) MoSe2 films.

Figure S10 Proposed model for phase and resistance switching. The schematic illustration of the current flow, the Cu intercalation, and the corresponding atomic geometry at a pristine condition, b after RESET, and c SET processes.