Supplement Materials for

Super-elasticity at 4K of Covalently Crosslinked Polyimide Aerogels with Ultrahigh Negative Poisson’s Ratio

Yang Cheng1, 2, Xiang Zhang3, Yixiu Qin4,Pei Dong5, Wei Yao1,2, John Matz5, Pulickel M. Ajayan3, Jianfeng Shen1*, Mingxin Ye1*

1Institute of Special materials and Technology, Fudan University, Shanghai, P. R. China

2Department of Materials Science, Fudan University, Shanghai, P. R. China

3Department of Materials Science and Nanoengineering, Rice University, 6100 Main Street, Houston, TX 77005, USA

4State Key Laboratory of Molecular Engineering of Polymers, Fudan University, Shanghai, P. R. China

5Department of Mechanical Engineering, George Mason University, VA 22030, USA

*Corresponding Author. Email: mxye@fudan.edu.cn, jfshen@fudan.edu.cn

Supplementary Figure 1 Synthesis of covalently crosslinked polyimide from ODPA, ODA and TAB.

Supplementary Figure 2 Shear viscosity curves of DMSO solution containing PI oligomers with different molecular weight under increasing shear rate.

Supplementary Figure 3 Optical images after thawing frozen gel of PI oligomers without TAB.

Supplementary Figure 4 FT-IR spectra of PI aerogels with different crosslinking degree.

Supplementary Figure 5 Density and free volume of PAA precursor and PI simulated by Material Studio software.

Supplementary Figure 6 SEM image of PI aerogel fabricated by ice templates assisted freeze-drying process from 1 wt% PAS aqueous solution.

Supplementary Figure 7 Density and porosity of PI aerogels prepared from PI/TAB/DMSO with different solid contents.

Porosity=1- ρAρPI×100%

Where ρA represents the density of aerogels, and ρPI represents the density of constituent PI (ρPI=1.4gcm3).

Supplementary Figure 8 Schematic diagram of the mold.

Supplementary Figure 9 Stiff properties of PI aerogel on z direction.

Supplementary Figure 10 Optical images of PI aerogels before and after compression at 99% strain.

Supplementary Figure 11 Overview of PI-10 aerogels by In-situ SEM observations.

Supplementary Figure 12 SEM image of microstructure of PI-L aerogels after compression under 99% strain.

Supplementary Figure 13 (a) SEM images of PI-10 aerogels with different wall thickness, (b) Compressive stress-strain curves of PI-10 aerogels prepared from PI/TAB/DMSO mixtures with different solid content.

Supplementary Figure 14 TGA curves of PI aerogels with different crosslinking degree.

Supplementary Figure 15 Homemade apparatus for super-elastic tests of PI aerogels at 4 K.

Simulated mechanical properties of PI-10 (constituent materials of PI-10 aerogels)

- Build model

L

Supplementary Figure 16 Model for simulated mechanical properties of PI-10.

- Constant matrix of elastic stiffness and elastic compliance

- Approximate calculation for shear modulus and bulk modulus

- Shear Modulus G (GPa)

Reuss: GR=154C11+C22+C33-4C12+C23+C31+3C44+C55+C66

Voigt:15GV=C11+C22+C33-C12+C23+C31+3C44+C55+C66

Hill:GH=GV+GR2

- Bulk Modulus K (GPa)

Reuss:KR=1S11+S22+S33+2S12+S23+S31

Voigt:9KV=S11+S22+S33+2S12+S23+S31

Hill:KH=KV+KR2

- Young modulus and Poisson’s ratio

Young modulus: E=2G1+μ=3K1-2μ

Supplementary Figure 17 Apparatus for thermal shock tests of PI aerogels.