Supplement File

Computation of gamma radiation shielding parameters of lead monoxidefilled polycarbonate composite films

Vijayashri Ashok Kandagal and Blaise Lobo*

Depatment of Physics, Karnatak University’s Karnatak Science College, Dharwad 580 001,Karnataka, India

*Email: blaiselobo@kud.ac.in

Telephone: 9980250761

Fig.1 The variation of mass attenuation coefficient (in cm2/g) with respect to FL (in wt%) (a) energy starting from 59.54 keV up to 136 keV (b) energy starting from 356 keV up to 1332.5 keV

Fig.2 The variation of mass attenuation coefficient with respect to energy (a) energy starting from 59.54 keV up to 136 keV (b) energy starting from 356 keV up to 1332.5 keV

Fig. 1(a) and (b) represent the variation of mass attenuation coefficient μmwith respective filler level (FL) for lower energies (from 59.54 keV up to 136 keV) and higher energies (from 356 keV up to 1332.5 keV) respectively. From these graphs it is noted that, the μm is  increases as increase in FL. Fig. 2 (a) and (b) represent the variation of μm with respective energy for lower energies (from 59.54 keV up to 136 keV) and higher energies (from 356 keV up to 1332.5 keV) respectively. From graphs it is known that as increase in energy, the μm decreases.

Table 1 Calculated data of half value layer for selected filler concentration in the composite at different energies (i. e. energy starting from 59.54 keV up to 1332.5 keV)

| FL (wt%) | Half Value Layer (in cm) |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Gamma Energies ( in keV) |  |  |  |  |  |  |  |  |  |  |
|  | 59.54 | 81 | 122 | 136 | 356 | 511 | 661.6 | 834.86 | 1173.2 | 1274.5 | 1332.5 |
| 0 | 3.0856 | 3.3998 | 3.8253 | 3.9482 | 5.4854 | 6.3405 | 7.1048 | 7.8910 | 9.3315 | 9.7243 | 9.9419 |
| 0.25 | 2.8998 | 3.2830 | 3.6192 | 3.7807 | 5.4460 | 6.3178 | 7.0784 | 7.8713 | 9.3083 | 9.7000 | 9.9171 |
| 0.5 | 2.7366 | 3.1745 | 3.4362 | 3.6292 | 5.4164 | 6.2935 | 7.0666 | 7.8583 | 9.2928 | 9.6839 | 9.9006 |
| 0.75 | 2.5882 | 3.0717 | 3.2695 | 3.4881 | 5.3827 | 6.2710 | 7.0404 | 7.839 | 9.2697 | 9.6599 | 9.8760 |
| 1 | 2.4534 | 2.9749 | 3.1175 | 3.3570 | 5.3443 | 6.2418 | 7.0230 | 7.8193 | 9.2468 | 9.6259 | 9.8516 |
| 1.5 | 2.2249 | 2.8011 | 2.8587 | 3.1251 | 5.2829 | 6.20026 | 6.9856 | 7.7766 | 9.1939 | 9.5963 | 9.8110 |
| 2 | 2.0333 | 2.6197 | 2.6367 | 2.9232 | 5.2370 | 6.1505 | 6.9399 | 7.7447 | 9.1563 | 9.5570 | 9.7877 |
| 2.5 | 1.8693 | 2.5018 | 2.4455 | 2.7436 | 5.1449 | 6.1006 | 6.8976 | 7.6963 | 9.1115 | 9.5103 | 9.7398 |
| 3 | 1.7306 | 2.3759 | 2.2815 | 2.5867 | 5.0824 | 6.0627 | 6.8612 | 7.6547 | 9.0745 | 9.4717 | 9.7003 |
| 3.5 | 1.6084 | 2.2576 | 2.1362 | 2.4439 | 5.02146 | 6.0074 | 6.8196 | 7.6159 | 9.0305 | 9.4258 | 9.6533 |
| 4 | 1.5014 | 2.1513 | 2.0079 | 2.3149 | 4.9572 | 5.9593 | 6.7702 | 7.5705 | 8.9870 | 9.3803 | 9.6068 |
| 5 | 1.3248 | 1.9648 | 1.7920 | 2.0944 | 4.8279 | 5.8694 | 6.6784 | 7.4940 | 8.9082 | 9.3138 | 9.5226 |
| 8 | 0.9688 | 1.5476 | 1.3449 | 1.6174 | 4.4964 | 5.6029 | 6.4273 | 7.2611 | 8.6665 | 9.0611 | 9.2642 |
| 10 | 0.81533 | 1.3474 | 1.1461 | 1.3963 | 4.2854 | 5.4285 | 6.2676 | 7.1039 | 8.5017 | 8.8888 | 9.0881 |

Table 2 Calculated data of mean free path (i.e energy starting from 59.54 keV up to 1332.5 keV)

| FL (wt%) | Mean Free Path( in cm) |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Gamma Energies ( in keV) |  |  |  |  |  |  |  |  |  |  |
|  | 59.54 | 81 | 122 | 136 | 356 | 511 | 661.6 | 834.86 | 1173.2 | 1274.5 | 1332.5 |
| 0 | 4.4516 | 4.9048 | 5.5187 | 5.6960 | 7.9139 | 9.1474 | 10.2501 | 11.3843 | 13.4626 | 14.0292 | 14.3431 |
| 0.25 | 4.1834 | 4.7365 | 5.2214 | 5.4544 | 7.8568 | 9.1146 | 10.2120 | 11.3559 | 13.429 | 13.9942 | 14.3073 |
| 0.5 | 3.9480 | 4.5799 | 4.9574 | 5.2358 | 7.8143 | 9.0796 | 10.1950 | 11.3371 | 13.4067 | 13.9710 | 14.2856 |
| 0.75 | 3.7339 | 4.4316 | 4.7169 | 5.0323 | 7.7656 | 9.0471 | 10.1572 | 11.3089 | 13.3734 | 13.9363 | 14.2481 |
| 1 | 3.5394 | 4.2919 | 4.4976 | 4.8432 | 7.7102 | 9.0050 | 10.1321 | 11.2809 | 13.3403 | 13.9018 | 14.2128 |
| 1.5 | 3.2099 | 4.0411 | 4.1242 | 4.5086 | 7.6216 | 8.9485 | 10.0780 | 11.2192 | 13.2640 | 13.8446 | 14.1544 |
| 2 | 2.9334 | 3.7794 | 3.8040 | 4.2173 | 7.5554 | 8.8732 | 10.0122 | 11.1733 | 13.2097 | 13.7879 | 14.1207 |
| 2.5 | 2.6969 | 3.6093 | 3.5281 | 3.9582 | 7.4225 | 8.8012 | 9.9511 | 11.1035 | 13.1451 | 13.7205 | 14.0516 |
| 3 | 2.4967 | 3.4277 | 3.2915 | 3.7319 | 7.3323 | 8.7466 | 9.8986 | 11.0434 | 13.0918 | 13.6648 | 13.9946 |
| 3.5 | 2.3205 | 3.2571 | 3.0818 | 3.5258 | 7.2444 | 8.6669 | 9.8387 | 10.9899 | 13.0283 | 13.5985 | 13.9268 |
| 4 | 2.1661 | 3.1037 | 2.8968 | 3.3397 | 7.1518 | 8.5974 | 9.7674 | 10.9220 | 12.9655 | 13.5330 | 13.8596 |
| 5 | 1.9112 | 2.8346 | 2.5854 | 3.0217 | 6.9651 | 8.4677 | 9.6350 | 10.8116 | 12.8518 | 13.4370 | 13.7381 |
| 8 | 1.3978 | 2.2327 | 1.9404 | 2.3335 | 6.4870 | 8.0834 | 9.2727 | 10.4756 | 12.5031 | 13.0724 | 13.3654 |
| 10 | 1.1763 | 1.9439 | 1.6535 | 2.0144 | 6.1826 | 7.8317 | 9.0423 | 10.2487 | 12.2654 | 12.8239 | 13.1113 |

Half value layer (HVL) and mean free path (MFP) for PbO filled PC composites for different FL have been calculated using Eq. (6) and (7) respectively. The calculated values have been tabulated in Table 1 and 2. From Table 1 and 2, it is noted that both HVL and MFP decreases as increase in FL and increases with increase in energy of gamma photon. It is believed that the materials with low HVL and low MFP are having good shielding properties.

Authors Contributions	Vijayashri Ashok Kandagal:performed the calculations, writing of the original draft and analysis,Dr.Blaise Lobo: contributed withConceptualisation, Supervision and Editing of the written manuscript and its review.

Data availabilityThe data used in this work are openly available inNational Institute of Standards (NIST) XCOM website.http://physics.nist.gov/PhysRefData/Xcom/html/Xcoml.htm/

Declarations

Ethics approval 	Not applicable.

Consent to participate	Not applicable.

Consent for publish	Not applicable.

Funding		Not applicable.

Competing interests	The authors declare no competing interests.