ACUTE EXPOSURE OF UPCYTE® HEPATOCYTES TO SUB-LETHAL CONCENTRATIONS OF GRAPHENE OXIDE: IMPAIRMENT OF PHASE-I XENOBIOTIC METABOLISM AND ALBUMIN TRANSCRIPTION

Romaldini A.1#, Spanò R.1#, Sabella S.1,*

# These authors contributed equally to this work

1 Drug Discovery and Development Department, Istituto Italiano di Tecnologia, via Morego 30, 16136, Genoa, Italy

* Corresponding author: stefania.sabella@iit.it

SUPPLEMENTARY MATERIAL

Table 1. Primer pairs used for gene expression analysis by quantitative real-time PCR (qPCR).

| Target Gene | Direction | Primer Sequence (5'3') | Amplicon Size | Tannealing | ETarget |
| --- | --- | --- | --- | --- | --- |
| HO-1 | forward | CCCACGCCTACACCCGCTAC | 137 bp | 62°C | 2.01 |
|  | reverse | GGTGGCACTGGCAATGTTGG |  |  |  |
| SOD1 | forward | GGTGTGGCCGATGTGTCTAT | 110 bp | 60°C | 1.85 |
|  | reverse | CCTTTGCCCAAGTCATCTGC |  |  |  |
| TNFα | forward | TGGGATCATTGCCCTGTGAG | 92 bp | 60°C | 1.89 |
|  | reverse | GGTGTCTGAAGGAGGGGGTA |  |  |  |
| IL-1β | forward | ATGATGGCTTATTACAGTGGCAA | 132 bp | 58°C | 1.99 |
|  | reverse | GTCGGAGATTCGTAGCTGGA |  |  |  |
| IL-6 | forward | CCTGAACCTTCCAAAGATGGC | 75 bp | 60°C | 2.10 |
|  | reverse | TTCACCAGGCAAGTCTCCTCA |  |  |  |
| IL-8 | forward | CCAGGAAGAAACCACCGGA | 91 bp | 58°C | 2.12 |
|  | reverse | GAAATCAGGAAGGCTGCCAAG |  |  |  |
| CYP3A4 | forward | CCTTACACATACACACCCTTTGGAAGT | 382 bp | 62°C | 1.95 |
|  | reverse | AGCTCAATGCATGTACAGAATCCCCGGTTA |  |  |  |
| CYP2C9 | forward | ACGGATTTGTGTGGGAGAAGCCC | 287 bp | 62°C | 2.06 |
|  | reverse | TGAGATGACAGGTGAGAAAAGGCA |  |  |  |
| CYP2B6 | forward | GGGGCACTGAAAAAGACTGA | 118 bp | 58°C | 2.11 |
|  | reverse | AGTTCTGGAGGATGGTGGTG |  |  |  |
| CYP1A2 | forward | ATGGCATTGTCCCAGTCTGTT | 135 bp | 60°C | 2.00 |
|  | reverse | TGGCTCTGGTGGACTTTTCAG |  |  |  |
| GST | forward | GATACTGGGGTACTGGGACATCC | 130 bp | 61°C | 1.85 |
|  | reverse | CCACTGGCTTCTGTCATAATCAGG |  |  |  |
| ABCG2 | forward | CAGGTGGAGGCAAATCTTCGT | 247 bp | 58°C | 2.07 |
|  | reverse | ACCCTGTTAATCCGTTCGTTTT |  |  |  |
| PXR | forward | CTCACCTCCAGGTTTGCTTC | 114 bp | 55°C | 2.11 |
|  | reverse | TCCTTGATCGATCCTTTGC |  |  |  |
| CAR | forward | AAGTGCTTAGATGCTGGCATGAGG | 112 bp | 60°C | 2.05 |
|  | reverse | CTCAGTTGCACAGGTGTTTGC |  |  |  |
| Albumin | forward | CTTGAATGTGCTGATGACAGG | 157 bp | 57°C | 2.06 |
|  | reverse | GCAAGTCAGCAGGCATCTCAT |  |  |  |
| Reference Gene | Direction | Primer Sequence (5'3') | Amplicon Size | Tannealing | ERef |
| GAPDH | forward | AAGGTGAAGGTCGGAGTCAA | 108 bp | 55°C | 2.15 |
|  | reverse | AATGAAGGGGTCATTGATGG |  |  |  |

Notes. ‘Tannealing’ is the annealing temperature of each primer pair. ‘ETarget’ and ‘ERef’ refer to qPCR efficiencies of target and reference gene transcripts, respectively, calculated according to E = 10(-1/slope) [1].

Table 2. Hydrodynamic diameter of graphene oxide (GO) dispersed in Milli-Q® water and complete HHPM, as a function of concentration and incubation time by means of DLS analysis.

| Dispersant | Incubation | [GO] | Hydrodinamic Diameter (DH) |  |  | Relative Intensity |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | hours | μg/mL | peak #1 (nm) | peak #2 (nm) | peak #3 (nm) | peak #1 (%) | peak #2 (%) | peak #3 (%) |
| Milli-Q® water | 0 | 4 | - | 281.7 ± 25.8 | 5393.3 (n=3) | - | 98.9 | 1.1 |
|  |  | 20 | - | 320.9 ± 16.0 | 5196.0 (n=4) | - | 96.4 | 2.6 |
|  |  | 80 | - | 345.9 ± 34.0 | 4974.5 (n=4) | - | 97.2 | 2.8 |
| complete HHPM | 0 | 0 | 10.3 ± 0.3 | - | - | 94.0 | - | - |
|  | 2 | 4 | 7.9 ± 0.1 | 338.9 ± 29.0 | 5131.4 ± 274.8 | 23.5 | 73.1 | 3.4 |
|  |  | 20 | 8.1 (n=4) | 350.7 ± 42.6 | 5106.0 (n=3) | 4.5 | 93.0 | 1.5 |
|  |  | 80 | - | 352.9 ± 61.2 | 4845.5 (n=4) | - | 96.1 | 3.9 |
|  | 24 | 4 | 7.9 ± 0.1 | 344.3 ± 39.4 | 5274.5 (n=2) | 17.8 | 81.4 | 0.7 |
|  |  | 20 | 7.9 (n=3) | 337.0 ± 10.9 | 4790.8 (n=4) | 3.1 | 92.4 | 3.6 |
|  |  | 80 | - | 410.5 ± 32.7 | 4930.8 ± 176.0 | - | 95.6 | 3.2 |
| Milli-Q® water | 24* | 4 | - | 294.9 ± 8.3 | 5390.0 (n=1) | - | 99.6 | 0.4 |
|  |  | 20 | - | 319.6 ± 3.9 | 5313.5 (n=4) | - | 98.6 | 1.4 |
|  |  | 80 | - | 347.4 ± 21.0 | 5185.0 (n=1) | - | 99.7 | 0.3 |

Notes. The symbol ‘*’ means that GO was incubated in complete HHPM for 24 hours. At the end of incubation, GO suspensions were centrifuged at 15’000g for 15 minutes at 4°C and corresponding pellets were washed three times adding a volume of Milli-Q® water equal to the initial volume [2,3]. ‘n = 1’ , ‘n = 2’ , ‘n = 3’ and ‘n = 4’ mean the frequency of detection of the corresponding peak, namely, the detection of the peak in only one, two, three, four out of the five measurements performed, respectively. The symbol ‘-‘ means that the peak has never been detected in five measurements.

Figure S1. (A) Representative scanning electron microscopy image of 4 μg/mL GO in Milli-Q® water (12’000x; scale bars = 1 μm). Image on the right side is a magnification of highlighted area (100’000x; scale bar = 100 nm). (B) Size distribution profile of complete HHPM obtained via DLS analysis. (C) Size distribution profiles by means of DLS analysis of GO dispersed in Milli-Q® water (green curves) and of particle-corona complexes derived from 24-hour incubation of GO in complete HHPM and re-dispersed in Milli-Q® water (brown curves). Measurements refer to three GO concentrations.

Figure S2. (A) Cell viability of upcyte® hepatocytes treated for 24 hours with 320 μg/mL GO or with 0.03% Triton X-100 (indicated as ‘Triton’) or un-treated (indicated as ‘CTRL’), evaluated by resazurin reduction assay. Results are expressed as percentage values compared to CTRL (set as 100%). Results represent means ± SD of three independent experiments. The symbol ‘****’ refers to p < 0.0001, calculated with respect to CTRL (ordinary one-way ANOVA). ‘ns’ means there are not statistically significant differences between 320 μg/mL GO and Triton conditions. (B) Linear correlation between cell viability and cytotoxicity data (both expressed as fold increase).

Figure S3. Cell necrosis of upcyte® hepatocytes treated for up to 24 hours with 0.5 μM Staurosporine or un-treated (indicated as ‘CTRL’), evaluated by apoptosis and necrosis assay. Results are expressed as net increase of absorbance for each condition, after having subtracted the basal value of CTRL obtained after 3 hours of incubation (set as 0 a.u.). Results represent means ± SD of three independent experiments. The symbol ‘****’ refers to p < 0.0001, calculated with respect to CTRL (two-way ANOVA).

Figure S4. (A, B) Linear correlation between relative gene expression and metabolic activity data (both expressed as fold increase with respect to CTRL) for CYP3A4 (A) and CYP2C9 (B). (C, D) Relative gene expression of CYP2B6 in cells treated daily, for 72 hours with 50 μM Rifampicin (C) or with 100 μM Ciprofloxacin (D) versus un-treated cells (CTRL). Results are expressed as means ± SD values of three independent experiments. (E) Relative gene expression of CYP2B6 in cells treated for 24 hours with sub-lethal GO doses versus CTRL. Results are expressed as means ± SD values of three independent experiments. The symbols ‘**’ and ‘****’ refer to p = 0.0069 and p < 0.0001, respectively, calculated against CTRL (ordinary one-way ANOVA). (F, G) Relative gene expression of CYP1A2 in cells treated daily, for 72 hours with 50 μM Rifampicin (F) or with 100 μM Ciprofloxacin (G) versus CTRL. Results are expressed as means ± SD values of three independent experiments. (H) Relative gene expression of CYP1A2 in cells treated for 24 hours with sub-lethal GO doses versus CTRL. Results are expressed as means ± SD values of three independent experiments. The symbols ‘**’ and ‘****’ refer to p = 0.0052 and p < 0.0001, respectively, calculated against CTRL (ordinary one-way ANOVA).

Figure S5. (A, B) Relative gene expression of PXR (A) and CAR (B) in cells treated for 24 hours with sub-lethal GO doses versus un-treated cells (CTRL). Results are expressed as means ± SD values of three independent experiments. The symbol ‘*’ refers to p = 0.0224, calculated with respect to CTRL (ordinary one-way ANOVA).

REFERENCES

1. Pfaffl MW. A new mathematical model for relative quantification in real-time RT-PCR. Nucleic Acids Res [Internet]. 2001;29:45e – 45. Available from: https://academic.oup.com/nar/article-lookup/doi/10.1093/nar/29.9.e45

2. Magrì D, Sánchez-Moreno P, Caputo G, Gatto F, Veronesi M, Bardi G, et al. Laser Ablation as a Versatile Tool To Mimic Polyethylene Terephthalate Nanoplastic Pollutants: Characterization and Toxicology Assessment. ACS Nano [Internet]. 2018;12:7690–700. Available from: https://pubs.acs.org/doi/10.1021/acsnano.8b01331

3. Maiorano G, Sabella S, Sorce B, Brunetti V, Malvindi MA, Cingolani R, et al. Effects of Cell Culture Media on the Dynamic Formation of Protein−Nanoparticle Complexes and Influence on the Cellular Response. ACS Nano [Internet]. 2010;4:7481–91. Available from: https://pubs.acs.org/doi/10.1021/nn101557e