# Supplementary materials

Modeling and optimization of adsorption conditions using response surface methodology for tetracycline removal by MnFe2O4/MWCNTs

Weigao Zhao1, Chenjie Hao1, Yiping Guo2, Chunfeng Guan1, Hongwei Zhang1, Yimei Tian1, Peng Zhao1*

1Department of Environmental Engineering, School of Environmental Science and Engineering, Tianjin University, Tianjin 300072, China

2School of Environmental and Municipal Engineering, North China University of Water Resources and Electric Power, Zhengzhou 450046, China

Corresponding Author: Peng Zhao: zhp_tj@126.com

Fig. S1. (a) Transmission electron microscopy observation of magnetic carbon nanotubes at 20 nm (Quanta-250, FEI, US); (b) Zeta potential of MWCNTs and MMWCNTs (pH = 2-10); (c) FT-IR of MnFe2O4, MWCNTs and MMWCNTs.

Fig. S2. Effect of adsorption time on TC adsorbent adsorption capacity. Initial TC concentration of 20 mg/L; adsorbent dosage of 12 mg; pH 7.0 ±0.1, reaction temperature of 298.15 K.

Fig. S3. Schematic mechanism of the π-π interactions and cationic-π bonding between MMWCNTs and TC molecules.

Fig. S4. The main components of TC (phenolic hydroxyl group (C-OH); dimethyl amino group (-N(CH3)2); acylamino group (-CONH2); and the keto-enol conjugated double bond system) and the acidity coefficient of each component.

Fig. S5. Residual diagnostic chart of TC adsorption test results: (a) Normal % probability versus internally studentized residuals; (b) Residuals versus predicted values; (c) Residuals versus run number; (d) Plot of model predicted value versus actual experimental value.

Fig. S6. Main effect plots for (a) Dosage; (b) pH and (c) Contact time for the response surface method.

Fig. S7. Interaction plots of dosage, contact time and pH.

Table S1 Optimization methods of various adsorption processes.

Table S2 Current status of BBD-RSM in the optimization of TC adsorption process with different adsorbents.

Table S3 Current status of BBD-RSM in the optimization of MWCNTs adsorption process with different adsorbents.

Table S4 The experimental factors, levels and coded values for TC removal experiment, including 3 factors and 3 response levels.

Table S5 Parameters of kinetic models for the adsorption of TC by MMWCNTs.

Table S6 Statistical analysis of the effectiveness of models for modeling the process of TC adsorption by MnFe2O4/MWCNTs (confidence interval = 95%).

Table S7 Analysis of variance (ANOVA) for TC removal according to the response surface quadratic model (confidence interval: 95%).

Characterization of MMWCNTs

The magnetic multi-walled carbon nanotubes (MMWCNTs) were characterized using a transmission electron microscope (TEM, Tecnai G2 F20 s-Twin, FEI, US) to observe the structure and morphology of the adsorbent material before and after modification. A Zetasizer (Nano ZS90, Malvern Instruments, UK) microprocessor unit was applied to measure the Zeta potential of solutions. A Nicolet NEXUS 670 Fourier transform infrared spectrophotometer was utilized to record the infrared spectra of MMWCNTs from 400 to 4000 cm−1.

Transmission electron microscopy images at 20 nm are shown in Fig. S1 (a), exhibiting that MnFe2O4 had been uniformly attached to the surface of MMWCNTs. The size of MMWCNTs was about 10~50 nm. Zeta potential plots of MWNTs and MMWCNTs (e.g., pre- and post-modification) at pH 2-10 are displayed in Fig. S1 (b). The potential of the two materials declined with increasing pH. The pHzpc of MMWCNTs was 4.5. When the pH was in the range of 3-7, the potential of MWCNTs was greater than that of MMWCNTs, due to the negative charge of MnFe2O4. The Fourier transform infrared spectra of MnFe2O4, MWCNTs and MMWCNTs are shown in Fig. S1 (c), revealing the existence of O-H (1400, 2400, 3500 cm−1) and C=O (1600 cm−1) functional groups, suggesting that oxygen-containing groups (-OH, -COOH) were introduced into the MMWCNTs.

Adsorption kinetics models

The non-linear pseudo-first-order model and non-linear pseudo-second-order model are shown in Equations (1) and (2), respectively (Zhao et al. 2021):

(1)

(2)

where, qe (mg/g) is the equilibrium adsorption capacity of the adsorbent; qt (mg/g) is the adsorption capacity; t (min) is the reaction time; k1 (min-1) is a rate constant for the pseudo-first-order model; k2 (g/(mg min)) is a rate constant for pseudo-second-order model.

The Elovich equation assumes that solid surfaces are energetically heterogeneous as described in Equation (3) (Sen Gupta &Bhattacharyya 2011):

(3)

where, α (mg g-1 min-1) and β (g mg-1) are Elovich constants.

The intracellular diffusion model is described in Equation (4) as follows (Mary Ealias &Saravanakumar 2018):

(4)

where, kd1 (mg g-1 min-1/2) and I1 are intraparticle diffusion constants.

The Bangham model is an application of the Freundlich and Helle kinetic models and is expressed according to Equation (5) as follows (Largitte &Pasquier 2016):

(5)

where, k (min-m) and m are Bangham constants.

Model analysis method

The BBD model generally utilizes the first-order linear model (Equation (6)) or the second-order nonlinear model (Equation (7)) (Zhao et al. 2021).

(6)

(7)

Here, Y indicates the dependent variable; X1, X2, and X3 represent the respective process variables; γ0, γ1, γ2, and γ3 represent the respective linear coefficients; γ12, γ13, and γ23 represent the respective cross product coefficients; and γ11, γ22, and γ33 are the respective quadratic coefficients.

The F-test was employed to determine the statistical significance of each model, with the F-value determined by the sum of the model, the error square and the degree of freedom, as shown in Equation (8). The determinant coefficient (R2) refers to the ratio of the sum of squares of regression of linear regression, to the sum of squares of total residuals, which is a measure used to estimate the goodness of fit of a regression equation, indicating the degree of fitting between the model predicted value and the actual value (calculation shown in Equation (9)). The adjustment coefficient (Radj2) (Equation (10)) was established from the regression equations and used to correct the correlation coefficient value. Residual analysis was used to assess whether the model fit well with the experimental data. The residual referred to the difference between the actual observed data value and the estimated value, which reflects the error when using the regression equation to predict the experimental value (Moon et al. 2013). The F-value for the models and the error values were calculated using Equations (11) and (12), while the R2 for the model was calculated using Equation (13) and the Radj2 for the model was calculated using Equation (14) (values taken from Table S5).

(8)

(9)

(10)

Here, SSmodel is the sum of squares between groups; SSerror is the sum of square error; DF1 and DF2 are the model and residual degrees of freedom; n is the total number of observed values; p is the total number of terms (including constant terms) in the regression equation.

(11)

(12)

(13)

(14)

Residual analysis

The adequacy of the model is critical for the actual experiment and to establish the ideal optimization conditions (Chen et al. 2015). Fig. S5 (a) shows the normal probability plot of the residuals, indicating the variation in normal percentage probability compared to internally studentized residuals (Dalvand et al. 2016). The linear fitting results show that the equation R2 = 0.913, with the plot forming a straight line, indicating that the errors were normally distributed and the model was universally significant. Fig. S5 (b) exhibits a scatterplot with the predicted values for response variable fitting as the horizontal axis, randomly distributed around axis 0. As the predicted value changed, the model error was randomly distributed without any evident trend. Fig. S5 (c) shows a point plot with the order of observed values displayed as the horizontal axis. Each point fluctuated randomly and irregularly on the horizontal axis, indicating that the residual was independent. Fig. S5 (d) exhibits the fitting graph of predicted values and actual values, with R2 (0.966) and Radj2 (0.963) values indicating a high degree of fitting between the estimated value and the experimental results. Therefore, the simulated linear equation could accurately predict the TC removal rate by MMWCNTs.

(c)

(b)

(a)

Fig. S1. (a) Transmission electron microscopy observation of magnetic carbon nanotubes at 20 nm (Quanta-250, FEI, US); (b) Zeta potential of MWCNTs and MMWCNTs (pH = 2-10); (c) FT-IR of MnFe2O4, MWCNTs and MMWCNTs (Zhao et al. 2021).

Fig. S2. Effect of adsorption time on TC adsorbent adsorption capacity. Initial TC concentration of 20 mg/L; adsorbent dosage of 12 mg; pH 7.0 ±0.1, reaction temperature of 298.15 K.

Fig. S3. Schematic mechanism of the π-π interactions and cationic-π bonding between MMWCNTs and TC molecules.

Fig. S4. The main components of TC (phenolic hydroxyl group (C-OH); dimethyl amino group (-N(CH3)2); acylamino group (-CONH2); and the keto-enol conjugated double bond system) and the acidity coefficient of each component.

(b)

(a)

(c)

(d)

Fig. S5. Residual diagnostic chart of TC adsorption test results: (a) Normal % probability versus internally studentized residuals; (b) Residuals versus predicted values; (c) Residuals versus run number; (d) Plot of model predicted value versus actual experimental value.

(a)

(b)

(c)

Fig. S6. Main effect plots for (a) Dosage; (b) pH and (c) Reaction time for the response surface method.

Fig. S7. Interaction plot of dosage, reaction time and pH.

Table S1 Optimization methods of various adsorption processes.

| Methods | Adsorbents | Contaminants | Strength | Weakness | References |
| --- | --- | --- | --- | --- | --- |
| BBD a | Fly ash | Chitosan | A moderate amount of experiment, few data, simple software operation |  | (Mohammed et al. 2020) |
| CCD b | Nanocellulose/Chitosan aerogel | Cr (VI), Co (III) and Cu (II) | Orthogonal rotation design of data | Complex formula | (Shahnaz et al. 2020) |
| FFD c | Solid residue | Methylene blue | Comprehensive data analysis | A large number of experiments required | (Bonetto et al. 2021) |
| PB d | Fe3O4@SiO2 | Melatonin | Simple experiments, few data | Small analog quantity | (Dil et al. 2021) |
| DE e | Chitosan-coated Fe3O4 | Pb (II) | Fast convergence, few control parameters and simple setting, robust optimization results | Programming complexity; Missing parameter | (Rasoulzadeh et al. 2020) |
| Single factor experiments | Magnetic-modified multi-walled carbon nanotubes | Crystal violet, thionine, Janus Green B, and methylene blue | No need for complex software operations, clear and concise experiment design | A large amount of test | (Madrakian et al. 2011) |
| Taguchi | Activated carbon-HKUST-1-MOF | Ternary organic dyes |  | A large amount of test | (Azad et al. 2016) |

Continued Table S1 Optimization methods of various adsorption processes.

| Methods | Adsorbents | Contaminants | Strength | Weakness | References |
| --- | --- | --- | --- | --- | --- |
| ANN f | Water treatment residuals | Disperse Blue 79 | Self-learning function, associative storage function, the ability to find optimal solutions at high speed | A large amount of calculation; The number of hidden neurons is unknown | (Gadekar &Ahammed 2019) |
| GA g | Multi-walled carbon nanotubes and Al2O3 | Co (II) | Self-learning function, associative storage function, the ability to find optimal solutions at high speed | Computational heaviness | (Dehghani et al. 2020) |
| MLPNN h | nZVI | Cr (VI) |  | Slow convergence; Over the installation | (Yu et al. 2013) |
| RBFNN i | Pumice | Cu (II) |  | Training data and hidden neuron requirements | (Turan et al. 2011) |
| ANFIS j | Activated carbon | Red 46 and Cu (II) |  | Large amount of test | (Dolatabadi et al. 2018) |

a BBD—Box-Behnken design;

b CCD—Central composite design;

c FFD—Full factorial design;

d PB—Plackett-Burman;

e DE—Differential evolution;

f ANN—Artificial Neural Network;

g GA—Genetic Algorithm;

h MLPNN—Multi-Layer Perceptron neural network;

i RBFNN—Radial basis function neural network;

j ANFIS—Adaptive network-based fuzzy inference system.

Table S2 Current status of BBD-RSM in the optimization of TC adsorption process with different adsorbents.

| Adsorbents | Optimized conditions | Response | Optimal value | References |
| --- | --- | --- | --- | --- |
| Zr doped SrAl2O4 | Zr loading amount, solution pH and contact time | Adsorption capacity | 75.19 mg g-1 | (Demircivi &Bugdayci 2019) |
| Aminated graphitic carbonaceous | TC concentration, dosage, contact time and pH | Removal rate | 100.00% | (Haghighat et al. 2020) |
| SiO2 NPs | TC concentration, dosage and contact time | Adsorption capacity | 552.48 mg g-1 | (El Messaoudi et al. 2022) |
| Porous carbon | Pyrolysis temperature, pyrolysis time and mass ratio | Adsorption capacity | 515.17 mg g-1 | (Gu et al. 2021) |

Table S3 Current status of BBD-RSM in the optimization of MWCNTs adsorption process with different adsorbents.

| Adsorbents | Optimized conditions | Response | Optimal value | References |
| --- | --- | --- | --- | --- |
| 4-Nitrophenol | pH, CA/MWCNTs, and temperature | Adsorption capacity | 168.40 mg g-1 | (Ashrafi et al. 2021) |
| Pb (II) | pH, feed concentration and contact time | Adsorption capacity | 79.69 mg g-1 | (Islam et al. 2021) |
| Diclofenac and naproxen | Dosage, temperature and pH | Removal rate | 19.00% and 54.00% | (Huaccallo-Aguilar et al. 2021) |
| Zn (II) | Dosage, pH; contact time, and contact speed | Removal rate | 99.50% | (Aliyu 2019) |
| Magenta dye | laccase-ACNTs composite, Magenta dye concentration, and reaction time | Removal rate | 95.00% | (Thiyagarajan et al. 2020) |

Continued Table S3 Current status of BBD-RSM in the optimization of MWCNTs adsorption process with different adsorbents.

| Adsorbents | Optimized conditions | Response | Optimal value | References |
| --- | --- | --- | --- | --- |
| Direct Green 26 | Dosage, solution pH | Removal rate | 95.86% | (Bahare &Fariba 2020) |
| Pb（II） | pH, feed concentration and contact time | Adsorption capacity | 79.69 mg g-1 | (Islam et al. 2021) |
| As (III) | Concentration, pH and sorbent dose | Removal rate | 90.00% | (Tomaszewska et al. 2018) |
| Rhodamine B | Dosage, pH, time and TX-100 concentration | Removal rate | 94.24% | (Safa &Osaghi 2021) |
| Methylene blue | Concentration, dosage, and pH | Degradation rate | 99.95% | (Tayeb et al. 2020) |

Table S4 The experimental factors, levels and coded values for TC removal experiment, including three factors and three response levels.

| Independent variable | Symbol | Coded variable response level |  |  |
| --- | --- | --- | --- | --- |
|  | Coded | Low (-1) | Central (0) | High (+1) |
| Dosage (mg) | A | 6 | 9 | 12 |
| Reaction time (min) | B | 120 | 300 | 480 |
| pH | C | 4 | 5 | 6 |

Table S5. Parameters of kinetic models for the adsorption of TC by MMWCNTs.

| Type | Parameter | Value | qe (mg/g) | R2 |
| --- | --- | --- | --- | --- |
| Pseudo-first-order model | k1 (min-1) | 0.050 | 80.57 | 0.944 |
| Pseudo-second-order model | k2 (g/(mg·min)) | 0.001 | 84.13 | 0.975 |
| Elovich | α (mg g−1 min−1) | 5057.379 | 87.05 | 0.729 |
|  | β (g mg−1) | 0.161 |  |  |
| Intramolecular diffusion | kd1 (mg g-1 min -1/2) | 0.542 | 87.82 | 0.412 |
|  | I1 | 66.830 |  |  |
| Bangham | k (min-m) | 49.917 | 87.02 | 0.668 |
|  | m | 13.152 |  |  |

Table S6. Statistical analysis of the effectiveness of models for modeling the process of TC adsorption by MnFe2O4/MWCNTs (confidence interval = 95%).

| Source | F-value | P-value (Prob > F) | F-value (lack of fit) | p-value (lack of fit) | Std. Dev. | R-squared | Adjusted R-squared |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Linear | 0.20 | 0.897 | 15.26 | 0.009 | 8.36 | 0.043 | -0.177 | Aliased |
| 2FI | 4.87 | 0.024 | 8.91 | 0.026 | 6.08 | 0.611 | 0.378 | Aliased |
| Quadratic | 22.10 | 0.0002 | 0.34 | 0.798 | 2.15 | 0.966 | 0.922 | Suggested |
| Cubic | 0.34 | 0.798 | - | - | 2.54 | 0.973 | 0.892 | Aliased |

Table S7. Analysis of variance (ANOVA) for TC removal according to the response surface quadratic model (confidence interval: 95%).

| Source | Sum of Squares | DF | Mean Square | F-value | P-value (Prob > F) | Significance |
| --- | --- | --- | --- | --- | --- | --- |
| Model | 918.36 | 9 | 102.04 | 22.10 | 0.0002 | significant |
| A-Dosage | 18.97 | 1 | 18.97 | 4.11 | 0.082 | - |
| B-Time | 0.33 | 1 | 0.33 | 0.07 | 0.796 | - |
| C-pH | 21.95 | 1 | 21.95 | 4.75 | 0.066 | - |
| AB | 69.56 | 1 | 69.56 | 15.07 | 0.006 | - |
| AC | 37.88 | 1 | 37.88 | 8.21 | 0.024 | - |
| BC | 432.22 | 1 | 432.22 | 93.62 | 0.000 | - |
| A2 | 22.11 | 1 | 22.11 | 4.79 | 0.065 | - |
| B2 | 0.43 | 1 | 0.43 | 0.09 | 0.768 | - |
| C2 | 321.32 | 1 | 321.32 | 69.60 | 0.000 | - |
| Residual | 32.32 | 7 | 4.62 | - | - | - |
| Lack of fit | 6.58 | 3 | 2.20 | 0.34 | 0.798 | not significant |
| Pure error | 25.73 | 4 | 6.43 | - | - | - |
| Total | 950.67 | 16 | - | - | - | - |

References:

Aliyu A (2019) Synthesis, electron microscopy properties and adsorption studies of Zinc (II) ions (Zn2+) onto as-prepared Carbon Nanotubes (CNTs) using Box-Behnken Design (BBD). Sci Afr 3: 1-10.

Ashrafi SD, Safari GH, Sharafi K, Kamani H, Jaafari J (2021) Adsorption of 4-Nitrophenol on calcium alginate-multiwall carbon nanotube beads: Modeling, kinetics, equilibriums and reusability studies. Int J Biol Macromol 185: 66-76.

Azad FN, Ghaedi M, Dashtian K, Hajati S, Pezeshkpour V (2016) Ultrasonically assisted hydrothermal synthesis of activated carbon-HKUST-1-MOF hybrid for efficient simultaneous ultrasound-assisted removal of ternary organic dyes and antibacterial investigation: Taguchi optimization. Ultrason Sonochem 31: 383-393.

Bahare O, Fariba S (2020) Cloud Point Extraction in Presence of Multi-walled Carbon Nanotubes for Removal of Direct Green 26 from Aqueous Solutions: Optimization by Box-Behnken Design and Desirability Functions. J Anal Chem 75: 802-811.

Bonetto LR, Crespo JS, Guegan R, Esteves VI, Giovanela M (2021) Removal of methylene blue from aqueous solutions using a solid residue of the apple juice industry: Full factorial design, equilibrium, thermodynamics and kinetics aspects. J Mol Struct 1224: 1-14.

Chen F, Zu Y, Yang L (2015) A novel approach for isolation of essential oil from fresh leaves of Magnolia sieboldii using microwave-assisted simultaneous distillation and extraction. Sep Purif Technol 154: 271-280.

Dalvand A, Nabizadeh R, Reza Ganjali M, Khoobi M, Nazmara S, Hossein Mahvi A (2016) Modeling of Reactive Blue 19 azo dye removal from colored textile wastewater using L-arginine-functionalized Fe3O4 nanoparticles: Optimization, reusability, kinetic and equilibrium studies. J Magn Magn Mater 404: 179-189.

Dehghani MH, Yetilmezsoy K, Salari M, Heidarinejad Z, Yousefi M, Sillanpaa M (2020) Adsorptive removal of cobalt(II) from aqueous solutions using multi-walled carbon nanotubes and gamma-alumina as novel adsorbents: Modelling and optimization based on response surface methodology and artificial neural network. J Mol Liq 299: 1-14.

Demircivi P, Bugdayci M (2019) Synthesis and thermodynamic simulation of Zr Doped SrAl2O4 ceramic powders: enhanced adsorptive properties for antibiotic tetracycline. Mater Res Express 6(8): 1-12.

Dil EA, Doustimotlagh AH, Javadian H, Asfaram A, Ghaedi M (2021) Nano-sized Fe3O4@SiO2-molecular imprinted polymer as a sorbent for dispersive solid-phase microextraction of melatonin in the methanolic extract of Portulaca oleracea, biological, and water samples. Talanta 221: 1-10.

Dolatabadi M, Mehrabpour M, Esfandyari M, Alidadi H, Davoudi M (2018) Modeling of simultaneous adsorption of dye and metal ion by sawdust from aqueous solution using of ANN and ANFIS. Chemom Intell Lab Syst 181: 72-78.

El Messaoudi N, El Khomri M, Ablouh E-H, Bouich A, Lacherai A, Jada A, Lima EC, Sher F (2022) Biosynthesis of SiO2 nanoparticles using extract of Nerium oleander leaves for the removal of tetracycline antibiotic. Chemosphere 287: 1-10.

Gadekar MR, Ahammed MM (2019) Modelling dye removal by adsorption onto water treatment residuals using combined response surface methodology-artificial neural network approach. J Environ Manage 231: 241-248.

Gu S, Zhang D, Gao Y, Qi R, Chen W, Xu Z (2021) Fabrication of porous carbon derived from cotton/polyester waste mixed with oyster shells: Pore-forming process and application for tetracycline removal. Chemosphere 270: 1-12.

Haghighat GA, Saghi MH, Anastopoulos I, Javid A, Roudbari A, Talebi SS, Ghadiri SK, Giannakoudakis DA, Shams M (2020) Aminated graphitic carbon derived from corn stover biomass as adsorbent against antibiotic tetracycline: Optimizing the physicochemical parameters. J Mol Liq 313: 1-9.

Huaccallo-Aguilar Y, Álvarez-Torrellas S, Martínez-Nieves J, Delgado-Adámez J, Gil MV, Ovejero G, García J (2021) Magnetite-Based Catalyst in the Catalytic Wet Peroxide Oxidation for Different Aqueous Matrices Spiked with Naproxen–Diclofenac Mixture. Catal 11: 514.

Islam A, Chauhan A, Javed H, Rais S, Ahmad I (2021) Magnetic Carbon Nanotubes-Silica Binary Composite for Effective Pb(II) Sequestration from Industrial Effluents: Multivariate Process Optimization. Clean: Soil Air Water 49(8):1-10.

Largitte L, Pasquier R (2016) A review of the kinetics adsorption models and their application to the adsorption of lead by an activated carbon. Chem Eng Res Des 109: 495-504.

Madrakian T, Afkhami A, Ahmadi M, Bagheri H (2011) Removal of some cationic dyes from aqueous solutions using magnetic-modified multi-walled carbon nanotubes. J Hazard Mater 196: 109-114.

Mary Ealias A, Saravanakumar MP (2018) Facile synthesis and characterisation of AlNs using Protein Rich Solution extracted from sewage sludge and its application for ultrasonic assisted dye adsorption: Isotherms, kinetics, mechanism and RSM design. J Environ Manage 206: 215-227.

Mohammed IA, Jawad AH, Abdulhameed AS, Mastuli MS (2020) Physicochemical modification of chitosan with fly ash and tripolyphosphate for removal of reactive red 120 dye: Statistical optimization and mechanism study. Int J Biol Macromol 161: 503-513.

Moon C, Singh R, Chaganti SR, Lalman JA (2013) Modeling sulfate removal by inhibited mesophilic mixed anaerobic communities using a statistical approach. Water Res 47: 2341-2351.

Rasoulzadeh H, Dehghani MH, Mohammadi AS, Karri RR, Nabizadeh R, Nazmara S, Kim K-H, Sahu JN (2020) Parametric modelling of Pb(II) adsorption onto chitosan-coated Fe3O4 particles through RSM and DE hybrid evolutionary optimization framework. J Mol Liq 297: 111893.

Safa F, Osaghi B (2021) Adsorption onto MWCNTs Coupled with Cloud Point Extraction for Dye Removal from Aqueous Solutions: Optimization by Experimental Design. Comb. Chem. High Throughput Screening 24: 246-258.

Sen Gupta S, Bhattacharyya KG (2011) Kinetics of adsorption of metal ions on inorganic materials: A review Adv Colloid Interface Sci 162: 39-58.

Shahnaz T, Sharma V, Subbiah S, Narayanasamy S (2020) Multivariate optimisation of Cr (VI), Co (III) and Cu (II) adsorption onto nanobentonite incorporated nanocellulose/chitosan aerogel using response surface methodology. J Water Process Eng 36: 1-12.

Tayeb AM, Hussein DS, Farouq R (2020) Optimization of photocatalytic degradation of methylene blue dye using titanate nanotube. J Nanophotonics 14(2):1-11.

Thiyagarajan P, Selvam K, Sudhakar C, Selvankumar T (2020) Enhancement of Adsorption of Magenta Dye by Immobilized Laccase on Functionalized Biosynthesized Activated Carbon Nanotubes. Water Air Soil Pollut 231: 364.

Tomaszewska J, Smektala P, Zglobicka I, Michalski J, Kurzydlowski KJ, Krzeminski P, Escudero-Onate C (2018) Non-woven polypropylene fabric modified with carbon nanotubes and decorated with nanoakaganeite for arsenite removal. Int J Environ Sci Technol 15: 1831-1842.

Turan NG, Mesci B, Ozgonenel O (2011) The use of artificial neural networks (ANN) for modeling of adsorption of Cu(II) from industrial leachate by pumice. Chem Eng J 171: 1091-1097.

Yu R-F, Lin C-H, Chen H-W, Cheng W-P, Kao M-C (2013) Possible control approaches of the Electro-Fenton process for textile wastewater treatment using on-line monitoring of DO and ORP. Chem Eng J 218: 341-349.

Zhao W, Tian Y, Chu X, Cui L, Zhang H, Li M, Zhao P (2021) Preparation and characteristics of a magnetic carbon nanotube adsorbent: Its efficient adsorption and recoverable performances. Sep Purif Technol 257: 117917.