Measurements, emission characteristics and control methods of fire effluents from tunnel asphalt pavement during fire: A review

Wenzhen Wang 1, Aiqin Shen 1,2,*, Lusheng Wang 1, and Hongchang Liu 1

1 School of Highway, Chang’an University, Xi’an, Shaanxi 710064, China

2 Key Laboratory for Special Area Highway Engineering of Ministry of Education, Chang’an University, Xi’an 710064, China

* Corresponding author: Aiqin Shen

Address: Middle Section of Nan Erhuan Road, Xi’an City, Shaanxi Province, China, 710064

Telephone number: +86 13709262063

E-mail: 1667117390@qq.com

SUPPLEMENTARY DATA

Appendix A

The species of volatiles released from bitumen and bituminous mixtures obtained from FTIR test see Table A1.

Table A1 FTIR peak wavenumbers and corresponding gas species.

| FTIR peak wavenumbers (cm-1) | Corresponding gas | Causes | Reference |
| --- | --- | --- | --- |
| 600−400 | H2O | The decomposition reaction of Ca(OH)2 in hydrated lime modified binder | (Zhu et al., 2018) |
| 615−737 | CO2 | The deformation vibration or the antisymmetric stretching of CO2 | (Shi et al., 2017a; Shi et al., 2017b; Xia et al., 2020, 2021a; Xu et al., 2018) |
| 770−630 | Aromatic compounds | The separation of aromatic compounds | (Zhu et al., 2018) |
| 790−630 | CO2 | The fracture and reforming of carboxyl (−COOH) and carbonyl groups (C=O) | (Zhu et al., 2018) |
| 667 | CO2 | The asymmetrical stretching of CO2 | (Xu et al., 2013) |
| 669 | CO2 | The bending vibration absorption peak | (Hao et al., 2017; Li et al., 2018; Xu and Huang, 2010a, b; Xu et al., 2014) |
| 730, 690 | Monosubstituted aromatic hydrocarbons |  | (Hao et al., 2017) |
| 700−900 |  | The styrene part of the styrene–butadiene–styrene (SBS) | (Xu and Huang, 2010a) |
| 900−700 |  | The out−of−phase bending vibration of the aromatic C−H | (Hao et al., 2017) |
| 747 | CO2 | The breakage of both −OH bonds and side chains of aliphatic hydrocarbons | (Yang et al., 2020) |
| 910, 911 | Unsaturated alkenes or aliphatic olefins (R−CH=CH2) |  | (Hao et al., 2017; Xu et al., 2013) |
| 921 |  | The out−of−plane bending vibration of O−H | (Xu et al., 2018) |
| 950 | Olefin, ethylene or alkenes and aromatic hydrocarbons | C−H out−of−plane deformation vibration | (Hao et al., 2017; Shi et al., 2017b; Xu et al., 2018) |
| 950−1150 | Aliphatic hydrocarbons |  | (Qian et al., 2015) |
| 960−1085 | Methanol | The reforming of free hydroxyl groups and C−O groups | (Pei et al., 2014; Xu and Huang, 2010a) |
| 990 | Unsaturated alkenes or R−CH=CH2 |  | (Hao et al., 2017; Xu et al., 2013) |
| 1032 | Sulfoxides | The stretching of the sulfur=oxygen (S=O) bond | (Hao et al., 2017) |
| 1061 | Ether | The C−O−C stretching vibration of ether | (Shi et al., 2017b) |
| 1074−1209 | Alcohols | The stretching vibration of C−O | (Hao et al., 2017) |
| 1107 | Alcohols |  | (Shi et al., 2017b) |
| 1167 | Phenols |  | (Shi et al., 2017a; Shi et al., 2017b) |
| 1173 | Formic acid | The fragmentations of hydroxyl methylene groups | (Xu et al., 2014) |
| 2100−1200 | H2O | The decomposition reaction of Ca(OH)2 in hydrated lime modified binder | (Zhu et al., 2018) |
| 1210 | Alcohols | The C−O stretching vibration peak | (Shi et al., 2017b) |
| 1250−1500 | Aliphatic hydrocarbons |  | (Qian et al., 2015) |
| 1251 | Ethers | C−O stretching vibration | (Yang et al., 2020) |
| 1267 | Hydrogen sulfide | Thermal decomposition of thioethers | (Hao et al., 2017) |
| 1270 |  | The C−O stretching vibration of ester | (Shi et al., 2017b) |
| 1287 | Phenols and carboxylic acids or NO2 |  | (Shi et al., 2017a; Shi et al., 2017b) |
| 1290−1410 | SO2 | stretching vibration of S=O | (Xia et al., 2020) |
| 1300−1400 | SO2 | the combustion of sulfur components in asphalt, the stretching vibration of S=O | (Zhu et al., 2018) |
| 1300−1400 | Alcohols and phenols | the vibration of O−H bond of alcohols and phenolic | (Pei et al., 2014; Xu and Huang, 2010a; Xu et al., 2014) |
| 1450−1300 | Methyl (−CH3) and methylene (−CH2−) |  | (Xu et al., 2018) |
| 1500−1300 | −CH3 and −CH2− or Hydrocarbons |  | (Shi et al., 2017b; Yang et al., 2020) |
| 1500−1300 | Alkanes | The symmetric and anti−symmetric stretching vibration of −CH2− | (Shi et al., 2017a) |
| 1300−1500 | Phenols, alcohols, etc. | The stretching and bending modes of saturated aliphatic hydrocarbons | (Pei et al., 2014; Xia et al., 2021a; Xu and Huang, 2010a) |
| 1303 | Methane (CH4) |  | (Hao et al., 2017) |
| 1339 | SO2 | The stretching vibration of S=O | (Xia et al., 2021a) |
| 1360 | H2O |  | (Shi et al., 2017b) |
| 1475−1360 | Hydrocarbons |  | (Shi et al., 2017a) |
| 1548−1370 | Hydrocarbons |  | (Xu et al., 2014) |
| 1374 | SO2 | The stretching vibration of S=O bond | (Pei et al., 2014; Xu and Huang, 2010a, b; Xu et al., 2013) |
| 1375 | NO2 |  | (Xu et al., 2014) |
| 1376 | SO2 | S=O bond stretching vibration | (Hao et al., 2017; Yang et al., 2020) |
| 1376, 1457 | Aliphatic hydrocarbons |  | (Hao et al., 2017) |
| 1377 |  | The bending vibration of −CH2− and −CH3 | (Hao et al., 2017) |
| 1388 | NO2 |  | (Xu et al., 2014) |
| 1450 | SO2 |  | (Shi et al., 2017b; Xu et al., 2018) |
| 1458 | Aromatic compounds | The bending vibration of −CH2− and −CH3 | (Hao et al., 2017; Xu et al., 2014) |
| 1460 |  | The asymmetric deformation vibration of the C−H bond in −CH3 | (Pei et al., 2014; Xu et al., 2014) |
| 1462 | Hydrocarbon chain fragments |  | (Xu et al., 2013) |
| 1465 | C−CH3 bands | The small aromatic ring clusters with alkyl tails in aromatic substitution | (Xu and Huang, 2010a) |
| 1475 | SO2 | The absorption peak of stretching vibration of S=O | (Shi et al., 2017b) |
| 1600−1500 | Benzene rings or NO2 | The stretching vibrations of aromatic ring skeletons | (Shi et al., 2017b; Xu et al., 2018) |
| 1507 | Hydrocarbon fragments |  | (Xia et al., 2021a) |
| 1508 | Aromatic compounds | The important source of smoke toxicity | (Xu and Huang, 2010a, b; Xu et al., 2013) |
| 1511 | NO2 |  | (Xu et al., 2014) |
| 1795−1524 | Aromatic C=C |  | (Hao et al., 2017) |
| 1541 | SO2 | The S=O bond stretching vibration | (Xu et al., 2014) |
| 1545 | SO2 | The S=O bond stretching vibration | (Shi et al., 2017a; Shi et al., 2017b) |
| 1550 | Aromatic hydrocarbons | The stretching vibration of aromatic ring | (Shi et al., 2017b) |
| 1630−1550 | NO2 | The combustion reaction temperature is relatively low | (Zhu et al., 2018) |
| 1600 | Olefin or aromatic compounds | The stretching of aromatic C−C bond and the substitution for the aromatic rings | (Shi et al., 2017b; Xu and Huang, 2010a; Xu et al., 2014) |
| 1601 |  | The stretching vibration of the aromatic C=C | (Hao et al., 2017) |
| 1604, 1606 | Aromatic ring skeleton | The stretching vibration of the C=C bond | (Hao et al., 2017) |
| 1620 |  | The stretching vibration of the aromatic C=C | (Hao et al., 2017) |
| 1642 | Unsaturated alkenes |  | (Xu et al., 2014; Xu et al., 2013) |
| 1647 | R−CH=CH2 |  | (Hao et al., 2017) |
| 1800−1650 | − | The stretching vibrations of C=O bonds | (Shi et al., 2017b) |
| 1680−1720 | Oxygen−type compounds |  | (Xu and Huang, 2010a) |
| 1700−1850 | CO2 |  | (Qian et al., 2015) |
| 1708 |  | The stretching vibration of the C=O groups | (Hao et al., 2017) |
| 1716 |  | The transmittance of stretching vibration of C−O in hydroxy methylene groups | (Xu and Huang, 2010a, b) |
| 1720 | Acetaldehyde, and other aldehydes | The vibration of C=O | (Zhu et al., 2018) |
| 1740−1720 | Oxygen−containing compounds | The stretching vibration of C=O | (Xu et al., 2018) |
| 1729 | Hydroxyl methylene groups | The stretching vibration peak of C=O | (Shi et al., 2017a; Shi et al., 2017b) |
| 1735 | − | The stretching vibrations of C=O bonds | (Xu et al., 2018) |
| 1737 | Aldehyde compounds |  | (Li et al., 2018) |
| 1745 | Formic acid | The fragmentations of hydroxyl methylene groups | (Xu and Huang, 2010a; Xu et al., 2014) |
| 1950−1750 | NO | The combustion reaction temperature is relatively low | (Zhu et al., 2018) |
| 1751 | Carboxyl (esters) | C=O bond stretching vibration | (Yang et al., 2020) |
| 1950−1800 | NO |  | (Shi et al., 2017b) |
| 2108 | CO | The bond breakage of C=O and C−O−C | (Shi et al., 2017b) |
| 2109 | CO |  | (Li et al., 2018) |
| 2164 | CO | The break of C−O−C and C=O | (Xu and Huang, 2010b; Xu et al., 2013) |
| 2170 | CO |  | (Xu et al., 2014) |
| 2172, 2117 | CO |  | (Hao et al., 2017) |
| 2181 | CO | The bond breakage between C=O and C−O−C | (Shi et al., 2017a; Shi et al., 2017b) |
| 2200−2050 | CO |  | (Zhu et al., 2018) |
| 2060−2240 | CO | The bond breakage of C=O and C–O–C | (Pei et al., 2014; Xia et al., 2020, 2021a; Xu and Huang, 2010a) |
| 2200−2100 | CO | The bond breakage of C=O and C−O−C | (Xu et al., 2018) |
| 2400−2230 | CO2 | The fracture and reforming of −COOH and C=O groups | (Zhu et al., 2018) |
| 2240−2400 | CO2 | The cracking and reforming of carbonyl and carboxyl groups | (Shi et al., 2017a; Shi et al., 2017b; Xia et al., 2020, 2021a; Xu and Huang, 2010a; Xu et al., 2014; Xu et al., 2018) |
| 2250−2300 | CO |  | (Qian et al., 2015) |
| 2251 | CO | The breaking of C—O—C and C=O bonds | (Yang et al., 2020) |
| 2300−2400 | CO2 |  | (Qian et al., 2015) |
| 2357 | CO2 | The asymmetrical stretching vibration absorption peak | (Li et al., 2018) |
| 2359 | CO2 | The decarboxylation reaction | (Hao et al., 2017) |
| 2360 | CO2 | The cracking and restructuring of carbonyl and carboxyl | (Pei et al., 2014; Xu and Huang, 2010a, b; Xu et al., 2013) |
| 2361 | CO2 | The deacidification reaction of the −COOH functional groups | (Yang et al., 2020) |
| 2675−3115 |  | The stretching and flexural vibrations of saturated aliphatic hydrocarbon | (Pei et al., 2014; Xu and Huang, 2010a) |
| 3000−2700 | Aldehydes |  | (Shi et al., 2017b; Xu et al., 2018) |
| 2710−3140 | Methanol or low molecular weight chain−alkanes | The recombination of the free hydroxyl and C−O bond | (Pei et al., 2014; Xu and Huang, 2010a; Xu et al., 2014; Xu et al., 2013) |
| 2726 | Aldehydes | Two C−H stretching vibration peaks | (Shi et al., 2017b) |
| 2750 | Aldehydes | The stretching vibration of C–H | (Yang et al., 2020) |
| 3000−2800 | Methane or alkanes | The symmetric and antisymmetric stretching vibration of −CH3 and −CH2− | (Shi et al., 2017a; Shi et al., 2017b; Xu et al., 2018) |
| 3050−2800 | Aliphatic and aromatic compounds | The pyrolysis of the light oil components (saturates, aromatics and resin) | (Zhu et al., 2018) |
| 2800−3150 | Aliphatic hydrocarbons |  | (Qian et al., 2015) |
| 3211−2802 | Hydrocarbons |  | (Xu et al., 2014) |
| 2820 | Formaldehyde and other aldehydes | The vibration of C–H | (Zhu et al., 2018) |
| 2853 | Hydrocarbon chain fragments | The symmetrical stretching of −CH2− | (Hao et al., 2017; Xu et al., 2014; Xu et al., 2013) |
| 2860 |  | The symmetric stretching vibration of −CH3 | (Li et al., 2018) |
| 2900 | Benzene or phenol compounds with hydrocarbons | The stretching vibration of C–H in CH2 or CH3 | (Zhu et al., 2018) |
| 2926 | Hydrocarbon chain fragments | The asymmetric stretching vibration of C−H in −CH2− | (Hao et al., 2017; Pei et al., 2014; Xu and Huang, 2010a, b; Xu et al., 2014; Xu et al., 2013) |
| 2930 | Low−molecular−weight alkanes | The asymmetric stretching vibration absorption of −CH2− | (Li et al., 2018; Yang et al., 2020) |
| 2933 | Low molecular weights chain−alkanes | The asymmetric stretching of −CH2− | (Xia et al., 2021a) |
| 2958, 2957 | Aliphatic hydrocarbons |  | (Hao et al., 2017) |
| 2967 | CH4 | The asymmetric stretching vibration absorption of −CH3 | (Li et al., 2018; Xu and Huang, 2010a) |
| 2968 | CH4 | The cracking of methoxyl (−O−CH3) and the breaking of −CH2− | (Xu et al., 2014) |
| 2990 | Tetrahydrofuran | C−H stretching in CH2 or CH3 | (Xu and Huang, 2010a) |
| 3000 | −CH3 | The decomposition of aliphatic hydrocarbon and aromatic alkyl side chain | (Zhu et al., 2018) |
| 3100−3000 | Olefin or short−chain alkanes | C−H stretching vibration of unsaturated hydrocarbons | (Shi et al., 2017b; Xu et al., 2018) |
| 3014 | CH4 | The cracking of −O−CH3 and the breaking of −CH2− | (Hao et al., 2017; Pei et al., 2014; Xu and Huang, 2010b; Xu et al., 2013) |
| 3015 | CH4 |  | (Li et al., 2018; Xu et al., 2018) |
| 3017 | CH4 | The breakage of −CH2− and −O−CH3 | (Shi et al., 2017b; Xia et al., 2020, 2021a; Xu et al., 2018) |
| 3030 | Unsaturated polycyclic aromatic hydrocarbons | The stretching vibration of C–H in unsaturated polycyclic aromatic hydrocarbons | (Zhu et al., 2018) |
| 3034 | Aromatic ring | The stretching vibration of the C−H bond | (Hao et al., 2017) |
| 3050 | Aromatic compounds | The important source of toxicity | (Xu et al., 2014) |
| 3058 |  | The stretching vibration of aromatic C−H | (Hao et al., 2017) |
| 3063 | Aromatic ring | The stretching vibration of the C−H bond | (Hao et al., 2017) |
| 3078 | Aromatic compounds | The important source of smoke toxicity | (Xu and Huang, 2010a, b; Xu et al., 2013) |
| 3080 | Unsaturated alkenes |  | (Xu et al., 2014; Xu et al., 2013) |
| 3081 | R−CH=CH2 |  | (Hao et al., 2017) |
| 3211 | Aromatics |  | (Xu et al., 2014) |
| 3400 |  | The stretching vibration of –OH in alcohols, phenols and carboxylic acids | (Shi et al., 2017b) |
| 3400−4000 | H2O | The stretching vibration of O−H bond | (Qian et al., 2015; Xu et al., 2014; Xu et al., 2013; Zhu et al., 2018) |
| 3443 |  | The stretching vibration of O−H | (Hao et al., 2017) |
| 3500 |  | The stretching vibration of the O−H bond | (Pei et al., 2014) |
| 3500−3775 | H2O | The stretching vibration of the O−H bond | (Li et al., 2018) |
| 3500−4000 | H2O | The dehydration reaction of hydroxyl functional groups | (Pei et al., 2014; Shi et al., 2017a; Shi et al., 2017b; Xia et al., 2020, 2021a; Xu and Huang, 2010a; Xu et al., 2018) |
| 3594, 3735 | H2O | The stretching of O–H bond | (Xu and Huang, 2010b) |
| 3741, 3750 | H2O | The bending vibration of O–H bonds | (Yang et al., 2020) |

The main identified volatile constituents of different bitumen under the combustion conditions see Table A2.

Table A2 Main identified volatile constituents during the combustion of different bitumen.

| Reference | Sample |  | Volatile constituents |
| --- | --- | --- | --- |
| Xia et al. (2021a) | Bitumen |  | H2O (18), H2S (34), C3H6 (42), C2H2O (42), CH2N2 (42), CO2 (44), C2H4O (44), C3H8(44), N2O (44), CH2O2 (46), NO2 (46), CH4S (48), C4H2 (50), C3H8O (60), C2H8N2 (60), C2H4O2 (60), C2H4S (60), SO2 (64), C6H6 (78), C4H2N2 (78), C2H6OS (78) and CH6N2O2 (78) |
|  | CFR bitumen |  | H2O (18), C2H3N (41), C3H6 (42), C2H2O (42), CH2O2 (46), NO2 (46), CH4S (48), C4H4 (52), C4H10 (58), C2H2O2 (58) and SO2 (64) |
| Shi et al. (2017b) | Saturates at 349 ℃ |  | CO2, H2O, low−molecular weight hydrocarbons, CO, alcohol, a small number of aldehydes and ethers, a trace number of olefins, esters, ketones, etc. |
|  | Saturates at 539 ℃ |  | CO2, H2O, a small number of short alkanes, alcohol, CO, esters, ketones, etc. |
|  | Aromatics at 400 ℃ |  | CO2, H2O, short alkanes, CO, a small number of alkenes, aromatic hydrocarbons, alcohols, aldehydes and phenols. It may also contain ether, esters, ketones, etc. |
|  | Aromatics at 600 ℃ |  | CO2, H2O, a small number of CO, NO, NO2, nitro compounds, SO2, phenols, etc. |
|  | Resins at 457 ℃ |  | CO2, H2O, short alkanes, methane, CO, NO, NO2, nitro compounds, alkenes, aromatic hydrocarbons, aldehydes and phenols. |
|  | Resins at 590 ℃ |  | CO2, H2O, CO, NO, NO2, SO2, nitro compounds, phenols, carboxylic acid and so on. |
|  | Asphaltenes at 451 ℃ |  | CO2, H2O, CO, NO, NO2, nitro compounds, short alkanes, CH4, alkenes, aromatic hydrocarbons, aldehydes and phenols. |
|  | Asphaltenes at 563 ℃ |  | CO2, H2O, CO, NO, NO2, SO2, nitro compounds, phenols, carboxylic acid and so on. |
| Xia et al. (2019a) | Saturates | Stage 1 | H2O (18), CO (28), C2H4 (28), C2H6 (30), CH2O (30), C3H6 (42), C2H2O (42), CO2 (44), C2H4O (44), C3H8 (44), C4H2 (50), C4H8 (56), C3H4O (56), C3H6O (58), C4H10 (58), C2H2O2 (58), C3H8O (60), and C2H4O2 (60) |
|  |  | Stage 2 | CO2 (44), C2H4O (44), C3H8 (44), C3H8O (60), and C2H4O2 (60) |
|  | Aromatics | Stage 1 | CH4(16), H2O (18), CO (28), C2H4 (28), CH4O (32), H2O2 (34), C3H4 (40), CO2 (44), C2H4O (44), C3H8 (44), C3H8O (60), C2H4O2 (60), C2H6O2 (62) |
|  |  | Stage 2 | CO2 (44), C2H4O (44), C3H8 (44), C3H8O (60), C2H4O2 (60), C2H6O2 (62) |
|  | Resins | Stage 1 | H2O (18), CO (28), C2H4 (28), CH4O (32), N2H4 (32), H2S (34), C3H4 (40), C3H8 (44), N2O (44), CO2 (44), and C2H4O (44), S2 (64), and SO2 (64) |
|  |  | Stage 2 | H2O (18), CO2 (44), CH2O2 (44), C2H4O (44), C3H8 (44), C2H6O (46), CH2O2 (46), NO2 (46), SO2 (64), S2 (64), C5H3NO (93), and C6H7N (93) |
|  | Asphaltenes | Stage 1 | H2O (18), CO (28), C2H4 (28), C2H6 (30), CH2O (30), NO (30), CH4O (32), N2H4 (32), CH3CN (41), C3H8 (44), CO2 (44), C2H4O (44), C2H6O (46), CH2O2 (46), NO2 (46), CH4S (48), SO (48), S2 (64), SO2 (64), C4H4O (68), C4H8O (71), and C6H6 (78) |
|  |  | Stage 2 | H2O (18), CO2 (44), C2H4O (44), C3H8 (44), CH4S (48), SO (48), SO2 (64), S2 (64), and C10H8 (128) |
| Zhao et al. (2015) | Saturates | Peak 1 | H2O, CO2, C, alcohol, ethers alkene, acetone, butane |
|  |  | Peak 2 | CO2, C, alcohol |
|  | Aromatics | Peak 1 | H2O, CO2, C, SO2, C3H5, methanol, ethers, alkenes, acetone |
|  |  | Peak 2 | CO2, C, SO2, methanol, C5H6, diacetylene |
|  | Resins | Peak 1 | H2O, CO2, C, SO2, C3H5, methanol, ethers, alkenes, acetone |
|  |  | Peak 2 | CO2, C, SO2, methanol, C5H6, diacetylene |
|  | Asphaltenes | Peak 1 | H2O, CO2, C, C3H5, C3H6 |
|  |  | Peak 2 | CO2, C, SO2, methanol, C5H6, formic acid |