# Supplementary Information

Polyolefin depolymerization over silica-alumina-based catalysts: mechanistic classifications and benchmarking

Wei-Tse Lee1, Antoine van Muyden1, Felix D. Bobbink1, Mounir D. Mensi1, Jed R. Carullo1, Paul J. Dyson1,*

1Institute of Chemical Sciences and Engineering, École Polytechnique Fédérale de Lausanne (EPFL), Lausanne, Switzerland.

Supplementary Figure 1 Powder X-ray of SiO2-Al2O3, Co/SiO2-Al2O3, Ni/SiO2-Al2O3 and Ru/SiO2-Al2O3 with 2𝜃 = 4-50 degree.

Supplementary Figure 2 Powder X-ray of Zeo-Y_H, Co/Zeo-Y_H, Ni/Zeo-Y_H and Ru/Zeo-Y_H with 2𝜃 = 4-50 degree.

Supplementary Figure 3 Powder X-ray of ZSM-5_H, Co/ZSM-5_H, Ni/ZSM-5_H and Ru/ZSM-5_H with 2𝜃 = 4-50 degree.

Supplementary Figure 4 Curve fitted XPS analysis of Co 2p region of Co/ZSM-5_H catalyst (fitting according to Mark Biesinger et al.).1 The detailed fitting table can be revealed through the raw data upon reasonable request.

Supplementary Figure 5 Curve fitted XPS analysis of Ni 2p region of Ni/ZSM-5_H catalyst (fitting according to Mark Biesinger et al.).1 The detailed fitting table can be revealed through the raw data upon reasonable request.

Supplementary Figure 6 Curve fitted XPS analysis of Ru 3d and C 1s region of Ru/ZSM-5_H catalyst (fitting according to David J. Morgan).2 The detailed fitting table can be revealed through the raw data upon reasonable request.

| a | c |
| --- | --- |
| b | d |

Supplementary Figure 7 a SEM images showing the particle distributions of ZSM-5_H (6.4-9.4 𝜇m), b Co/ZSM-5_H (6.3-9.7 𝜇m), c Ni/ZSM-5_H (6.3-8.6 𝜇m) and d Ru/ZSM-5_H (6.0-10.4 𝜇m).

| a |  | b |  |
| --- | --- | --- | --- |
| d c |  | e | f |
| g | h |  |  |

Supplementary Figure 8 a TEM bright-field image of ZSM-5_H. b HAADF image of ZSM-5_H. c STEM-EDS elemental mapping of Al, d Si, e O, f Co, g Ni and h Ru.

| a |  | e b |  |
| --- | --- | --- | --- |
| c d |  |  | f |

Supplementary Figure 9 a TEM bright-field image of Ru/ZSM-5_H. b HAADF image of Ru/ZSM-5_H with Ru NP distributions = 5.4±0.8 nm. c STEM-EDS elemental mapping of Al, d Si, e O and f Ru.

| a | b | d |
| --- | --- | --- |
|  | c C | e |

Supplementary Figure 10 a HAADF image of Co/ZSM-5_H with Co NP distributions = 3.6±0.5 nm. b STEM-EDS elemental mapping of Al, c Si, d O and e Co.

| b a |  | d |
| --- | --- | --- |
|  | c e |  |

Supplementary Figure 11 a HAADF image of Ni/ZSM-5_H with Ni NP distributions = 3.1±0.4 nm. b STEM-EDS elemental mapping of Al, c Si, d O and e Ni.

Supplementary Figure 12 Product distributions after nC16 (1.59 g) deconstructions in the presence of unmodified silica-alumina catalysts (0.1 g): SiO2-Al2O3, Zeo-Y_H and ZSM-5_H, 45 bar H2, 2 hrs. Note that nC12 signal originated from the addition as an internal standard has been suppressed, and the yield of C12 products herein was resulted from the nC16 deconstruction.

Supplementary Figure 13 Product distributions after nC16 (1.59 g) deconstructions in the presence of Co-modified catalysts (0.1 g, metal loading = 2.5 wt%): Co/SiO2-Al2O3, Co/Zeo-Y_H and Co/ZSM-5_H, 45 bar H2, 2 hrs. Note that nC12 signal originated from the addition as an internal standard has been suppressed, and the yield of C12 products herein was resulted from the nC16 deconstruction.

Supplementary Figure 14 Product distributions after nC16 (1.59 g) deconstructions in the presence of Ni-modified catalysts (0.1 g, metal loading = 2.5 wt%): Ni/SiO2-Al2O3, Ni/Zeo-Y_H and Ni/ZSM-5_H, 45 bar H2, 2 hrs. Note that nC12 signal originated from the addition as an internal standard has been suppressed, and the yield of C12 products herein was resulted from the nC16 deconstruction.

Supplementary Figure 15 Product distributions after nC16 (1.59 g) deconstructions in the presence of Ru-modified catalysts (0.1 g, metal loading = 2.5 wt%): Ru/SiO2-Al2O3, Ru/Zeo-Y_H and Ru/ZSM-5_H, 45 bar H2, 2 hrs. Note that nC12 signal originated from the addition as an internal standard has been suppressed, and the yield of C12 products herein was resulted from the nC16 deconstruction.

| a |  |
| --- | --- |
| b |  |

Supplementary Figure 16 a Product distributions after nC16 (1.59 g) deconstructions with 45 bar H2 at 375 ºC, 2 hrs, under a hydrogen and a nitrogen atmosphere in the presence of SiO2-Al2O3 (0.1 g) and b Zeo-Y_H (0.1 g). Note that nC12 signal originated from the addition as an internal standard has been suppressed, and the yield of C12 products herein was resulted from the nC16 deconstruction.

b a

c

Supplementary Figure 17 a GC-FID traces of liquid products after the nC16 (1.59 g) deconstruction with 45 bar H2 at 325 ºC, 2 hrs, in the presence of (A) Ru/SiO2-Al2O3 (0.1 g, metal loading = 2.5 wt%), b Ru/Zeo-Y_H (0.1 g, metal loading = 2.5 wt%) and c Ru/ZSM-5_H (0.1 g, metal loading = 2.5 wt%). Note that the peaks with retention time ~2.7 and ~14.1 min were diethyl ether (solvent for the GC sample) and nC12 (internal standard), respectively.

| a | b | c |
| --- | --- | --- |

Supplementary Figure 18 a nC16 (1.59 g) deconstructions with 45 bar H2 at 275, 325 and 375 ºC, 2 hrs, in the presence of SiO2-Al2O3-based catalysts (0.1 g, metal leading = 2.5 wt%): SiO2-Al2O3, Co/SiO2-Al2O3, Ni/SiO2-Al2O3, Ru/SiO2-Al2O3, b Zeo-Y_H-based catalysts (0.1 g, metal leading = 2.5 wt%): Zeo-Y_H, Co/Zeo-Y_H, Ni/Zeo-Y_H, Ru/Zeo-Y_H, c ZSM-5_H-based catalysts (0.1 g, metal leading = 2.5 wt%): ZSM-5_H, Co/ZSM-5_H, Ni/ZSM-5_H, Ru/ZSM-5_H.

a

b

c

Supplementary Figure 19 a nC16 (1.59 g) deconstructions with 45 bar H2, 2 hrs, in the presence of SiO2-Al2O3, Co/SiO2-Al2O3, Ni/SiO2-Al2O3, Ru/SiO2-Al2O3, Zeo-Y_H, Co/Zeo-Y_H, Ni/Zeo-Y_H, Ru/Zeo-Y_H, ZSM-5_H, Co/ZSM-5_H, Ni/ZSM-5_H and Ru/ZSM-5_H (cat. = 0.1 g, metal loading = 2.5 wt%) at 275 ºC, b 325 ºC and c 375 ºC.

Supplementary Table 1 XPS surface relative atomic concentration of the ZSM-5_H-based catalysts.

| Catalyst | Si% (2p) | Al% (2p) | O% (1s) | Co% (2p) | Ni% (2p) | Ru% (3d) |
| --- | --- | --- | --- | --- | --- | --- |
| ZSM-5_H | 28.6 | 2.8 | 68.7 | - | - | - |
| Co/ZSM-5_H | 22.4 | 0.8 | 67.0 | 9.8 | - | - |
| Ni/ZSM-5_H | 22.3 | 4.8 | 64.6 | - | 8.3 | - |
| Ru/ZSM-5_H | 26.6 | 3.2 | 67.6 | - | - | 2.6 |

Supplementary Table 2 XPS surface species and their relative concentrations of the ZSM-5_H-based catalysts.

| Catalyst | Specie % |  |  |  |
| --- | --- | --- | --- | --- |
| Co/ZSM-5_H | Co(0)% (2p) | CoO% (2p) | Co(OH)2% (2p) |  |
|  | 1.4 | 2.2 | 96.4 |  |
| Ni/ZSM-5_H | Ni(0)% (2p) | NiO% (2p) | Ni(O)OH% (2p) | Ni(OH)2% (2p) |
|  | 1.8 | 0.3 | 60.4 | 37.5 |
| Ru/ZSM-5_H | Ru(0)% (3d) | RuO2% (3d) | RuO2·H2O% (3d) | RuCl3% (3d) |
|  | 86.0 | 3.9 | 6.7 | 3.4 |

## References

1.	Biesinger, M. C. et al. Resolving surface chemical states in XPS analysis of first row transition metals, oxides and hydroxides: Cr, Mn, Fe, Co and Ni. Appl. Surf. Sci. 257, 2717–2730 (2011).

2.	Morgan, D. J. Resolving ruthenium: XPS studies of common ruthenium materials. Surf. Interface Anal. 47, 1072–1079 (2015).