Supporting Information

Facile in-situ construction of granular–polyhedral Ag2O–Ag2CO3/lamellar Bi2O2CO3–Bi2MoO6 spherical heterojunction with enhanced photocatalytic activity towards pollutants

Yu Zhanga, Fengyan Maa*, Meihua Linga, Yanan Hana, Dandan Lva, Zhengjun Wanga, Wenzhi Zhanga, and Li Lia,b*

aCollege of Chemistry and Chemical Engineering, Qiqihar University, Qiqihar 161006, Heilongjiang, PR China

bCollege of Materials Science and Engineering, Qiqihar University, Qiqihar 161006, Heilongjiang, PR China

* Corresponding authors.

E-mail: qqhrlili@126.com

- Preparation of Bi2MoO6 hollow sphere

- Bi(NO3)3·5H2O (2 mmol) and Na2MoO4·2H2O (1 mmol) were separately dissolved in ethylene glycol ((CH2OH)2, 5 mL). Then the latter was dropped into the former followed by ethanol (C2H5OH, 20 mL) to form mixture solution under vigorously magnetically stirring for 2 h. Subsequently, the solution was moved to teflon–lined autoclave (50 mL), sealed and kept for 24 h at 180 °C. The solid was collected by centrifugation, washed thoroughly with water and ethanol three times, and desiccated at 60 °C to obtain a yellow-green Bi2MoO6 powder.

- Characterization

X-ray diffraction (XRD) patterns of the products were received on a diffractometer (Bruker–AXS/D8) using Cu Kα radiation in the range of 15°–60°. X-ray photoelectron spectra (XPS) measurements were done on a spectrometer (ESCALAB/250Xi) with Al Kα source using C1s peak at 284.6 eV as reference. Fourier transform infrared (FT–IR) spectra were gathered on a Nicolet 6700 spectrometer applying KBr to grind with test samples. The morphological analysis of the samples were performed by transmission electron microscopy (TEM, JEOL/JEM2100F) and scanning electron microscopy (SEM, HitachiS–4300).The photoluminescence spectra of different samples were performed by a spectrophotometer (PL, F–7000FL). The UV–vis diffuse reflection absorption spectra (DRS) were acquired by a spectrophotometer (Purkinje/TU-1901) using BaSO4 as reference.

- Photoelectrochemical tests were executed on an electrochemical workstation (PEC–1000, Bofill). In the transient photocurrent experiments, the working electrode is a titanium sheet coated with a 1.0 cm x 1.0 cm photocatalyst, the counter electrode is a platinum sheet, and the reference electrode is a saturated Ag/AgCl (saturated KCl) electrode. The working electrode was made as following: 0.1 g of catalyst was first put into 5 mL of ethanol, sonicated for 10 min, and then agitated to form a suspension. Thereafter, the suspension was coated onto a 2.0 cm x 1.0 cm titanium sheet and finally the prepared titanium sheet was desiccated in an drying chest at 50 °C for 30 min. The sodium sulphate solution and 300 W xenon lamp (λ > 420 nm) were uesed as the electrolyte and the light source during the test process, respectively. An open circuit voltage was approx. 0.3 V.

- In the electrochemical impedance experiments, the working electrode was a nickel foam coated with a 1.0 cm x 1.0 cm photocatalyst. The working electrode prepared and test conditions were similar to the above description.

Fig. S1 XRD patterns of stirring at room temperature for 2 h and 18 h before adding AgNO3.