Supplementary Information

Fabricated Hybrid Composites with Insect-Repellent Property

Hajara Babayo a, b, Haruna Musa a, Mustapha D. Garba a, c*

a Department of Pure and Industrial chemistry, Bayero University Kano, Nigeria P.M.B 3011

b Fibre and Polymer Science Program, North Carolina State University Raleigh, NC, 27606, USA

c School of Chemistry, University of Glasgow, Glasgow G12 8QQ, Scotland, UK.

e-mail: m.d.garba.11@gmail.com

Stage 1: Start of the reaction                                      Stage 2: Formation of homogenous solution

Stage 3: Dissolution of soap layer                          Stage 4: Formation of FFA at the top layer

Fig. S1: Extraction of free fatty acid; Stage 1 is the saponification of castor oil with a solution of sodium hydroxide, (1:1) ethanol and distilled-water. Stage 2 is the refluxing stage where a homogenous mixture is obtained. Stage 3 is the phase separation stage where the soap was obtained. At the final stage the soap was reacted with sulfuric acid to obtain free fatty acid.

a) Set up for the preparation of alkyd resin         b) Prepared alkyd resin.

Fig S2: Images for alkyd resin preparations

a) Raw Canarium schweinfurthii gum.        b) Dried powder of Canarium schweinfurthii gum.

c)  Dried untreated tiger nut fibre.            d) Benzoyl chloride treated tiger nut fibre.

Fig S3: Tiger nut and Canarium schweinfurthii gum treatments

Step 1: Melting of LDPE

Step 2:  Mixing of all the materials

Step 4: Compression Moulding

Step 3: Semi-finished composite (Sheet Moulding Compound)

Stage 5: Molded Composite

Fig. S4: Process of composite fabrication; step 1 is where the waste LDPE was melted, all components were mixed in step 2, the semi-finished composite was prepared in a mould in the 3rd step and compressed in the 4rd step, the final step is the moulded composite obtained.

a) Termite’s repellent activity/mortality rate

b) Cockroach repellent activity/ mortality rate

Fig. S5: Insect repellent test

Fig. S6: Water absorption of composites

Fig.S7: Density of the composites

Fig. S8: Tensile Strength of Composites

Fig. S9: Flexural strength of composites

Fig. S10: Hardness of the composites

Fig. S11: Impact load of composites

Fig. S12:  FTIR of Crude castor oil

Fig. S13: FTIR of castor oil FFA

Fig. S14: FTIR of castor oil FFA Resin

Fig. S15: FTIR of canarium schweinfurthii gum resin

Fig. S16: FTIR of untreated tiger nut fibre

Fig. S17: FTIR of Benzoyl Chloride Treated Tiger Nut Fibre

Fig. S18: FTIR of untreated Tiger Nut Fibre composite

Fig. S18: FTIR of Benzoyl Chloride Treated Tiger Nut Fibre composite

Table S1: Physicochemical properties of the crude castor oil

| Characteristics | Unit | Crude castor oil | Methods Used | Instrument |
| --- | --- | --- | --- | --- |
| Acid value | mg NaOH/g | 36.91 | BinQuader et al., (2018) |  |
| Specific density at 300C | g/cm3 | 0.956 | BinQuader et al., (2018) |  |
| Saponification value | mg/g | 216 | Jibrin et al., (2018) |  |
| Iodine value, Hanus | gI2/g | 179.8 | BinQuader et al., (2018) |  |
| Viscosity | MPas | 218.3 |  | Clandom viscometer, model VT-03 |
| pH |  | 4.71 | BinQuader et al., (2018) |  |
| Moisture Content | % | 1.33 | Abdulkadir and Jimoh., (2013) | Denver moisture analyzer (model IR-35) |
| FTIR | cm-1 |  |  | Car 630;Agilent Technology |

Table S2: Physical and Chemical Properties of Alkyd Resin.

| Properties | Specific value | Alkyd resin from castor oil |
| --- | --- | --- |
| Colour |  | Brown |
| Viscosity (absolute) | MPas | 419.63 |
| Solubility in; | Xylene Acetone Toluene Ethanol Cyclohexanol | Completely soluble Completely soluble Completely soluble Insoluble Limited solubility |
| FTIR | cm-1 |  |

Table S3: FTIR absorption bands of the crude castor oil

| Experimental frequency (cm-1) | Literature frequency (cm-1) | Remark |
| --- | --- | --- |
| 3007.91 | Near 3030 | =C-H |
| 3406.92 | 3570-3200 | O-H stretch |
| 1167.67 | Near 1100 | C-O stretch |
| 2925.55 2854.65 | 2926-2850 | C-H |
| 1462.78 1421.85 | 1485-1415 | C-H |
| 1741.64 | 1750-1735 | C=O |
| 1246.76 1167.67 1089.76 | 1245-1089 | C-O |

Table S4: FTIR absorption bands of the castor oil FFA

| Experimental frequency (cm-1) | Literature frequency (cm-1) |  | Remark |
| --- | --- | --- | --- |
| 3007.91 | 3010 – 3030 | =C-H Olefinic C-H stretching, this is a clear indication of the unsaturated fatty acids. |  |
| 3378.83 | 3570-3200 | O-H Broad peak around 3400 cm-1 corresponds to the hydroxyl group of high concentrated carboxylic acids. |  |
| 1707.73 | 1710 | C=O carbonyl stretching of carboxylic acids |  |
| 2925.55 2854.65 | 2926-2850 | C-H |  |
| 1482.78 | 1485-1440 | C=C |  |
| 1406.73 | 1410 | COO- Cis group |  |
| 1212.77 1086.78 1052.75 | 1245-1030 | C-O |  |
| 970.83 | 936-980 | Dimer of carboxylic acid |  |
| 728.66 |  | The rocking of multiple (>4) methylene groups |  |

Table S5: FTIR absorption bands of the castor oil FFA Resin (Hlaing and Oo., 2008: Sharif 2015)

| Experimental frequency (cm-1) | Literature frequency (cm-1) | Remark |
| --- | --- | --- |
| 3368.89 | 3200-2700 | O-H stretching |
| 3007.82 | 3030-3000 | C-H olefinic stretching due to fatty acid. |
| 2925.61 2854.70 | 2926-2850 | C-H |
| 1722.49 | 1730-1730 | C=O due to ester |
| 1585.81 1566.82 | 1600-1550 | Aromatic C=O stretching of the phthalate system. |
| 1462.76 | 1480-1460 | -CH2 bending vibration. |
| 1380.72 | 1343-1385 | -CH3 bending |
| 1279.52 1179.67 1123.57 |  | C-O stretching |
| 1074.56 | 1074-1000 | -C-O stretching of ether. |
| 747.64 | 750-730 | Rocking of multiple (>4) methylene groups of the fatty acids. |

Table S6: FTIR absorption bands of Canarium Schweinfurthii

| Experimental frequency (cm-1) | Literature frequency (cm-1) | Remark |
| --- | --- | --- |
| 3391.92 | 3400-3200 | O-H stretching |
| 2873.68 2921.62 | 2926-2880 | C-H |
| 1704.74 | 1725-1705 | C=O |
| 1454.73 | 1485-1440 | C=C stretching |
| 1380.70 | 1380-1370 | -C-H bending bend. |
| 1246.80 1100.85 1071.83 | 1245-1030 1150-1050 | C-H bends. C-O stretching |
| 918.82 996.73 | 900-600 | C-H out of plane |
| 892.82 | 900-600 | C-H out of plane |
| 709.87 | 900-600 | Rocking of multiple (<4) methylene group |
| 668.82 | 900-600 | C-H out of plane |

Table S7: FTIR absorption bands of the untreated tiger nut particulate fibre

| Experimental frequency (cm-1) | Literature frequency (cm-1) | Remark |
| --- | --- | --- |
| 3335.84 | 3570-3200 | O-H Broad peak around 3400 cm-1corresponds to the hydroxyl group. |
| 2921.83 2854.87 | 2926-2850 | C-H |
| 1719.91 1745.91 | 1760-1720 | C=O carbonyl of lignin in cellulose |
| 1462.89 | 1485-1440 | C=C |
| 1640.87 | 1680-1640 | C=O |
| 1376.87 | Near 1380 | C-H hemicellulose |
| 1156.83 | 1200-1100 | C-O |
| 672.74 | 700-670 | C-H |

Table S8:  FTIR absorption bands of Benzoyl Chloride Treated Tiger Nut Particulate Fibre

| Experimental frequency (cm-1) | Literature frequency (cm-1) | Remark |
| --- | --- | --- |
| 3204.98 | 3200-2700 | O-H weak peak corresponds to the hydroxyl group present in cellulose. |
| 3029.98 | 3070-3020 | =C-H stretching of aromatic due to phenyl nucleus |
| 1689.94 | 1770-1640 | C=O due to benzoyl carbonyl. |
| 1424.96 | 1424-1415 | Conjugated C-H bending vibrations. |
| 1328.96 | 1343-1319 | C-H in plane bending of hemicellulose. |
| 1290.94 | 1290-1266 | C-O syringyl ring breathing and C-O stretching in lignin and Xylan. |
| 1030.94 | 1043-1028 | C-O, C=C, symmetric glycosidic stretching. |
| 937.95 | 980-936 | Dimer of carboxylic acid |
| 808.96 | 860-800 | C-H |

Table S9: FTIR absorption bands of untreated and benzoyl chloride treated tiger nut particulate fibre composites

| Experimental frequency (cm-1)Untreated Composite | Experimental frequency (cm-1)Treated Composite | Literature frequency (cm-1) | Remark |
| --- | --- | --- | --- |
| 2847.49 | 2847.56 2914.51 | 2926-2850 | C-H |
| _ | 1722.90 | 1725-1700 | C=O due to benzoyl carbonyl. |
| 1469.74 | 1469.77 | 1470-1415 | C-H symmetrical bending vibration. |
| 1380.89 | 1380.89 | 1380-1319 | C-H in plane bending of hemicellulose. |

Table S10: Analysis of the composites

| Analysis | Instruments used | Unit | Composites |  |
| --- | --- | --- | --- | --- |
|  |  |  | Untreated | Treated |
| Water absorption ASTM D-3010 |  | Wt% | 0.288 | 0.085 |
| Thickness swelling ASTM D-570 |  | Wt% | No effect | No effect |
| Chemical resistance (Acids) ASTM D1693-05 |  | Wt% | 2.734 (H2SO4) 5.146 (HCL) | 0.331 0.450 |
| Chemical resistance (Bases) ASTM D1693-05 |  | Wt% | 1.016 (KOH) 2.113 (NaOH) | 0.728 0.982 |
| Density ASTM D2395-17 |  | g/cm3 | 0.0096 | 0.0092 |
| Tensile strength ASTM D-1037 | Tensile test (Universal material testing machine, Shimadzu, model AG-1) | Mpa | 27.78 | 35.08 |
| Flexural strength ASTM D-792 | flexural test (Universal material testing machine, Shimadzu, model AG-1) | Mpa | 426.4 | 456.3 |
| Hardness | hardness tester (Muver Franscisco, munoz Ireles, model 5019) | HV | 95 | 93 |
| Impact ASTM D-156 | Impact tester (Ceast Resil impactor, model P/N 6957 IZOD) | J/m | 779 | 730 |
| SEM (Favaro et al., 2010) | Scanning Electron Microscope (Prox: Phenom World 800-07334) |  |  |  |
| FTIR | Fourier Transform Infrared spectrophotometer (Car 630; Agilent Technology) | cm-1 |  |  |