SUPPLEMENTARY INFORMATION

Electrical manipulation of antiferromagnetic easy axis in IrMn/NiFe exchange-biased structures

Jaimin Kang1, Jeongchun Ryu1,*, Jong-Guk Choi1, Taekhyeon Lee2, Jaehyeon Park2, Soogil Lee1, Kab-Jin Kim2, and Byong-Guk Park1,*

1 Department of Materials Science and Engineering and KI for Nanocentury, KAIST, Daejeon 34141, Korea

2 Department of Physics, KAIST, Daejeon 34141, Korea

* Corresponding authors: Jeongchun Ryu (jcryu@kaist.ac.kr) & Byong-Guk Park (bgpark@kaist.ac.kr)

Figure S1 | Hysteresis loop and SOT switching in a Ta/NiFe structure. a, Hysteresis loops of the Ta (5nm)/NiFe (4 nm) structure measured with magnetic fields along the x-axis (solid blue) and y-axis (open red). b, RH versus in-plane current pulse (IP) of the Ta/NiFe bilayer. The arrows denote the sweeping direction of IP.

Figure S2 | Thickness dependence of SOT-induced AFM switching. a-e Hysteresis loop measured using a magnetic field along the x-axis, Bx (a), the φAFM versus current density (JP) curves of the IrMn (tIrMn)/NiFe (4 nm) samples with tIrMn = 5 nm (b), 10 nm (c), 15 nm (d), and 20 nm (e). f-k. Hysteresis loop measured using Bx (f), the φAFM versus JP curves of the IrMn (5 nm)/NiFe (tNiFe) samples with tNiFe = 3 nm (g), 4 nm (h), 5 nm (i), 7 nm (j), and 10 nm (k). The arrows denote the sweeping direction of JP.

Figure S3 | Memristive behaviour of AFM switching with the opposite current sweep. Minor φAFM vs IP curves for the IrMn (5 nm)/NiFe (4 nm)/Ta (1.5 nm) sample with a 4-μm-wide Hall bar, measured under the same sequence as shown in Fig. 4 of the main text with IP,ini = +32 mA and IP(-max) varying from -22 mA to -31 mA.