High-speed and efficient removal of Uranium (VI) from aqueous solution by hydroxyapatite modified ordered mesoporous carbon (CMK-3)

Hao Deng, Zhenyu Ren, Ming Ma*, Xin Zhong*

School of Life Science, Shaoxing University, Huancheng West Road 508, Shaoxing 312000, P.R. China

Corresponding author e-mail:

Ming Ma: 2020000096@usx.edu.cn

Xin Zhong: zhongxinmagic@163.com

1. Data processing and analysis

Eq. S1

Eq. S2

Eq. S3

In these formulas, qt (mg/g) represented the amount of equilibrium adsorption. C expressed the thickness of boundary layer. k1 (min-1), k2 (g/mg. min) and kp (g/mg. min0.5) were the rate constants of the pseudo-first, second-order and intra-particle diffusion, respectively.

Eq. S4

Eq. S5

In the formulas, KL (L/mg) and KF (mg1-1/n.g-1.L-1/n) were the isotherm constants of Langmuir and Freundlich, respectively. Qmax (mg/g) delegated the maximum adsorption amounts, and n was the Freundlich exponent.

Eq. S6

Eq. S7

Eq. S8

Where, K0 was the adsorption equilibrium constant, and R was the gas constant 8.314 J/(mol∙K).

2. Figures

Fig. S1 The EDX spectra of HAP@CMK-3.

Fig. S2 The pseudo-first-order model of HAP, CMK-3, HAP@CMK-3(1:2, 1:1, 2:1) (C0=50 mg/L, T=298 K, pH 3.0, m/V=0.5 g/L).

Fig. S3 The Freundlich fitting curves for U(VI) adsorption onto HAP, CMK-3, HAP@CMK-3(1:2, 1:1, 2:1) (C0=50 mg/L, T=298 K, pH 3.0, m/V=0.5 g/L).

Fig. S4 The XPS full-survey spectra of (a) CMK-3 after U(VI) adsorption; (b) HAP--Ca 2p; (c) CMK-3--O 1s; (d) HAP@CMK-3--C 1s before U(VI) adsorption; (e) CMK-3--C 1s and (f) HAP@CMK-3--C1s after U(VI) adsorption.