Novel Fe hydrides and magnetism in the Fe-H system at high pressures

I. Kupenko1,*, E. Bykova2,3, D.M. Vasiukov4,5, G. Aprilis4, V. Cerantola6, A.I. Chumakov6, J. Jacobs6, M. Bykov3, E. Koemets3, S. Chariton3, C. Sanchez-Valle1 and L. Dubrovinsky3

1Institut für Mineralogie, University of Münster, Corrensstr. 24, 48149 Münster, Germany

2Photon Science, Deutsches Elektronen-Synchrotron, Notkestrasse 85, 22607, Hamburg, Germany

3Bayerisches Geoinstitut, University of Bayreuth, D-95440, Bayreuth, Germany

4Material Physics and Technology at Extreme Conditions, Laboratory of Crystallography, University of Bayreuth, D-95440 Bayreuth, Germany

5Synchrotron Radiation Research, Lund University, Box 118, S-221 00 Lund, Sweden,

6ESRF-The European Synchrotron, CS 40220, 38043, Grenoble, Cedex 9, France

# *Corresponding author: kupenko@uni-muenster.de

# Supplementary data

Figure S1. Photo and scheme of a typical loading.

Fig. S2. Unrolled diffraction patterns of monoclinic Fe2H3 with C2/m space group at 65.1(2) GPa (a) and hcp-FeH at 49.0(6) GPa and room temperature. Diamond peaks and detector glitches are masked. A clear peak splitting (e.g. indicated by red ellipses) in the C2/m phase can be observed.

Fig S3. SMS spectrum of Fe2H3 at 63.2(1.4) GPa and ca. 1000 K. Solid lines show the theoretical fit, the percentage bar indicates the relative absorptions, and the residuals of the fit are indicated below the spectrum. Light-red nonmagnetic components are from the beamline optics.

Fig S4. SMS spectrum of amorphous Fe-H at 10.2(5) GPa and room temperature. The spectrum can be fitted by the single magnetic contribution with the hyperfine parameters similar to that of dhcp-FeH (Fig. 4a, table S1). Solid lines show the theoretical fit, the percentage bar indicates the relative absorptions, and the residuals of the fit are indicated below the spectrum. Light-red nonmagnetic components are from the beamline optics. A significant decrease in the relative absorption is likely related to the decrease of the Lamb-Mössbauer factor in the amorphous material.

Supplementary Table 1. Hyperfine parameters of iron hydrides.

| dhcp-FeH |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| P, GPa | H-site |  |  |  | C-site |  |  |  | Nonmagnetic component |  |
|  | CS | QS | Bfh | Relative weight | CS | QS | Bfh | Relative weight | CS | Relative weight |
| 6.05(7) | 0.423(8) | -0.022(15) | 30.70(7) | 56(2) | 0.419(8) | 0.043(15) | 27.23(7) | 44(2) |  |  |
| 12.1(4) | 0.39(1) | -0.03(2) | 29.57(10) | 50(3) | 0.386(9) | 0.036(17) | 26.03(8) | 50(3) |  |  |
| 17.4(6) | 0.36(1) | -0.02(3) | 28.03(14) | 46(4) | 0.356(11) | 0.04(2) | 24.64(11) | 53(4) | 0.34(14) | 1(1) |
| 23.0(1.3) | 0.353(8) | 0.00(2) | 25.62(10) | 54(5) | 0.34(2) | 0.05(4) | 22.6(3) | 40(5) | 0.26(4) | 6(2) |
| 24.6(1.8) | 0.35(1) | -0.03(2) | 25.30(12) | 48(4) | 0.34(1) | 0.046(18) | 22.01(11) | 45(4) | 0.31(4) | 7(2) |
| 28(4) | 0.32(1) | 0.00(2) | 23.74(16) | 53(6) | 0.311(12) | 0.02(7) | 19.4(5) | 27(7) | 0.288(12) | 20(3) |
| 36.4(1.3) | 0.3(1) | 0.11* | 18.5(8) | 37(4) |  |  |  |  | 0.270(13) | 63(4) |
| 40.98(11) | 0.29(4) | 0.11(7) | 18.4(3) | 32(3) |  |  |  |  | 0.244(13) | 68(3) |
| 46.8(5) | 0.2(1) | 0.11(15) | 10.7(8) | 26(5) |  |  |  |  | 0.235(12) | 74(5) |
| 61.2(1.4) |  |  |  |  |  |  |  |  | 0.190(5) | 100 |
| fcc-FeH |  |  |  |  |  |  |  |  | CS | Relative weight |
| 63.2(1.4) |  |  |  |  |  |  |  |  | 0.21(3) | 100 |
| Fe2H3 |  |  |  |  |  |  |  |  |  |  |
| P, GPa | Magnetic component |  |  |  |  |  |  |  | Nonmagnetic component |  |
|  | CS | QS | Bfh | Relative weight |  |  |  |  | CS | Relative weight |
| 63.2(5) | 0.32(3) | 0.03(5) | 21.1(2) | 68(2) |  |  |  |  | 0.16(2) | 32(2) |
| 63.2(5) 1000(100) K | 0.17(9) | -0.25(17) | 22.6(7) | 65(inf) |  |  |  |  | 0.23(inf) | 35(inf) |
| hcp-FeH |  |  |  |  |  |  |  |  |  |  |
| P, GPa | Magnetic component |  |  |  |  |  |  |  | Nonmagnetic component |  |
|  | CS | QS | Bfh | Relative weight |  |  |  |  | CS | Relative weight |
| 52.3(5) | 0.22(5) | 0.02(9) | 13.3(4) | 56(5) |  |  |  |  | 0.22(3) | 44(5) |
| 43.7(7) | 0.229(18) | 0.00(3) | 16.64(14) | 68(2) |  |  |  |  | 0.26(2) | 32(2) |
| 31.2(5) | 0.33(4) | 0* | 22.2(4) | 76(5) |  |  |  |  | 0.24(8) | 24(5) |
| Amorphous |  |  |  |  |  |  |  |  |  |  |
| P, GPa | Magnetic component |  |  |  |  |  |  |  |  |  |
|  | CS | QS | Bfh | Relative weight |  |  |  |  |  |  |
| 10.2(5) | 0.39(7) | 0* | 26.5(6) | 100 |  |  |  |  |  |  |

Supplementary Table 2. Unit cell parameters of the hcp-FeH and Fe2H3.

| Fe2H3 |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| P, GPa | a, Å | b, Å | c, Å | β, ° | c/b |
| 65.1(2) | 4.4995(5) | 2.5574(3) | 4.0819(7) | 90.956(11) | 1.596 |
| 62.7(2) | 4.5070(4) | 2.5598(2) | 4.0870(6) | 90.960(10) | 1.596 |
| 56.3(3) | 4.4564(7) | 2.5412(3) | 4.095(3) | 90.392(10) | 1.611 |
| hcp-FeH |  |  |  |  |  |
| P, GPa | a, Å |  | c, Å |  | c/a |
| 56.7(3) | 2.51165(16) |  | 4.0472(3) |  | 1.611 |
| 47.7(6) | 2.52557(13) |  | 4.0781(4) |  | 1.615 |
| 49.0(6) | 2.52616(11) |  | 4.0772(5) |  | 1.614 |
| 33.1(1) | 2.56507(11) |  | 4.1460(6) |  | 1.616 |
| 24.7 (1) | 2.59536(17) |  | 4.1987(7) |  | 1.618 |

Supplementary Table 3. Parameters of the equation of state obtained by the fit of the experimental data to the Birth-Murnaghan equation of state.

| Phase | V0, Å3 | K0, GPa | K0’ |
| --- | --- | --- | --- |
| Fe hcpa | 11.234 | 165* | 4.97 |
| FeH dhcpb | 13.341 | 193 | 3.54 |
| FeH fccc | 13.45 | 99 | 11.7 |
| FeH-hcp | 13.74 | 166 | 4* |
| FeH2 tetragonalb | 17.177 | 111 | 5.17 |

a: taken from ref. [50]; b: fitted data from ref. [14]; c: taken from ref. [21].The values marked by the asterisk symbol (*) were fixed during the refinement.