Cellulose-based hybrid composites enabled by metal organic frameworks for CO2 capture: The effect of cellulosic substrate

Saysam Qusai Jabbar1, Halimeh Janani1, Hamed Janani*1

1Chemical Engineering Department, Faculty of Engineering, Ferdowsi University of Mashhad

Azadi Sq., Mashhad, Iran, Postal Code: 9177948944

Supporting Information

Table S1. The parameters of kinetic models along with associated correlation functions for CO2 adsorption onto Cotton@MOF-199.

| Sample | Adsorption temperature | Kinetic Model | Supposed rate-limiting step | Model parameters | R2 |
| --- | --- | --- | --- | --- | --- |
| Cotton@MOF | RT | PFO dqtdt=k1qe-qt | External diffusion | k1=0.163 qe=1.300 | 0.995 |
|  |  | RNO dθdt=α(1-θ)n | Active site sorption | α=0.165 n=0.856 qe=1.24 | 0.993 |
|  |  | W&M qt=kW&Mt1/2 | Internal diffusion | kW&M=0.307 | 0.962 |
|  | 45 ℃ | PFO dqtdt=k1qe-qt | External diffusion | k1=0.084 qe=1.434 | 0.969 |
|  |  | RNO dθdt=α(1-θ)n | Active site sorption | α=0.098 n=0.412 qe=1.08 | 0.984 |
|  |  | W&M qt=kW&Mt1/2 | Internal diffusion | kW&M=0.255 | 0.856 |
|  | 65 ℃ | PFO dqtdt=k1qe-qt | External diffusion | k1=0.135 qe=0.704 | 0.938 |
|  |  | RNO dθdt=α(1-θ)n | Active site sorption | α=0.130 n=0.527 qe=0.62 | 0.964 |
|  |  | W&M qt=kW&Mt1/2 | Internal diffusion | kW&M=0.155 | 0.847 |

Table S2. The parameters of kinetic models along with associated correlation functions for CO2 adsorption onto NBC@MOF-199.

| Sample | Adsorption temperature | Kinetic Model | Supposed rate-limiting step | Model parameters | R2 |
| --- | --- | --- | --- | --- | --- |
| NBC@MOF | RT | PFO dqtdt=k1qe-qt | External diffusion | k1=0.1265 qe=3.2706 | 0.984 |
|  |  | RNO dθdt=α(1-θ)n | Active site sorption | α=0.1215 n=0.5397 qe=2.9 | 0.994 |
|  |  | W&M qt=kW&Mt1/2 | Internal diffusion | kW&M=0.7038 | 0.907 |
|  | 45 ℃ | PFO dqtdt=k1qe-qt | External diffusion | k1=0.1632 qe=2.0176 | 0.993 |
|  |  | RNO dθdt=α(1-θ)n | Active site sorption | α=0.1579 n=0.7457 qe=1.9 | 0.995 |
|  |  | W&M qt=kW&Mt1/2 | Internal diffusion | kW&M=0.4754 | 0.928 |
|  | 65 ℃ | PFO dqtdt=k1qe-qt | External diffusion | k1=0.2377 qe=1.2124 | 0.942 |
|  |  | RNO dθdt=α(1-θ)n | Active site sorption | α=0.2409 n=1.1418 qe=1.25 | 0.945 |
|  |  | W&M qt=kW&Mt1/2 | Internal diffusion | kW&M=0.3139 | 0.849 |

Figure S1. Adsorption and desorption experimental data at various temperatures fitted to the Langmuir’s kinetic equations.

Antibacterial activity of the composites:

To investigate the inhibitory effect of the cellulose@MOF-199, coagulase positive Staphylococcus aureus strain was used as an indicator of gram-positive bacteria and Escherichia coli strain was used as an indicator of gram-negative bacteria. These bacteria were inoculated in the culture medium and then the fabric with growth inhibitory properties was placed in the culture medium containing bacterial strain. After the incubation time, the tested plates were examined for growth halo and the results are as follows (Figure S2):

Diameter of non-growth halo of plate containing Escherichia coli strain (Figure S2a): 33 mm

Diameter of non-growth halo of plate containing Staphylococcus aureus coagulase (Figure S2b): 25 mm

| (a) | (b) |
| --- | --- |

Figure S2. Antibacterial effect (growth inhibitory zone) of the cellulose@MOF-199 on (a) Escherichia coli and (b) Staphylococcus aureus coagulase