Supplementary Materials

Achieving over 70 kg m-2 h-1 evaporation rate by a 3D polyacrylamide-based hydrogel

Yuying Chen, Jixiang Yang, Jinsong Guo, Fang Fang, Ruilin Bao, Linji, Xu

Figure S1. Evaporation rate of 2D CAH with different CNTs under 1 kW m-2

Figure S2. Infrared images of 3D CAH under sun and dark at room temperature (10 ℃).

Figure S3. Dark evaporation infrared images of 3D CAH at different temperatures.

Figure S4. 24-hour long-term evaporation of 3D CAH. The effective evaporation length was 35 cm (EAI=176) under 25 ℃.

Table S1. Ion charge density.

| Ionic species | Charge (Q, C) | Ionic radius (r, m) | Charge density (ρ, C m-3) |
| --- | --- | --- | --- |
| Cl- | 1.6×10-19 | 1.81×10-10 | 6.44×1012 |
| SO42- | 3.2×10-19 | 2.18×10-10 | 7.38×1012 |
| PO43- | 4.8×10-19 | 2.30×10-10 | 9.43×1012 |
| Na+ | 1.6×10-19 | 9.5×10-11 | 4.46×1013 |
| Ca2+ | 3.2×10-19 | 9.9×10-11 | 7.88×1013 |
| Mg2+ | 3.2×10-19 | 6.5×10-11 | 2.78×1014 |

Table S2. Comparison of cost-effectiveness over previous reported 3D solar evaporators.

| Ref | Raw Materials | Estimated single item cost ($/m2) | Total cost ($/m2) | Evaporation rate (kg m-2 h-1) | Cost-effectiveness (Rate/Price, g h-1 $-1) |
| --- | --- | --- | --- | --- | --- |
| 1 | NaOH | 0.0005 | 5022.20 | 34.7 | 6.91 |
|  | Graphene oxide (GO) | 4669.38 |  |  |  |
|  | 1,4-butanediol diglycidyl ether | 343.61 |  |  |  |
|  | Triethylenetetramine | 1.04 |  |  |  |
|  | Cotton core | 8.16 |  |  |  |
| 2 | Sucrose | 712.44 | 712.44 | 10.9 | 15.30 |
|  | H2SO4 | 33.75 |  |  |  |
| 3 | NiCl2·6H2O | 47.45 | 154260.17 | 2.42 | 0.016 |
|  | CoCl2·6H2O | 457.86 |  |  |  |
|  | NaBH4 | 137.34 |  |  |  |
|  | Dopamine hydrochloride | 153607.40 |  |  |  |
|  | Salicylic acid | 10.12 |  |  |  |
| 4 | Reduced graphene oxide (RGO) | 2029.82 | 2039.08 | 2.25 | 1.10 |
|  | Sodium alginate | 9.26 |  |  |  |
| 5 | Cu(NO3)2·3H2O | 1219.86 | 1706.84 | 2.04 | 1.20 |
|  | Mn(NO3)2·4H2O | 456.52 |  |  |  |
|  | Fe(NO3)3·9H2O | 30.46 |  |  |  |
| 6 | Pyrrole | 631.81 | 1955.21 | 3.72 | 1.90 |
|  | FeCl3·6H2O | 1265.81 |  |  |  |
|  | HCl | 57.59 |  |  |  |
| 7 | Polyacrylonitrile (PAN) | 30397.26 | 653274.54 | 2.27 | 0.003 |
|  | Dimethyl sulfoxide | 5039.55 |  |  |  |
|  | Graphene oxide (GO) | 1906.50 |  |  |  |
| 8 | Reduced graphene oxide (RGO) | 10354.10 | 10450.24 | 4 | 0.38 |
|  | Agarose | 961.45 |  |  |  |
|  | Urea | 96.15 |  |  |  |
| 9 | Carbon black | 98.79 | 294572.29 | 2.31 | 0.008 |
|  | Dopamine hydrochloride | 294473.50 |  |  |  |
| 10 | CoCl2·6H2O | 43.39 | 14601.25 | 3.71 | 0.25 |
|  | Dopamine hydrochloride | 14557.86 |  |  |  |
|  | Reduced graphene oxide (RGO) | 828.33 |  |  |  |
|  | Agarose | 192.29 |  |  |  |
|  | Urea | 0.02 |  |  |  |
| 11 | Polyvinylidene fluoride | 47 | 58.3 | 1.93 | 0.481 |
|  | Pyrrole | 4.4 |  |  |  |
|  | FeCl3 | 3.2 |  |  |  |
|  | Deionized water | 2.9 |  |  |  |
|  | Energy consumption | 0.8 |  |  |  |
| 12 | Reduced graphene oxide (RGO) | 17855.54 | 18042.28 | 7.6 | 0.42 |
|  | Sodium alginate | 81.42 |  |  |  |
|  | Ethanol | 105.32 |  |  |  |
| 13 | Nano-diamonds | 97.77 | 100.61 | 1.324 | 13.16 |
|  | Ethanol | 2.84 |  |  |  |
| This work | Acrylamide (AM) | 1545.69 | 2553.73 | 72.3 | 28.31 |
|  | Carbon nanotubes (CNTs) | 246.07 |  |  |  |
|  | Bis-polyacrylamide | 14.96 |  |  |  |
|  | Ammonium persulfate (APS) | 16.62 |  |  |  |
|  | N,N,N′,N′-tetramethyl ethylenediamine (TEMED) | 183.55 |  |  |  |
|  | Cotton core | 546.83 |  |  |  |

Reference

1.	Finnerty CTK, et al. Interfacial Solar Evaporation by a 3D Graphene Oxide Stalk for Highly Concentrated Brine Treatment. Environmental Science & Technology 55, 15435-15445 (2021).

2.	Li J, et al. Over 10 kg m(-2) h(-1) Evaporation Rate Enabled by a 3D Interconnected Porous Carbon Foam. Joule 4, 928-937 (2020).

3.	Shao B, et al. Stackable nickel-cobalt@polydopamine nanosheet based photothermal sponges for highly efficient solar steam generation. Journal of Materials Chemistry A 8, 11665-11673 (2020).

4.	Storer DP, Phelps JL, Wu X, Owens G, Khan NI, Xu H. Graphene and Rice-Straw-Fiber-Based 3D Photothermal Aerogels for Highly Efficient Solar Evaporation. Acs Applied Materials & Interfaces 12, 15279-15287 (2020).

5.	Shi Y, et al. A 3D Photothermal Structure toward Improved Energy Efficiency in Solar Steam Generation. Joule 2, 1171-1186 (2018).

6.	Xie Z, Zhu J, Zhang L. Three-Dimensionally Structured Polypyrrole-Coated Setaria viridis Spike Composites for Efficient Solar Steam Generation. Acs Applied Materials & Interfaces 13, 9027-9035 (2021).

7.	Wang L, et al. Three-Dimensional Wood-Inspired Bilayer Membrane Device Containing Microchannels for Highly Efficient Solar Steam Generation. Acs Applied Materials & Interfaces 12, 24328-24338 (2020).

8.	Wu X, Gao T, Han C, Xu J, Owens G, Xu H. A photothermal reservoir for highly efficient solar steam generation without bulk water. Science Bulletin 64, 1625-1633 (2019).

9.	Sui Y, Hao D, Guo Y, Cai Z, Xu B. A flowerlike sponge coated with carbon black nanoparticles for enhanced solar vapor generation. Journal of Materials Science 55, 298-308 (2020).

10.	Gao T, Wu X, Owens G, Xu H-L. A cobalt oxide@polydopamine-reduced graphene oxide-based 3D photothermal evaporator for highly efficient solar steam generation. Tungsten 2, 423-432 (2020).

11.	Wang Y, Sun X, Tao S. Rational 3D Coiled Morphology for Efficient Solar-Driven Desalination. Environmental Science & Technology 54, 16240-16248 (2020).

12.	Gao T, Wu X, Wang Y, Owens G, Xu H. A Hollow and Compressible 3D Photothermal Evaporator for Highly Efficient Solar Steam Generation without Energy Loss. Solar Rrl 5,  (2021).

13.	Zhang L, Bai B, Hu N, Wang H. Efficient 3D-interfacial solar steam generation enabled by photothermal nanodiamonds paint-coat with optimized heat management. Applied Thermal Engineering 171,  (2020).